Influence of Octahedral Cation Distribution in Montmorillonite on Interlayer Hydrogen Counter-Ion Retention Strength by DFT Simulation

Yayu W. Li1*, Cristian P. Schulthess1, Kevin Co2, Sanjubala Sahoo2 and Pamir Alpay2

1 Department of Plant Science and Landscape Architecture, University of Connecticut, Storrs, CT 06269-4067

2 Department of Material Science and Engineering, University of Connecticut, Storrs, CT 06269

*Corresponding author, Email: yayu.li@uconn.edu

====================================================================================

Title               (A) Montmorillonite cis-vacant cis-Mg       H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (A) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.43958  9.08312  9.53213  89.8907  91.0016  89.9689

Unit-cell volume = 903.733374 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.44209 | 0.32957 | 0.37158 | 1 |
| 2 Al | Al2 | 0.18985 | 0.83484 | 0.36982 | 1 |
| 3 Al | Al3 | 0.19158 | 0.167 | 0.37075 | 1 |
| 4 Al | Al4 | 0.94422 | 0.66761 | 0.36859 | 1 |
| 5 Al | Al5 | 0.70273 | 0.84399 | 0.36212 | 1 |
| 6 Al | Al6 | 0.6948 | 0.17012 | 0.37175 | 1 |
| 7 Si | Si1 | 0.28108 | 0.33348 | 0.0883 | 1 |
| 8 Si | Si2 | 0.27654 | 0.67549 | 0.08629 | 1 |
| 9 Si | Si3 | 0.11993 | 0.98983 | 0.65523 | 1 |
| 10 Si | Si4 | 0.11555 | 0.31793 | 0.65596 | 1 |
| 11 Si | Si5 | 0.03066 | 0.83341 | 0.08515 | 1 |
| 12 Si | Si6 | 0.03137 | 0.17543 | 0.08734 | 1 |
| 13 Si | Si7 | 0.87055 | 0.48763 | 0.65318 | 1 |
| 14 Si | Si8 | 0.86629 | 0.81748 | 0.65321 | 1 |
| 15 Si | Si9 | 0.78177 | 0.334 | 0.08951 | 1 |
| 16 Si | Si10 | 0.78193 | 0.67507 | 0.08493 | 1 |
| 17 Si | Si11 | 0.62108 | 0.98763 | 0.65373 | 1 |
| 18 Si | Si12 | 0.6147 | 0.31411 | 0.65872 | 1 |
| 19 Si | Si13 | 0.53414 | 0.83191 | 0.09255 | 1 |
| 20 Si | Si14 | 0.53227 | 0.17214 | 0.0901 | 1 |
| 21 Si | Si15 | 0.37161 | 0.48398 | 0.65572 | 1 |
| 22 Si | Si16 | 0.35982 | 0.81831 | 0.65348 | 1 |
| 23 O | O1 | 0.25933 | 0.5037 | 0.0413 | 1 |
| 24 O | O2 | 0.4143 | 0.73519 | 0.03204 | 1 |
| 25 O | O3 | 0.41491 | 0.2711 | 0.0266 | 1 |
| 26 O | O4 | 0.24051 | 0.00129 | 0.26334 | 1 |
| 27 O | O5 | 0.27038 | 0.69415 | 0.25569 | 1 |
| 28 O | O6 | 0.28309 | 0.31074 | 0.25949 | 1 |
| 29 O | O7 | 0.13577 | 0.15418 | 0.72022 | 1 |
| 30 O | O8 | 0.98395 | 0.38572 | 0.71711 | 1 |
| 31 O | O9 | 0.98013 | 0.9278 | 0.70073 | 1 |
| 32 O | O10 | 0.38302 | 0.48295 | 0.48614 | 1 |
| 33 O | O11 | 0.34898 | 0.18361 | 0.47357 | 1 |
| 34 O | O12 | 0.34089 | 0.8142 | 0.48375 | 1 |
| 35 O | O13 | 0.00509 | 0.00512 | 0.04377 | 1 |
| 36 O | O14 | 0.16401 | 0.23549 | 0.02246 | 1 |
| 37 O | O15 | 0.1619 | 0.7741 | 0.01523 | 1 |
| 38 O | O16 | 0.50237 | 0.48637 | 0.26578 | 1 |
| 39 O | O17 | 0.03558 | 0.18963 | 0.26093 | 1 |
| 40 O | O18 | 0.03198 | 0.8136 | 0.25721 | 1 |
| 41 O | O19 | 0.88639 | 0.65295 | 0.71628 | 1 |
| 42 O | O20 | 0.23192 | 0.88625 | 0.72368 | 1 |
| 43 O | O21 | 0.23193 | 0.42578 | 0.70486 | 1 |
| 44 O | O22 | 0.12909 | 0.00004 | 0.48302 | 1 |
| 45 O | O23 | 0.09423 | 0.69602 | 0.47827 | 1 |
| 46 O | O24 | 0.10373 | 0.30982 | 0.48255 | 1 |
| 47 O | O25 | 0.75663 | 0.50409 | 0.04425 | 1 |
| 48 O | O26 | 0.91351 | 0.73606 | 0.01875 | 1 |
| 49 O | O27 | 0.91411 | 0.27437 | 0.02426 | 1 |
| 50 O | O28 | 0.75629 | 0.00841 | 0.26327 | 1 |
| 51 O | O29 | 0.79042 | 0.69505 | 0.25786 | 1 |
| 52 O | O30 | 0.78345 | 0.31608 | 0.26186 | 1 |
| 53 O | O31 | 0.63913 | 0.14983 | 0.72219 | 1 |
| 54 O | O32 | 0.48586 | 0.38358 | 0.72533 | 1 |
| 55 O | O33 | 0.48241 | 0.92199 | 0.69489 | 1 |
| 56 O | O34 | 0.8765 | 0.50233 | 0.48027 | 1 |
| 57 O | O35 | 0.85086 | 0.18973 | 0.47853 | 1 |
| 58 O | O36 | 0.8511 | 0.80941 | 0.48013 | 1 |
| 59 O | O37 | 0.50681 | 0.00201 | 0.04614 | 1 |
| 60 O | O38 | 0.66405 | 0.23621 | 0.02536 | 1 |
| 61 O | O39 | 0.66388 | 0.77151 | 0.01999 | 1 |
| 62 O | O40 | 0.00487 | 0.50255 | 0.26634 | 1 |
| 63 O | O41 | 0.53947 | 0.1874 | 0.26244 | 1 |
| 64 O | O42 | 0.54979 | 0.81404 | 0.26309 | 1 |
| 65 O | O43 | 0.38964 | 0.65284 | 0.71316 | 1 |
| 66 O | O44 | 0.73041 | 0.87552 | 0.71504 | 1 |
| 67 O | O45 | 0.73169 | 0.42533 | 0.70003 | 1 |
| 68 O | O46 | 0.63776 | 0.99482 | 0.48188 | 1 |
| 69 O | O47 | 0.62077 | 0.66598 | 0.48531 | 1 |
| 70 O | O48 | 0.60049 | 0.30121 | 0.4866 | 1 |
| 71 H | H1 | 0.31828 | 0.00112 | 0.20911 | 1 |
| 72 H | H2 | 0.14065 | 0.61001 | 0.51248 | 1 |
| 73 H | H3 | 0.55083 | 0.47771 | 0.18067 | 1 |
| 74 H | H4 | 0.902 | 0.10026 | 0.48999 | 1 |
| 75 H | H5 | 0.84403 | 0.01248 | 0.23067 | 1 |
| 76 H | H6 | 0.66467 | 0.57485 | 0.45537 | 1 |
| 77 H | H7 | 0.098 | 0.50073 | 0.25673 | 1 |
| 78 H | H8 | 0.3913 | 0.08905 | 0.48795 | 1 |
| 79 H | H9 | 0.62775 | 0.66877 | 0.58819 | 1 |
| 80 Mg | Mg1 | 0.43416 | 0.66204 | 0.36517 | 1 |
| 81 Fe | Fe1 | 0.9431 | 0.33531 | 0.37134 | 1 |

====================================================================================

====================================================================================

Title               (B) Montmorillonite cis-vacant cis-Mg       H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (B) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.48654  9.10808  9.53502  90.1249  90.8561  89.9561

Unit-cell volume = 910.606555 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.44179 | 0.32982 | 0.37121 | 1 |
| 2 Al | Al2 | 0.19163 | 0.16707 | 0.3716 | 1 |
| 3 Al | Al3 | 0.94377 | 0.33494 | 0.37193 | 1 |
| 4 Al | Al4 | 0.6957 | 0.16804 | 0.37187 | 1 |
| 5 Al | Al5 | 0.70333 | 0.84455 | 0.36138 | 1 |
| 6 Al | Al6 | 0.18991 | 0.83555 | 0.36987 | 1 |
| 7 Si | Si1 | 0.28151 | 0.33167 | 0.08916 | 1 |
| 8 Si | Si2 | 0.27805 | 0.67501 | 0.08644 | 1 |
| 9 Si | Si3 | 0.11942 | 0.99093 | 0.65558 | 1 |
| 10 Si | Si4 | 0.11488 | 0.31854 | 0.65692 | 1 |
| 11 Si | Si5 | 0.03197 | 0.8321 | 0.08471 | 1 |
| 12 Si | Si6 | 0.03221 | 0.17371 | 0.08719 | 1 |
| 13 Si | Si7 | 0.87132 | 0.48925 | 0.65427 | 1 |
| 14 Si | Si8 | 0.86545 | 0.81891 | 0.65355 | 1 |
| 15 Si | Si9 | 0.7818 | 0.33085 | 0.09065 | 1 |
| 16 Si | Si10 | 0.78354 | 0.67281 | 0.08561 | 1 |
| 17 Si | Si11 | 0.62024 | 0.98964 | 0.65306 | 1 |
| 18 Si | Si12 | 0.6146 | 0.31748 | 0.65671 | 1 |
| 19 Si | Si13 | 0.53608 | 0.82996 | 0.091 | 1 |
| 20 Si | Si14 | 0.53199 | 0.16972 | 0.09023 | 1 |
| 21 Si | Si15 | 0.37073 | 0.48561 | 0.65451 | 1 |
| 22 Si | Si16 | 0.35919 | 0.81985 | 0.65299 | 1 |
| 23 O | O1 | 0.26238 | 0.5024 | 0.04395 | 1 |
| 24 O | O2 | 0.41484 | 0.7356 | 0.03174 | 1 |
| 25 O | O3 | 0.41348 | 0.26574 | 0.0266 | 1 |
| 26 O | O4 | 0.24132 | 0.00179 | 0.26399 | 1 |
| 27 O | O5 | 0.27145 | 0.69632 | 0.25541 | 1 |
| 28 O | O6 | 0.28304 | 0.3093 | 0.26021 | 1 |
| 29 O | O7 | 0.13264 | 0.15509 | 0.7212 | 1 |
| 30 O | O8 | 0.98537 | 0.39004 | 0.71977 | 1 |
| 31 O | O9 | 0.9806 | 0.92694 | 0.70026 | 1 |
| 32 O | O10 | 0.38187 | 0.48472 | 0.48487 | 1 |
| 33 O | O11 | 0.34752 | 0.18594 | 0.47534 | 1 |
| 34 O | O12 | 0.3405 | 0.8156 | 0.48335 | 1 |
| 35 O | O13 | 0.01117 | 0.00338 | 0.04265 | 1 |
| 36 O | O14 | 0.16259 | 0.2387 | 0.0224 | 1 |
| 37 O | O15 | 0.16173 | 0.76887 | 0.01487 | 1 |
| 38 O | O16 | 0.50152 | 0.4862 | 0.26438 | 1 |
| 39 O | O17 | 0.03588 | 0.1933 | 0.26016 | 1 |
| 40 O | O18 | 0.03265 | 0.81377 | 0.257 | 1 |
| 41 O | O19 | 0.88288 | 0.65499 | 0.71701 | 1 |
| 42 O | O20 | 0.23259 | 0.89007 | 0.72354 | 1 |
| 43 O | O21 | 0.23288 | 0.42387 | 0.70375 | 1 |
| 44 O | O22 | 0.12876 | 0.00049 | 0.48337 | 1 |
| 45 O | O23 | 0.09446 | 0.6964 | 0.47713 | 1 |
| 46 O | O24 | 0.09886 | 0.30697 | 0.48415 | 1 |
| 47 O | O25 | 0.76113 | 0.50136 | 0.04603 | 1 |
| 48 O | O26 | 0.91394 | 0.7361 | 0.01963 | 1 |
| 49 O | O27 | 0.91243 | 0.26784 | 0.02443 | 1 |
| 50 O | O28 | 0.76346 | 0.00703 | 0.26281 | 1 |
| 51 O | O29 | 0.7909 | 0.69531 | 0.25846 | 1 |
| 52 O | O30 | 0.78749 | 0.3159 | 0.26349 | 1 |
| 53 O | O31 | 0.63557 | 0.15286 | 0.71895 | 1 |
| 54 O | O32 | 0.48699 | 0.38916 | 0.72379 | 1 |
| 55 O | O33 | 0.48313 | 0.92104 | 0.69399 | 1 |
| 56 O | O34 | 0.88215 | 0.49892 | 0.48211 | 1 |
| 57 O | O35 | 0.85185 | 0.19284 | 0.47962 | 1 |
| 58 O | O36 | 0.8507 | 0.80922 | 0.48048 | 1 |
| 59 O | O37 | 0.51284 | 0.9997 | 0.04335 | 1 |
| 60 O | O38 | 0.66222 | 0.2377 | 0.02727 | 1 |
| 61 O | O39 | 0.66441 | 0.76515 | 0.01943 | 1 |
| 62 O | O40 | 0.99871 | 0.5004 | 0.26675 | 1 |
| 63 O | O41 | 0.53418 | 0.184 | 0.26285 | 1 |
| 64 O | O42 | 0.55159 | 0.81471 | 0.26177 | 1 |
| 65 O | O43 | 0.38595 | 0.65444 | 0.71253 | 1 |
| 66 O | O44 | 0.7312 | 0.88133 | 0.71481 | 1 |
| 67 O | O45 | 0.7331 | 0.42494 | 0.69938 | 1 |
| 68 O | O46 | 0.63593 | 0.99339 | 0.48055 | 1 |
| 69 O | O47 | 0.61968 | 0.66529 | 0.48362 | 1 |
| 70 O | O48 | 0.59848 | 0.30899 | 0.48428 | 1 |
| 71 H | H1 | 0.32483 | 0.00174 | 0.22143 | 1 |
| 72 H | H2 | 0.14129 | 0.60943 | 0.50691 | 1 |
| 73 H | H3 | 0.54799 | 0.47665 | 0.17797 | 1 |
| 74 H | H4 | 0.89698 | 0.10085 | 0.49788 | 1 |
| 75 H | H5 | 0.85593 | 0.01364 | 0.25247 | 1 |
| 76 H | H6 | 0.65691 | 0.57177 | 0.45027 | 1 |
| 77 H | H7 | 0.08505 | 0.5017 | 0.23083 | 1 |
| 78 H | H8 | 0.39002 | 0.09229 | 0.49166 | 1 |
| 79 H | H9 | 0.62708 | 0.66426 | 0.58638 | 1 |
| 80 Mg | Mg1 | 0.43383 | 0.66312 | 0.36428 | 1 |
| 81 Fe | Fe1 | 0.94468 | 0.66787 | 0.36867 | 1 |

====================================================================================

====================================================================================

Title               (C) Montmorillonite cis-vacant cis-Mg       H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (C) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.48654  9.10808  9.53502  90.1249  90.8561  89.9561

Unit-cell volume = 910.606555 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.44179 | 0.32982 | 0.37121 | 1 |
| 2 Al | Al2 | 0.19163 | 0.16707 | 0.3716 | 1 |
| 3 Al | Al3 | 0.94377 | 0.33494 | 0.37193 | 1 |
| 4 Al | Al4 | 0.94468 | 0.66787 | 0.36867 | 1 |
| 5 Al | Al5 | 0.70333 | 0.84455 | 0.36138 | 1 |
| 6 Al | Al6 | 0.18991 | 0.83555 | 0.36987 | 1 |
| 7 Si | Si1 | 0.28151 | 0.33167 | 0.08916 | 1 |
| 8 Si | Si2 | 0.27805 | 0.67501 | 0.08644 | 1 |
| 9 Si | Si3 | 0.11942 | 0.99093 | 0.65558 | 1 |
| 10 Si | Si4 | 0.11488 | 0.31854 | 0.65692 | 1 |
| 11 Si | Si5 | 0.03197 | 0.8321 | 0.08471 | 1 |
| 12 Si | Si6 | 0.03221 | 0.17371 | 0.08719 | 1 |
| 13 Si | Si7 | 0.87132 | 0.48925 | 0.65427 | 1 |
| 14 Si | Si8 | 0.86545 | 0.81891 | 0.65355 | 1 |
| 15 Si | Si9 | 0.7818 | 0.33085 | 0.09065 | 1 |
| 16 Si | Si10 | 0.78354 | 0.67281 | 0.08561 | 1 |
| 17 Si | Si11 | 0.62024 | 0.98964 | 0.65306 | 1 |
| 18 Si | Si12 | 0.6146 | 0.31748 | 0.65671 | 1 |
| 19 Si | Si13 | 0.53608 | 0.82996 | 0.091 | 1 |
| 20 Si | Si14 | 0.53199 | 0.16972 | 0.09023 | 1 |
| 21 Si | Si15 | 0.37073 | 0.48561 | 0.65451 | 1 |
| 22 Si | Si16 | 0.35919 | 0.81985 | 0.65299 | 1 |
| 23 O | O1 | 0.26238 | 0.5024 | 0.04395 | 1 |
| 24 O | O2 | 0.41484 | 0.7356 | 0.03174 | 1 |
| 25 O | O3 | 0.41348 | 0.26574 | 0.0266 | 1 |
| 26 O | O4 | 0.24132 | 0.00179 | 0.26399 | 1 |
| 27 O | O5 | 0.27145 | 0.69632 | 0.25541 | 1 |
| 28 O | O6 | 0.28304 | 0.3093 | 0.26021 | 1 |
| 29 O | O7 | 0.13264 | 0.15509 | 0.7212 | 1 |
| 30 O | O8 | 0.98537 | 0.39004 | 0.71977 | 1 |
| 31 O | O9 | 0.9806 | 0.92694 | 0.70026 | 1 |
| 32 O | O10 | 0.38187 | 0.48472 | 0.48487 | 1 |
| 33 O | O11 | 0.34752 | 0.18594 | 0.47534 | 1 |
| 34 O | O12 | 0.3405 | 0.8156 | 0.48335 | 1 |
| 35 O | O13 | 0.01117 | 0.00338 | 0.04265 | 1 |
| 36 O | O14 | 0.16259 | 0.2387 | 0.0224 | 1 |
| 37 O | O15 | 0.16173 | 0.76887 | 0.01487 | 1 |
| 38 O | O16 | 0.50152 | 0.4862 | 0.26438 | 1 |
| 39 O | O17 | 0.03588 | 0.1933 | 0.26016 | 1 |
| 40 O | O18 | 0.03265 | 0.81377 | 0.257 | 1 |
| 41 O | O19 | 0.88288 | 0.65499 | 0.71701 | 1 |
| 42 O | O20 | 0.23259 | 0.89007 | 0.72354 | 1 |
| 43 O | O21 | 0.23288 | 0.42387 | 0.70375 | 1 |
| 44 O | O22 | 0.12876 | 0.00049 | 0.48337 | 1 |
| 45 O | O23 | 0.09446 | 0.6964 | 0.47713 | 1 |
| 46 O | O24 | 0.09886 | 0.30697 | 0.48415 | 1 |
| 47 O | O25 | 0.76113 | 0.50136 | 0.04603 | 1 |
| 48 O | O26 | 0.91394 | 0.7361 | 0.01963 | 1 |
| 49 O | O27 | 0.91243 | 0.26784 | 0.02443 | 1 |
| 50 O | O28 | 0.76346 | 0.00703 | 0.26281 | 1 |
| 51 O | O29 | 0.7909 | 0.69531 | 0.25846 | 1 |
| 52 O | O30 | 0.78749 | 0.3159 | 0.26349 | 1 |
| 53 O | O31 | 0.63557 | 0.15286 | 0.71895 | 1 |
| 54 O | O32 | 0.48699 | 0.38916 | 0.72379 | 1 |
| 55 O | O33 | 0.48313 | 0.92104 | 0.69399 | 1 |
| 56 O | O34 | 0.88215 | 0.49892 | 0.48211 | 1 |
| 57 O | O35 | 0.85185 | 0.19284 | 0.47962 | 1 |
| 58 O | O36 | 0.8507 | 0.80922 | 0.48048 | 1 |
| 59 O | O37 | 0.51284 | 0.9997 | 0.04335 | 1 |
| 60 O | O38 | 0.66222 | 0.2377 | 0.02727 | 1 |
| 61 O | O39 | 0.66441 | 0.76515 | 0.01943 | 1 |
| 62 O | O40 | 0.99871 | 0.5004 | 0.26675 | 1 |
| 63 O | O41 | 0.53418 | 0.184 | 0.26285 | 1 |
| 64 O | O42 | 0.55159 | 0.81471 | 0.26177 | 1 |
| 65 O | O43 | 0.38595 | 0.65444 | 0.71253 | 1 |
| 66 O | O44 | 0.7312 | 0.88133 | 0.71481 | 1 |
| 67 O | O45 | 0.7331 | 0.42494 | 0.69938 | 1 |
| 68 O | O46 | 0.63593 | 0.99339 | 0.48055 | 1 |
| 69 O | O47 | 0.61968 | 0.66529 | 0.48362 | 1 |
| 70 O | O48 | 0.59848 | 0.30899 | 0.48428 | 1 |
| 71 H | H1 | 0.32483 | 0.00174 | 0.22143 | 1 |
| 72 H | H2 | 0.14129 | 0.60943 | 0.50691 | 1 |
| 73 H | H3 | 0.54799 | 0.47665 | 0.17797 | 1 |
| 74 H | H4 | 0.89698 | 0.10085 | 0.49788 | 1 |
| 75 H | H5 | 0.85593 | 0.01364 | 0.25247 | 1 |
| 76 H | H6 | 0.65691 | 0.57177 | 0.45027 | 1 |
| 77 H | H7 | 0.08505 | 0.5017 | 0.23083 | 1 |
| 78 H | H8 | 0.39002 | 0.09229 | 0.49166 | 1 |
| 79 H | H9 | 0.62708 | 0.66426 | 0.58638 | 1 |
| 80 Mg | Mg1 | 0.43383 | 0.66312 | 0.36428 | 1 |
| 81 Fe | Fe1 | 0.6957 | 0.16804 | 0.37187 | 1 |

====================================================================================

====================================================================================

Title               (E) Montmorillonite cis-vacant cis-Mg       H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (E) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.49479  9.09154  9.54629  90.0083  90.7842  90.1062

Unit-cell volume = 910.760636 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.44291 | 0.32962 | 0.37107 | 1 |
| 2 Al | Al2 | 0.18968 | 0.83537 | 0.36989 | 1 |
| 3 Al | Al3 | 0.19232 | 0.16708 | 0.37079 | 1 |
| 4 Al | Al4 | 0.94423 | 0.33377 | 0.37087 | 1 |
| 5 Al | Al5 | 0.94419 | 0.66806 | 0.36811 | 1 |
| 6 Al | Al6 | 0.6942 | 0.16816 | 0.37213 | 1 |
| 7 Si | Si1 | 0.28362 | 0.33262 | 0.08889 | 1 |
| 8 Si | Si2 | 0.27699 | 0.67619 | 0.08648 | 1 |
| 9 Si | Si3 | 0.11981 | 0.99045 | 0.65507 | 1 |
| 10 Si | Si4 | 0.11481 | 0.31839 | 0.65602 | 1 |
| 11 Si | Si5 | 0.03082 | 0.8333 | 0.08496 | 1 |
| 12 Si | Si6 | 0.03402 | 0.17498 | 0.08696 | 1 |
| 13 Si | Si7 | 0.87097 | 0.48862 | 0.65283 | 1 |
| 14 Si | Si8 | 0.86576 | 0.81889 | 0.65311 | 1 |
| 15 Si | Si9 | 0.78447 | 0.33147 | 0.08945 | 1 |
| 16 Si | Si10 | 0.78188 | 0.67362 | 0.08668 | 1 |
| 17 Si | Si11 | 0.61909 | 0.9889 | 0.65379 | 1 |
| 18 Si | Si12 | 0.61413 | 0.31616 | 0.65703 | 1 |
| 19 Si | Si13 | 0.53467 | 0.83282 | 0.09072 | 1 |
| 20 Si | Si14 | 0.53473 | 0.17257 | 0.08869 | 1 |
| 21 Si | Si15 | 0.37098 | 0.48454 | 0.65463 | 1 |
| 22 Si | Si16 | 0.35853 | 0.81875 | 0.6533 | 1 |
| 23 O | O1 | 0.26236 | 0.50334 | 0.04377 | 1 |
| 24 O | O2 | 0.41314 | 0.73873 | 0.03124 | 1 |
| 25 O | O3 | 0.41697 | 0.2705 | 0.0268 | 1 |
| 26 O | O4 | 0.24078 | 0.00138 | 0.26333 | 1 |
| 27 O | O5 | 0.27058 | 0.69599 | 0.25543 | 1 |
| 28 O | O6 | 0.28553 | 0.30931 | 0.25967 | 1 |
| 29 O | O7 | 0.13328 | 0.1548 | 0.72057 | 1 |
| 30 O | O8 | 0.98445 | 0.38843 | 0.71794 | 1 |
| 31 O | O9 | 0.97959 | 0.9292 | 0.70006 | 1 |
| 32 O | O10 | 0.38299 | 0.4836 | 0.48525 | 1 |
| 33 O | O11 | 0.34893 | 0.1843 | 0.47334 | 1 |
| 34 O | O12 | 0.34017 | 0.8147 | 0.48389 | 1 |
| 35 O | O13 | 0.01095 | 0.00478 | 0.04229 | 1 |
| 36 O | O14 | 0.16602 | 0.23715 | 0.02247 | 1 |
| 37 O | O15 | 0.16016 | 0.76911 | 0.01533 | 1 |
| 38 O | O16 | 0.50347 | 0.48714 | 0.26586 | 1 |
| 39 O | O17 | 0.03803 | 0.19474 | 0.25952 | 1 |
| 40 O | O18 | 0.0315 | 0.81445 | 0.25688 | 1 |
| 41 O | O19 | 0.88385 | 0.65452 | 0.7161 | 1 |
| 42 O | O20 | 0.2315 | 0.88814 | 0.72355 | 1 |
| 43 O | O21 | 0.23246 | 0.42398 | 0.70338 | 1 |
| 44 O | O22 | 0.13031 | 0.00007 | 0.48331 | 1 |
| 45 O | O23 | 0.09452 | 0.69553 | 0.47644 | 1 |
| 46 O | O24 | 0.09952 | 0.30688 | 0.48355 | 1 |
| 47 O | O25 | 0.76076 | 0.50205 | 0.04536 | 1 |
| 48 O | O26 | 0.91183 | 0.73847 | 0.02043 | 1 |
| 49 O | O27 | 0.91625 | 0.27164 | 0.02338 | 1 |
| 50 O | O28 | 0.75691 | 0.00272 | 0.26603 | 1 |
| 51 O | O29 | 0.78933 | 0.68942 | 0.25995 | 1 |
| 52 O | O30 | 0.78873 | 0.31006 | 0.26078 | 1 |
| 53 O | O31 | 0.63629 | 0.15182 | 0.72131 | 1 |
| 54 O | O32 | 0.48629 | 0.38697 | 0.72371 | 1 |
| 55 O | O33 | 0.48206 | 0.92048 | 0.69514 | 1 |
| 56 O | O34 | 0.88161 | 0.49926 | 0.48095 | 1 |
| 57 O | O35 | 0.84835 | 0.19629 | 0.47787 | 1 |
| 58 O | O36 | 0.85555 | 0.81132 | 0.47983 | 1 |
| 59 O | O37 | 0.51199 | 0.0026 | 0.04241 | 1 |
| 60 O | O38 | 0.66596 | 0.23681 | 0.02414 | 1 |
| 61 O | O39 | 0.66288 | 0.76633 | 0.0216 | 1 |
| 62 O | O40 | 0.99866 | 0.50064 | 0.26633 | 1 |
| 63 O | O41 | 0.54139 | 0.18716 | 0.26091 | 1 |
| 64 O | O42 | 0.54451 | 0.81741 | 0.26218 | 1 |
| 65 O | O43 | 0.38631 | 0.65335 | 0.71281 | 1 |
| 66 O | O44 | 0.73012 | 0.87884 | 0.71235 | 1 |
| 67 O | O45 | 0.73203 | 0.42571 | 0.69806 | 1 |
| 68 O | O46 | 0.63436 | 0.00089 | 0.48201 | 1 |
| 69 O | O47 | 0.62177 | 0.66433 | 0.48111 | 1 |
| 70 O | O48 | 0.59946 | 0.303 | 0.48512 | 1 |
| 71 H | H1 | 0.32149 | 0.00076 | 0.21502 | 1 |
| 72 H | H2 | 0.14126 | 0.6078 | 0.50433 | 1 |
| 73 H | H3 | 0.5493 | 0.47825 | 0.17904 | 1 |
| 74 H | H4 | 0.89107 | 0.1139 | 0.52289 | 1 |
| 75 H | H5 | 0.8497 | 0.99769 | 0.25786 | 1 |
| 76 H | H6 | 0.66267 | 0.5732 | 0.44691 | 1 |
| 77 H | H7 | 0.08459 | 0.50263 | 0.22948 | 1 |
| 78 H | H8 | 0.39065 | 0.08994 | 0.48866 | 1 |
| 79 H | H9 | 0.63297 | 0.66602 | 0.58347 | 1 |
| 80 Mg | Mg1 | 0.43283 | 0.66279 | 0.36483 | 1 |
| 81 Fe | Fe1 | 0.6989 | 0.83782 | 0.369 | 1 |

====================================================================================

====================================================================================

Title               (F) Montmorillonite cis-vacant cis-Mg      H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (F) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.49479  9.09154  9.54629  90.0083  90.7842  90.1062

Unit-cell volume = 910.760636 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.6989 | 0.83782 | 0.369 | 1 |
| 2 Al | Al2 | 0.18968 | 0.83537 | 0.36989 | 1 |
| 3 Al | Al3 | 0.19232 | 0.16708 | 0.37079 | 1 |
| 4 Al | Al4 | 0.94423 | 0.33377 | 0.37087 | 1 |
| 5 Al | Al5 | 0.94419 | 0.66806 | 0.36811 | 1 |
| 6 Al | Al6 | 0.6942 | 0.16816 | 0.37213 | 1 |
| 7 Si | Si1 | 0.28362 | 0.33262 | 0.08889 | 1 |
| 8 Si | Si2 | 0.27699 | 0.67619 | 0.08648 | 1 |
| 9 Si | Si3 | 0.11981 | 0.99045 | 0.65507 | 1 |
| 10 Si | Si4 | 0.11481 | 0.31839 | 0.65602 | 1 |
| 11 Si | Si5 | 0.03082 | 0.8333 | 0.08496 | 1 |
| 12 Si | Si6 | 0.03402 | 0.17498 | 0.08696 | 1 |
| 13 Si | Si7 | 0.87097 | 0.48862 | 0.65283 | 1 |
| 14 Si | Si8 | 0.86576 | 0.81889 | 0.65311 | 1 |
| 15 Si | Si9 | 0.78447 | 0.33147 | 0.08945 | 1 |
| 16 Si | Si10 | 0.78188 | 0.67362 | 0.08668 | 1 |
| 17 Si | Si11 | 0.61909 | 0.9889 | 0.65379 | 1 |
| 18 Si | Si12 | 0.61413 | 0.31616 | 0.65703 | 1 |
| 19 Si | Si13 | 0.53467 | 0.83282 | 0.09072 | 1 |
| 20 Si | Si14 | 0.53473 | 0.17257 | 0.08869 | 1 |
| 21 Si | Si15 | 0.37098 | 0.48454 | 0.65463 | 1 |
| 22 Si | Si16 | 0.35853 | 0.81875 | 0.6533 | 1 |
| 23 O | O1 | 0.26236 | 0.50334 | 0.04377 | 1 |
| 24 O | O2 | 0.41314 | 0.73873 | 0.03124 | 1 |
| 25 O | O3 | 0.41697 | 0.2705 | 0.0268 | 1 |
| 26 O | O4 | 0.24078 | 0.00138 | 0.26333 | 1 |
| 27 O | O5 | 0.27058 | 0.69599 | 0.25543 | 1 |
| 28 O | O6 | 0.28553 | 0.30931 | 0.25967 | 1 |
| 29 O | O7 | 0.13328 | 0.1548 | 0.72057 | 1 |
| 30 O | O8 | 0.98445 | 0.38843 | 0.71794 | 1 |
| 31 O | O9 | 0.97959 | 0.9292 | 0.70006 | 1 |
| 32 O | O10 | 0.38299 | 0.4836 | 0.48525 | 1 |
| 33 O | O11 | 0.34893 | 0.1843 | 0.47334 | 1 |
| 34 O | O12 | 0.34017 | 0.8147 | 0.48389 | 1 |
| 35 O | O13 | 0.01095 | 0.00478 | 0.04229 | 1 |
| 36 O | O14 | 0.16602 | 0.23715 | 0.02247 | 1 |
| 37 O | O15 | 0.16016 | 0.76911 | 0.01533 | 1 |
| 38 O | O16 | 0.50347 | 0.48714 | 0.26586 | 1 |
| 39 O | O17 | 0.03803 | 0.19474 | 0.25952 | 1 |
| 40 O | O18 | 0.0315 | 0.81445 | 0.25688 | 1 |
| 41 O | O19 | 0.88385 | 0.65452 | 0.7161 | 1 |
| 42 O | O20 | 0.2315 | 0.88814 | 0.72355 | 1 |
| 43 O | O21 | 0.23246 | 0.42398 | 0.70338 | 1 |
| 44 O | O22 | 0.13031 | 0.00007 | 0.48331 | 1 |
| 45 O | O23 | 0.09452 | 0.69553 | 0.47644 | 1 |
| 46 O | O24 | 0.09952 | 0.30688 | 0.48355 | 1 |
| 47 O | O25 | 0.76076 | 0.50205 | 0.04536 | 1 |
| 48 O | O26 | 0.91183 | 0.73847 | 0.02043 | 1 |
| 49 O | O27 | 0.91625 | 0.27164 | 0.02338 | 1 |
| 50 O | O28 | 0.75691 | 0.00272 | 0.26603 | 1 |
| 51 O | O29 | 0.78933 | 0.68942 | 0.25995 | 1 |
| 52 O | O30 | 0.78873 | 0.31006 | 0.26078 | 1 |
| 53 O | O31 | 0.63629 | 0.15182 | 0.72131 | 1 |
| 54 O | O32 | 0.48629 | 0.38697 | 0.72371 | 1 |
| 55 O | O33 | 0.48206 | 0.92048 | 0.69514 | 1 |
| 56 O | O34 | 0.88161 | 0.49926 | 0.48095 | 1 |
| 57 O | O35 | 0.84835 | 0.19629 | 0.47787 | 1 |
| 58 O | O36 | 0.85555 | 0.81132 | 0.47983 | 1 |
| 59 O | O37 | 0.51199 | 0.0026 | 0.04241 | 1 |
| 60 O | O38 | 0.66596 | 0.23681 | 0.02414 | 1 |
| 61 O | O39 | 0.66288 | 0.76633 | 0.0216 | 1 |
| 62 O | O40 | 0.99866 | 0.50064 | 0.26633 | 1 |
| 63 O | O41 | 0.54139 | 0.18716 | 0.26091 | 1 |
| 64 O | O42 | 0.54451 | 0.81741 | 0.26218 | 1 |
| 65 O | O43 | 0.38631 | 0.65335 | 0.71281 | 1 |
| 66 O | O44 | 0.73012 | 0.87884 | 0.71235 | 1 |
| 67 O | O45 | 0.73203 | 0.42571 | 0.69806 | 1 |
| 68 O | O46 | 0.63436 | 0.00089 | 0.48201 | 1 |
| 69 O | O47 | 0.62177 | 0.66433 | 0.48111 | 1 |
| 70 O | O48 | 0.59946 | 0.303 | 0.48512 | 1 |
| 71 H | H1 | 0.32149 | 0.00076 | 0.21502 | 1 |
| 72 H | H2 | 0.14126 | 0.6078 | 0.50433 | 1 |
| 73 H | H3 | 0.5493 | 0.47825 | 0.17904 | 1 |
| 74 H | H4 | 0.89107 | 0.1139 | 0.52289 | 1 |
| 75 H | H5 | 0.8497 | 0.99769 | 0.25786 | 1 |
| 76 H | H6 | 0.66267 | 0.5732 | 0.44691 | 1 |
| 77 H | H7 | 0.08459 | 0.50263 | 0.22948 | 1 |
| 78 H | H8 | 0.39065 | 0.08994 | 0.48866 | 1 |
| 79 H | H9 | 0.63297 | 0.66602 | 0.58347 | 1 |
| 80 Mg | Mg1 | 0.43283 | 0.66279 | 0.36483 | 1 |
| 81 Fe | Fe1 | 0.44291 | 0.32962 | 0.37107 | 1 |

====================================================================================

====================================================================================

Title               (H) Montmorillonite cis-vacant trans-Mg     H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (H) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.45516  9.07586  9.68824  89.3838  91.2745  90.1292

Unit-cell volume = 919.030789 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.44098 | 0.331 | 0.37161 | 1 |
| 2 Al | Al2 | 0.43009 | 0.66296 | 0.36314 | 1 |
| 3 Al | Al3 | 0.18897 | 0.83377 | 0.369 | 1 |
| 4 Al | Al4 | 0.943 | 0.33474 | 0.37138 | 1 |
| 5 Al | Al5 | 0.94447 | 0.66555 | 0.37077 | 1 |
| 6 Al | Al6 | 0.69387 | 0.17111 | 0.36911 | 1 |
| 7 Si | Si1 | 0.27886 | 0.33133 | 0.09176 | 1 |
| 8 Si | Si2 | 0.27717 | 0.6749 | 0.08656 | 1 |
| 9 Si | Si3 | 0.12534 | 0.98745 | 0.65243 | 1 |
| 10 Si | Si4 | 0.11607 | 0.31579 | 0.65195 | 1 |
| 11 Si | Si5 | 0.02907 | 0.83292 | 0.0893 | 1 |
| 12 Si | Si6 | 0.02917 | 0.17493 | 0.09263 | 1 |
| 13 Si | Si7 | 0.87382 | 0.48706 | 0.6529 | 1 |
| 14 Si | Si8 | 0.87285 | 0.8146 | 0.65092 | 1 |
| 15 Si | Si9 | 0.77922 | 0.33538 | 0.09185 | 1 |
| 16 Si | Si10 | 0.78219 | 0.67281 | 0.09163 | 1 |
| 17 Si | Si11 | 0.62726 | 0.9925 | 0.64796 | 1 |
| 18 Si | Si12 | 0.61667 | 0.31601 | 0.6528 | 1 |
| 19 Si | Si13 | 0.52807 | 0.82905 | 0.09757 | 1 |
| 20 Si | Si14 | 0.53019 | 0.17337 | 0.0946 | 1 |
| 21 Si | Si15 | 0.37156 | 0.48551 | 0.65007 | 1 |
| 22 Si | Si16 | 0.36861 | 0.81596 | 0.64903 | 1 |
| 23 O | O1 | 0.25566 | 0.50287 | 0.04754 | 1 |
| 24 O | O2 | 0.41194 | 0.7335 | 0.02586 | 1 |
| 25 O | O3 | 0.41226 | 0.272 | 0.03008 | 1 |
| 26 O | O4 | 0.25081 | 0.99903 | 0.26689 | 1 |
| 27 O | O5 | 0.28026 | 0.69206 | 0.25709 | 1 |
| 28 O | O6 | 0.28355 | 0.31447 | 0.26237 | 1 |
| 29 O | O7 | 0.14286 | 0.15197 | 0.71438 | 1 |
| 30 O | O8 | 0.98545 | 0.38021 | 0.71649 | 1 |
| 31 O | O9 | 0.98864 | 0.92296 | 0.70134 | 1 |
| 32 O | O10 | 0.38013 | 0.49513 | 0.47989 | 1 |
| 33 O | O11 | 0.35212 | 0.186 | 0.4761 | 1 |
| 34 O | O12 | 0.35113 | 0.80142 | 0.47926 | 1 |
| 35 O | O13 | 0.00412 | 0.00498 | 0.04897 | 1 |
| 36 O | O14 | 0.16156 | 0.23476 | 0.02781 | 1 |
| 37 O | O15 | 0.16102 | 0.77411 | 0.02239 | 1 |
| 38 O | O16 | 0.49383 | 0.49969 | 0.27115 | 1 |
| 39 O | O17 | 0.03286 | 0.19207 | 0.26238 | 1 |
| 40 O | O18 | 0.03738 | 0.81119 | 0.2581 | 1 |
| 41 O | O19 | 0.89032 | 0.65047 | 0.71847 | 1 |
| 42 O | O20 | 0.24066 | 0.88397 | 0.71384 | 1 |
| 43 O | O21 | 0.23244 | 0.42674 | 0.69598 | 1 |
| 44 O | O22 | 0.1327 | 0.9939 | 0.48173 | 1 |
| 45 O | O23 | 0.10252 | 0.6894 | 0.47376 | 1 |
| 46 O | O24 | 0.09923 | 0.31004 | 0.48218 | 1 |
| 47 O | O25 | 0.7534 | 0.50459 | 0.04191 | 1 |
| 48 O | O26 | 0.9117 | 0.73737 | 0.02313 | 1 |
| 49 O | O27 | 0.91122 | 0.27288 | 0.02917 | 1 |
| 50 O | O28 | 0.74342 | 0.02043 | 0.2535 | 1 |
| 51 O | O29 | 0.79499 | 0.6822 | 0.2594 | 1 |
| 52 O | O30 | 0.78511 | 0.32122 | 0.26138 | 1 |
| 53 O | O31 | 0.64022 | 0.15333 | 0.71997 | 1 |
| 54 O | O32 | 0.48503 | 0.38233 | 0.71402 | 1 |
| 55 O | O33 | 0.49003 | 0.91936 | 0.68868 | 1 |
| 56 O | O34 | 0.88403 | 0.49694 | 0.48356 | 1 |
| 57 O | O35 | 0.84926 | 0.19423 | 0.47458 | 1 |
| 58 O | O36 | 0.86318 | 0.80378 | 0.48334 | 1 |
| 59 O | O37 | 0.50293 | 0.00177 | 0.05819 | 1 |
| 60 O | O38 | 0.66124 | 0.23651 | 0.02934 | 1 |
| 61 O | O39 | 0.66202 | 0.77312 | 0.03476 | 1 |
| 62 O | O40 | 0.0033 | 0.49917 | 0.26995 | 1 |
| 63 O | O41 | 0.53479 | 0.19809 | 0.26329 | 1 |
| 64 O | O42 | 0.52739 | 0.7991 | 0.26498 | 1 |
| 65 O | O43 | 0.39602 | 0.65084 | 0.71043 | 1 |
| 66 O | O44 | 0.73845 | 0.88158 | 0.70719 | 1 |
| 67 O | O45 | 0.73244 | 0.42771 | 0.69561 | 1 |
| 68 O | O46 | 0.63423 | 0.01059 | 0.4812 | 1 |
| 69 O | O47 | 0.60693 | 0.65729 | 0.487 | 1 |
| 70 O | O48 | 0.59988 | 0.31074 | 0.48262 | 1 |
| 71 H | H1 | 0.34169 | 0.00199 | 0.24596 | 1 |
| 72 H | H2 | 0.14895 | 0.59954 | 0.49725 | 1 |
| 73 H | H3 | 0.55361 | 0.50228 | 0.19605 | 1 |
| 74 H | H4 | 0.89365 | 0.10166 | 0.49296 | 1 |
| 75 H | H5 | 0.816 | 0.02923 | 0.19365 | 1 |
| 76 H | H6 | 0.65237 | 0.56664 | 0.4606 | 1 |
| 77 H | H7 | 0.0938 | 0.49751 | 0.24887 | 1 |
| 78 H | H8 | 0.39905 | 0.09341 | 0.48709 | 1 |
| 79 H | H9 | 0.60678 | 0.65688 | 0.58842 | 1 |
| 80 Mg | Mg1 | 0.7019 | 0.84253 | 0.36376 | 1 |
| 81 Fe | Fe1 | 0.19275 | 0.16498 | 0.37186 | 1 |

====================================================================================

====================================================================================

Title               (I) Montmorillonite cis-vacant trans-Mg     H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (I) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.47899  9.10698  9.50369  89.5294  90.5795  89.9188

Unit-cell volume = 906.877644 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.44089 | 0.33132 | 0.3716 | 1 |
| 2 Al | Al2 | 0.43064 | 0.6626 | 0.36324 | 1 |
| 3 Al | Al3 | 0.18959 | 0.8335 | 0.36944 | 1 |
| 4 Al | Al4 | 0.19196 | 0.16593 | 0.3715 | 1 |
| 5 Al | Al5 | 0.94506 | 0.66521 | 0.37105 | 1 |
| 6 Al | Al6 | 0.69379 | 0.17147 | 0.36898 | 1 |
| 7 Si | Si1 | 0.28214 | 0.33203 | 0.08659 | 1 |
| 8 Si | Si2 | 0.2808 | 0.67409 | 0.0818 | 1 |
| 9 Si | Si3 | 0.12252 | 0.98734 | 0.65728 | 1 |
| 10 Si | Si4 | 0.11206 | 0.31566 | 0.65637 | 1 |
| 11 Si | Si5 | 0.03249 | 0.83281 | 0.08566 | 1 |
| 12 Si | Si6 | 0.03255 | 0.17481 | 0.08863 | 1 |
| 13 Si | Si7 | 0.86891 | 0.48683 | 0.65675 | 1 |
| 14 Si | Si8 | 0.87064 | 0.81522 | 0.65562 | 1 |
| 15 Si | Si9 | 0.78209 | 0.33585 | 0.08818 | 1 |
| 16 Si | Si10 | 0.78616 | 0.67282 | 0.0866 | 1 |
| 17 Si | Si11 | 0.62534 | 0.99264 | 0.65197 | 1 |
| 18 Si | Si12 | 0.61232 | 0.31585 | 0.65801 | 1 |
| 19 Si | Si13 | 0.53145 | 0.82834 | 0.09436 | 1 |
| 20 Si | Si14 | 0.53302 | 0.17313 | 0.09096 | 1 |
| 21 Si | Si15 | 0.36725 | 0.48603 | 0.65429 | 1 |
| 22 Si | Si16 | 0.36623 | 0.81604 | 0.65346 | 1 |
| 23 O | O1 | 0.26358 | 0.50292 | 0.03984 | 1 |
| 24 O | O2 | 0.41487 | 0.73651 | 0.02095 | 1 |
| 25 O | O3 | 0.41446 | 0.26762 | 0.02373 | 1 |
| 26 O | O4 | 0.24657 | -0.00003 | 0.26671 | 1 |
| 27 O | O5 | 0.28189 | 0.69132 | 0.2555 | 1 |
| 28 O | O6 | 0.28418 | 0.312 | 0.25921 | 1 |
| 29 O | O7 | 0.13503 | 0.15218 | 0.72065 | 1 |
| 30 O | O8 | 0.98162 | 0.38287 | 0.72017 | 1 |
| 31 O | O9 | 0.98863 | 0.91724 | 0.70843 | 1 |
| 32 O | O10 | 0.37879 | 0.49626 | 0.48116 | 1 |
| 33 O | O11 | 0.34707 | 0.19187 | 0.47739 | 1 |
| 34 O | O12 | 0.34945 | 0.80073 | 0.48088 | 1 |
| 35 O | O13 | 0.01048 | 0.00481 | 0.04443 | 1 |
| 36 O | O14 | 0.16379 | 0.23807 | 0.02198 | 1 |
| 37 O | O15 | 0.16431 | 0.77193 | 0.01739 | 1 |
| 38 O | O16 | 0.4946 | 0.49916 | 0.26908 | 1 |
| 39 O | O17 | 0.03857 | 0.18893 | 0.2619 | 1 |
| 40 O | O18 | 0.03838 | 0.80975 | 0.25744 | 1 |
| 41 O | O19 | 0.88164 | 0.65021 | 0.72279 | 1 |
| 42 O | O20 | 0.24049 | 0.88957 | 0.72016 | 1 |
| 43 O | O21 | 0.22845 | 0.4254 | 0.70034 | 1 |
| 44 O | O22 | 0.13396 | 0.99631 | 0.48433 | 1 |
| 45 O | O23 | 0.10132 | 0.69047 | 0.47704 | 1 |
| 46 O | O24 | 0.102 | 0.30661 | 0.48292 | 1 |
| 47 O | O25 | 0.76075 | 0.50454 | 0.03578 | 1 |
| 48 O | O26 | 0.91497 | 0.74024 | 0.01754 | 1 |
| 49 O | O27 | 0.91337 | 0.26951 | 0.02578 | 1 |
| 50 O | O28 | 0.74482 | 0.0207 | 0.25035 | 1 |
| 51 O | O29 | 0.79748 | 0.68144 | 0.25743 | 1 |
| 52 O | O30 | 0.78256 | 0.32325 | 0.26147 | 1 |
| 53 O | O31 | 0.63171 | 0.15311 | 0.72604 | 1 |
| 54 O | O32 | 0.48122 | 0.3853 | 0.71983 | 1 |
| 55 O | O33 | 0.48982 | 0.91488 | 0.69207 | 1 |
| 56 O | O34 | 0.87914 | 0.49986 | 0.48375 | 1 |
| 57 O | O35 | 0.85011 | 0.1876 | 0.47554 | 1 |
| 58 O | O36 | 0.86264 | 0.805 | 0.48475 | 1 |
| 59 O | O37 | 0.50755 | 0.0012 | 0.05544 | 1 |
| 60 O | O38 | 0.66386 | 0.23881 | 0.02526 | 1 |
| 61 O | O39 | 0.6652 | 0.77098 | 0.02944 | 1 |
| 62 O | O40 | 0.01003 | 0.49998 | 0.26864 | 1 |
| 63 O | O41 | 0.53614 | 0.19911 | 0.26225 | 1 |
| 64 O | O42 | 0.52998 | 0.79695 | 0.2644 | 1 |
| 65 O | O43 | 0.38826 | 0.65091 | 0.71658 | 1 |
| 66 O | O44 | 0.738 | 0.88648 | 0.71392 | 1 |
| 67 O | O45 | 0.72937 | 0.42396 | 0.70144 | 1 |
| 68 O | O46 | 0.63487 | 0.01111 | 0.48234 | 1 |
| 69 O | O47 | 0.60639 | 0.65728 | 0.49049 | 1 |
| 70 O | O48 | 0.59862 | 0.31004 | 0.48496 | 1 |
| 71 H | H1 | 0.32523 | 0.00019 | 0.21357 | 1 |
| 72 H | H2 | 0.14775 | 0.60288 | 0.50655 | 1 |
| 73 H | H3 | 0.55892 | 0.5014 | 0.1965 | 1 |
| 74 H | H4 | 0.89745 | 0.09492 | 0.47585 | 1 |
| 75 H | H5 | 0.81222 | 0.02997 | 0.18199 | 1 |
| 76 H | H6 | 0.65444 | 0.56842 | 0.46322 | 1 |
| 77 H | H7 | 0.10298 | 0.49371 | 0.26392 | 1 |
| 78 H | H8 | 0.39392 | 0.10352 | 0.50425 | 1 |
| 79 H | H9 | 0.6049 | 0.65652 | 0.59379 | 1 |
| 80 Mg | Mg1 | 0.70295 | 0.84296 | 0.36305 | 1 |
| 81 Fe | Fe1 | 0.94303 | 0.3345 | 0.3717 | 1 |

====================================================================================

====================================================================================

Title               (J) Montmorillonite cis-vacant trans-Mg    H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (J) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.47899  9.10698  9.50369  89.5294  90.5795  89.9188

Unit-cell volume = 906.877644 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.94303 | 0.3345 | 0.3717 | 1 |
| 2 Al | Al2 | 0.43064 | 0.6626 | 0.36324 | 1 |
| 3 Al | Al3 | 0.18959 | 0.8335 | 0.36944 | 1 |
| 4 Al | Al4 | 0.19196 | 0.16593 | 0.3715 | 1 |
| 5 Al | Al5 | 0.94506 | 0.66521 | 0.37105 | 1 |
| 6 Al | Al6 | 0.69379 | 0.17147 | 0.36898 | 1 |
| 7 Si | Si1 | 0.28214 | 0.33203 | 0.08659 | 1 |
| 8 Si | Si2 | 0.2808 | 0.67409 | 0.0818 | 1 |
| 9 Si | Si3 | 0.12252 | 0.98734 | 0.65728 | 1 |
| 10 Si | Si4 | 0.11206 | 0.31566 | 0.65637 | 1 |
| 11 Si | Si5 | 0.03249 | 0.83281 | 0.08566 | 1 |
| 12 Si | Si6 | 0.03255 | 0.17481 | 0.08863 | 1 |
| 13 Si | Si7 | 0.86891 | 0.48683 | 0.65675 | 1 |
| 14 Si | Si8 | 0.87064 | 0.81522 | 0.65562 | 1 |
| 15 Si | Si9 | 0.78209 | 0.33585 | 0.08818 | 1 |
| 16 Si | Si10 | 0.78616 | 0.67282 | 0.0866 | 1 |
| 17 Si | Si11 | 0.62534 | 0.99264 | 0.65197 | 1 |
| 18 Si | Si12 | 0.61232 | 0.31585 | 0.65801 | 1 |
| 19 Si | Si13 | 0.53145 | 0.82834 | 0.09436 | 1 |
| 20 Si | Si14 | 0.53302 | 0.17313 | 0.09096 | 1 |
| 21 Si | Si15 | 0.36725 | 0.48603 | 0.65429 | 1 |
| 22 Si | Si16 | 0.36623 | 0.81604 | 0.65346 | 1 |
| 23 O | O1 | 0.26358 | 0.50292 | 0.03984 | 1 |
| 24 O | O2 | 0.41487 | 0.73651 | 0.02095 | 1 |
| 25 O | O3 | 0.41446 | 0.26762 | 0.02373 | 1 |
| 26 O | O4 | 0.24657 | -0.00003 | 0.26671 | 1 |
| 27 O | O5 | 0.28189 | 0.69132 | 0.2555 | 1 |
| 28 O | O6 | 0.28418 | 0.312 | 0.25921 | 1 |
| 29 O | O7 | 0.13503 | 0.15218 | 0.72065 | 1 |
| 30 O | O8 | 0.98162 | 0.38287 | 0.72017 | 1 |
| 31 O | O9 | 0.98863 | 0.91724 | 0.70843 | 1 |
| 32 O | O10 | 0.37879 | 0.49626 | 0.48116 | 1 |
| 33 O | O11 | 0.34707 | 0.19187 | 0.47739 | 1 |
| 34 O | O12 | 0.34945 | 0.80073 | 0.48088 | 1 |
| 35 O | O13 | 0.01048 | 0.00481 | 0.04443 | 1 |
| 36 O | O14 | 0.16379 | 0.23807 | 0.02198 | 1 |
| 37 O | O15 | 0.16431 | 0.77193 | 0.01739 | 1 |
| 38 O | O16 | 0.4946 | 0.49916 | 0.26908 | 1 |
| 39 O | O17 | 0.03857 | 0.18893 | 0.2619 | 1 |
| 40 O | O18 | 0.03838 | 0.80975 | 0.25744 | 1 |
| 41 O | O19 | 0.88164 | 0.65021 | 0.72279 | 1 |
| 42 O | O20 | 0.24049 | 0.88957 | 0.72016 | 1 |
| 43 O | O21 | 0.22845 | 0.4254 | 0.70034 | 1 |
| 44 O | O22 | 0.13396 | 0.99631 | 0.48433 | 1 |
| 45 O | O23 | 0.10132 | 0.69047 | 0.47704 | 1 |
| 46 O | O24 | 0.102 | 0.30661 | 0.48292 | 1 |
| 47 O | O25 | 0.76075 | 0.50454 | 0.03578 | 1 |
| 48 O | O26 | 0.91497 | 0.74024 | 0.01754 | 1 |
| 49 O | O27 | 0.91337 | 0.26951 | 0.02578 | 1 |
| 50 O | O28 | 0.74482 | 0.0207 | 0.25035 | 1 |
| 51 O | O29 | 0.79748 | 0.68144 | 0.25743 | 1 |
| 52 O | O30 | 0.78256 | 0.32325 | 0.26147 | 1 |
| 53 O | O31 | 0.63171 | 0.15311 | 0.72604 | 1 |
| 54 O | O32 | 0.48122 | 0.3853 | 0.71983 | 1 |
| 55 O | O33 | 0.48982 | 0.91488 | 0.69207 | 1 |
| 56 O | O34 | 0.87914 | 0.49986 | 0.48375 | 1 |
| 57 O | O35 | 0.85011 | 0.1876 | 0.47554 | 1 |
| 58 O | O36 | 0.86264 | 0.805 | 0.48475 | 1 |
| 59 O | O37 | 0.50755 | 0.0012 | 0.05544 | 1 |
| 60 O | O38 | 0.66386 | 0.23881 | 0.02526 | 1 |
| 61 O | O39 | 0.6652 | 0.77098 | 0.02944 | 1 |
| 62 O | O40 | 0.01003 | 0.49998 | 0.26864 | 1 |
| 63 O | O41 | 0.53614 | 0.19911 | 0.26225 | 1 |
| 64 O | O42 | 0.52998 | 0.79695 | 0.2644 | 1 |
| 65 O | O43 | 0.38826 | 0.65091 | 0.71658 | 1 |
| 66 O | O44 | 0.738 | 0.88648 | 0.71392 | 1 |
| 67 O | O45 | 0.72937 | 0.42396 | 0.70144 | 1 |
| 68 O | O46 | 0.63487 | 0.01111 | 0.48234 | 1 |
| 69 O | O47 | 0.60639 | 0.65728 | 0.49049 | 1 |
| 70 O | O48 | 0.59862 | 0.31004 | 0.48496 | 1 |
| 71 H | H1 | 0.32523 | 0.00019 | 0.21357 | 1 |
| 72 H | H2 | 0.14775 | 0.60288 | 0.50655 | 1 |
| 73 H | H3 | 0.55892 | 0.5014 | 0.1965 | 1 |
| 74 H | H4 | 0.89745 | 0.09492 | 0.47585 | 1 |
| 75 H | H5 | 0.81222 | 0.02997 | 0.18199 | 1 |
| 76 H | H6 | 0.65444 | 0.56842 | 0.46322 | 1 |
| 77 H | H7 | 0.10298 | 0.49371 | 0.26392 | 1 |
| 78 H | H8 | 0.39392 | 0.10352 | 0.50425 | 1 |
| 79 H | H9 | 0.6049 | 0.65652 | 0.59379 | 1 |
| 80 Mg | Mg1 | 0.70295 | 0.84296 | 0.36305 | 1 |
| 81 Fe | Fe1 | 0.44089 | 0.33132 | 0.3716 | 1 |

====================================================================================

====================================================================================

Title               (L) Montmorillonite cis-vacant trans-Mg     H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (L) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.46352  9.10413  9.60218  89.4914  91.0227  89.8512

Unit-cell volume = 914.530739 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.43939 | 0.33116 | 0.36977 | 1 |
| 2 Al | Al2 | 0.19045 | 0.83362 | 0.37091 | 1 |
| 3 Al | Al3 | 0.19146 | 0.16563 | 0.37181 | 1 |
| 4 Al | Al4 | 0.94278 | 0.33512 | 0.37116 | 1 |
| 5 Al | Al5 | 0.94537 | 0.66506 | 0.37162 | 1 |
| 6 Al | Al6 | 0.69372 | 0.17141 | 0.36767 | 1 |
| 7 Si | Si1 | 0.28123 | 0.3314 | 0.08815 | 1 |
| 8 Si | Si2 | 0.28192 | 0.67333 | 0.08609 | 1 |
| 9 Si | Si3 | 0.12376 | 0.98737 | 0.65552 | 1 |
| 10 Si | Si4 | 0.11376 | 0.31476 | 0.6553 | 1 |
| 11 Si | Si5 | 0.03184 | 0.83274 | 0.08976 | 1 |
| 12 Si | Si6 | 0.03178 | 0.1751 | 0.09053 | 1 |
| 13 Si | Si7 | 0.87154 | 0.48724 | 0.65508 | 1 |
| 14 Si | Si8 | 0.87157 | 0.81434 | 0.6536 | 1 |
| 15 Si | Si9 | 0.78081 | 0.33542 | 0.08823 | 1 |
| 16 Si | Si10 | 0.78511 | 0.67228 | 0.0889 | 1 |
| 17 Si | Si11 | 0.62638 | 0.99322 | 0.64915 | 1 |
| 18 Si | Si12 | 0.61442 | 0.31689 | 0.65381 | 1 |
| 19 Si | Si13 | 0.53003 | 0.82863 | 0.09366 | 1 |
| 20 Si | Si14 | 0.53195 | 0.17368 | 0.09137 | 1 |
| 21 Si | Si15 | 0.3679 | 0.48556 | 0.65113 | 1 |
| 22 Si | Si16 | 0.36711 | 0.81781 | 0.65065 | 1 |
| 23 O | O1 | 0.25983 | 0.50292 | 0.0445 | 1 |
| 24 O | O2 | 0.41399 | 0.73511 | 0.02183 | 1 |
| 25 O | O3 | 0.41283 | 0.26798 | 0.02443 | 1 |
| 26 O | O4 | 0.24408 | 0.00041 | 0.26692 | 1 |
| 27 O | O5 | 0.28341 | 0.69197 | 0.25857 | 1 |
| 28 O | O6 | 0.28417 | 0.31087 | 0.25899 | 1 |
| 29 O | O7 | 0.13873 | 0.15153 | 0.71951 | 1 |
| 30 O | O8 | 0.9831 | 0.38095 | 0.71931 | 1 |
| 31 O | O9 | 0.98815 | 0.9202 | 0.70431 | 1 |
| 32 O | O10 | 0.37391 | 0.49188 | 0.47884 | 1 |
| 33 O | O11 | 0.34825 | 0.18993 | 0.47507 | 1 |
| 34 O | O12 | 0.34718 | 0.80909 | 0.47973 | 1 |
| 35 O | O13 | 0.00849 | 0.00462 | 0.04906 | 1 |
| 36 O | O14 | 0.16265 | 0.23724 | 0.02369 | 1 |
| 37 O | O15 | 0.1643 | 0.7723 | 0.024 | 1 |
| 38 O | O16 | 0.49414 | 0.49698 | 0.26283 | 1 |
| 39 O | O17 | 0.03807 | 0.1952 | 0.26135 | 1 |
| 40 O | O18 | 0.03778 | 0.80924 | 0.25971 | 1 |
| 41 O | O19 | 0.8862 | 0.65022 | 0.72133 | 1 |
| 42 O | O20 | 0.24046 | 0.88671 | 0.71895 | 1 |
| 43 O | O21 | 0.22971 | 0.42594 | 0.69895 | 1 |
| 44 O | O22 | 0.13368 | 0.99679 | 0.48431 | 1 |
| 45 O | O23 | 0.10266 | 0.68901 | 0.47616 | 1 |
| 46 O | O24 | 0.09937 | 0.30347 | 0.48418 | 1 |
| 47 O | O25 | 0.75966 | 0.5046 | 0.03718 | 1 |
| 48 O | O26 | 0.91442 | 0.73932 | 0.02193 | 1 |
| 49 O | O27 | 0.91223 | 0.26944 | 0.02631 | 1 |
| 50 O | O28 | 0.74504 | 0.02039 | 0.25194 | 1 |
| 51 O | O29 | 0.7951 | 0.6804 | 0.2586 | 1 |
| 52 O | O30 | 0.78508 | 0.32252 | 0.25961 | 1 |
| 53 O | O31 | 0.63587 | 0.15428 | 0.72111 | 1 |
| 54 O | O32 | 0.48282 | 0.38457 | 0.71527 | 1 |
| 55 O | O33 | 0.49031 | 0.91763 | 0.68992 | 1 |
| 56 O | O34 | 0.88372 | 0.49664 | 0.48434 | 1 |
| 57 O | O35 | 0.84857 | 0.19518 | 0.47376 | 1 |
| 58 O | O36 | 0.86201 | 0.80256 | 0.48454 | 1 |
| 59 O | O37 | 0.50621 | 0.00165 | 0.05551 | 1 |
| 60 O | O38 | 0.66276 | 0.23765 | 0.02581 | 1 |
| 61 O | O39 | 0.6646 | 0.77209 | 0.03159 | 1 |
| 62 O | O40 | 0.00444 | 0.49857 | 0.27032 | 1 |
| 63 O | O41 | 0.53614 | 0.19923 | 0.26136 | 1 |
| 64 O | O42 | 0.52915 | 0.8023 | 0.26374 | 1 |
| 65 O | O43 | 0.39341 | 0.65138 | 0.70903 | 1 |
| 66 O | O44 | 0.7384 | 0.88497 | 0.7104 | 1 |
| 67 O | O45 | 0.73039 | 0.42701 | 0.69708 | 1 |
| 68 O | O46 | 0.63523 | 0.0116 | 0.48114 | 1 |
| 69 O | O47 | 0.6035 | 0.65296 | 0.48642 | 1 |
| 70 O | O48 | 0.59897 | 0.3127 | 0.48194 | 1 |
| 71 H | H1 | 0.32548 | 0.00018 | 0.21987 | 1 |
| 72 H | H2 | 0.15077 | 0.59987 | 0.49759 | 1 |
| 73 H | H3 | 0.58174 | 0.50257 | 0.23017 | 1 |
| 74 H | H4 | 0.89269 | 0.1031 | 0.49447 | 1 |
| 75 H | H5 | 0.8128 | 0.02933 | 0.18512 | 1 |
| 76 H | H6 | 0.64998 | 0.56073 | 0.46635 | 1 |
| 77 H | H7 | 0.09428 | 0.49637 | 0.24624 | 1 |
| 78 H | H8 | 0.39528 | 0.10023 | 0.49784 | 1 |
| 79 H | H9 | 0.59317 | 0.65404 | 0.58813 | 1 |
| 80 Mg | Mg1 | 0.70286 | 0.84315 | 0.36311 | 1 |
| 81 Fe | Fe1 | 0.4362 | 0.6619 | 0.3685 | 1 |

====================================================================================

====================================================================================

Title               (M) Montmorillonite cis-vacant trans-Mg    H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (M) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.46352  9.10413  9.60218  89.4914  91.0227  89.8512

Unit-cell volume = 914.530739 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.43939 | 0.33116 | 0.36977 | 1 |
| 2 Al | Al2 | 0.19045 | 0.83362 | 0.37091 | 1 |
| 3 Al | Al3 | 0.19146 | 0.16563 | 0.37181 | 1 |
| 4 Al | Al4 | 0.94278 | 0.33512 | 0.37116 | 1 |
| 5 Al | Al5 | 0.4362 | 0.6619 | 0.3685 | 1 |
| 6 Al | Al6 | 0.69372 | 0.17141 | 0.36767 | 1 |
| 7 Si | Si1 | 0.28123 | 0.3314 | 0.08815 | 1 |
| 8 Si | Si2 | 0.28192 | 0.67333 | 0.08609 | 1 |
| 9 Si | Si3 | 0.12376 | 0.98737 | 0.65552 | 1 |
| 10 Si | Si4 | 0.11376 | 0.31476 | 0.6553 | 1 |
| 11 Si | Si5 | 0.03184 | 0.83274 | 0.08976 | 1 |
| 12 Si | Si6 | 0.03178 | 0.1751 | 0.09053 | 1 |
| 13 Si | Si7 | 0.87154 | 0.48724 | 0.65508 | 1 |
| 14 Si | Si8 | 0.87157 | 0.81434 | 0.6536 | 1 |
| 15 Si | Si9 | 0.78081 | 0.33542 | 0.08823 | 1 |
| 16 Si | Si10 | 0.78511 | 0.67228 | 0.0889 | 1 |
| 17 Si | Si11 | 0.62638 | 0.99322 | 0.64915 | 1 |
| 18 Si | Si12 | 0.61442 | 0.31689 | 0.65381 | 1 |
| 19 Si | Si13 | 0.53003 | 0.82863 | 0.09366 | 1 |
| 20 Si | Si14 | 0.53195 | 0.17368 | 0.09137 | 1 |
| 21 Si | Si15 | 0.3679 | 0.48556 | 0.65113 | 1 |
| 22 Si | Si16 | 0.36711 | 0.81781 | 0.65065 | 1 |
| 23 O | O1 | 0.25983 | 0.50292 | 0.0445 | 1 |
| 24 O | O2 | 0.41399 | 0.73511 | 0.02183 | 1 |
| 25 O | O3 | 0.41283 | 0.26798 | 0.02443 | 1 |
| 26 O | O4 | 0.24408 | 0.00041 | 0.26692 | 1 |
| 27 O | O5 | 0.28341 | 0.69197 | 0.25857 | 1 |
| 28 O | O6 | 0.28417 | 0.31087 | 0.25899 | 1 |
| 29 O | O7 | 0.13873 | 0.15153 | 0.71951 | 1 |
| 30 O | O8 | 0.9831 | 0.38095 | 0.71931 | 1 |
| 31 O | O9 | 0.98815 | 0.9202 | 0.70431 | 1 |
| 32 O | O10 | 0.37391 | 0.49188 | 0.47884 | 1 |
| 33 O | O11 | 0.34825 | 0.18993 | 0.47507 | 1 |
| 34 O | O12 | 0.34718 | 0.80909 | 0.47973 | 1 |
| 35 O | O13 | 0.00849 | 0.00462 | 0.04906 | 1 |
| 36 O | O14 | 0.16265 | 0.23724 | 0.02369 | 1 |
| 37 O | O15 | 0.1643 | 0.7723 | 0.024 | 1 |
| 38 O | O16 | 0.49414 | 0.49698 | 0.26283 | 1 |
| 39 O | O17 | 0.03807 | 0.1952 | 0.26135 | 1 |
| 40 O | O18 | 0.03778 | 0.80924 | 0.25971 | 1 |
| 41 O | O19 | 0.8862 | 0.65022 | 0.72133 | 1 |
| 42 O | O20 | 0.24046 | 0.88671 | 0.71895 | 1 |
| 43 O | O21 | 0.22971 | 0.42594 | 0.69895 | 1 |
| 44 O | O22 | 0.13368 | 0.99679 | 0.48431 | 1 |
| 45 O | O23 | 0.10266 | 0.68901 | 0.47616 | 1 |
| 46 O | O24 | 0.09937 | 0.30347 | 0.48418 | 1 |
| 47 O | O25 | 0.75966 | 0.5046 | 0.03718 | 1 |
| 48 O | O26 | 0.91442 | 0.73932 | 0.02193 | 1 |
| 49 O | O27 | 0.91223 | 0.26944 | 0.02631 | 1 |
| 50 O | O28 | 0.74504 | 0.02039 | 0.25194 | 1 |
| 51 O | O29 | 0.7951 | 0.6804 | 0.2586 | 1 |
| 52 O | O30 | 0.78508 | 0.32252 | 0.25961 | 1 |
| 53 O | O31 | 0.63587 | 0.15428 | 0.72111 | 1 |
| 54 O | O32 | 0.48282 | 0.38457 | 0.71527 | 1 |
| 55 O | O33 | 0.49031 | 0.91763 | 0.68992 | 1 |
| 56 O | O34 | 0.88372 | 0.49664 | 0.48434 | 1 |
| 57 O | O35 | 0.84857 | 0.19518 | 0.47376 | 1 |
| 58 O | O36 | 0.86201 | 0.80256 | 0.48454 | 1 |
| 59 O | O37 | 0.50621 | 0.00165 | 0.05551 | 1 |
| 60 O | O38 | 0.66276 | 0.23765 | 0.02581 | 1 |
| 61 O | O39 | 0.6646 | 0.77209 | 0.03159 | 1 |
| 62 O | O40 | 0.00444 | 0.49857 | 0.27032 | 1 |
| 63 O | O41 | 0.53614 | 0.19923 | 0.26136 | 1 |
| 64 O | O42 | 0.52915 | 0.8023 | 0.26374 | 1 |
| 65 O | O43 | 0.39341 | 0.65138 | 0.70903 | 1 |
| 66 O | O44 | 0.7384 | 0.88497 | 0.7104 | 1 |
| 67 O | O45 | 0.73039 | 0.42701 | 0.69708 | 1 |
| 68 O | O46 | 0.63523 | 0.0116 | 0.48114 | 1 |
| 69 O | O47 | 0.6035 | 0.65296 | 0.48642 | 1 |
| 70 O | O48 | 0.59897 | 0.3127 | 0.48194 | 1 |
| 71 H | H1 | 0.32548 | 0.00018 | 0.21987 | 1 |
| 72 H | H2 | 0.15077 | 0.59987 | 0.49759 | 1 |
| 73 H | H3 | 0.58174 | 0.50257 | 0.23017 | 1 |
| 74 H | H4 | 0.89269 | 0.1031 | 0.49447 | 1 |
| 75 H | H5 | 0.8128 | 0.02933 | 0.18512 | 1 |
| 76 H | H6 | 0.64998 | 0.56073 | 0.46635 | 1 |
| 77 H | H7 | 0.09428 | 0.49637 | 0.24624 | 1 |
| 78 H | H8 | 0.39528 | 0.10023 | 0.49784 | 1 |
| 79 H | H9 | 0.59317 | 0.65404 | 0.58813 | 1 |
| 80 Mg | Mg1 | 0.70286 | 0.84315 | 0.36311 | 1 |
| 81 Fe | Fe1 | 0.94537 | 0.66506 | 0.37162 | 1 |

====================================================================================

====================================================================================

Title               (O) Montmorillonite trans-vacant cis-Mg     H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (O) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.54677  9.07216  9.65603  89.9876  91.3552  90.0700

Unit-cell volume = 923.649379 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.44151 | 0.31162 | 0.36422 | 1 |
| 2 Al | Al2 | 0.18725 | 0.83495 | 0.37042 | 1 |
| 3 Al | Al3 | 0.1853 | 0.16395 | 0.36957 | 1 |
| 4 Al | Al4 | 0.93881 | 0.66974 | 0.369 | 1 |
| 5 Al | Al5 | 0.69159 | 0.83453 | 0.36705 | 1 |
| 6 Al | Al6 | 0.6929 | 0.1624 | 0.36857 | 1 |
| 7 Si | Si1 | 0.34881 | 0.83156 | 0.65058 | 1 |
| 8 Si | Si2 | 0.27443 | 0.674 | 0.09197 | 1 |
| 9 Si | Si3 | 0.27794 | 0.32947 | 0.09145 | 1 |
| 10 Si | Si4 | 0.0993 | 0.33063 | 0.6496 | 1 |
| 11 Si | Si5 | 0.1002 | 0.67449 | 0.65217 | 1 |
| 12 Si | Si6 | 0.02704 | 0.17296 | 0.09036 | 1 |
| 13 Si | Si7 | 0.02726 | 0.82945 | 0.0886 | 1 |
| 14 Si | Si8 | 0.34943 | 0.16965 | 0.65148 | 1 |
| 15 Si | Si9 | 0.77784 | 0.67388 | 0.08704 | 1 |
| 16 Si | Si10 | 0.8513 | 0.82927 | 0.65088 | 1 |
| 17 Si | Si11 | 0.7774 | 0.33107 | 0.09029 | 1 |
| 18 Si | Si12 | 0.60059 | 0.3274 | 0.64917 | 1 |
| 19 Si | Si13 | 0.60465 | 0.67499 | 0.64696 | 1 |
| 20 Si | Si14 | 0.52859 | 0.16906 | 0.08534 | 1 |
| 21 Si | Si15 | 0.53039 | 0.83033 | 0.08584 | 1 |
| 22 Si | Si16 | 0.84999 | 0.17257 | 0.65009 | 1 |
| 23 O | O1 | 0.25819 | 0.50078 | 0.04995 | 1 |
| 24 O | O2 | 0.40679 | 0.73656 | 0.03144 | 1 |
| 25 O | O3 | 0.40739 | 0.26393 | 0.02789 | 1 |
| 26 O | O4 | 0.27061 | 0.69257 | 0.26014 | 1 |
| 27 O | O5 | 0.24275 | 0.0009 | 0.26506 | 1 |
| 28 O | O6 | 0.22106 | 0.76405 | 0.7178 | 1 |
| 29 O | O7 | 0.34946 | 0.49106 | 0.4948 | 1 |
| 30 O | O8 | 0.21921 | 0.2367 | 0.71209 | 1 |
| 31 O | O9 | 0.37231 | 0.00128 | 0.70105 | 1 |
| 32 O | O10 | 0.28365 | 0.30433 | 0.26231 | 1 |
| 33 O | O11 | 0.34403 | 0.18523 | 0.48026 | 1 |
| 34 O | O12 | 0.33615 | 0.8204 | 0.48286 | 1 |
| 35 O | O13 | 0.00755 | 0.00174 | 0.0475 | 1 |
| 36 O | O14 | 0.15636 | 0.76599 | 0.02236 | 1 |
| 37 O | O15 | 0.15746 | 0.23749 | 0.02773 | 1 |
| 38 O | O16 | 0.12135 | 0.50172 | 0.69318 | 1 |
| 39 O | O17 | 0.46961 | 0.733 | 0.70601 | 1 |
| 40 O | O18 | 0.031 | 0.80952 | 0.25927 | 1 |
| 41 O | O19 | 0.03269 | 0.19061 | 0.26114 | 1 |
| 42 O | O20 | 0.48978 | 0.48189 | 0.27776 | 1 |
| 43 O | O21 | 0.46644 | 0.27128 | 0.71158 | 1 |
| 44 O | O22 | 0.12382 | 0.00237 | 0.47266 | 1 |
| 45 O | O23 | 0.09271 | 0.6926 | 0.48162 | 1 |
| 46 O | O24 | 0.1001 | 0.31553 | 0.47824 | 1 |
| 47 O | O25 | 0.75982 | 0.50164 | 0.04615 | 1 |
| 48 O | O26 | 0.90773 | 0.73777 | 0.02315 | 1 |
| 49 O | O27 | 0.90724 | 0.26579 | 0.02807 | 1 |
| 50 O | O28 | 0.78585 | 0.69427 | 0.25743 | 1 |
| 51 O | O29 | 0.75635 | 0.00176 | 0.26696 | 1 |
| 52 O | O30 | 0.77758 | 0.31276 | 0.26143 | 1 |
| 53 O | O31 | 0.87123 | 0.00153 | 0.69249 | 1 |
| 54 O | O32 | 0.71938 | 0.23532 | 0.71456 | 1 |
| 55 O | O33 | 0.87469 | 0.50348 | 0.47191 | 1 |
| 56 O | O34 | 0.72223 | 0.76573 | 0.71799 | 1 |
| 57 O | O35 | 0.65773 | 0.23875 | 0.02525 | 1 |
| 58 O | O36 | 0.65785 | 0.76255 | 0.01906 | 1 |
| 59 O | O37 | 0.50952 | 0.00026 | 0.03478 | 1 |
| 60 O | O38 | 0.84755 | 0.80919 | 0.48064 | 1 |
| 61 O | O39 | 0.84385 | 0.19125 | 0.47982 | 1 |
| 62 O | O40 | 0.99998 | 0.50328 | 0.26556 | 1 |
| 63 O | O41 | 0.5356 | 0.18004 | 0.25701 | 1 |
| 64 O | O42 | 0.54382 | 0.81976 | 0.25374 | 1 |
| 65 O | O43 | 0.97069 | 0.73723 | 0.71658 | 1 |
| 66 O | O44 | 0.61672 | 0.50046 | 0.68665 | 1 |
| 67 O | O45 | 0.59125 | 0.30029 | 0.47989 | 1 |
| 68 O | O46 | 0.60618 | 0.69428 | 0.47946 | 1 |
| 69 O | O47 | 0.6351 | 0.99954 | 0.47342 | 1 |
| 70 O | O48 | 0.96928 | 0.26731 | 0.71228 | 1 |
| 71 H | H1 | 0.32836 | -0.00066 | 0.23021 | 1 |
| 72 H | H2 | 0.25795 | 0.48572 | 0.47129 | 1 |
| 73 H | H3 | 0.58014 | 0.48215 | 0.25951 | 1 |
| 74 H | H4 | 0.03374 | 0.00262 | 0.49215 | 1 |
| 75 H | H5 | 0.78202 | 0.50229 | 0.47403 | 1 |
| 76 H | H6 | 0.84629 | 0.00254 | 0.24702 | 1 |
| 77 H | H7 | 0.09128 | 0.50075 | 0.25107 | 1 |
| 78 H | H8 | 0.54711 | 0.99752 | 0.50098 | 1 |
| 79 H | H9 | 0.35575 | 0.48926 | 0.59634 | 1 |
| 80 Mg | Mg1 | 0.44002 | 0.6763 | 0.36601 | 1 |
| 81 Fe | Fe1 | 0.93818 | 0.33781 | 0.36943 | 1 |

====================================================================================

====================================================================================

Title               (Q) Montmorillonite trans-vacant cis-Mg     H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (Q) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.54677  9.07216  9.65603  89.9876  91.3552  90.0700

Unit-cell volume = 923.649379 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.4409 | 0.31094 | 0.36458 | 1 |
| 2 Al | Al2 | 0.18832 | 0.83531 | 0.37082 | 1 |
| 3 Al | Al3 | 0.18476 | 0.16394 | 0.37046 | 1 |
| 4 Al | Al4 | 0.69168 | 0.16267 | 0.36907 | 1 |
| 5 Al | Al5 | 0.69266 | 0.83353 | 0.36728 | 1 |
| 6 Al | Al6 | 0.93824 | 0.33664 | 0.36839 | 1 |
| 7 Si | Si1 | 0.34996 | 0.83227 | 0.65121 | 1 |
| 8 Si | Si2 | 0.2753 | 0.67431 | 0.09294 | 1 |
| 9 Si | Si3 | 0.27725 | 0.3288 | 0.09282 | 1 |
| 10 Si | Si4 | 0.09892 | 0.32901 | 0.64999 | 1 |
| 11 Si | Si5 | 0.10144 | 0.67356 | 0.65133 | 1 |
| 12 Si | Si6 | 0.02626 | 0.17223 | 0.0897 | 1 |
| 13 Si | Si7 | 0.02758 | 0.82953 | 0.08887 | 1 |
| 14 Si | Si8 | 0.34933 | 0.16958 | 0.65282 | 1 |
| 15 Si | Si9 | 0.7784 | 0.67293 | 0.08744 | 1 |
| 16 Si | Si10 | 0.85226 | 0.82857 | 0.65112 | 1 |
| 17 Si | Si11 | 0.77679 | 0.32975 | 0.09018 | 1 |
| 18 Si | Si12 | 0.5999 | 0.32767 | 0.64913 | 1 |
| 19 Si | Si13 | 0.60499 | 0.67546 | 0.64757 | 1 |
| 20 Si | Si14 | 0.52745 | 0.16735 | 0.08571 | 1 |
| 21 Si | Si15 | 0.53123 | 0.8295 | 0.08496 | 1 |
| 22 Si | Si16 | 0.84978 | 0.17198 | 0.6498 | 1 |
| 23 O | O1 | 0.2555 | 0.50062 | 0.05315 | 1 |
| 24 O | O2 | 0.40823 | 0.73394 | 0.0314 | 1 |
| 25 O | O3 | 0.40664 | 0.2636 | 0.02874 | 1 |
| 26 O | O4 | 0.27289 | 0.695 | 0.26064 | 1 |
| 27 O | O5 | 0.24234 | 0.00174 | 0.2654 | 1 |
| 28 O | O6 | 0.22229 | 0.76277 | 0.71737 | 1 |
| 29 O | O7 | 0.34698 | 0.49326 | 0.49256 | 1 |
| 30 O | O8 | 0.21872 | 0.23581 | 0.71334 | 1 |
| 31 O | O9 | 0.37156 | 0.00153 | 0.70351 | 1 |
| 32 O | O10 | 0.283 | 0.30341 | 0.26339 | 1 |
| 33 O | O11 | 0.3435 | 0.1852 | 0.48162 | 1 |
| 34 O | O12 | 0.33823 | 0.82224 | 0.48324 | 1 |
| 35 O | O13 | 0.00815 | 0.00121 | 0.04638 | 1 |
| 36 O | O14 | 0.15717 | 0.76603 | 0.02316 | 1 |
| 37 O | O15 | 0.15679 | 0.23776 | 0.02801 | 1 |
| 38 O | O16 | 0.12266 | 0.50057 | 0.69164 | 1 |
| 39 O | O17 | 0.47035 | 0.73314 | 0.70719 | 1 |
| 40 O | O18 | 0.03159 | 0.80985 | 0.25947 | 1 |
| 41 O | O19 | 0.03118 | 0.19399 | 0.26005 | 1 |
| 42 O | O20 | 0.49001 | 0.48086 | 0.27711 | 1 |
| 43 O | O21 | 0.46592 | 0.27249 | 0.71248 | 1 |
| 44 O | O22 | 0.12458 | 0.00169 | 0.47281 | 1 |
| 45 O | O23 | 0.09471 | 0.69311 | 0.48104 | 1 |
| 46 O | O24 | 0.0947 | 0.30975 | 0.47953 | 1 |
| 47 O | O25 | 0.75878 | 0.50076 | 0.04654 | 1 |
| 48 O | O26 | 0.90918 | 0.73523 | 0.02385 | 1 |
| 49 O | O27 | 0.90658 | 0.26515 | 0.02622 | 1 |
| 50 O | O28 | 0.78605 | 0.69527 | 0.25762 | 1 |
| 51 O | O29 | 0.76206 | 0.00193 | 0.26883 | 1 |
| 52 O | O30 | 0.78305 | 0.31326 | 0.26096 | 1 |
| 53 O | O31 | 0.87149 | 0.00105 | 0.69206 | 1 |
| 54 O | O32 | 0.71863 | 0.23428 | 0.71265 | 1 |
| 55 O | O33 | 0.88239 | 0.50223 | 0.47243 | 1 |
| 56 O | O34 | 0.7234 | 0.76503 | 0.7184 | 1 |
| 57 O | O35 | 0.65666 | 0.2375 | 0.02693 | 1 |
| 58 O | O36 | 0.65918 | 0.7626 | 0.01863 | 1 |
| 59 O | O37 | 0.5092 | 0.99901 | 0.03315 | 1 |
| 60 O | O38 | 0.84783 | 0.80941 | 0.48081 | 1 |
| 61 O | O39 | 0.84882 | 0.19233 | 0.47936 | 1 |
| 62 O | O40 | 0.99623 | 0.50171 | 0.26598 | 1 |
| 63 O | O41 | 0.53018 | 0.17468 | 0.2578 | 1 |
| 64 O | O42 | 0.54555 | 0.82076 | 0.2531 | 1 |
| 65 O | O43 | 0.97193 | 0.73656 | 0.71597 | 1 |
| 66 O | O44 | 0.61915 | 0.50068 | 0.68659 | 1 |
| 67 O | O45 | 0.58893 | 0.30424 | 0.47971 | 1 |
| 68 O | O46 | 0.60646 | 0.69528 | 0.48006 | 1 |
| 69 O | O47 | 0.62979 | 0.99847 | 0.47338 | 1 |
| 70 O | O48 | 0.96829 | 0.2674 | 0.71386 | 1 |
| 71 H | H1 | 0.32822 | 0.00139 | 0.23127 | 1 |
| 72 H | H2 | 0.25692 | 0.49571 | 0.46264 | 1 |
| 73 H | H3 | 0.58118 | 0.48075 | 0.2633 | 1 |
| 74 H | H4 | 0.03614 | 0.00143 | 0.49889 | 1 |
| 75 H | H5 | 0.79474 | 0.50464 | 0.50132 | 1 |
| 76 H | H6 | 0.85473 | 0.00764 | 0.27309 | 1 |
| 77 H | H7 | 0.07249 | 0.5029 | 0.21169 | 1 |
| 78 H | H8 | 0.537 | 0.99955 | 0.47256 | 1 |
| 79 H | H9 | 0.34711 | 0.4912 | 0.59414 | 1 |
| 80 Mg | Mg1 | 0.44142 | 0.67639 | 0.36607 | 1 |
| 81 Fe | Fe1 | 0.9402 | 0.66847 | 0.36838 | 1 |

====================================================================================

====================================================================================

Title               (R) Montmorillonite trans-vacant cis-Mg     H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (R) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.54677  9.07216  9.65603  89.9876  91.3552  90.0700

Unit-cell volume = 923.649379 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.4409 | 0.31094 | 0.36458 | 1 |
| 2 Al | Al2 | 0.18832 | 0.83531 | 0.37082 | 1 |
| 3 Al | Al3 | 0.18476 | 0.16394 | 0.37046 | 1 |
| 4 Al | Al4 | 0.9402 | 0.66847 | 0.36838 | 1 |
| 5 Al | Al5 | 0.69266 | 0.83353 | 0.36728 | 1 |
| 6 Al | Al6 | 0.93824 | 0.33664 | 0.36839 | 1 |
| 7 Si | Si1 | 0.34996 | 0.83227 | 0.65121 | 1 |
| 8 Si | Si2 | 0.2753 | 0.67431 | 0.09294 | 1 |
| 9 Si | Si3 | 0.27725 | 0.3288 | 0.09282 | 1 |
| 10 Si | Si4 | 0.09892 | 0.32901 | 0.64999 | 1 |
| 11 Si | Si5 | 0.10144 | 0.67356 | 0.65133 | 1 |
| 12 Si | Si6 | 0.02626 | 0.17223 | 0.0897 | 1 |
| 13 Si | Si7 | 0.02758 | 0.82953 | 0.08887 | 1 |
| 14 Si | Si8 | 0.34933 | 0.16958 | 0.65282 | 1 |
| 15 Si | Si9 | 0.7784 | 0.67293 | 0.08744 | 1 |
| 16 Si | Si10 | 0.85226 | 0.82857 | 0.65112 | 1 |
| 17 Si | Si11 | 0.77679 | 0.32975 | 0.09018 | 1 |
| 18 Si | Si12 | 0.5999 | 0.32767 | 0.64913 | 1 |
| 19 Si | Si13 | 0.60499 | 0.67546 | 0.64757 | 1 |
| 20 Si | Si14 | 0.52745 | 0.16735 | 0.08571 | 1 |
| 21 Si | Si15 | 0.53123 | 0.8295 | 0.08496 | 1 |
| 22 Si | Si16 | 0.84978 | 0.17198 | 0.6498 | 1 |
| 23 O | O1 | 0.2555 | 0.50062 | 0.05315 | 1 |
| 24 O | O2 | 0.40823 | 0.73394 | 0.0314 | 1 |
| 25 O | O3 | 0.40664 | 0.2636 | 0.02874 | 1 |
| 26 O | O4 | 0.27289 | 0.695 | 0.26064 | 1 |
| 27 O | O5 | 0.24234 | 0.00174 | 0.2654 | 1 |
| 28 O | O6 | 0.22229 | 0.76277 | 0.71737 | 1 |
| 29 O | O7 | 0.34698 | 0.49326 | 0.49256 | 1 |
| 30 O | O8 | 0.21872 | 0.23581 | 0.71334 | 1 |
| 31 O | O9 | 0.37156 | 0.00153 | 0.70351 | 1 |
| 32 O | O10 | 0.283 | 0.30341 | 0.26339 | 1 |
| 33 O | O11 | 0.3435 | 0.1852 | 0.48162 | 1 |
| 34 O | O12 | 0.33823 | 0.82224 | 0.48324 | 1 |
| 35 O | O13 | 0.00815 | 0.00121 | 0.04638 | 1 |
| 36 O | O14 | 0.15717 | 0.76603 | 0.02316 | 1 |
| 37 O | O15 | 0.15679 | 0.23776 | 0.02801 | 1 |
| 38 O | O16 | 0.12266 | 0.50057 | 0.69164 | 1 |
| 39 O | O17 | 0.47035 | 0.73314 | 0.70719 | 1 |
| 40 O | O18 | 0.03159 | 0.80985 | 0.25947 | 1 |
| 41 O | O19 | 0.03118 | 0.19399 | 0.26005 | 1 |
| 42 O | O20 | 0.49001 | 0.48086 | 0.27711 | 1 |
| 43 O | O21 | 0.46592 | 0.27249 | 0.71248 | 1 |
| 44 O | O22 | 0.12458 | 0.00169 | 0.47281 | 1 |
| 45 O | O23 | 0.09471 | 0.69311 | 0.48104 | 1 |
| 46 O | O24 | 0.0947 | 0.30975 | 0.47953 | 1 |
| 47 O | O25 | 0.75878 | 0.50076 | 0.04654 | 1 |
| 48 O | O26 | 0.90918 | 0.73523 | 0.02385 | 1 |
| 49 O | O27 | 0.90658 | 0.26515 | 0.02622 | 1 |
| 50 O | O28 | 0.78605 | 0.69527 | 0.25762 | 1 |
| 51 O | O29 | 0.76206 | 0.00193 | 0.26883 | 1 |
| 52 O | O30 | 0.78305 | 0.31326 | 0.26096 | 1 |
| 53 O | O31 | 0.87149 | 0.00105 | 0.69206 | 1 |
| 54 O | O32 | 0.71863 | 0.23428 | 0.71265 | 1 |
| 55 O | O33 | 0.88239 | 0.50223 | 0.47243 | 1 |
| 56 O | O34 | 0.7234 | 0.76503 | 0.7184 | 1 |
| 57 O | O35 | 0.65666 | 0.2375 | 0.02693 | 1 |
| 58 O | O36 | 0.65918 | 0.7626 | 0.01863 | 1 |
| 59 O | O37 | 0.5092 | 0.99901 | 0.03315 | 1 |
| 60 O | O38 | 0.84783 | 0.80941 | 0.48081 | 1 |
| 61 O | O39 | 0.84882 | 0.19233 | 0.47936 | 1 |
| 62 O | O40 | 0.99623 | 0.50171 | 0.26598 | 1 |
| 63 O | O41 | 0.53018 | 0.17468 | 0.2578 | 1 |
| 64 O | O42 | 0.54555 | 0.82076 | 0.2531 | 1 |
| 65 O | O43 | 0.97193 | 0.73656 | 0.71597 | 1 |
| 66 O | O44 | 0.61915 | 0.50068 | 0.68659 | 1 |
| 67 O | O45 | 0.58893 | 0.30424 | 0.47971 | 1 |
| 68 O | O46 | 0.60646 | 0.69528 | 0.48006 | 1 |
| 69 O | O47 | 0.62979 | 0.99847 | 0.47338 | 1 |
| 70 O | O48 | 0.96829 | 0.2674 | 0.71386 | 1 |
| 71 H | H1 | 0.32822 | 0.00139 | 0.23127 | 1 |
| 72 H | H2 | 0.25692 | 0.49571 | 0.46264 | 1 |
| 73 H | H3 | 0.58118 | 0.48075 | 0.2633 | 1 |
| 74 H | H4 | 0.03614 | 0.00143 | 0.49889 | 1 |
| 75 H | H5 | 0.79474 | 0.50464 | 0.50132 | 1 |
| 76 H | H6 | 0.85473 | 0.00764 | 0.27309 | 1 |
| 77 H | H7 | 0.07249 | 0.5029 | 0.21169 | 1 |
| 78 H | H8 | 0.537 | 0.99955 | 0.47256 | 1 |
| 79 H | H9 | 0.34711 | 0.4912 | 0.59414 | 1 |
| 80 Mg | Mg1 | 0.44142 | 0.67639 | 0.36607 | 1 |
| 81 Fe | Fe1 | 0.69168 | 0.16267 | 0.36907 | 1 |

====================================================================================

====================================================================================

Title               (S) Montmorillonite trans-vacant cis-Mg     H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (S) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.52547  9.03844  9.50056  90.3360  91.1663  89.8747

Unit-cell volume = 903.619886 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.18786 | 0.83421 | 0.37087 | 1 |
| 2 Al | Al2 | 0.18508 | 0.16271 | 0.37017 | 1 |
| 3 Al | Al3 | 0.93948 | 0.66876 | 0.36902 | 1 |
| 4 Al | Al4 | 0.69198 | 0.83551 | 0.36809 | 1 |
| 5 Al | Al5 | 0.69226 | 0.16449 | 0.36971 | 1 |
| 6 Al | Al6 | 0.93819 | 0.33689 | 0.36958 | 1 |
| 7 Si | Si1 | 0.34953 | 0.83232 | 0.656 | 1 |
| 8 Si | Si2 | 0.27512 | 0.67406 | 0.08812 | 1 |
| 9 Si | Si3 | 0.27575 | 0.32902 | 0.08829 | 1 |
| 10 Si | Si4 | 0.09926 | 0.33046 | 0.65479 | 1 |
| 11 Si | Si5 | 0.10157 | 0.67463 | 0.65524 | 1 |
| 12 Si | Si6 | 0.02571 | 0.17187 | 0.08645 | 1 |
| 13 Si | Si7 | 0.0268 | 0.82811 | 0.08553 | 1 |
| 14 Si | Si8 | 0.34916 | 0.16887 | 0.65553 | 1 |
| 15 Si | Si9 | 0.77731 | 0.67253 | 0.08439 | 1 |
| 16 Si | Si10 | 0.85246 | 0.8312 | 0.65481 | 1 |
| 17 Si | Si11 | 0.77603 | 0.32963 | 0.08655 | 1 |
| 18 Si | Si12 | 0.60123 | 0.33007 | 0.65241 | 1 |
| 19 Si | Si13 | 0.60538 | 0.67711 | 0.6521 | 1 |
| 20 Si | Si14 | 0.52642 | 0.1704 | 0.08428 | 1 |
| 21 Si | Si15 | 0.53021 | 0.8304 | 0.08329 | 1 |
| 22 Si | Si16 | 0.85045 | 0.1745 | 0.65494 | 1 |
| 23 O | O1 | 0.25344 | 0.5005 | 0.04568 | 1 |
| 24 O | O2 | 0.4088 | 0.73287 | 0.02683 | 1 |
| 25 O | O3 | 0.40689 | 0.26665 | 0.02426 | 1 |
| 26 O | O4 | 0.27322 | 0.69203 | 0.25896 | 1 |
| 27 O | O5 | 0.24256 | 0.99987 | 0.26213 | 1 |
| 28 O | O6 | 0.22021 | 0.76764 | 0.72294 | 1 |
| 29 O | O7 | 0.3482 | 0.48464 | 0.48403 | 1 |
| 30 O | O8 | 0.2181 | 0.2344 | 0.7183 | 1 |
| 31 O | O9 | 0.37594 | 0.00195 | 0.70904 | 1 |
| 32 O | O10 | 0.27779 | 0.30721 | 0.26165 | 1 |
| 33 O | O11 | 0.34126 | 0.17728 | 0.48181 | 1 |
| 34 O | O12 | 0.33731 | 0.82039 | 0.48554 | 1 |
| 35 O | O13 | 0.00313 | 0.00016 | 0.04396 | 1 |
| 36 O | O14 | 0.15772 | 0.7679 | 0.01827 | 1 |
| 37 O | O15 | 0.15695 | 0.23438 | 0.02279 | 1 |
| 38 O | O16 | 0.12654 | 0.50205 | 0.69708 | 1 |
| 39 O | O17 | 0.46902 | 0.73137 | 0.7125 | 1 |
| 40 O | O18 | 0.03141 | 0.80855 | 0.25831 | 1 |
| 41 O | O19 | 0.03077 | 0.19389 | 0.25929 | 1 |
| 42 O | O20 | 0.50062 | 0.4823 | 0.27173 | 1 |
| 43 O | O21 | 0.46403 | 0.27778 | 0.71115 | 1 |
| 44 O | O22 | 0.12229 | 0.00115 | 0.47366 | 1 |
| 45 O | O23 | 0.09496 | 0.69213 | 0.48235 | 1 |
| 46 O | O24 | 0.09515 | 0.31106 | 0.48162 | 1 |
| 47 O | O25 | 0.75563 | 0.50031 | 0.04196 | 1 |
| 48 O | O26 | 0.90918 | 0.73221 | 0.01983 | 1 |
| 49 O | O27 | 0.90696 | 0.26629 | 0.02175 | 1 |
| 50 O | O28 | 0.78507 | 0.69446 | 0.25709 | 1 |
| 51 O | O29 | 0.75464 | 0.00243 | 0.2658 | 1 |
| 52 O | O30 | 0.78161 | 0.30989 | 0.25947 | 1 |
| 53 O | O31 | 0.87518 | 0.00359 | 0.69751 | 1 |
| 54 O | O32 | 0.71745 | 0.23381 | 0.7196 | 1 |
| 55 O | O33 | 0.88187 | 0.50325 | 0.47485 | 1 |
| 56 O | O34 | 0.72207 | 0.77082 | 0.72264 | 1 |
| 57 O | O35 | 0.65691 | 0.23517 | 0.02201 | 1 |
| 58 O | O36 | 0.65941 | 0.7655 | 0.01537 | 1 |
| 59 O | O37 | 0.50524 | 0.00066 | 0.03385 | 1 |
| 60 O | O38 | 0.84833 | 0.81105 | 0.48206 | 1 |
| 61 O | O39 | 0.84568 | 0.19607 | 0.48255 | 1 |
| 62 O | O40 | 0.99518 | 0.50087 | 0.26412 | 1 |
| 63 O | O41 | 0.53423 | 0.18175 | 0.25929 | 1 |
| 64 O | O42 | 0.54338 | 0.8206 | 0.25369 | 1 |
| 65 O | O43 | 0.97035 | 0.73542 | 0.72033 | 1 |
| 66 O | O44 | 0.62243 | 0.50266 | 0.69293 | 1 |
| 67 O | O45 | 0.59791 | 0.30591 | 0.47982 | 1 |
| 68 O | O46 | 0.60639 | 0.69484 | 0.48193 | 1 |
| 69 O | O47 | 0.63471 | 0.00165 | 0.47664 | 1 |
| 70 O | O48 | 0.96756 | 0.27254 | 0.71989 | 1 |
| 71 H | H1 | 0.32994 | 0.99944 | 0.23104 | 1 |
| 72 H | H2 | 0.25744 | 0.48267 | 0.45439 | 1 |
| 73 H | H3 | 0.59353 | 0.47633 | 0.27181 | 1 |
| 74 H | H4 | 0.03189 | 0.00035 | 0.49288 | 1 |
| 75 H | H5 | 0.79493 | 0.50587 | 0.50732 | 1 |
| 76 H | H6 | 0.84258 | 0.00275 | 0.23671 | 1 |
| 77 H | H7 | 0.07379 | 0.50149 | 0.21249 | 1 |
| 78 H | H8 | 0.54513 | 0.00078 | 0.49969 | 1 |
| 79 H | H9 | 0.35044 | 0.47488 | 0.58712 | 1 |
| 80 Mg | Mg1 | 0.44195 | 0.67737 | 0.36592 | 1 |
| 81 Fe | Fe1 | 0.43855 | 0.32043 | 0.36929 | 1 |

====================================================================================

====================================================================================

Title               (U) Montmorillonite trans-vacant cis-Mg     H[Al6MgFe]Si16O40(OH)8

Corresponds to configuration (U) in Table 1

Li et al., 2019 (submitted)

Lattice type        P

Space group name    P 1

Space group number  1

Setting number      1

Lattice parameters

a        b        c       alpha    beta     gamma

10.52547  9.03844  9.50056  90.3360  91.1663  89.8747

Unit-cell volume = 903.619886 Å^3

Structure parameters

|  |  | x | y | z | Occ. |
| --- | --- | --- | --- | --- | --- |
| 1 Al | Al1 | 0.18786 | 0.83421 | 0.37087 | 1 |
| 2 Al | Al2 | 0.18508 | 0.16271 | 0.37017 | 1 |
| 3 Al | Al3 | 0.93948 | 0.66876 | 0.36902 | 1 |
| 4 Al | Al4 | 0.43855 | 0.32043 | 0.36929 | 1 |
| 5 Al | Al5 | 0.69226 | 0.16449 | 0.36971 | 1 |
| 6 Al | Al6 | 0.93819 | 0.33689 | 0.36958 | 1 |
| 7 Si | Si1 | 0.34953 | 0.83232 | 0.656 | 1 |
| 8 Si | Si2 | 0.27512 | 0.67406 | 0.08812 | 1 |
| 9 Si | Si3 | 0.27575 | 0.32902 | 0.08829 | 1 |
| 10 Si | Si4 | 0.09926 | 0.33046 | 0.65479 | 1 |
| 11 Si | Si5 | 0.10157 | 0.67463 | 0.65524 | 1 |
| 12 Si | Si6 | 0.02571 | 0.17187 | 0.08645 | 1 |
| 13 Si | Si7 | 0.0268 | 0.82811 | 0.08553 | 1 |
| 14 Si | Si8 | 0.34916 | 0.16887 | 0.65553 | 1 |
| 15 Si | Si9 | 0.77731 | 0.67253 | 0.08439 | 1 |
| 16 Si | Si10 | 0.85246 | 0.8312 | 0.65481 | 1 |
| 17 Si | Si11 | 0.77603 | 0.32963 | 0.08655 | 1 |
| 18 Si | Si12 | 0.60123 | 0.33007 | 0.65241 | 1 |
| 19 Si | Si13 | 0.60538 | 0.67711 | 0.6521 | 1 |
| 20 Si | Si14 | 0.52642 | 0.1704 | 0.08428 | 1 |
| 21 Si | Si15 | 0.53021 | 0.8304 | 0.08329 | 1 |
| 22 Si | Si16 | 0.85045 | 0.1745 | 0.65494 | 1 |
| 23 O | O1 | 0.25344 | 0.5005 | 0.04568 | 1 |
| 24 O | O2 | 0.4088 | 0.73287 | 0.02683 | 1 |
| 25 O | O3 | 0.40689 | 0.26665 | 0.02426 | 1 |
| 26 O | O4 | 0.27322 | 0.69203 | 0.25896 | 1 |
| 27 O | O5 | 0.24256 | 0.99987 | 0.26213 | 1 |
| 28 O | O6 | 0.22021 | 0.76764 | 0.72294 | 1 |
| 29 O | O7 | 0.3482 | 0.48464 | 0.48403 | 1 |
| 30 O | O8 | 0.2181 | 0.2344 | 0.7183 | 1 |
| 31 O | O9 | 0.37594 | 0.00195 | 0.70904 | 1 |
| 32 O | O10 | 0.27779 | 0.30721 | 0.26165 | 1 |
| 33 O | O11 | 0.34126 | 0.17728 | 0.48181 | 1 |
| 34 O | O12 | 0.33731 | 0.82039 | 0.48554 | 1 |
| 35 O | O13 | 0.00313 | 0.00016 | 0.04396 | 1 |
| 36 O | O14 | 0.15772 | 0.7679 | 0.01827 | 1 |
| 37 O | O15 | 0.15695 | 0.23438 | 0.02279 | 1 |
| 38 O | O16 | 0.12654 | 0.50205 | 0.69708 | 1 |
| 39 O | O17 | 0.46902 | 0.73137 | 0.7125 | 1 |
| 40 O | O18 | 0.03141 | 0.80855 | 0.25831 | 1 |
| 41 O | O19 | 0.03077 | 0.19389 | 0.25929 | 1 |
| 42 O | O20 | 0.50062 | 0.4823 | 0.27173 | 1 |
| 43 O | O21 | 0.46403 | 0.27778 | 0.71115 | 1 |
| 44 O | O22 | 0.12229 | 0.00115 | 0.47366 | 1 |
| 45 O | O23 | 0.09496 | 0.69213 | 0.48235 | 1 |
| 46 O | O24 | 0.09515 | 0.31106 | 0.48162 | 1 |
| 47 O | O25 | 0.75563 | 0.50031 | 0.04196 | 1 |
| 48 O | O26 | 0.90918 | 0.73221 | 0.01983 | 1 |
| 49 O | O27 | 0.90696 | 0.26629 | 0.02175 | 1 |
| 50 O | O28 | 0.78507 | 0.69446 | 0.25709 | 1 |
| 51 O | O29 | 0.75464 | 0.00243 | 0.2658 | 1 |
| 52 O | O30 | 0.78161 | 0.30989 | 0.25947 | 1 |
| 53 O | O31 | 0.87518 | 0.00359 | 0.69751 | 1 |
| 54 O | O32 | 0.71745 | 0.23381 | 0.7196 | 1 |
| 55 O | O33 | 0.88187 | 0.50325 | 0.47485 | 1 |
| 56 O | O34 | 0.72207 | 0.77082 | 0.72264 | 1 |
| 57 O | O35 | 0.65691 | 0.23517 | 0.02201 | 1 |
| 58 O | O36 | 0.65941 | 0.7655 | 0.01537 | 1 |
| 59 O | O37 | 0.50524 | 0.00066 | 0.03385 | 1 |
| 60 O | O38 | 0.84833 | 0.81105 | 0.48206 | 1 |
| 61 O | O39 | 0.84568 | 0.19607 | 0.48255 | 1 |
| 62 O | O40 | 0.99518 | 0.50087 | 0.26412 | 1 |
| 63 O | O41 | 0.53423 | 0.18175 | 0.25929 | 1 |
| 64 O | O42 | 0.54338 | 0.8206 | 0.25369 | 1 |
| 65 O | O43 | 0.97035 | 0.73542 | 0.72033 | 1 |
| 66 O | O44 | 0.62243 | 0.50266 | 0.69293 | 1 |
| 67 O | O45 | 0.59791 | 0.30591 | 0.47982 | 1 |
| 68 O | O46 | 0.60639 | 0.69484 | 0.48193 | 1 |
| 69 O | O47 | 0.63471 | 0.00165 | 0.47664 | 1 |
| 70 O | O48 | 0.96756 | 0.27254 | 0.71989 | 1 |
| 71 H | H1 | 0.32994 | 0.99944 | 0.23104 | 1 |
| 72 H | H2 | 0.25744 | 0.48267 | 0.45439 | 1 |
| 73 H | H3 | 0.59353 | 0.47633 | 0.27181 | 1 |
| 74 H | H4 | 0.03189 | 0.00035 | 0.49288 | 1 |
| 75 H | H5 | 0.79493 | 0.50587 | 0.50732 | 1 |
| 76 H | H6 | 0.84258 | 0.00275 | 0.23671 | 1 |
| 77 H | H7 | 0.07379 | 0.50149 | 0.21249 | 1 |
| 78 H | H8 | 0.54513 | 0.00078 | 0.49969 | 1 |
| 79 H | H9 | 0.35044 | 0.47488 | 0.58712 | 1 |
| 80 Mg | Mg1 | 0.44195 | 0.67737 | 0.36592 | 1 |
| 81 Fe | Fe1 | 0.69198 | 0.83551 | 0.36809 | 1 |

====================================================================================