Supporting information

# SYNTHESIS, STRUCTURE AND FERROELECTRICITY OF KAOLINITE-p-AMINOBENZAMIDE INTERCALATION COMPOUND

SHUN-PING ZHAO1*, YU GUO2, MIAO-MIAO ZHU1, JIE WANG1, XIAO-LIANG FENG1, QIAO QIAO3, AND HENG XU1

1Anhui Key Laboratory of Photoelectric-Magnetic Functional Materials, Anhui Key Laboratory of Functional Coordination Compounds, Institutes and School of Chemistry and Chemical Engineering, Anqing Normal University, Anqing 246011, P.R. China

2 School of Physics and Electrical Engineering, Anqing Normal University, Anqing 246011, P.R. China

3 State Key Laboratory of Materials-Oriented Chemical Engineering and College of Chemistry and Molecular Engineering, Nanjing Tech University, Nanjing 210009, P. R. China

Email: zsp200109@163.com

Table S1 Comparison of optimized structural models

|  | A model | B model |
| --- | --- | --- |
| space group | P1 | P1 |
| a, b, c(Å) | 5.35/9.79/14.50 | 5.35/ 9.75/ 14.50 |
| α, β, γ(°) | 91.55/94.31/88.03 | 93.25/ 91.81/ 84.97 |
| V(Å3) | 756.19 | 751.74 |
| Intermolecular hydrogen bonds | N2-H…O(Al-sheet) N1-H…O(Si- sheet) N1-H…O1 | O1…H-O(Al-sheet) N2…H- O(Si- sheet) N1-H…O1 |

Table S2 optimized parameters of PABA molecular

|  |  | ## A model | ## B model | ## crystal[1,2] |
| --- | --- | --- | --- | --- |
| Bond length(Å) | C1-C7 | 1.466 | 1.502 | 1.490 |
|  | C7-O1 | 1.381 | 1.345 | 1.220 |
|  | C7-N1 | 1.446 | 1.427 | 1.353 |
|  | C4-N2 | 1.428 | 1.467 | 1.391 |
| angle(degree) | ∠1 | 109.946 | 102.652 | 149.794 |
|  | ∠2 | 103.272 | 113.015 | 85.285 |
| Torsion angle(degree) | H8-N2-C4-C5 | 33.009 | -3.891 | -47.645 |
|  | H1-N2-C4-C3 | -27.881 | 53.371 | -18.939 |
|  | O1-C7-C1-C2 | 17.530 | 36.199 | -25.468 |
|  | N1-C7-C1-C6 | 18.426 | 43.148 | -29.579 |
|  | H7-N1-C7-C1 | -2.624 | -17.776 | 32.721 |
|  | H6-N1-C7-O1 | -66.377 | 31.493 | -29.831 |

[1] Alléaume, M.,1967. Etude cristallographique de composés sulfamidés (Doctoral dissertation, Université de Bordeaux).

[2] Berkovitch-Yellin, Z., Van Mil, J., Addadi, L., Idelson, M., Lahav, M., Leiserowitz, L.,1985. Crystal morphology engineering by" tailor-made" inhibitors; a new probe to fine intermolecular interactions. J. Amer. Chem. Soc. 107(11), 3111-3122.

Fig.S1  Simulated and experimental XRD patterns of K-PABA.

Fig.S2 The optimized structural model B of K-PABA viewed along b axis: the amino group closed to Al-sheet. Different hydrogen bonds are marked on the graph, 1 and 2  respectively refer to intermolecular hydrogen bonds formed in amino groups-kaolinite, amide groups-kaolinite, while 3 refers to intermolecular hydrogen bonds between PABA molecules.

Fig.S3 Schematic diagram of molecular dimension