The pH values were measured using a Lab860 pH-meter (Schott Instrument, Hattenbergstrasse, Germany) at 25°C, with a water to powder mass ratio of 10.

Fig. pH values of (K5(1-x)A25(x)) mixtures calcined at  (●) 600 and (■) 750 °C

Table  Mineral phases determined by XRD and associated chemical formula and JCPDS files

| Mineral phase | Chemical formula | JCPDS files |
| --- | --- | --- |
| Quartz | SiO2 | 01-086-1630 |
| Calcite | CaCO3 | 04-012-0489 |
| Arcanite | K2SO4 | 04-006-8317 |
| Muscovite | KAl3Si3O10(OH)2 | 01-082-3733 |
| Dehydroxylated muscovite | KAl3Si3O11 | 00-046-0741 |
| Zeolite type | KAlSiO4 | 00-048-1028 |
| Leucite type | KAlSi2O6 | 01-071-1147 |
| Diopside | CaMgSi2O6 | 00-041-1370 |
| Wollastonite | CaSiO3 | 00-027-0088 |
| Hematite | Fe2O3 | 00-033-0664 |
| Anatase | TiO2 | 01-071-1166 |
| Krotite | CaAl2O4 | 04-013-0779 |