|  | 1- Funnel 2-0.45μm microporous membrane 3-Metal clamp 4- Flask 5-Vacuum pump |
| --- | --- |
| Fig. S1 Sand core filtration device |  |

|  | 1-Lid of Stainless steel reactor 2-Stainless steel backing board 3-Stainless steel rod 4- Stainless steel reinforcing gland 5-Lid of PTFE reactor 6- PTFE reactor 7- Stainless steel reactor |
| --- | --- |
| Fig. S2 The high temperature stainless steel reactor |  |

Fig. S3 The schematic diagram of asphaltene adsorbed on the mineral Fig. S4 Height of the clay minerals under various conditions.

Table S1 The parameters of Fig. 7a

|  |  | Value | Standard Error | t-Value | Prob>¦t¦ |
| --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Intercept | 331.3714 | 17.9427 | 18.4683 | 0.0000 |
|  | Slope | 0.2654 | 0.0452 | 5.8779 | 0.0020 |
| Quartz sand (200 mesh) | Intercept | 120.0356 | 13.2983 | 9.0264 | 0.0003 |
|  | Slope | 0.2622 | 0.0358 | 7.3306 | 0.0007 |
| Montmorillonite (200 mesh) | Intercept | 2.3108 | 0.5057 | 4.5697 | 0.0060 |
|  | Slope | 0.0617 | 0.0095 | 6.4910 | 0.0013 |
| Kaolinite (200 mesh) | Intercept | 9.3475 | 0.8766 | 10.6631 | 0.0001 |
|  | Slope | 0.0561 | 0.0081 | 6.9311 | 0.0010 |
| Illite (200 mesh) | Intercept | 48.3230 | 11.8667 | 4.0722 | 0.0096 |
|  | Slope | 0.3777 | 0.0336 | 11.2550 | 0.0001 |
| Chlorite (200 mesh) | Intercept | 3.1734 | 0.5225 | 6.0740 | 0.0018 |
|  | Slope | 0.0620 | 0.0086 | 7.2284 | 0.0008 |

Table S2 The statistics of Fig. 7a

|  | Quartz sand (60 mesh) | Quartz sand (200 mesh) | Montmorillonite (200 mesh) | Kaolinite (200 mesh) | Illite (200 mesh) | Chlorite (200 mesh) |
| --- | --- | --- | --- | --- | --- | --- |
| Number of Points | 7 | 7 | 7 | 7 | 7 | 7 |
| Degrees of Freedom | 5 | 5 | 5 | 5 | 5 | 5 |
| Residual Sum of Squares | 6674.0118 | 3756.5911 | 6.0440 | 17.1383 | 3106.7610 | 6.5333 |
| Pearson's r | 0.9347 | 0.9565 | 0.9455 | 0.9517 | 0.9808 | 0.9553 |
| R-Square (COD) | 0.8736 | 0.9149 | 0.9357 | 0.9290 | 0.9674 | 0.8489 |
| Adj. R-Square | 0.8483 | 0.8979 | 0.8727 | 0.8869 | 0.9544 | 0.8952 |

Table S3 The ANOVA of Fig. 7a

|  |  | DF | Sum of Squares | Mean Square | F Value | Prob>F |
| --- | --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Model | 1 | 46116.9727 | 46116.9727 | 34.5497 | 0.0020 |
|  | Error | 5 | 6674.0118 | 1334.8024 |  |  |
|  | Total | 6 | 52790.9846 |  |  |  |
| Quartz sand (200 mesh) | Model | 1 | 40373.7013 | 40373.7013 | 53.7372 | 0.0007 |
|  | Error | 5 | 3756.5911 | 751.3182 |  |  |
|  | Total | 6 | 44130.2925 |  |  |  |
| Montmorillonite (200 mesh) | Model | 1 | 50.9314 | 50.9314 | 42.1336 | 0.0013 |
|  | Error | 5 | 6.0440 | 1.2088 |  |  |
|  | Total | 6 | 56.9754 |  |  |  |
| Kaolinite (200 mesh) | Model | 1 | 164.6665 | 164.6665 | 48.0406 | 0.0010 |
|  | Error | 5 | 17.1383 | 3.4277 |  |  |
|  | Total | 6 | 181.8048 |  |  |  |
| Illite (200 mesh) | Model | 1 | 78709.7855 | 78709.7855 | 126.6750 | 0.0001 |
|  | Error | 5 | 3106.7610 | 621.3522 |  |  |
|  | Total | 6 | 81816.5465 |  |  |  |
| Chlorite (200 mesh) | Model | 1 | 68.2729 | 68.2729 | 52.2496 | 0.0008 |
|  | Error | 5 | 6.5333 | 1.3067 |  |  |
|  | Total | 6 | 74.8063 |  |  |  |

Table S4 The parameters of Fig. 7b

|  |  | Value | Standard Error | t-Value | Prob>¦t¦ |
| --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Intercept | 202.0866 | 23.3165 | 8.6671 | 0.0003 |
|  | Slope | 0.2070 | 0.0605 | 3.4201 | 0.0188 |
| Quartz sand (200 mesh) | Intercept | 43.0438 | 2.3072 | 18.6560 | 0.0000 |
|  | Slope | 0.0646 | 0.0087 | 7.4438 | 0.0007 |
| Montmorillonite (200 mesh) | Intercept | 0.8707 | 0.0426 | 20.4385 | 0.0000 |
|  | Slope | 0.0085 | 0.0062 | 1.3645 | 0.2306 |
| Kaolinite (200 mesh) | Intercept | 1.0733 | 0.0693 | 15.4954 | 0.0000 |
|  | Slope | 0.0376 | 0.0047 | 8.0101 | 0.0005 |
| Illite (200 mesh) | Intercept | 4.2405 | 0.4242 | 9.9963 | 0.0002 |
|  | Slope | 0.0682 | 0.0071 | 9.6022 | 0.0002 |
| Chlorite (200 mesh) | Intercept | 0.7147 | 0.0491 | 14.5588 | 0.0000 |
|  | Slope | 0.0238 | 0.0062 | 3.8161 | 0.0124 |

Table S5 The statistics of Fig. 7b

|  | Quartz sand (60 mesh) | Quartz sand (200 mesh) | Montmorillonite (200 mesh) | Kaolinite (200 mesh) | Illite (200 mesh) | Chlorite (200 mesh) |
| --- | --- | --- | --- | --- | --- | --- |
| Number of Points | 7 | 7 | 7 | 7 | 7 | 7 |
| Degrees of Freedom | 5 | 5 | 5 | 5 | 5 | 5 |
| Residual Sum of Squares | 11381.0141 | 112.9191 | 0.0350 | 0.1079 | 4.1101 | 0.0508 |
| Pearson's r | 0.8370 | 0.9577 | 0.5209 | 0.9632 | 0.9739 | 0.8628 |
| R-Square (COD) | 0.7553 | 0.9172 | 0.7540 | 0.7556 | 0.8956 | 0.9486 |
| Adj. R-Square | 0.6407 | 0.9007 | 0.1256 | 0.9133 | 0.9383 | 0.6933 |

Table S6 The ANOVA of Fig. 7b

|  |  | DF | Sum of Squares | Mean Square | F Value | Prob>F |
| --- | --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Model | 1 | 26624.3791 | 26624.3791 | 11.6968 | 0.0188 |
|  | Error | 5 | 11381.0141 | 2276.2028 |  |  |
|  | Total | 6 | 38005.3932 |  |  |  |
| Quartz sand (200 mesh) | Model | 1 | 1251.3601 | 1251.3601 | 55.4096 | 0.0007 |
|  | Error | 5 | 112.9191 | 22.5838 |  |  |
|  | Total | 6 | 1364.2791 |  |  |  |
| Montmorillonite (200 mesh) | Model | 1 | 0.0130 | 0.0130 | 1.8619 | 0.2306 |
|  | Error | 5 | 0.0350 | 0.0070 |  |  |
|  | Total | 6 | 0.0480 |  |  |  |
| Kaolinite (200 mesh) | Model | 1 | 1.3845 | 1.3845 | 64.1610 | 0.0005 |
|  | Error | 5 | 0.1079 | 0.0216 |  |  |
|  | Total | 6 | 1.4924 |  |  |  |
| Illite (200 mesh) | Model | 1 | 75.7912 | 75.7912 | 92.2022 | 0.0002 |
|  | Error | 5 | 4.1101 | 0.8220 |  |  |
|  | Total | 6 | 79.9013 |  |  |  |
| Chlorite (200 mesh) | Model | 1 | 0.1479 | 0.1479 | 14.5628 | 0.0124 |
|  | Error | 5 | 0.0508 | 0.0102 |  |  |
|  | Total | 6 | 0.1987 |  |  |  |

Table S7 The parameters of Fig. 8a

|  |  | Value | Standard Error | t-Value | Prob>¦t¦ |
| --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Intercept | 200.0165 | 25.1126 | 7.9648 | 0.0005 |
|  | Slope | 6.2630 | 0.0592 | 105.8294 | 0.0000 |
| Quartz sand (200 mesh) | Intercept | 155.7049 | 10.6927 | 14.5617 | 0.0000 |
|  | Slope | 0.6497 | 0.0278 | 23.3922 | 0.0000 |
| Montmorillonite (200 mesh) | Intercept | 22.8970 | 8.3817 | 2.7318 | 0.0412 |
|  | Slope | 0.4477 | 0.0240 | 18.6210 | 0.0000 |
| Kaolinite (200 mesh) | Intercept | 25.9598 | 6.2369 | 4.1623 | 0.0088 |
|  | Slope | 0.7103 | 0.0155 | 45.7701 | 0.0000 |
| Illite (200 mesh) | Intercept | 64.8197 | 7.4379 | 8.7148 | 0.0003 |
|  | Slope | 1.0873 | 0.0182 | 59.6395 | 0.0000 |
| Chlorite (200 mesh) | Intercept | 25.4224 | 7.1930 | 3.5343 | 0.0167 |
|  | Slope | 0.5058 | 0.0177 | 28.5381 | 0.0000 |

Table S8 The statistics of Fig. 8a

|  | Quartz sand (60 mesh) | Quartz sand (200 mesh) | Montmorillonite (200 mesh) | Kaolinite (200 mesh) | Illite (200 mesh) | Chlorite (200 mesh) |
| --- | --- | --- | --- | --- | --- | --- |
| Number of Points | 7 | 7 | 7 | 7 | 7 | 7 |
| Degrees of Freedom | 5 | 5 | 5 | 5 | 5 | 5 |
| Residual Sum of Squares | 13060.0123 | 2398.1972 | 1614.5079 | 897.4346 | 1200.1857 | 1200.9475 |
| Pearson's r | 0.9998 | 0.9955 | 0.9929 | 0.9988 | 0.9993 | 0.9969 |
| R-Square (COD) | 0.9996 | 0.9909 | 0.9903 | 0.9988 | 0.9992 | 0.9963 |
| Adj. R-Square | 0.9995 | 0.9891 | 0.9829 | 0.9971 | 0.9983 | 0.9927 |

Table S9 The ANOVA of Fig. 8a

|  |  | DF | Sum of Squares | Mean Square | F Value | Prob>F |
| --- | --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Model | 1 | 29254100.0000 | 29254100.0000 | 11199.8714 | 1.4E-09 |
|  | Error | 5 | 13060.0123 | 2612.0025 |  |  |
|  | Total | 6 | 29267200.0000 |  |  |  |
| Quartz sand (200 mesh) | Model | 1 | 262456.1832 | 262456.1832 | 547.1948 | 2.7E-06 |
|  | Error | 5 | 2398.1972 | 479.6394 |  |  |
|  | Total | 6 | 264854.3804 |  |  |  |
| Montmorillonite (200 mesh) | Model | 1 | 111963.8950 | 111963.8950 | 346.7431 | 8.2E-06 |
|  | Error | 5 | 1614.5079 | 322.9016 |  |  |
|  | Total | 6 | 113578.4029 |  |  |  |
| Kaolinite (200 mesh) | Model | 1 | 376007.4192 | 376007.4192 | 2094.9016 | 9.4E-08 |
|  | Error | 5 | 897.4346 | 179.4869 |  |  |
|  | Total | 6 | 376904.8537 |  |  |  |
| Illite (200 mesh) | Model | 1 | 853781.7914 | 853781.7914 | 3556.8737 | 2.5E-08 |
|  | Error | 5 | 1200.1857 | 240.0371 |  |  |
|  | Total | 6 | 854981.9772 |  |  |  |
| Chlorite (200 mesh) | Model | 1 | 195615.8874 | 195615.8874 | 814.4231 | 9.9E-07 |
|  | Error | 5 | 1200.9475 | 240.1895 |  |  |
|  | Total | 6 | 196816.8349 |  |  |  |

Table S10 The parameters of Fig. 8b

|  |  | Value | Standard Error | t-Value | Prob>¦t¦ |
| --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Intercept | 207.3681 | 29.2335 | 7.0935 | 0.0009 |
|  | Slope | 2.5643 | 0.0690 | 37.1622 | 0.0000 |
| Quartz sand (200 mesh) | Intercept | 113.8163 | 12.7957 | 8.8949 | 0.0003 |
|  | Slope | 0.6735 | 0.0320 | 21.0803 | 0.0000 |
| Montmorillonite (200 mesh) | Intercept | 14.8691 | 3.1523 | 4.7169 | 0.0053 |
|  | Slope | 0.1824 | 0.0133 | 13.7066 | 0.0000 |
| Kaolinite (200 mesh) | Intercept | 25.7601 | 7.9468 | 3.2416 | 0.0229 |
|  | Slope | 0.4133 | 0.0222 | 18.6043 | 0.0000 |
| Illite (200 mesh) | Intercept | 72.9262 | 6.4822 | 11.2503 | 0.0001 |
|  | Slope | 0.2973 | 0.0181 | 16.4508 | 0.0000 |
| Chlorite (200 mesh) | Intercept | 20.3701 | 4.7526 | 4.2861 | 0.0078 |
|  | Slope | 0.2383 | 0.0148 | 16.1012 | 0.0000 |

Table S11 The statistics of Fig. 8b

|  | Quartz sand (60 mesh) | Quartz sand (200 mesh) | Montmorillonite (200 mesh) | Kaolinite (200 mesh) | Illite (200 mesh) | Chlorite (200 mesh) |
| --- | --- | --- | --- | --- | --- | --- |
| Number of Points | 7 | 7 | 7 | 7 | 7 | 7 |
| Degrees of Freedom | 5 | 5 | 5 | 5 | 5 | 5 |
| Residual Sum of Squares | 17930.8232 | 3495.6113 | 228.3608 | 1459.8942 | 913.5904 | 526.4574 |
| Pearson's r | 0.9982 | 0.9944 | 0.9870 | 0.9929 | 0.9909 | 0.9905 |
| R-Square (COD) | 0.9964 | 0.9903 | 0.9741 | 0.9858 | 0.9819 | 0.9811 |
| Adj. R-Square | 0.9957 | 0.9867 | 0.9689 | 0.9829 | 0.9782 | 0.9773 |

Table S12 The ANOVA of Fig. 8b

|  |  | DF | Sum of Squares | Mean Square | F Value | Prob>F |
| --- | --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Model | 1 | 4952595.1308 | 4952595.1308 | 1381.0284 | 2.66E-07 |
|  | Error | 5 | 17930.8232 | 3586.1646 |  |  |
|  | Total | 6 | 4970525.9539 |  |  |  |
| Quartz sand (200 mesh) | Model | 1 | 310676.4537 | 310676.4537 | 444.3807 | 4.45E-06 |
|  | Error | 5 | 3495.6113 | 699.1223 |  |  |
|  | Total | 6 | 314172.0650 |  |  |  |
| Montmorillonite (200 mesh) | Model | 1 | 8580.5077 | 8580.5077 | 187.8717 | 3.71E-05 |
|  | Error | 5 | 228.3608 | 45.6722 |  |  |
|  | Total | 6 | 8808.8685 |  |  |  |
| Kaolinite (200 mesh) | Model | 1 | 101059.9126 | 101059.9126 | 346.1207 | 8.26E-06 |
|  | Error | 5 | 1459.8942 | 291.9788 |  |  |
|  | Total | 6 | 102519.8068 |  |  |  |
| Illite (200 mesh) | Model | 1 | 49448.9377 | 49448.9377 | 270.6297 | 1.51E-05 |
|  | Error | 5 | 913.5904 | 182.7181 |  |  |
|  | Total | 6 | 50362.5281 |  |  |  |
| Chlorite (200 mesh) | Model | 1 | 27296.4864 | 27296.4864 | 259.2469 | 1.68E-05 |
|  | Error | 5 | 526.4574 | 105.2915 |  |  |
|  | Total | 6 | 27822.9438 |  |  |  |

Table S13 The parameters of Fig. 9a

|  |  | Value | Standard Error | t-Value | Prob>¦t¦ |
| --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Intercept | -5.1318 | 0.0269 | -190.7853 | 7.51E-11 |
|  | Slope | 0.8266 | 0.0054 | 152.4539 | 2.30E-10 |
| Quartz sand (200 mesh) | Intercept | -3.6197 | 0.0334 | -108.3711 | 1.27E-09 |
|  | Slope | 0.6790 | 0.0069 | 97.9810 | 2.10E-09 |
| Montmorillonite (200 mesh) | Intercept | -0.3051 | 0.0356 | -8.5682 | 3.57E-04 |
|  | Slope | 0.5887 | 0.0128 | 45.8707 | 9.30E-08 |
| Kaolinite (200 mesh) | Intercept | -1.6510 | 0.0411 | -40.1959 | 1.80E-07 |
|  | Slope | 0.7402 | 0.0116 | 63.8155 | 1.79E-08 |
| Illite (200 mesh) | Intercept | -2.0416 | 0.0879 | -23.2396 | 2.75E-06 |
|  | Slope | 0.4378 | 0.0189 | 23.1685 | 2.79E-06 |
| Chlorite (200 mesh) | Intercept | -0.7080 | 0.0717 | -9.8742 | 1.82E-04 |
|  | Slope | 0.6578 | 0.0253 | 26.0241 | 1.57E-06 |

Table S14 The statistics of Fig. 9a

|  | Quartz sand (60 mesh) | Quartz sand (200 mesh) | Montmorillonite (200 mesh) | Kaolinite (200 mesh) | Illite (200 mesh) | Chlorite (200 mesh) |
| --- | --- | --- | --- | --- | --- | --- |
| Number of Points | 7 | 7 | 7 | 7 | 7 | 7 |
| Degrees of Freedom | 5 | 5 | 5 | 5 | 5 | 5 |
| Residual Sum of Squares | 0.0016 | 0.0029 | 0.0183 | 0.0094 | 0.0268 | 0.0627 |
| Pearson's r | 0.9999 | 0.9997 | 0.9988 | 0.9994 | 0.9954 | 0.9963 |
| R-Square (COD) | 0.9998 | 0.9995 | 0.9976 | 0.9988 | 0.9908 | 0.9927 |
| Adj. R-Square | 0.9997 | 0.9994 | 0.9972 | 0.9985 | 0.9889 | 0.9912 |

Table S15 The ANOVA of Fig. 9a

|  |  | DF | Sum of Squares | Mean Square | F Value | Prob>F |
| --- | --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Model | 1 | 7.2036 | 7.2036 | 23242.1824 | 2.30E-10 |
|  | Error | 5 | 0.0016 | 0.0003 |  |  |
|  | Total | 6 | 7.2052 |  |  |  |
| Quartz sand (200 mesh) | Model | 1 | 5.6136 | 5.6136 | 9600.2666 | 2.10E-09 |
|  | Error | 5 | 0.0029 | 0.0006 |  |  |
|  | Total | 6 | 5.6165 |  |  |  |
| Montmorillonite (200 mesh) | Model | 1 | 7.6821 | 7.6821 | 2104.1250 | 9.30E-08 |
|  | Error | 5 | 0.0183 | 0.0037 |  |  |
|  | Total | 6 | 7.7003 |  |  |  |
| Kaolinite (200 mesh) | Model | 1 | 7.6343 | 7.6343 | 4072.4237 | 1.79E-08 |
|  | Error | 5 | 0.0094 | 0.0019 |  |  |
|  | Total | 6 | 7.6437 |  |  |  |
| Illite (200 mesh) | Model | 1 | 2.8742 | 2.8742 | 536.7794 | 2.79E-06 |
|  | Error | 5 | 0.0268 | 0.0054 |  |  |
|  | Total | 6 | 2.9010 |  |  |  |
| Chlorite (200 mesh) | Model | 1 | 8.4914 | 8.4914 | 677.2560 | 1.57E-06 |
|  | Error | 5 | 0.0627 | 0.0125 |  |  |
|  | Total | 6 | 8.5541 |  |  |  |

Table S16 The parameters of Fig. 9b

|  |  | Value | Standard Error | t-Value | Prob>¦t¦ |
| --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Intercept | -4.3528 | 0.1272 | -34.2098 | 4.01E-07 |
|  | Slope | 0.7609 | 0.0260 | 29.3217 | 8.65E-07 |
| Quartz sand (200 mesh) | Intercept | -3.1541 | 0.0926 | -34.0574 | 4.10E-07 |
|  | Slope | 0.8153 | 0.0205 | 39.7777 | 1.89E-07 |
| Montmorillonite (200 mesh) | Intercept | 0.0716 | 0.0436 | 1.6428 | 1.61E-01 |
|  | Slope | 1.1015 | 0.0335 | 32.8568 | 4.91E-07 |
| Kaolinite (200 mesh) | Intercept | -0.0726 | 0.0535 | -1.3564 | 2.33E-01 |
|  | Slope | 0.9413 | 0.0332 | 28.3352 | 1.03E-06 |
| Illite (200 mesh) | Intercept | -1.1383 | 0.0856 | -13.2949 | 4.30E-05 |
|  | Slope | 0.7432 | 0.0290 | 25.6197 | 1.69E-06 |
| Chlorite (200 mesh) | Intercept | 0.3807 | 0.0440 | 8.6558 | 3.40E-04 |
|  | Slope | 0.8236 | 0.0281 | 29.3225 | 8.65E-07 |

Table S17 The statistics of Fig. 9b

|  | Quartz sand (60 mesh) | Quartz sand (200 mesh) | Montmorillonite (200 mesh) | Kaolinite (200 mesh) | Illite (200 mesh) | Chlorite (200 mesh) |
| --- | --- | --- | --- | --- | --- | --- |
| Number of Points | 7 | 7 | 7 | 7 | 7 | 7 |
| Degrees of Freedom | 5 | 5 | 5 | 5 | 5 | 5 |
| Residual Sum of Squares | 0.0374 | 0.0241 | 0.0402 | 0.0536 | 0.0543 | 0.0522 |
| Pearson's r | 0.9971 | 0.9984 | 0.9977 | 0.9969 | 0.9962 | 0.9971 |
| R-Square (COD) | 0.9942 | 0.9968 | 0.9954 | 0.9937 | 0.9909 | 0.9917 |
| Adj. R-Square | 0.9931 | 0.9962 | 0.9945 | 0.9926 | 0.9909 | 0.9931 |

Table S18 The ANOVA of Fig. 9b

|  |  | DF | Sum of Squares | Mean Square | F Value | Prob>F |
| --- | --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Model | 1 | 6.4273 | 6.4273 | 859.7589 | 8.65E-07 |
|  | Error | 5 | 0.0374 | 0.0075 |  |  |
|  | Total | 6 | 6.4646 |  |  |  |
| Quartz sand (200 mesh) | Model | 1 | 7.6183 | 7.6183 | 1582.2675 | 1.89E-07 |
|  | Error | 5 | 0.0241 | 0.0048 |  |  |
|  | Total | 6 | 7.6424 |  |  |  |
| Montmorillonite (200 mesh) | Model | 1 | 8.6789 | 8.6789 | 1079.5664 | 4.91E-07 |
|  | Error | 5 | 0.0402 | 0.0080 |  |  |
|  | Total | 6 | 8.7191 |  |  |  |
| Kaolinite (200 mesh) | Model | 1 | 8.6031 | 8.6031 | 802.8834 | 1.03E-06 |
|  | Error | 5 | 0.0536 | 0.0107 |  |  |
|  | Total | 6 | 8.6567 |  |  |  |
| Illite (200 mesh) | Model | 1 | 7.1287 | 7.1287 | 656.3682 | 1.69E-06 |
|  | Error | 5 | 0.0543 | 0.0109 |  |  |
|  | Total | 6 | 7.1830 |  |  |  |
| Chlorite (200 mesh) | Model | 1 | 8.9758 | 8.9758 | 859.8107 | 8.65E-07 |
|  | Error | 5 | 0.0522 | 0.0104 |  |  |
|  | Total | 6 | 9.0280 |  |  |  |

Table S19 The parameters of Fig. 10a

|  |  | Value | Standard Error | t-Value | Prob>¦t¦ |
| --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Intercept | -3.3727 | 0.2805 | -12.0227 | 7.02E-05 |
|  | Slope | 0.2432 | 0.0559 | 4.3533 | 7.34E-03 |
| Quartz sand (200 mesh) | Intercept | -3.6069 | 0.1854 | -19.4559 | 6.62E-06 |
|  | Slope | 0.5808 | 0.0379 | 15.3370 | 2.14E-05 |
| Montmorillonite (200 mesh) | Intercept | -1.0255 | 0.0767 | -13.3716 | 4.19E-05 |
|  | Slope | 0.2701 | 0.0172 | 15.7135 | 1.90E-05 |
| Kaolinite (200 mesh) | Intercept | -1.2627 | 0.1233 | -10.2410 | 1.52E-04 |
|  | Slope | 0.2448 | 0.0267 | 9.1651 | 2.59E-04 |
| Illite (200 mesh) | Intercept | -2.1763 | 0.2214 | -9.8291 | 1.86E-04 |
|  | Slope | 0.3182 | 0.0456 | 6.9759 | 9.31E-04 |
| Chlorite (200 mesh) | Intercept | -1.1735 | 0.0925 | -12.6904 | 5.40E-05 |
|  | Slope | 0.2750 | 0.0201 | 13.6552 | 3.78E-05 |

Table 20S The statistics of FIG 11a

|  | Quartz sand (60 mesh) | Quartz sand (200 mesh) | Montmorillonite (200 mesh) | Kaolinite (200 mesh) | Illite (200 mesh) | Chlorite (200 mesh) |
| --- | --- | --- | --- | --- | --- | --- |
| Number of Points | 7 | 7 | 7 | 7 | 7 | 7 |
| Degrees of Freedom | 5 | 5 | 5 | 5 | 5 | 5 |
| Residual Sum of Squares | 0.1670 | 0.0806 | 0.0313 | 0.0667 | 0.1354 | 0.0393 |
| Pearson's r | 0.8895 | 0.9895 | 0.9900 | 0.9715 | 0.9523 | 0.9869 |
| R-Square (COD) | 0.7912 | 0.9792 | 0.9802 | 0.9438 | 0.9068 | 0.9739 |
| Adj. R-Square | 0.7495 | 0.9750 | 0.9762 | 0.9326 | 0.8882 | 0.9687 |

Table S21 The ANOVA of Fig. 10a

|  |  | DF | Sum of Squares | Mean Square | F Value | Prob>F |
| --- | --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Model | 1 | 0.6328 | 0.6328 | 18.9510 | 7.34E-03 |
|  | Error | 5 | 0.1670 | 0.0334 |  |  |
|  | Total | 6 | 0.7998 |  |  |  |
| Quartz sand (200 mesh) | Model | 1 | 3.7930 | 3.7930 | 235.2228 | 2.14E-05 |
|  | Error | 5 | 0.0806 | 0.0161 |  |  |
|  | Total | 6 | 3.8736 |  |  |  |
| Montmorillonite (200 mesh) | Model | 1 | 1.5436 | 1.5436 | 246.9155 | 1.90E-05 |
|  | Error | 5 | 0.0313 | 0.0063 |  |  |
|  | Total | 6 | 1.5749 |  |  |  |
| Kaolinite (200 mesh) | Model | 1 | 1.1202 | 1.1202 | 83.9985 | 2.59E-04 |
|  | Error | 5 | 0.0667 | 0.0133 |  |  |
|  | Total | 6 | 1.1869 |  |  |  |
| Illite (200 mesh) | Model | 1 | 1.3182 | 1.3182 | 48.6634 | 9.31E-04 |
|  | Error | 5 | 0.1354 | 0.0271 |  |  |
|  | Total | 6 | 1.4536 |  |  |  |
| Chlorite (200 mesh) | Model | 1 | 1.4666 | 1.4666 | 186.4639 | 3.78E-05 |
|  | Error | 5 | 0.0393 | 0.0079 |  |  |
|  | Total | 6 | 1.5059 |  |  |  |

Table S22 The parameters of Fig. 10b

|  |  | Value | Standard Error | t-Value | Prob>¦t¦ |
| --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Intercept | -3.1983 | 0.2285 | -13.9943 | 3.35E-05 |
|  | Slope | 0.3349 | 0.0458 | 7.3102 | 7.50E-04 |
| Quartz sand (200 mesh) | Intercept | -2.9917 | 0.1506 | -19.8709 | 5.96E-06 |
|  | Slope | 0.4895 | 0.0308 | 15.9212 | 1.78E-05 |
| Montmorillonite (200 mesh) | Intercept | -1.2529 | 0.0504 | -24.8715 | 1.96E-06 |
|  | Slope | 0.4571 | 0.0122 | 37.4591 | 2.55E-07 |
| Kaolinite (200 mesh) | Intercept | -1.1620 | 0.0440 | -26.4158 | 1.45E-06 |
|  | Slope | 0.2985 | 0.0098 | 30.4478 | 7.17E-07 |
| Illite (200 mesh) | Intercept | -2.9489 | 0.1008 | -29.2575 | 8.74E-07 |
|  | Slope | 0.5984 | 0.0213 | 28.1193 | 1.07E-06 |
| Chlorite (200 mesh) | Intercept | -1.2965 | 0.0595 | -21.8068 | 3.76E-06 |
|  | Slope | 0.4048 | 0.0137 | 29.6561 | 8.17E-07 |

Table S23 The statistics of Fig. 10b

|  | Quartz sand (60 mesh) | Quartz sand (200 mesh) | Montmorillonite (200 mesh) | Kaolinite (200 mesh) | Illite (200 mesh) | Chlorite (200 mesh) |
| --- | --- | --- | --- | --- | --- | --- |
| Number of Points | 7 | 7 | 7 | 7 | 7 | 7 |
| Degrees of Freedom | 5 | 5 | 5 | 5 | 5 | 5 |
| Residual Sum of Squares | 0.1171 | 0.0556 | 0.0151 | 0.0102 | 0.0292 | 0.0199 |
| Pearson's r | 0.9563 | 0.9903 | 0.9982 | 0.9973 | 0.9969 | 0.9972 |
| R-Square (COD) | 0.9144 | 0.9807 | 0.9964 | 0.9946 | 0.9937 | 0.9943 |
| Adj. R-Square | 0.8973 | 0.9768 | 0.9957 | 0.9936 | 0.9925 | 0.9932 |

Table S24 The ANOVA of Fig. 10b

|  |  | DF | Sum of Squares | Mean Square | F Value | Prob>F |
| --- | --- | --- | --- | --- | --- | --- |
| Quartz sand (60 mesh) | Model | 1 | 1.2514 | 1.2514 | 53.4395 | 7.50E-04 |
|  | Error | 5 | 0.1171 | 0.0234 |  |  |
|  | Total | 6 | 1.3685 |  |  |  |
| Quartz sand (200 mesh) | Model | 1 | 2.8197 | 2.8197 | 253.4831 | 1.78E-05 |
|  | Error | 5 | 0.0556 | 0.0111 |  |  |
|  | Total | 6 | 2.8754 |  |  |  |
| Montmorillonite (200 mesh) | Model | 1 | 4.2339 | 4.2339 | 1403.1825 | 2.55E-07 |
|  | Error | 5 | 0.0151 | 0.0030 |  |  |
|  | Total | 6 | 4.2490 |  |  |  |
| Kaolinite 200 mesh) | Model | 1 | 1.8919 | 1.8919 | 927.0675 | 7.17E-07 |
|  | Error | 5 | 0.0102 | 0.0020 |  |  |
|  | Total | 6 | 1.9021 |  |  |  |
| Illite (200 mesh) | Model | 1 | 4.6187 | 4.6187 | 790.6959 | 1.07E-06 |
|  | Error | 5 | 0.0292 | 0.0058 |  |  |
|  | Total | 6 | 4.6479 |  |  |  |
| Chlorite (200 mesh) | Model | 1 | 3.4909 | 3.4909 | 879.4869 | 8.17E-07 |
|  | Error | 5 | 0.0199 | 0.0040 |  |  |
|  | Total | 6 | 3.5107 |  |  |  |