PREPARATION AND PROPERTIES OF ANTIBACTERIAL POLYHEXAMETHYLENE BIGUANIDE/PALYGORSKITE COMPOSITES AS ZEARALENONE ADSORBENTS

YU R. KANG, B MU*, G ZHU, YONG F. ZHU, AI Q. WANG*

Key Laboratory of Clay Mineral Applied Research of Gansu Province, Center of Eco-materials and Green Chemistry, Lanzhou Institute of Chemical Physics, Chinese Academy of Sciences, Lanzhou 730000, P. R. China

* E-mail addresses of corresponding authors: mubin@licp.cas.cn, aqwang@licp.cas.cn

Table S1 The minimum inhibitory concentration (MIC) values of Plg, PHMB, PHMB/Plg composites against E. coli and S. aureus

| Samples | MIC (mg/ml) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | E. coli R12 |  |  |  | S. aureus R22 |  |  |  |
|  | 5 | 2.5 | 1.25 | 0.625 | 5 | 2.5 | 1.25 | 0.625 |
| Plg | + | + | + | + | + | + | + | + |
| PHMB | - | - | - | - | - | - | - | - |
| PHMB/Plg-4 | + | + | + | + | + | + | + | + |
| PHMB/Plg-5 | - | - | + | + | - | - | + | + |

"+" indicates bacterial growth, "-" indicates no bacterial growth

Table S2 In vitro adsorption of mycotoxins by different adsorbents

| Adsorbent | Adsorption capacity(mg/g) | Isotherms | Reference |
| --- | --- | --- | --- |
| Montmorillonite K-10, Al-K10, Fe-K10 | 0.202,1.305, 1.028 | Langmuir | Bekci, et al. 2011 |
|  | 0.264, 0.096, 0.255 | Freundlich |  |
| Polyvinylpyrrolidone Cholestyramine Montmorillonite Bentonite Sepiolite Magnesium trisilicate | 0.3137 >0.3 0.1922 0.1124 0.07437 0.02261 | Freundlich | Ramos, et al. 1996 |
| Cetyltrimethyl ammonium bromide -modified montmorillonite and Montmorillonite | 8.83 and 0.60 5.07 and 0.19 | Langmuir Freundlich | Feng, et al. 2008 |
| Stearyl trimethyl ammoium bromide modified montmorillonite and montmorillonite | 10.49 and 1.91 | Langmuir | Zhang. et al. 2020 |
| Octylphenol polyoxyethylene ether modified montmorillonite | 59.88 | Langmuir | Wang, et al. 2018 |
| Cetylpyridinium chloride modified albite | 10.580 | Langmuir | Zhang, et al. 2019 |
| yeast cell wall | 260 | Langmuir | Pereyra, et al. 2013 |
| Dioctadecylmethylbenzylammonium chloride modified montmorillonite and montmorillonite | 5.0761 and 0.4529 | Langmuir | Li, et al. 2014 |
| Polyoxyethylene ether and lauramidopropyl betaine modified montmorillonite | 9.09 23.40 | Langmuir | Sun, et al. 2020 |
| Trimethylstearylammonium bromide modified rectorite | 34.6741 | Langmuir | Sun, et al. 2018 |
| Cetylpyridinium chloride modified zeolite | 32.79 | Langmuir | Markovi, et al. 2016 |
| Octadecyldimethylbenzyl- ammonium chloride modified zeolitic | 12.311 | Langmuir | DaKović, et al. 2007 |

References:

Bekci, Z.M. , Antep, M.K. , Merdivan, M. , & Yurdakoc, K. (2011). Zearalenone removal in synthetic media and aqueous part of canned corn by montmorillonite k10 and pillared montmorillonite k10. Journal of Food Protection, 74(6), 954.

DaKović, A. , Matijašević, S., Rottinghaus, G.E., Dondur, V., Pietrass, T., & Clewett, C.F.M. (2007). Adsorption of zearalenone by organomodified natural zeolitic tuff. Journal of Colloid & Interface Science, 311(1), 8-13.

Feng, J., Mei, S., Du, H., Han, X., & Xu, Z. (2008). In vitro adsorption of zearalenone by cetyltrimethyl ammonium bromide-modified montmorillonite nanocomposites. Microporous & Mesoporous Materials, 113(1-3), 99-105.

Li, Y.J., Zeng, L., Zhou, Y., Wang, T.F., & Zhang, Y.J. (2014). Preparation and characterization of montmorillonite intercalation compounds with quaternary ammonium surfactant: adsorption effect of zearalenone. Journal of Nanomaterials, 2014, 167402.

Markovi, M., Dakovi, A., Rottinghaus, G.E. , Kragovi, M., & Gennaro, B.D. (2016). Adsorption of the mycotoxin zearalenone by clinoptilolite and phillipsite zeolites treated with cetylpyridinium surfactant. Colloids and surfaces B: Biointerfaces, 151, 324.

Pereyra, C.M. , Cavaglieri, L.R. , Chiacchiera, S.M. , & Dalcero, A. (2013). The corn influence on the adsorption levels of aflatoxin b1 and zearalenone by yeast cell wall. Journal of Applied Microbiology, 114(3), 655-662.

Ramos, A.J., Hernández, E., Plá-Delfina, J.M. & Merinoc, M. (1996). Intestinal absorption of zearalenone and in vitro study of non-nutritive sorbent materials. International Journal of Pharmaceutics, 128(1-2), 129-137.

Sun, Z.M., Lian, C., Li, C.Q., & Zheng, S.L. (2020). Investigations on organo-montmorillonites modified by binary nonionic/zwitterionic surfactant mixtures for simultaneous adsorption of aflatoxin b1 and zearalenone. Journal of Colloid and Interface Science, 565, 11-22.

Sun, Z.M., Song, A.K., Wang, B. , Wang, G.F., & Zheng, S.L. (2018). Adsorption behaviors of aflatoxin b 1 and zearalenone by organo-rectorite modified with quaternary ammonium salts. Journal of Molecular Liquids, 264, 645-651.

Wang, G.F., Lian, C., Xi, Y.F., Sun, Z.M., & Zheng, S.L. (2018). Evaluation of nonionic surfactant modified montmorillonite as mycotoxins adsorbent for aflatoxin b1 and zearalenone. Journal of Colloid and Interface Science, 518, 48-56.

Zhang, W., Zhang, L., Jiang, X., Liu, X., Li, Y., & Zhang, Y. (2020). Enhanced adsorption removal of aflatoxin b 1, zearalenone and deoxynivalenol from dairy cow rumen fluid by modified nano-montmorillonite and evaluation of its mechanism. Animal Feed Science and Technology, 259, 114366.

Zhang, W., Zhang, S.H., Wang J.J., Dong J.W., Cheng, B.J., Xu, L., & Shan, A.S. (2019). A novel adsorbent albite modified with cetylpyridinium chloride for efficient removal of zearalenone. Toxins, 11(11), 674.