Preparation and characterization of porous palygorskite/carbon composites through zinc chloride activation for wastewater treatment

Fig. S1 XRD pattern of pure palygorskite

Yan Wanga, Yu Zhuanga, Sheng Wanga, Yin Liua,b,c*, Lingbing Kongd,*, Jianjun Lia, and Huayong Chene

The optimal adsorption capacity of the composites in the present work are listed in Table S1 in order to compare them with those of carbon and related composites reported in the open literature.

Table S1 Adsorption capacity and specific surface area of the Plg/C composites together with the literature data.

| Adsorbent for adsorbing MB | Surface area (m2/g) | Adsorption capacity (mg/g) | Ref. |
| --- | --- | --- | --- |
| Sorghum-waste-derived/porous carbon | 948.60 | 98.10 | (Hou et al., 2020) |
| MXene/acidified activated carbon | 1651 | 311.50 | (Li et al., 2020) |
| CuZnFe2O4/ activated carbon | 209 | 100.91 | (Zhang et al., 2020) |
| Activated carbon (Chitosan flake) | 318.40 | 143.53 | (Marrakchi et al., 2017) |
| Plg/C | 1497.88 | 381.04 | This work |

Hou, J., Hou, J., Liu, Y., Wen, S., Li, W., Liao, R., & Wang, L. (2020) Sorghum-Waste-Derived High-Surface Area KOH-Activated Porous Carbon for Highly Efficient Methylene Blue and Pb (II) Removal. ACS Omega, 5, 13548–13556. https://doi.org/10.1021/acsomega.9b04452

Li, Y., Pan, C., Kamdem, P., & Jin, X.J. (2020) Binder-Free Two-Dimensional MXene/Acid Activated Carbon for High-Performance Supercapacitors and Methylene Blue Adsorption.  Energy and Fuels. 10120–10130. https://doi.org/10.1021/acs.energyfuels.0c01352

Marrakchi, F., Ahmed, M.J., Khanday, W.A., Asif, M., & Hameed, B.H. (2017) Mesoporous-activated carbon prepared from chitosan flakes via single-step sodium hydroxide activation for the adsorption of methylene blue. International Journal of Biological Macromolecules, 98, 233–239. https://doi.org/10.1016/j.ijbiomac.2017.01.119

Zhang, L. & Yang, K. (2020) Facilely Magnetized CuZnFe2O4-Activated Carbon Composite as an Efficient Recyclable Adsorbent of Cationic Dyes. Journal of Chemical and Engineering Data, 65, 5532–5544. https://doi.org/10.1021/acs.jced.0c00643