Supplementary Data:

Figure S1. The XRD spectra of raw material montmorillonite.

Figure S2. The XPS spectras and the peak-fitting data of MFe2O4-montmorillonite. a) Fe3O4-montmorillonite. b) MnFe2O4-montmorillonite. c) ZnFe2O4-montmorillonite. d) CoFe2O4-montmorillonite. e) NiFe2O4-montmorillonite.

Table S1. The actual adsorption capacities and the metal ion removal rate of MFe2O4-montmorillonite adsorbent in the initial ions concentration of 60 mg·g-1.

| MFe2O4-montmorillonite |  | the actual adsorption capacity (C0=60 mg·L-1) | Xn+ Removal rate | MFe2O4-montmorillonite |  | the actual adsorption capacity (C0=60 mg·L-1) | Xn+ Removal rate |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ions | M | qe(mg·g-1) | % | Ions | M | qe(mg·g-1) | % |
| UO22+ | Fe | 28.4 | 28.4 | Mn2+ | Fe | 68.0 | 68.0 |
|  | Mn | 25.4 | 25.4 |  | Mn | 28.9 | 28.9 |
|  | Zn | 40.8 | 40.8 |  | Zn | 70.6 | 70.6 |
|  | Co | 21.8 | 21.8 |  | Co | 69.7 | 69.7 |
|  | Ni | 43.4 | 43.4 |  | Ni | 70.8 | 70.8 |
| Cr3+ | Fe | 84.3 | 84.3 | Ni2+ | Fe | 74.5 | 74.5 |
|  | Mn | 74.2 | 74.2 |  | Mn | 66.2 | 66.2 |
|  | Zn | 89.2 | 89.2 |  | Zn | 75.7 | 75.7 |
|  | Co | 85.1 | 85.1 |  | Co | 75.1 | 75.1 |
|  | Ni | 82.6 | 82.6 |  | Ni | 61.5 | 61.5 |
| Rb+ | Fe | 15.1 | 15.1 | Zn2+ | Fe | 53.6 | 53.6 |
|  | Mn | 13.4 | 13.4 |  | Mn | 45.6 | 45.6 |
|  | Zn | 15.1 | 15.1 |  | Zn | 46.9 | 46.9 |
|  | Co | 14.8 | 14.8 |  | Co | 55.2 | 55.2 |
|  | Ni | 16.2 | 16.2 |  | Ni | 56.6 | 56.6 |
| Sr2+ | Fe | 36.4 | 36.4 | Cd2+ | Fe | 21.6 | 21.6 |
|  | Mn | 53.9 | 53.9 |  | Mn | 18.6 | 18.6 |
|  | Zn | 35.7 | 35.7 |  | Zn | 26.5 | 26.5 |
|  | Co | 56.3 | 56.3 |  | Co | 22.9 | 22.9 |
|  | Ni | 31.4 | 31.4 |  | Ni | 25.8 | 25.8 |