SUPPORTING INFORMATION

SIMULTANEOUS IMMOBILIZATION OF Zn(II) AND Cr(III) IN SPINEL CRYSTALS FROM BENEFICIAL UTILIZATION OF WASTE BROWNFIELD-SITE SOILS

FEI WU 1,2,3, #, YUANYUAN TANG 4, #, XINGWEN LU 5, CHENGSHUAI LIU 1,2, *, YAHUI LV 2, HUI TONG 2, ZENGPING NING 1, CHANGZHONG LIAO 2, AND FANGBAI LI 2

1 State Key Laboratory of Environmental Geochemistry, Institute of Geochemistry, Chinese Academy of Sciences, Guiyang 550081, China

2 Guangdong Key Laboratory of Integrated Agro-Environmental Pollution Control and Management, Guangdong Institute of Eco-Environmental Sciences & Technology, Guangzhou 510650, China

3 University of Chinese Academy of Sciences, Beijing 100049, China

4 School of Environmental Science and Engineering, Southern University of Science and Technology, Shenzhen 518055, China

5 Research Centre for Environmental Health and Pollution Control, School of Environmental Science and Engineering, Guangdong University of Technology, Guangzhou 510006, China

* E-mail address of corresponding author: liuchengshuai@vip.gyig.ac.cn (C. Liu)

#These authors contributed equally to this work.

Number of pages: 4

Number of Figures: 2

Number of Tables: 2

Tables:

Table S1. The atomic composition of ZnCr2O4 for a sample calcined at 1350C (results from TEM-EDS).

| Element Line | Atom% (results from EDS) | Atom % Error |
| --- | --- | --- |
| O K | 18.63 | ±0.35 |
| Cr K | 52.91 | ±0.18 |
| Zn K | 28.46 | ±0.24 |
| Total | 100.00 |  |

Table S2. The main components of the soil studied (results from the principal component analysis of the soils by XRF).

| Main Components | SiO2 | Al2O3 | O | Fe2O3 | K2O | ZnO |
| --- | --- | --- | --- | --- | --- | --- |
| Relative Mass (wt.%) | 58.01 | 22.25 | 5.34 | 2.93 | 2.56 | 1.42 |
| Main Components | TiO2 | CuO | MgO | Cr2O3 | P2O5 | SO3 |
| Relative Mass (wt.%) | 0.87 | 0.63 | 0.52 | 0.51 | 0.22 | 0.20 |