Supplementary Information

Influence of mineral composition and firing temperature on the micro- and mesoporosity of replicate archaeological ceramics

Jan-Michael C. Caymea,*, Rasmus Palma,b, Peeter Somelarc, Signe Vahura, Ivo Leitoa, Ester Orasa,d,e

a Institute of Chemistry, University of Tartu, Ravila 14A, 50411, Tartu, Estonia

b Department of Applied Physics, KTH Royal Institute of Technology, SE-106 91 Stockholm, Sweden

c Department of Geology, University of Tartu, Ravila 14A, 50411, Tartu, Estonia

d Department of Archaeology, University of Tartu, Jakobi 2, 51014, Tartu, Estonia

e Swedish Collegium for Advanced Study (SCAS), Linneanum, Thunbergsvägen 2, 752 38, Uppsala, Sweden

*Corresponding author: E-mail: jan-michael.cayme@ut.ee

Table S1 Mass percentage of mineral components in the unfired raw materials and fired briquettes using quantitative XRD

| Raw Materials/ Fired Briquettes | Mass Ratios |  |  | 2:1 group | Kaolinite | Quartz | K-feldspar | Plagioclase | Hematite | Calcite | Dolomite | Anatase | Amphibole | Portlandite | Lime | Larnite | Merwinite | Brownmillerite |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | % Clay | % Sand | % Chalk |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| RC- 1 | 100 | - | - | 51.4 | 14.2 | 26.6 | 2.9 |  | 4.0 |  |  | 0.8 |  |  |  |  |  |  |
| RC-2 | 100 | - | - | 48.4 | 14.2 | 28.9 | 3.4 |  | 4.0 | tr. |  | 0.6 |  |  |  |  |  |  |
| RC-3 | 100 | - | - | 49.1 | 13.8 | 29.6 | 2.9 |  | 4.1 |  |  | tr. |  |  |  |  |  |  |
| WC-1 | 100 | - | - | 15.8 | 73.6 | 3.8 | 6.7 |  |  |  |  |  |  |  |  |  |  |  |
| WC-2 | 100 | - | - | 18.3 | 73.8 | 2.7 | 5.2 |  |  |  |  |  |  |  |  |  |  |  |
| WC-3 | 100 | - | - | 18.6 | 73.3 | 2.6 | 5.4 |  |  |  |  |  |  |  |  |  |  |  |
| CH-1 | - | - | 100 |  |  | tr. |  |  |  | 98.8 | 0.9 |  |  |  |  |  |  |  |
| CH-2 | - | - | 100 |  |  | tr. |  |  |  | 98.8 | 1.0 |  |  |  |  |  |  |  |
| CH-3 | - | - | 100 |  |  | tr. |  |  |  | 98.8 | 0.9 |  |  |  |  |  |  |  |
| S-1 | - | 100 | - | 4.0 |  | 74.6 | 9.5 | 7.3 |  | tr. | 3.0 |  | 1.1 |  |  |  |  |  |
| S-2 | - | 100 | - | 6.2 | tr. | 73.8 | 7.7 | 7.2 |  | tr. | 3.7 |  | 1.0 |  |  |  |  |  |
| S-3 | - | 100 | - | 5.9 | tr. | 73.8 | 6.9 | 8.3 |  | tr. | 3.8 |  | 0.9 |  |  |  |  |  |
| RC600-S1 | 15 | 85 | - | 9.8 |  | 71.2 | 9.5 | 5.7 | 0.6 | 1.4 | 1.8 |  |  |  |  |  |  |  |
| RC600-S2 | 20 | 80 | - | 10.3 |  | 69.6 | 9.2 | 6.0 | 0.9 | 1.8 | 2.2 |  |  |  |  |  |  |  |
| RC600-S3 | 25 | 75 | - | 9.9 |  | 69.6 | 9.6 | 6.5 | 1.1 | 1.2 | 2.2 |  |  |  |  |  |  |  |
| RC600-S4 | 50 | 50 | - | 21.8 |  | 61.7 | 5.1 | 5.3 | 1.3 | 1.3 | 2.5 |  | 1.1 |  |  |  |  |  |
| RC600-S5 | 75 | 25 | - | 44.7 |  | 42.9 | 3.4 | 4.0 | 3.3 | 0.7 | 1.0 |  |  |  |  |  |  |  |
| RC600-S6 | 100 | 0 | - | 55.3 |  | 34.8 | 1.6 | 2.5 | 3.9 | 1.4 | tr. |  |  |  |  |  |  |  |
| RC800-S1 | 15 | 85 | - | 4.7 |  | 78.1 | 10.1 | 6.1 | tr. | tr. | tr. |  |  |  |  |  |  |  |
| RC800-S2 | 20 | 80 | - | 5.3 |  | 75.8 | 10.5 | 6.5 | 0.6 | 0.7 | tr. |  |  |  |  |  |  |  |
| RC800-S3 | 25 | 75 | - | 13.8 |  | 71.4 | 6.9 | 6.2 | 0.8 | tr. | tr. |  |  |  |  |  |  |  |
| RC800-S4 | 50 | 50 | - | 18.0 |  | 64.7 | 7.3 | 6.9 | 1.8 | 0.8 | 0.6 |  |  |  |  |  |  |  |
| RC800-S5 | 75 | 25 | - | 38.1 |  | 50.4 | 3.8 | 3.9 | 2.3 | 0.6 | 0.8 |  |  |  |  |  |  |  |
| RC800-S6 | 100 | 0 | - | 56.4 |  | 32.6 | 1.2 | 3.3 | 3.9 |  | 1.0 | 1.5 |  |  |  |  |  |  |
| RC600-CH1 | 20 | 32 | 48 | 5.9 |  | 31.7 | 6.4 |  | 1.5 | 51.9 | 2.6 |  |  |  |  |  |  |  |
| RC600-CH2 | 25 | 30 | 45 | 6.0 |  | 32.7 | 4.2 | 3.6 | 1.9 | 49.1 | 2.3 |  |  |  |  |  |  |  |
| RC600-CH3 | 50 | 20 | 30 | 22.2 |  | 32.7 | 3.6 | 2.8 | 2.7 | 34.6 | 1.3 |  |  |  |  |  |  |  |
| RC600-CH4 | 75 | 10 | 15 | 38.9 |  | 32.9 | 3.9 | 2.7 | 3.9 | 16.7 | 1.1 |  |  |  |  |  |  |  |
| RC600-CH5 | 90 | 5 | 5 | 39.4 |  | 38.7 | 5.9 | 5.5 | 2.1 | 7.6 | 0.8 |  |  |  |  |  |  |  |
| RC800-CH1 | 20 | 32 | 48 | 3.5 |  | 38.2 | 5.8 | 4.6 | 2.4 | 0.6 |  |  |  | 16.2 | 6.8 | 18.2 | 2.8 | 1.0 |
| RC800-CH2 | 25 | 30 | 45 | 3.5 |  | 41.3 | 5.5 | 4.5 | 1.3 | 1.0 |  |  |  | 18.5 | 4.7 | 16.7 | 1.2 | 1.9 |
| RC800-CH3 | 50 | 20 | 30 | 18.7 |  | 43.0 | 5.7 | 5.0 | 3.5 | 1.0 |  |  |  | 6.3 | 3.8 | 10.4 | 1.9 | tr. |
| RC800-CH4 | 75 | 10 | 15 | 31.9 |  | 42.9 | 6.0 | 5.4 | 4.1 | 0.7 |  |  |  | 1.8 | 1.6 | 4.3 | 1.3 |  |
| RC800-CH5 | 90 | 5 | 5 | 46.5 |  | 38.2 | 3.4 | 3.5 | 4.2 | 0.6 |  |  |  |  | 1.5 | 1.4 | 0.6 |  |
| WC600-S1 | 15 | 85 | - | 3.6 |  | 74.7 | 8.4 | 8.0 |  | 1.2 | 2.9 |  | 1.2 |  |  |  |  |  |
| WC600-S2 | 20 | 80 | - | 10.5 |  | 70.9 | 6.7 | 7.0 |  | 1.5 | 2.5 |  | 0.9 |  |  |  |  |  |
| WC600-S3 | 25 | 75 | - | 12.0 |  | 67.4 | 6.8 | 7.7 |  | 1.5 | 3.8 |  | 0.8 |  |  |  |  |  |
| WC600-S4 | 50 | 50 | - | 19.0 |  | 61.7 | 5.7 | 7.5 |  | 1.5 | 2.7 |  | 1.8 |  |  |  |  |  |
| WC600-S5 | 75 | 25 | - | 37.1 |  | 47.1 | 6.7 | 5.4 |  |  | 3.7 |  |  |  |  |  |  |  |
| WC600-S6 | 100 | 0 | - | 65.7 |  | 19.3 | 8.9 | 2.6 |  |  | 1.7 |  |  |  |  |  |  |  |
| WC800-S1 | 15 | 85 | - | 2.9 |  | 76.1 | 8.5 | 7.6 |  |  |  |  | 4.3 | tr. | 0.6 |  |  |  |
| WC800-S2 | 20 | 80 | - | 10.6 |  | 68.4 | 13.6 | 6.5 |  |  |  |  |  | tr. | 0.8 |  |  |  |
| WC800-S3 | 25 | 75 | - | 11.9 |  | 65.7 | 15.7 | 5.8 |  |  |  |  |  |  | 0.8 |  |  |  |
| WC800-S4 | 50 | 50 | - | 15.4 |  | 57.6 | 19.0 | 7.4 |  |  |  |  |  |  | 0.7 |  |  |  |
| WC800-S5 | 75 | 25 | - | 25.3 |  | 46.5 | 20.0 | 7.7 |  |  |  |  |  |  | 0.5 |  |  |  |
| WC800-S6 | 100 | 0 | - | 53.2 |  | 20.4 | 20.2 | 5.1 |  |  |  |  |  |  | 0.7 |  |  |  |
| WC600-CH1 | 20 | 32 | 48 | 5.6 |  | 29.3 | 5.7 | 5.2 |  | 51.7 | 2.5 |  |  |  |  |  |  |  |
| WC600-CH2 | 25 | 30 | 45 | 7.8 |  | 31.2 | 3.1 | 4.5 |  | 51.0 | 2.4 |  |  |  |  |  |  |  |
| WC600-CH3 | 50 | 20 | 30 | 17.8 |  | 26.9 | 3.6 | 3.6 |  | 45.1 | 3.0 |  |  |  |  |  |  |  |
| WC600-CH4 | 75 | 10 | 15 | 39.3 |  | 21.6 | 5.1 | 1.2 |  | 31.5 | 1.3 |  |  |  |  |  |  |  |
| WC600-CH5 | 90 | 5 | 5 | 54.6 |  | 23.9 | 5.7 | 1.9 |  | 12.5 | 1.4 |  |  |  |  |  |  |  |
| WC800-CH1 | 20 | 32 | 48 | 3.6 |  | 43.2 | 6.7 | 5.9 |  | 1.4 | 0.9 |  |  | 17.3 | 9.6 | 10.1 | 1.3 |  |
| WC800-CH2 | 25 | 30 | 45 | 4.5 |  | 40.2 | 8.3 | 5.4 |  | 1.4 | tr. |  |  | 15.9 | 12.5 | 9.9 | 1.0 |  |
| WC800-CH3 | 50 | 20 | 30 | 10.1 |  | 39.7 | 9.2 | 6.2 |  | 1.6 | tr. |  |  | 6.5 | 18.2 | 7.5 | tr. |  |
| WC800-CH4 | 75 | 10 | 15 | 33.7 |  | 35.3 | 9.9 | 7.3 |  | tr. |  |  |  | 1.1 | 8.8 | 3.2 | tr. |  |
| WC800-CH5 | 90 | 5 | 5 | 45.3 |  | 28.9 | 10.8 | 9.2 |  |  |  |  |  | tr. | 2.9 | 2.4 |  |  |

The raw materials are RC (illite and mixed layered illite-smectite) clay, WC (kaolinite) clay, CH (chalk), and S (sand). The raw materials were tested in triplicates or three different preparations of unoriented powder, labelled as 1, 2, and 3, respectively. The numbers 600 and 800 in the briquette codes denote firing temperatures at 600°C and 800°C. The percentage weight amount of clay and tempers used to make the reference pottery briquettes are also shown in the table. Trace amounts are denoted by “tr.”.

Table S2 Surface area and pore volume parameters obtained from the N2 adsorption data for samples of the reference pottery briquettes

| Fired Briquettes | Specific surface area |  |  | Specific Pore volume |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | SBET (m2 g1) | SNLDFT (m2 g1) | Smicro (%) | V0.95 (mm3 g1) | VNLDFT (mm3 g1) | Vmicro (%) |
| RC with sand temper at 600°C |  |  |  |  |  |  |
| RC600-S1 | 5.3 | 4.3 | 62 | 9.7 | 5.0 | 22 |
| RC600-S2 | 7.6 | 8.4 | 59 | 14 | 9.3 | 18 |
| RC600-S3 | 8.3 | 9.4 | 60 | 15 | 10 | 18 |
| RC600-S4 | 18 | 20 | 57 | 33 | 23 | 17 |
| RC600-S5 | 30 | 35 | 55 | 56 | 40 | 16 |
| RC600-S6 | 40 | 46 | 51 | 75 | 57 | 16 |
| RC with sand temper at 800°C |  |  |  |  |  |  |
| RC800-S1 | 5.4 | 5.5 | 48 | 11 | 7.3 | 14 |
| RC800-S2 | 7.7 | 9.5 | 49 | 15 | 13 | 13 |
| RC800-S3 | 9.0 | 10 | 51 | 18 | 13 | 14 |
| RC800-S4 | 18 | 22 | 50 | 35 | 28 | 14 |
| RC800-S5 | 25 | 32 | 50 | 52 | 42 | 13 |
| RC800-S6 | 35 | 44 | 48 | 74 | 59 | 13 |
| WC with sand temper at 600°C |  |  |  |  |  |  |
| WC600-S1 | 1.7 | 2.1 | 58 | 3.8 | 2.8 | 16 |
| WC600-S2 | 2.2 | 2.6 | 61 | 4.9 | 3.4 | 17 |
| WC600-S3 | 2.6 | 3.0 | 61 | 5.5 | 3.9 | 18 |
| WC600-S4 | 4.6 | 5.7 | 54 | 10 | 8.0 | 15 |
| WC600-S5 | 6.3 | 8.1 | 56 | 15 | 11 | 15 |
| WC600-S6 | 8.6 | 11 | 53 | 20 | 16 | 14 |
| WC with sand temper at 800°C |  |  |  |  |  |  |
| WC800-S1 | 2.3 | 2.8 | 55 | 4.8 | 3.7 | 16 |
| WC800-S2 | 2.9 | 3.5 | 55 | 5.8 | 4.6 | 16 |
| WC800-S3 | 3.2 | 4.1 | 54 | 6.6 | 5.3 | 16 |
| WC800-S4 | 4.6 | 5.8 | 52 | 10 | 8.2 | 14 |
| WC800-S5 | 6.3 | 8.0 | 54 | 14 | 11 | 15 |
| WC800-S6 | 8.2 | 10 | 51 | 19 | 15 | 14 |
| RC with chalk and sand tempers at 600°C |  |  |  |  |  |  |
| RC600-CH1 | 6.1 | 6.2 | 57 | 11 | 7.7 | 21 |
| RC600-CH2 | 7.0 | 6.5 | 68 | 13 | 6.5 | 22 |
| RC600-CH3 | 16 | 15 | 70 | 30 | 15 | 23 |
| RC600-CH4 | 26 | 31 | 62 | 52 | 34 | 18 |
| RC600-CH5 | 29 | 35 | 62 | 58 | 39 | 18 |
| RC with chalk and sand tempers at 800°C |  |  |  |  |  |  |
| RC800-CH1 | 6.3 | 7.6 | 52 | 14 | 11 | 16 |
| RC800-CH2 | 5.4 | 6.4 | 56 | 13 | 8.5 | 17 |
| RC800-CH3 | 7.2 | 8.5 | 56 | 17 | 11 | 14 |
| RC800-CH4 | 15 | 19 | 53 | 34 | 24 | 13 |
| RC800-CH5 | 26 | 31 | 54 | 54 | 38 | 14 |
| WC with chalk and sand tempers at 600°C |  |  |  |  |  |  |
| WC600-CH1 | 2.6 | 2.1 | 66 | 4.6 | 2.4 | 24 |
| WC600-CH2 | 2.6 | 2.6 | 63 | 5.1 | 3.3 | 22 |
| WC600-CH3 | 4.5 | 5.2 | 57 | 9.3 | 7.0 | 17 |
| WC600-CH4 | 6.0 | 6.8 | 57 | 14 | 9.4 | 16 |
| WC600-CH5 | 7.0 | 9.0 | 53 | 17 | 13 | 14 |
| WC with chalk and sand tempers at 800°C |  |  |  |  |  |  |
| WC800-CH1 | 7.0 | 8.4 | 49 | 19 | 13 | 13 |
| WC800-CH2 | 6.7 | 8.0 | 51 | 17 | 12 | 14 |
| WC800-CH3 | 8.2 | 10 | 51 | 16 | 13 | 16 |
| WC800-CH4 | 10 | 13 | 48 | 20 | 16 | 14 |
| WC800-CH5 | 8.3 | 10 | 51 | 19 | 15 | 14 |

Fig. S1 N2 adsorption isotherms with p/p° in log scale (symbols) and with the fits to the NLDFT model for pillared clays (dashed lines) of the reference pottery briquettes obtained at 77K. The labels denote the following: RC (illite and illite-smectite) clay, WC (kaolinite clay), CH (chalk), and S (sand). The number 600 and 800 in the briquette codes are the firing temperatures at 600°C and 800°C. The mass ratios corresponding to the briquette codes are seen in Table 1

Appendix 1

Repeatability and uncertainties of the N2 adsorption values. The repeatability and precision of the N2 adsorption values reported in this study was verified by utilizing one briquette, RC600-S4 (50% illite and illite-smectite clay: 50% sand ratio) and prepared in triplicates. Each triplicate was measured in the N2 porosimeter two times (2x), producing a total of 6 additional sets of data. The same methodology and experimental parameters used in this study were employed for the repeatability and uncertainty experiments.

Three NLDFT models developed for oxides and for cylindrical pores were applied to the isotherm data and the results were compared with each other (Fig. A1). These models are: (1) pillard clays (Pore Size Distribution, PSD, of pillared clays and the NLDFT model preferred in this study, (2) oxides strong potential (PSD of oxides and Na, Ca, K exchanged zeolite), and (3) Oxides Tarazona (PSD of oxides and H and NH exchanged zeolites). Results show that the isotherm of RC600-S4 fits well with the three models and the repeat measurements are almost equivalent.

Fig. A1 N2 adsorption isotherms with p/p° in linear scale (symbols) and with fits to the NLDFT model for pillared clays (dashed lines) (a), to the NLDFT model for oxide with strong potential (b), and to the NLDFT model for oxide Tarazona (c) of the 7 RC600-S4 briquettes obtained at 77 K.

For the pore size distribution, the pillared clay NLDFT model yielded the lowest root-mean square (RMS) error and the highest roughness at equivalent regularization compared to the other models. Furthermore, the distribution and separation of pore sizes were better compared to the other models (Fig. A2). Hence, the pillared clay model is the most appropriate model to use, and it established that the values reported were repeatable.

Fig. A2 Pore size distributions obtained by applying the pillared clay NLDFT model (a), the oxide strong potential NLDFT model (b), and the oxide Tarazona NLDFT model (c) to the N2 adsorption isotherm data of RC600-S4 6 repeat measurements obtained at 77 K. The root-mean square (RMS), roughness, and regularization parameters obtained from fitting all three NLDFT models is presented in the Table.

From the 6 repeat measurements with 3 separately prepared briquettes using RC600-S4, standard deviations of main parameters were calculated and tabulated (Table A1). The relative standard deviations for the Smicro and Vmicro were 12.5% and 8.0%, respectively, and smaller than the SNLDFT and VNLDFT values. From these standard deviations an appraisal to the precision of the obtained parameters in the whole set as a relative standard deviation value to each parameter was obtained.

Table A1 Example of standard deviations of obtained parameters between separately prepared briquette samples

| NLDFT model | SBET m2 g1 | SBET relative standard deviation as % | V0.95 cm3 g1 | V0.95 relative standard deviation as % | SNLDFT m2 g1 | SNLDFT relative standard deviation as % | VNLDFT cm3 g1 | VNLDFT relative standard deviation as % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pillared clay | 17.5 (7) | 4.0 | 0.032 (1) | 4.6 | 11 (2) | 17 | 0.016 (3) | 22 |

Where: SBET - BET theory based specific surface area calculated from N2 isotherm; V0.95 - Pore volume calculated from adsorbed amount of N2 at p/p° = 0.95; SNLDFT - Specific surface obtained from applying the NLDFT model to the N2 adsorption isotherm; VNLDFT - Pore volume obtained from applying the NLDFT model to the N2 adsorption isotherm

Appendix 2

Correlation graphs of SBET and V0.95 with the added clay. Despite the NLDFT model’s usefulness, the pillared clays NLDFT model does not represent the investigated material’s exact porous structure, hence, the pore size distributions obtained were not perfectly accurate, even though they are precise (Thommes et al., 2015). The specific surface area values, SBET and SNLDFT, and specific pore volume values, V0.95 and VNLDFT, exhibited diverging values across the method of calculation, up to a maximum difference of 26% (see WC800-CH4 briquette) and 67% (see RC600-CH2 and RC600-CH3 briquettes) for the specific surface area and specific pore volume, respectively (see Table 2). The volume differences (V0.95 consistently larger than VNLDFT) were due mainly to differences in the probed porosity, where V0.95 corresponds to pores with widths up to 41 nm and VNLDFT to pores with widths up to 35 nm. The differences in the surface area values can be attributed to the BET method yielding misrepresentative results for some materials (Sing, 2001) and to the NLDFT model being specific to pillared clays, which  have an artificial porosity different in character from that expected for the obtained briquettes. Thus, the results from these two approaches were used in parallel to obtain possible ranges of surface area and pore volume values to be compared with the various compositions and firing conditions. The correlations of the porosity parameters SBET and V0.95 with the initial clay content (Figs. A3 and A4) are very nearly the same as the correlations of SNLDFT and VNLDFT (Figs. 5 and 6). That and the fact that many of the correlation cefficients are close to unity are evidence that the calculated parameters are precise enough that, for example, some small effects of different firing temperatures, may be reliably interpreted.

Fig. A3 Graph of the clay mass fraction (%) used to make the briquettes vs. the pore volume (SBET)

Fig. A4 Graph of the clay mass fraction (%) used to make the briquettes vs. the pore volume (V0.95)