**Development and characterization of organically grafted clay minerals for the removal of methylene blue from water**

**Aizhan M. Serikbayeva1,2,3, Fernanda F. Roman1,2, Helder T. Gomes1,2, and Marzhan S. Kalmakhanova3,\***

1 Centro de investigação de Montanha (CIMO), Instituto Politécnico de Bragança, Campus de Santa Apolónia, 5300-253 Bragança, Portugal

2 Laboratório para a Sustentabilidade e Tecnologia em RegiõesdeMontanha, Instituto Politécnico de Bragança, Campus de Santa Apolónia, 5300-253 Bragança, Portugal**.**

3 M.Kh. Dulaty Taraz Regional University, Department of Chemistry and Chemical Technology, Taraz 080012, Kazakhstan

**Supplemental Material**

****

**Figure S1.** Number of publications: (a) related to clay modification and application in adsorption processes (Research was conducted using Clarivate’s *Web of Science* on January 15th, 2024 using the keywords ‘clay AND organic grafting AND methylene blue,’ ‘clay AND organic grafting AND adsorption,’ ‘clay AND pillared AND methylene blue,’ ‘clay AND pillared AND adsorption,’ ‘clay AND magnetic AND methylene blue,’ ‘clay AND magnetic AND adsorption,’ ‘clay AND activated AND methylene blue,’ and ‘clay AND activated AND adsorption’); and (b) related to organoclays and the type of clay used (Research was conducted on July 11th, 2024 using Clarivate’s *Web of Science* with the keywords ‘organoclay,’ ‘montmorillonite,’ ‘bentonite,’ and ‘kaolin\*’).

(b)

(a)

**A diagram of different types of energy

Description automatically generated with medium confidenceA diagram of a calcite reaction

Description automatically generated with medium confidence**

**Figure S2.** Thermogravimetric analysis of: (a) Shymkent natural clay and (b) Shymkent-TEAO.

**Text S1. Calculation to determine surface areas**

The Langmuir method is given in eqn 1 (Diaz de Tuesta et al., 2022; Lowell et al., 2004) and was calculated in the *P*/*P*0 range of 0.05–0.35:

|  |  |
| --- | --- |
|  | (1) |

Where qe refers to the adsorbate (in this case, N2) adsorbed per mass of adsorbent at equilibria stage, qm and K are constants, and *P* is the pressure. The Langmuir equation can be rewritten as eqn 2:

|  |  |
| --- | --- |
|  | (2) |

By plotting *P/q*e versus *P*, the parameters K and qm can be obtained. The surface area can then be derived from eqn 3 (Lowell et al., 2004):

|  |  |
| --- | --- |
|  | (3) |

where *A* is the cross-sectional area of the adsorbate (in this case, N2 and equals 0.162 nm2 (Bardestani et al., 2019)), N is Avogrado’s number and *M* is the adsorbate molar mass (Bardestani et al., 2019).

The value of *S*BET was calculated using eqn 4 (Bardestani et al., 2019) in the *P*/*P*0 range of 0.05–0.35:

|  |  |
| --- | --- |
|  | (4) |

where *W* is the mass adsorbed at relative vapour pressure, *P* and *P0* are the actual and saturated vapor pressures of the adsorbate, *W*ml is the mass of adsorbate that forms a complete monolayer, and C is a constant. Plotting versus allows us to obtain values for β0 (intercept) and β1 (slope). The mass of adsorbate that forms a monolayer, *W*ml*,* is obtained from the sum of β0 and β1, as shown in eqn 5, and *S*BET can be calculated from eqn 6:

|  |  |
| --- | --- |
|  | (5) |
|  | (6) |

where *M* is adsorbate molar mass, m is the sample mass, *A* is the adsorbate cross-sectional area (for N2 it equals 0.162 nm2) and N is Avogadro’s number (Bardestani et al., 2019).

**Table S1**. Literature reporting adsorption of dyes with organoclays.

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Clay | Grafted molecule | Pollutant | Conditions | Results | References |
| Bentonite | Silylating agents (chlorotrimethylsilane,  n-octyltrichlorosilane,  n-octadecyltrichlorosilane, phenyltrichlorosilane, diphenyldichlorosilane, triphenylchlorosilane) | Sudan (II) | pH = 4.0, [adsorbent] =  0.4 g/L, [adsorbate] =  50 mg/L | 60-80% of Sudan removal depending on grafted molecule (Q = 73-95 mg/g) | [Saeed](https://doi.org/10.1016/j.micromeso.2019.109697" \t "_blank" \o "Persistent link using digital object identifier) et al. (2019) |
| Commercial Vermiculite | 3-aminopropyltriethoxysilane | Alizarin Red S | pH = 2.0, [adsorbent] =  0.8 g/L, [adsorbate] = 400 mg/L | Q = 18.2 mg/g (max. removal of 90%) | [Ali](https://doi.org/10.1016/j.eti.2020.101001). et al. (2020) |
| Natural clay [(Na,Ca)0.3(Al,Mg)2Si4O10(OH)2.nH2O)] from Cameroon | N1-(3-trimethoxysilylpropyl)diethylenetriamine | Reactive Blue 19 and Reactive Green 19 | [adsorbent] =  1.5 g/L, [adsorbate] =  300 mg/L, pH = 2.0. | Q = 200 mg/g for both pollutants | Teixeira et al. (2023) |
| Montmorillonite from industrial facility | N-methylimidazolium tetrafluoroborate or N-butylimidazolium tetrafluoroborate | Orange-II | [adsorbate] =  10 mg/L, pH 2.0. | Q = 2.29 mg/g (90% removal) | Yilmazoğlu et al. (2022) |
| Commercial bentonite | Silica-polyethylene glycol | Methylene Blue | [adsorbate] =  100 mg/L, pH 6.0, [adsorbent] =  2 g/L, 2 h | Q = 50 mg/g | Suchithra et al. (2012) |
| Kaolin from São Paulo, Brasil | 2-hydroxyethyl methacrylate and 3-(trimethoxysilyl)propyl methacrylate | Methylene Blue | [adsorbate] =  50 mg/L, [adsorbent] =  1 g/L, 5 min | Q = 9 mg/g | Ferreira et al. (2017) |
| Commercial Montmorillonite | Sodium eicosenoate, cetyltrimethylammonium chloride and Fe3O4 | Methylene Blue | [adsorbate] =  50 mg/L, [adsorbent] =  0.4 g/L, pH = 7 | Q = 125 mg/g | Rahmani et al. (2019) |
| Commercial Montmorillonite | dodecyl sulfobetaine surfactant | Methylene Blue | [adsorbate] =  40 mg/L, [adsorbent] = 1 g/L, pH = 5 | Q = 250 mg/g | Fan et al. (2014) |
| Natural clay (kaolinite) from Shymkent deposit, KZ | Triethanolamine | Methylene Blue | [adsorbate] =  50 mg/L, pH 3.0, [adsorbent] =  0.25 g/L | 86% removal (equivalent to a Q = 159 mg/g\*) | Present study |

\*calculated according to [Saeed](https://doi.org/10.1016/j.micromeso.2019.109697" \t "_blank" \o "Persistent link using digital object identifier) et. al. (2019)

**REFERENCES**

Ali N., Ali F., Ullah I., Ali Z., Duclaux L., Reinert L., Lévêque J.M., Farooq A., Bilal M., Ahmad I. (2020) Organically modified micron-sized vermiculite and silica for efficient removal of Alizarin Red S dye pollutant from aqueous solution. *Environmental Technology & Innovation*, **19**, 101001. DOI: 10.1016/j.eti.2020.101001.

Bardestani R., Patience G. S., Kaliaguine S. (2019) Experimental methods in chemical engineering: specific surface area and pore size distribution measurements—BET, BJH, and DFT. *The Canadian Journal of Chemical Engineering,* **97**, 2781–2791. DOI: 10.1002/cjce.23632.

Diaz De Tuesta J.L., Roman F.F., Marques V.C., Silva A.S., Silva A.P.F., Bosco T.C., Shinibekova A.A., Aknur S., Kalmakhanova M.S., Massalimova B.K., Arrobas M., Silva A.M.T., Gomes, H.T. (2022) Performance and modeling of Ni(II) adsorption from low concentrated wastewater on carbon microspheres prepared from tangerine peels by FeCl3-assisted hydrothermal carbonization. *Journal of Environmental Chemical Engineering,* **10**, 108143. DOI: 10.1016/j.jece.2022.108143.

Fan H., Zhou L., Jiang X., Huang Q., Lang W. (2014) Adsorption of Cu2+ and methylene blue on dodecyl sulfobetaine surfactant-modified montmorillonite. *Applied Clay Science*, **95**, 150–158. DOI: 10.1016/j.clay.2014.04.001

Ferreira B.F., Ciuffi K.J., Nassar E.J., Vicente M.A., Trujillano R., Rives V., Faria E.H. (2017) Kaolinite-polymer compounds by grafting of 2-hydroxyethyl methacrylate and 3-(trimethoxysilyl)propyl methacrylate. *Applied Clay Science*, **146**, 526-534. DOI: 10.1016/j.clay.2017.07.009.

Lowell S., Shields J.E., Thomas M.A., & Thommes, M. (2004). Surface Area Analysis from the Langmuir and BET Theories. In: Characterization of Porous Solids and Powders: Surface Area, Pore Size and Density. Particle Technology Series, vol 16. Springer, Dordrecht. DOI: 10.1007/978-1-4020-2303-3\_5.

Rahmani S., Zeynizadeh B., Karami S. (2020) Removal of cationic methylene blue dye using magnetic and anionic-cationic modified montmorillonite: kinetic, isotherm and thermodynamic studies. *Applied Clay Science*, **184**, 105391. DOI: 10.1016/j.clay.2019.105391.

Saeed M., Munir M., Nafees M., Shah S.S.A., Ullah H., Waseem, A. (2020) Synthesis, characterization and applications of silylation based grafted bentonites for the removal of Sudan dyes: Isothermal, kinetic and thermodynamic studies. *Microporous and Mesoporous Materials*, **291**, 109697. DOI: 10.1016/j.micromeso.2019.109697.

Suchithra P.S., Vazhayal L., Mohamed A.P., Ananthakumar S. (2012) Mesoporous organic–inorganic hybrid aerogels through ultrasonic assisted sol–gel intercalation of silica–PEG in bentonite for effective removal of dyes, volatile organic pollutants and petroleum products from aqueous solution. *Chemical Engineering Journal*, **200–202**, 589–600. DOI: 10.1016/j.cej.2012.06.083.

Teixeira R.A., Lima E.C., Benetti A.D., Naushad M., Thue P.S., Mello B.L., Reis G.S., Rabiee N., Franco D., Seliem, M.K. (2023) Employ a Clay@TMSPDETA hybrid material as an adsorbent to remove textile dyes from wastewater effluents. *Environmental Science & Pollution Research*, **30**, 86010–86024. DOI: 10.1007/s11356-023-28568-9.

Yılmazoğlu M., Turan B., Demircivi D., Hızal J. (2022) Synthesis and characterization of imidazolium based ionic liquid modified montmorillonite for the adsorption of Orange II dye: Effect of chain length. *Journal of Molecular Structure*, **1249**, 131628. DOI : 10.1016/j.molstruc.2021.131628.