The glass beads of Kaitshàa: new insights on early Indian Ocean trade into the far interior of southern Africa

James Denbow1,2, Carla Klehm3 & Laure Dussubieux4

1Department of Anthropology, University of Texas at Austin, 2201 Speedway C3200, TX 78712, USA (Email: jdenbow@austin.utexas.edu)

2School of Geography, Archaeology and Environmental Studies, University of the Witwatersrand, 1 Jan Smuts Avenue, Braamfontein 2000, South Africa

3Department of Anthropology, Washington University in St. Louis, Campus Box 1114, One Brookings Drive, St Louis, MO 63130-4899, USA

4Elemental Analysis Facility, The Field Museum, 1400 S Lake Shore Drive, Chicago, IL 60605, USA

The later African Iron Age saw a shift to centralised polities, as seen in the expansion of hegemonies such as Great Zimbabwe. During this period, trade with the interior of Africa became increasingly centrally controlled. Excavations at the site of Kaitshàa, on the edge of the Makgadikgadi saltpans in Botswana, have revealed how a small settlement based on prehistoric salt trading was able to take its place in the Indian Ocean trade network before such centralised polities arose. Using compositional analysis of glass beads, the authors argue that this site in the central Kalahari Desert exemplifies the role of heterarchy and indigenous agency in the evolving political economy of the subcontinent.

Keywords: Botswana, Iron Age, Indian Ocean trade, glass beads, ivory, saltpans

This paper is published in Antiquity vol. 88 issue 344 April 2015. Here we publish supplementary material.

Table S1. Physical description of the Kaitshàa bead sample.

| Unit | Depth (m) | Length (cm) | Diameter (cm) | Diameter category | Length/ diameter (cm) | Length ratio designation | Munsell colour | Colour | Diaphaneity | Shape | End treatment |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C4 | 0.4–0.5 | 4.3 | 3.6 | medium | 1.2 | standard | 2.5B 5/5 | blue-green | translucent-opaque | tubular | untreated |
| C4 | 0.4–0.5 | 2.2 | 1.8 | minute | 1.2 | standard | 5G 6/6 | green | translucent-transparent | tubular | untreated |
| C4 | 0.7–0.8 | 3.6 | 3.6 | medium | 1.0 | standard | 7.5B 4/4 | blue | transparent-translucent | tubular | untreated |
| C4 | 0.7–0.8 | 1.4 | 1.8 | minute | 0.8 | short | 5BG 3/6 | green | transparent-translucent | cylinder | untreated |
| C4 | 0.7–0.8 | 1.8 | 2.5 | minute | 0.7 | short | 10G 4/5 | green | translucent | cylinder | untreated |
| C4 | 0.7–0.8 | 3.2 | 2.7 | small | 1.2 | standard | 2.5PB 5/4 | blue | translucent-opaque | tubular | untreated |
| C4 | 0.7–0.8 | 3.0 | 4.0 | medium | 0.8 | short | 7.5B 4/4 | blue | translucent | tubular | untreated |
| C4 | 0.8–0.9 | 2.4 | 3.5 | medium | 0.7 | short | 10Y 7/5 | yellow | opaque | cylinder | untreated |
| C4 | 0.8–0.9 | 2.9 | 2.7 | small | 1.1 | standard | 5.0Y 8/8 | yellow | opaque | cylinder | untreated |
| C4 | 0.8–0.9 | 3.8 | 2.9 | small | 1.3 | long | 7.5BG 6/3 | blue-green | translucent-opaque | tubular | untreated |
| C4 | 0.8–0.9 | 3.4 | 3.8 | medium | 0.9 | standard | 7.5B 4/4 | blue | transparent | tubular | untreated |
| C4 | 0.8–0.9 | 3.2 | 4.2 | medium | 0.8 | short | 7.5B 4/4 | blue | translucent-transparent | tubular | untreated |
| C1 | 1.0–1.1 | 3.3 | 4.4 | medium | 0.7 | short | 10B 5/6 | blue | transparent-translucent | tubular | untreated |
| C1 | 1.0–1.1 | 6.0 | 5.4 | large | 1.1 | standard | 7.5B 4/4 | blue | translucent-transparent | tubular | untreated |
| C1 | 1.0–1.1 | 3.0 | 3.7 | medium | 0.8 | short | 7.5B 4/4 | blue | translucent | tubular | untreated |
| C1 | 1.1–1.2 | 5.1 | 4.3 | medium | 1.2 | standard | 7.5B 4/4 | blue | translucent | tubular | untreated |
| C1 | 1.3–1.4 | 3.1 | 4.7 | large | 0.7 | short | 5B 5/7 | blue-green | transparent | tubular | untreated |
| C1 | 1.3–1.4 | 3.5 | 4.1 | medium | 0.9 | standard | 2.5PB 5/2 | blue | opaque | cylinder | untreated |
| C1 | 1.3–1.4 | 2.2 | 3.0 | small | 0.7 | short | 2.5B 6/4 | blue-green | transparent-translucent | cylinder | untreated |
| C4 | 1.7–1.8 | 2.4 | 3.5 | medium | 0.7 | short | 10Y 8/10 | yellow | opaque | tubular | untreated |
| C4 | 1.7–1.8 | 2.6 | 3.0 | small | 0.9 | standard | 5Y 8/10 | yellow | opaque | tubular | untreated |
| C4 | 1.7–1.8 | 2.2 | 3.0 | small | 0.7 | short | 10B 4/6 | blue | transparent | tubular | untreated |
| C4 | 1.7–1.8 | 3.2 | 3.0 | small | 1.1 | standard | 7.5BG 8/4 | blue-green | translucent | tubular | untreated |

Table S2. Measured composition in %w of oxides and parts per million of elements.

|  | KC4181 | KC4182 | KC4184 | KC1141 | KC1142 | KC1143 | KC4092 | KC4094 | KC4095 | KC4096 | KC4082 | KC4083 | KC4084 | KC4085 | KC1111 | KC1112 | KC1113 | KC1121 | KC4051 | KC4052 | KC4096 | KC4183 | KC4093 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SiO2 | 63.7% | 62.7% | 65.6% | 66.7% | 64.6% | 68.4% | 60.4% | 64.1% | 63.7% | 61.7% | 66.4% | 67.2% | 60.8% | 46.4% | 70.3% | 68.0% | 64.6% | 67.6% | 66.7% | 34.9% | 61.7% | 62.4% | 66.9% |
| Na2O | 10.4% | 10.9% | 14.9% | 13.2% | 14.4% | 14.2% | 15.7% | 15.3% | 13.3% | 14.2% | 12.3% | 15.0% | 12.3% | 10.0% | 10.0% | 14.7% | 15.5% | 13.8% | 13.8% | 7.3% | 14.2% | 15.5% | 16.2% |
| MgO | 4.15% | 3.96% | 4.76% | 4.22% | 3.92% | 4.45% | 4.98% | 4.03% | 3.93% | 4.63% | 3.88% | 4.54% | 3.84% | 3.30% | 2.59% | 4.46% | 4.34% | 3.89% | 3.54% | 2.83% | 4.63% | 2.83% | 2.37% |
| Al2O3 | 2.86% | 2.71% | 2.81% | 2.77% | 3.59% | 1.76% | 2.65% | 3.67% | 3.54% | 2.63% | 3.28% | 3.04% | 2.31% | 2.14% | 5.30% | 2.86% | 3.93% | 3.42% | 3.56% | 2.02% | 2.63% | 4.38% | 3.41% |
| P2O3 | 0.19% | 0.14% | 0.19% | 0.19% | 0.32% | 0.30% | 0.18% | 0.29% | 0.26% | 0.07% | 0.37% | 0.17% | 0.26% | 0.12% | 0.15% | 0.15% | 0.16% | 0.20% | 0.20% | 0.20% | 0.07% | 0.56% | 0.41% |
| K2O | 6.38% | 6.77% | 3.56% | 4.70% | 4.01% | 3.38% | 3.19% | 3.73% | 5.72% | 2.92% | 3.03% | 2.77% | 2.50% | 1.91% | 5.28% | 3.09% | 2.85% | 3.71% | 4.11% | 1.52% | 2.92% | 5.15% | 4.73% |
| CaO | 5.06% | 4.59% | 5.89% | 5.85% | 6.52% | 5.79% | 5.97% | 6.48% | 6.41% | 4.71% | 7.41% | 5.30% | 5.77% | 4.34% | 4.23% | 5.07% | 6.50% | 5.26% | 5.81% | 4.18% | 4.71% | 5.30% | 3.58% |
| MnO | 1.14% | 1.26% | 0.72% | 0.55% | 1.24% | 0.07% | 1.14% | 0.53% | 1.23% | 0.58% | 1.24% | 0.90% | 0.22% | 0.12% | 0.64% | 0.30% | 0.75% | 0.83% | 0.73% | 0.07% | 0.58% | 0.52% | 0.37% |
| Fe2O3 | 0.60% | 0.49% | 0.89% | 0.67% | 0.98% | 0.59% | 0.50% | 1.21% | 1.29% | 0.46% | 1.53% | 0.69% | 0.95% | 1.13% | 1.25% | 0.88% | 1.04% | 1.02% | 1.26% | 0.73% | 0.46% | 2.31% | 1.71% |
| CuO | 0.00% | 0.00% | 0.08% | 0.06% | 0.04% | 0.79% | 0.00% | 0.08% | 0.08% | 0.00% | 0.12% | 0.05% | 1.61% | 1.33% | 0.05% | 0.07% | 0.07% | 0.04% | 0.09% | 0.70% | 0.00% | 0.88% | 0.22% |
| SnO2 | 0.57% | 0.84% | 0.06% | 0.11% | 0.04% | 0.02% | 0.72% | 0.06% | 0.07% | 0.73% | 0.03% | 0.02% | 0.06% | 0.07% | 0.03% | 0.03% | 0.02% | 0.01% | 0.02% | 0.58% | 0.73% | 0.01% | 0.01% |
| PbO2 | 4.89% | 5.52% | 0.43% | 0.94% | 0.36% | 0.10% | 4.52% | 0.41% | 0.36% | 7.29% | 0.36% | 0.26% | 8.89% | 28.8% | 0.18% | 0.36% | 0.22% | 0.14% | 0.16% | 44.9% | 7.29% | 0.13% | 0.08% |
| Ti | 512 | 427 | 474 | 429 | 680 | 389 | 387 | 736 | 741 | 347 | 706 | 484 | 444 | 364 | 644 | 607 | 701 | 619 | 687 | 414 | 347 | 1251 | 903 |
| V | 13 | 13 | 12 | 10 | 19 | 13 | 13 | 20 | 20 | 189 | 27 | 14 | 15 | 13 | 22 | 12 | 18 | 18 | 21 | 358 | 189 | 31 | 25 |
| Cr | 32 | 38 | 39 | 41 | 50 | 48 | 33 | 48 | 63 | 23 | 48 | 34 | 36 | 35 | 43 | 38 | 47 | 42 | 41 | 37 | 23 | 25 | 22 |
| Ni | 19 | 15 | 81 | 65 | 62 | 32 | 20 | 98 | 39 | 14 | 37 | 60 | 64 | 55 | 146 | 63 | 46 | 89 | 124 | 28 | 14 | 34 | 17 |
| Co | 3 | 3 | 370 | 199 | 216 | 12 | 3 | 448 | 363 | 2 | 347 | 167 | 16 | 8 | 420 | 355 | 195 | 351 | 337 | 7 | 2 | 10 | 25 |
| Zn | 43 | 43 | 114 | 48 | 111 | 612 | 35 | 133 | 231 | 33 | 245 | 65 | 3160 | 2218 | 74 | 123 | 86 | 100 | 122 | 886 | 33 | 95 | 42 |
| As | 54 | 47 | <dl | 2 | <dl | <dl | 4 | <dl | <dl | <dl | <dl | <dl | 160 | 884 | <dl | <dl | <dl | <dl | <dl | 443 | <dl | 8 | 0 |
| Rb | 112 | 52 | 23 | 23 | 20 | 18 | 22 | 21 | 23 | 19 | 23 | 20 | 15 | 12 | 38 | 21 | 20 | 26 | 29 | 12 | 19 | 54 | 36 |
| Sr | 548 | 474 | 550 | 512 | 465 | 455 | 540 | 456 | 466 | 466 | 521 | 471 | 431 | 350 | 277 | 428 | 465 | 396 | 381 | 330 | 466 | 701 | 621 |
| Zr | 62 | 58 | 52 | 63 | 76 | 21 | 41 | 77 | 75 | 41 | 74 | 59 | 37 | 37 | 101 | 68 | 75 | 79 | 68 | 32 | 41 | 98 | 62 |
| Nb | 2 | 2 | 2 | 2 | 3 | 1 | 2 | 3 | 3 | 2 | 3 | 2 | 2 | 2 | 3 | 2 | 3 | 3 | 3 | 2 | 2 | 5 | 4 |
| Cs | 1.5 | 0.5 | 0.6 | 0.3 | 0.4 | 0.6 | 0.4 | 0.4 | 0.4 | 0.2 | 0.5 | 0.3 | 0.4 | 0.3 | 0.3 | 0.3 | 0.2 | 0.3 | 0.4 | 0.3 | 0.2 | 2.2 | 1.5 |
| Ba | 283 | 287 | 225 | 201 | 272 | 103 | 217 | 225 | 289 | 147 | 286 | 226 | 162 | 119 | 157 | 171 | 220 | 207 | 213 | 96 | 147 | 236 | 566 |
| Y | 5 | 5 | 5 | 4 | 6 | 3 | 4 | 6 | 6 | 4 | 5 | 5 | 4 | 3 | 4 | 5 | 6 | 5 | 6 | 3 | 4 | 13 | 9 |
| U | 0.8 | 0.5 | 0.8 | 0.6 | 0.8 | 0.5 | 0.6 | 0.8 | 0.8 | 0.9 | 1.0 | 0.8 | 0.6 | 0.5 | 0.9 | 0.6 | 0.8 | 0.8 | 0.8 | 0.4 | 0.9 | 2.4 | 1.5 |
| Hf | 2.0 | 1.9 | 1.7 | 1.8 | 2.4 | 0.9 | 1.2 | 2.0 | 2.1 | 1.1 | 2.5 | 2.1 | 1.4 | 1.2 | 2.5 | 2.0 | 2.0 | 2.1 | 2.0 | 0.8 | 1.1 | 2.8 | 1.7 |
| Th | 1.7 | 1.4 | 1.6 | 1.2 | 1.8 | 0.9 | 1.2 | 1.8 | 1.7 | 1.1 | 2.1 | 1.7 | 1.2 | 1.0 | 1.5 | 1.5 | 1.7 | 1.5 | 1.7 | 0.8 | 1.1 | 6.6 | 4.3 |