**Analysis Report – Sample B**

**Global R-Values**

Rexp : 3.98 Rwp : 12.30 Rp : 9.01 GOF : 3.09

Rexp`: 7.61 Rwp`: 23.51 Rp` : 19.36 DW : 0.21

**R-Values**

Rexp : 3.98 Rwp : 12.30 Rp : 9.01 GOF : 3.09

Rexp`: 7.61 Rwp`: 23.51 Rp` : 19.36 DW : 0.21

**Quantitative Analysis - Rietveld**

Phase 1 : quartz\_icdd\_00-046-1045 1.331 %

Phase 2 : "kaolinite \_bish\_icdd\_00-014-0164" 89.318 %

Phase 3 : microcline\_icdd\_00-019-0926 4.007 %

Phase 4 : muscovite\_icdd\_04-015-8226 5.344 %

**Background**

Chebychev polynomial, Coefficient 0 385.9971

1 -244.7688

2 137.152

3 -86.36836

4 57.79736

5 -42.16327

**Instrument**

Primary radius (mm) 200.5

Secondary radius (mm) 200.5

Linear PSD 2Th angular range (°) 4

FDS angle (°) 0.3

Beam spill, sample length (mm) 20

Intensity corrected

Full Axial Convolution

Filament length (mm) 12

Sample length (mm) 15

Receiving Slit length (mm) 12

Primary Sollers (°) 2.5

Secondary Sollers (°) 2.5

**Corrections**

Specimen displacement 0.2857258

LP Factor 0

Absorption (1/cm) 4.289493

**Miscellaneous**

Start X 5

**Structure 1**

Phase name quartz\_icdd\_00-046-1045

R-Bragg 0.000

Spacegroup 154

Scale 4.41852e-004

Cell Mass 180.253

Cell Volume (Å^3) 109.77341

Wt% - Rietveld 1.331

Crystal Linear Absorption Coeff. (1/cm) 141.434

Crystal Density (g/cm^3) 2.727

Lattice parameters

a (Å) 4.8572869

c (Å) 5.3725320

Site Np x y z Atom Occ Beq

Si\_1 3 0.47230 0.00000 0.66667 Si 1 0.5953

O\_1 6 0.41600 0.26580 0.78810 O 1 1.379

**Structure 2**

Phase name kaolinite \_bish\_icdd\_00-014-0164

R-Bragg 0.000

Spacegroup C1

Scale 3.54404e-003

Cell Mass 508.257

Cell Volume (Å^3) 325.76763

Wt% - Rietveld 89.318

Double-Voigt|Approach

Cry size Lorentzian 20.0

Cry size Gaussian 10000.0

k: 1 LVol-IB (nm) 12.721

k: 0.89 LVol-FWHM (nm) 17.778

Strain

Strain L 1.140966

Strain G 1.877819

e0 0.00560

Crystal Linear Absorption Coeff. (1/cm) 115.064

Crystal Density (g/cm^3) 2.591

Preferred Orientation (Dir 1 : 0 0 1) 0.3680248

(Dir 2 : 0 2 0) 1

Fraction of Dir 1 0.04610595

Lattice parameters

a (Å) 5.1200000

b (Å) 8.9000000

c (Å) 7.4067664

alpha (°) 92.3

beta (°) 104.9859

gamma (°) 89.61008

Site Np x y z Atom Occ Beq

s1 2 0.99420 0.33930 0.09090 SI+4 1 0.44

s2 2 0.50640 0.16650 0.09130 SI+4 1 0.44

s3 2 0.29710 0.49570 0.47210 AL+3 1 0.83

s4 2 0.79260 0.33000 0.46990 AL+3 1 0.83

s5 2 0.05010 0.35390 0.31700 O-2 1 0.71

s6 2 0.12140 0.66040 0.31750 O-2 1 0.71

s7 2 0.00000 0.50000 0.00000 O-2 1 0.71

s8 2 0.20850 0.23050 0.02470 O-2 1 0.71

s9 2 0.20120 0.76570 0.00320 O-2 1 0.71

s10 2 0.05100 0.96980 0.32200 O-2 1 0.9

s11 2 0.96490 0.16650 0.60510 O-2 1 0.9

s12 2 0.03480 0.47690 0.60800 O-2 1 0.9

s13 2 0.03340 0.85700 0.60940 O-2 1 0.9

**Structure 3**

Phase name microcline\_icdd\_00-019-0926

R-Bragg 0.000

Spacegroup C-1

Scale 3.27696e-005

Cell Mass 1113.326

Cell Volume (Å^3) 721.60834

Wt% - Rietveld 4.007

Crystal Linear Absorption Coeff. (1/cm) 186.736

Crystal Density (g/cm^3) 2.562

Preferred Orientation (Dir 1 : 0 0 1) 1

(Dir 2 : 0 0 2) 0.1934569

Fraction of Dir 1 0.9921175

Lattice parameters

a (Å) 8.6590000

b (Å) 12.9809448

c (Å) 7.1500682

alpha (°) 90.56368

beta (°) 115.9462

gamma (°) 87

Site Np x y z Atom Occ Beq

s1 4 0.28310 -0.00670 0.13600 K+1 1 1.35

s2 4 0.00960 0.18800 0.21790 AL+3 0.9 0.6

SI+4 0.1 0.6

s3 4 0.00980 0.81910 0.23270 AL+3 0.03 0.61

SI+4 0.97 0.61

s4 4 0.71170 0.12000 0.34000 AL+3 0.07 0.56

SI+4 0.93 0.56

s5 4 0.70670 0.88580 0.34950 SI+4 1 0.54

s6 4 0.00070 0.14480 -0.01790 O-2 1 1.11

s7 4 0.63610 0.00530 0.28620 O-2 1 0.58

s8 4 0.82180 0.14760 0.22000 O-2 1 1.14

s9 4 0.83070 0.85680 0.24350 O-2 1 1.42

s10 4 0.03470 0.31880 0.25640 O-2 1 0.67

s11 4 0.03820 0.69550 0.26460 O-2 1 0.74

s12 4 0.19000 0.12280 0.40550 O-2 1 1.14

s13 4 0.17540 0.87450 0.40910 O-2 1 1.31

**Structure 4**

Phase name muscovite\_icdd\_04-015-8226

R-Bragg 0.000

Spacegroup 15

Scale 2.42724e-005

Cell Mass 1606.311

Cell Volume (Å^3) 900.51933

Wt% - Rietveld 5.344

Crystal Linear Absorption Coeff. (1/cm) 187.006

Crystal Density (g/cm^3) 2.962

Preferred Orientation (Dir 1 : 0 0 1) 1

Lattice parameters

a (Å) 5.0903496

b (Å) 8.9119763

c (Å) 19.9498316

beta (°) 95.72

Site Np x y z Atom Occ Beq

O\_1 8 0.74930 0.31190 0.15780 O 1 1.364

O\_2 8 0.24770 0.36840 0.16880 O 1 1.12

O\_3 8 0.41980 0.09290 0.16830 O 1 1.263

O\_4 8 0.38640 0.25140 0.05345 O 1 1

O\_5 8 0.96110 0.44280 0.05344 O 1 0.6483

O\_6 8 0.95600 0.06280 0.05033 O 0.925 0.9666

O\_7 8 0.95600 0.06280 0.05033 O 0.055 0.9666

F\_1 8 0.95600 0.06280 0.05033 F 0.02 0.9666

Si\_1 8 0.45230 0.25823 0.13538 Si 0.753 0.4673

Al\_1 8 0.45230 0.25823 0.13538 Al 0.247 0.4673

Si\_2 8 0.96500 0.42943 0.13534 Si 0.753 0.4458

Al\_2 8 0.96500 0.42943 0.13534 Al 0.247 0.4458

Al\_3 4 0.75000 0.25000 0.00000 Al 0.0896 1.24

Fe\_1 4 0.75000 0.25000 0.00000 Fe 0.0057 1.24

Mg\_1 4 0.75000 0.25000 0.00000 Mg 0.0033 1.24

Ti\_1 4 0.75000 0.25000 0.00000 Ti 0.0014 1.24

Al\_4 8 0.24960 0.08351 -0.00001 Al 0.896 0.8226

Fe\_2 8 0.24960 0.08351 -0.00001 Fe 0.057 0.8226

Mg\_2 8 0.24960 0.08351 -0.00001 Mg 0.033 0.8226

Ti\_2 8 0.24960 0.08351 -0.00001 Ti 0.014 0.8226

K\_1 4 0.00000 0.09830 0.25000 K 0.9398 1.886

Na\_1 4 0.00000 0.09830 0.25000 Na 0.04018 1.886