|  |  |  |
| --- | --- | --- |
| Ink | H (microns) | R (microns) |
| A | 17.3 | 112.8 |
| B | 17.9 | 103.3 |
| C | 15.6 | 116.1 |
| D | 15.7 | 112.5 |
| E | 14.5 | 111.7 |
| F | 3.4 | 250.2 |
| G | 15.0 | 121.6 |
| H | 8.6 | 160.4 |

Thin, binary liquid droplets, containing polymer: an investigation of the parameters controlling film shape  
by Adam Eales; Nick Dartnell; Simon Goddard and Alexander Routh

Supplementary Information

Experimental Details for data reported in figures 14-16