|  |  | Atom | CN | <d> | dmin | dmax |  | Vs | Vp | υ | ECCv | SPHv | Valence sum |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | balićžunićite |  |  |  |  |  |  |  |  |
|  | Bi(1) |  | 7 | 2.5(1) | 2.081(14) | 2.993(16) | 78.712 |  | 19.8(2) | 0.3340 | 0.5858 | 0.9300 | 3.09 |  |
|  | Bi(2) |  | 8 | 2.5(3) | 2.164(16) | 2.874(16) | 71.886 |  | 27.3(3) | 0.1224 | 0.4873 | 0.9236 | 3.16 |  |
|  | Bi(3) |  | 7 | 2.5(3) | 2.108(15) | 2.918(16) | 68.605 |  | 23.6(3) | 0.0899 | 0.4548 | 0.8179 | 3.17 |  |
|  | Bi(4) |  | 7 | 2.5(4) | 2.116(14) | 3.012(16) | 76.962 |  | 21.7(3) | 0.2540 | 0.5657 | 0.9122 | 3.18 |  |
|  | Bi(5) |  | 7 | 2.5(3) | 2.090(13) | 2.879(19) | 70.209 |  | 19.4(2) | 0.2700 | 0.4848 | 0.9479 | 3.13 |  |
|  | Bi(6) |  | 6 | 2.4(1) | 2.265(14) | 2.524(16) | 59.793 |  | 15.7(2) | 0.1766 | 0.2080 | 0.9621 | 2.75** |  |
|  | S(1) |  | 4 | 1.49(3) | 1.448(17) | 1.511(15) | 13.700 |  | 1.67(4) | 0.0049 | 0.0902 | 1.0000 | 5.835 |  |
|  | S(2) |  | 4 | 1.49(3) | 1.465(15) | 1.532(16) | 13.800 |  | 1.69(3) | 0.0014 | 0.0896 | 1.0000 | 5.787 |  |
|  | S(3) |  | 4 | 1.45(3) | 1.43(2) | 1.487(15) | 12.685 |  | 1.55(5) | 0.0021 | 0.0811 | 0.9999 | 6.475 |  |
|  | S(4) |  | 4 | 1.48(4) | 1.44(2) | 1.525(15) | 13.496 |  | 1.65(4) | 0.0007 | 0.1038 | 0.9999 | 5.972 |  |
|  | S(5) |  | 4 | 1.48(4) | 1.445(15) | 1.521(16) | 13.455 |  | 1.65(4) | 0.0008 | 0.1020 | 1.0000 | 5.987 |  |
|  | S(6) |  | 4 | 1.48(2) | 1.469(15) | 1.506(17) | 13.688 |  | 1.68(4) | 0.0009 | 0.0483 | 0.9996 | 5.840 |  |
|  |  |  |  |  | Syn Bi2O(SO4)2 (Aurivillius 1988) |  |  |  |  |  |  |  |  |  |
|  | Bi(1) |  | 7 | 2.5(3) | 2.118(55) | 2.969(82) | 67.737 |  | 22(1) | 0.1554 | 0.4377 | 0.9852 | 3.082 |  |
|  | Bi(2) |  | 7 | 2.5(3) | 2.090(35) | 2.931(51) | 67.693 |  | 21(1) | 0.1761 | 0.4897 | 0.8630 | 3.493 |  |
|  | Bi(3) |  | 7 | 2.5(3) | 2.221(55) | 2.858(56) | 67.100 |  | 21(1) | 0.1892 | 0.3991 | 0.8892 | 2.979 |  |
|  | Bi(4) |  | 7 | 2.5(3) | 2.062(58) | 2.874(81) | 67.865 |  | 21(1) | 0.1784 | 0.4281 | 0.9203 | 3.144 |  |
|  | Bi(5) |  | 7 | 2.5(3) | 2.173(53) | 2.871(61) | 70.448 |  | 22(1) | 0.1663 | 0.4037 | 0.9206 | 2.708 |  |
|  | Bi(6) |  | 7 | 2.5(4) | 2.093(48) | 3.320(51) | 78.758 |  | 23(1) | 0.2235 | 0.5865 | 0.9105 | 3.173 |  |
|  | S(1) |  | 4 | 1.49(9) | 1.39(7) | 1.56(6) | 13.715 |  | 1.7(2) | 0.0059 | 0.2495 | 0.9992 | 5.944 |  |
|  | S(2) |  | 4 | 1.50(4) | 1.45(5) | 1.55(5) | 14.288 |  | 1.7(2) | 0.0118 | 0.1194 | 0.9999 | 5.555 |  |
|  | S(3) |  | 4 | 1.50(4) | 1.46(8) | 1.54(4) | 14.123 |  | 1.7(2) | 0.0055 | 0.1133 | 0.9970 | 5.631 |  |
|  | S(4) |  | 4 | 1.53(5) | 1.51(5) | 1.56(5) | 15.016 |  | 1.8(2) | 0.0024 | 0.0545 | 0.9990 | 5.154 |  |
|  | S(5) |  | 4 | 1.48(10) | 1.34(4) | 1.58(6) | 13.549 |  | 1.6(2) | 0.0222 | 0.2809 | 1.0000 | 6.139 |  |
|  | S(6) |  | 4 | 1.48(7) | 1.41(8) | 1.57(4) | 13.396 |  | 1.6(2) | 0.0130 | 0.2143 | 0.9985 | 6.074 |  |

Table 6. Coordination parameters* for Bi atoms and sulfate groups in the crystal structures  of balićžunićite and syn Bi2O(SO4)2 (Aurivillius 1988)

<d>: average bond distance, Vs: volume of the circumscribed sphere, Vp: volume of the coordination polyhedron, : volume distortion, ECCv: volume-based eccentricity of the coordination, SPHv: volume-based sphericity of the coordination.

(*) The parameters for atom coordinations are defined in Balić-Žunić & Makovicky (1996) and in Makovicky & Balić-Žunić (1998). Bond valence calculations were made using the parameters of Brese & O'Keeffe (1991). All calculations were done by IVTON  (Balić-Žunić & Vicković 1996). For the mixed sites the calculated valences of individual species are multiplied by the fractional occupancies and summed.

(**)  Bond valance sum is equal to 2.99 for CN8.