data_davidlloydite

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'H1.14 As0.29 O1.71 Zn0.43'

_chemical_formula_weight          78.00

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'O'  'O'   0.0106   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'H'  'H'   0.0000   0.0000

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Zn'  'Zn'   0.2839   1.4301

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'As'  'As'   0.0499   2.0058

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            ?

_symmetry_space_group_name_H-M    ?

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x, -y, -z'

_cell_length_a                    5.9756(4)

_cell_length_b                    7.6002(5)

_cell_length_c                    5.4471(4)

_cell_angle_alpha                 84.2892(9)

_cell_angle_beta                  90.4920(9)

_cell_angle_gamma                 87.9958(9)

_cell_volume                      245.99(3)

_cell_formula_units_Z             7

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     ?

_cell_measurement_theta_min       ?

_cell_measurement_theta_max       ?

_exptl_crystal_description        ?

_exptl_crystal_colour             ?

_exptl_crystal_size_max           ?

_exptl_crystal_size_mid           ?

_exptl_crystal_size_min           ?

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     3.686

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              260

_exptl_absorpt_coefficient_mu     13.991

_exptl_absorpt_correction_type    ?

_exptl_absorpt_correction_T_min   ?

_exptl_absorpt_correction_T_max   ?

_exptl_absorpt_process_details    ?

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71073

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type   ?

_diffrn_measurement_method        ?

_diffrn_detector_area_resol_mean  ?

_diffrn_standards_number          ?

_diffrn_standards_interval_count  ?

_diffrn_standards_interval_time   ?

_diffrn_standards_decay_%         ?

_diffrn_reflns_number             2946

_diffrn_reflns_av_R_equivalents   0.0091

_diffrn_reflns_av_sigmaI/netI     0.0134

_diffrn_reflns_limit_h_min        -8

_diffrn_reflns_limit_h_max        8

_diffrn_reflns_limit_k_min        -10

_diffrn_reflns_limit_k_max        10

_diffrn_reflns_limit_l_min        -7

_diffrn_reflns_limit_l_max        7

_diffrn_reflns_theta_min          2.70

_diffrn_reflns_theta_max          30.24

_reflns_number_total              1477

_reflns_number_gt                 1422

_reflns_threshold_expression      >2sigma(I)

_computing_data_collection        ?

_computing_cell_refinement        ?

_computing_data_reduction         ?

_computing_structure_solution     'SHELXS-97 (Sheldrick, 1990)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 1997)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.0139P)^2^+0.3444P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      direct

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     mixed

_refine_ls_extinction_method      none

_refine_ls_extinction_coef        ?

_refine_ls_number_reflns          1477

_refine_ls_number_parameters      96

_refine_ls_number_restraints      4

_refine_ls_R_factor_all           0.0159

_refine_ls_R_factor_gt            0.0151

_refine_ls_wR_factor_ref          0.0413

_refine_ls_wR_factor_gt           0.0411

_refine_ls_goodness_of_fit_ref    1.263

_refine_ls_restrained_S_all       1.261

_refine_ls_shift/su_max           0.001

_refine_ls_shift/su_mean          0.000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symmetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

Zn1 Zn 0.0000 0.5000 0.5000 0.01224(12) Uani 0.937(2) 2 d SP . .

Zn2 Zn 0.23922(4) 0.10407(3) 0.81081(4) 0.01226(7) Uani 1 1 d . . .

As1 As 0.25896(3) 0.87032(3) 0.33696(4) 0.00916(6) Uani 1 1 d . . .

O1 O 0.4813(3) 0.7644(2) 0.2259(3) 0.0153(3) Uani 1 1 d . . .

O2 O 0.2996(3) 0.8972(2) 0.6354(3) 0.0146(3) Uani 1 1 d . . .

O3 O 0.0271(3) 0.7464(2) 0.3144(3) 0.0128(3) Uani 1 1 d . . .

O4 O 0.1952(3) 0.0630(2) 0.1674(3) 0.0145(3) Uani 1 1 d . . .

O5 O 0.2229(3) 0.4010(2) 0.2726(3) 0.0181(3) Uani 1 1 d D . .

O6 O 0.2711(3) 0.5420(2) 0.7834(3) 0.0208(3) Uani 1 1 d D . .

H1 H 0.211(6) 0.2762(14) 0.245(7) 0.039(10) Uiso 1 1 d D . .

H2 H 0.232(7) 0.453(5) 0.101(3) 0.056(13) Uiso 1 1 d D . .

H3 H 0.413(4) 0.481(5) 0.748(8) 0.058(13) Uiso 1 1 d D . .

H4 H 0.325(7) 0.662(2) 0.791(8) 0.059(13) Uiso 1 1 d D . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

Zn1 0.01425(19) 0.01053(18) 0.01178(19) -0.00034(12) 0.00126(12) 0.00005(13)

Zn2 0.01204(12) 0.01445(12) 0.01032(11) -0.00186(8) -0.00006(8) 0.00121(9)

As1 0.00945(10) 0.00940(10) 0.00869(10) -0.00125(7) 0.00025(7) 0.00002(7)

O1 0.0119(7) 0.0140(7) 0.0204(8) -0.0045(6) 0.0037(6) 0.0007(5)

O2 0.0200(8) 0.0144(7) 0.0096(7) -0.0027(5) -0.0011(5) 0.0006(6)

O3 0.0103(6) 0.0120(7) 0.0157(7) 0.0002(5) -0.0012(5) -0.0014(5)

O4 0.0209(8) 0.0116(7) 0.0105(7) 0.0010(5) -0.0006(6) 0.0014(6)

O5 0.0253(9) 0.0134(7) 0.0155(7) -0.0007(6) 0.0037(6) 0.0009(6)

O6 0.0190(8) 0.0162(8) 0.0270(9) -0.0008(6) 0.0031(7) -0.0009(6)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

Zn1 O5 2.0048(17) 2_566 ?

Zn1 O5 2.0048(17) . ?

Zn1 O3 2.0496(15) . ?

Zn1 O3 2.0496(15) 2_566 ?

Zn1 O6 2.2806(19) 2_566 ?

Zn1 O6 2.2806(19) . ?

Zn2 O2 1.9444(16) 1_545 ?

Zn2 O4 1.9578(15) 1_556 ?

Zn2 O1 1.9778(16) 2_666 ?

Zn2 O3 1.9976(15) 2_566 ?

Zn2 O6 3.3290(18) . ?

Zn2 O5 3.5155(17) . ?

Zn2 O5 3.5422(17) 1_556 ?

As1 O2 1.6751(15) . ?

As1 O1 1.6777(15) . ?

As1 O4 1.6817(15) 1_565 ?

As1 O3 1.7129(15) . ?

As1 O6 3.3050(18) . ?

As1 O5 3.6325(17) . ?

O1 Zn2 1.9778(16) 2_666 ?

O1 O6 2.720(2) 2_666 ?

O1 O5 3.200(2) . ?

O1 O6 3.339(2) 1_554 ?

O1 O5 3.353(2) 2_666 ?

O2 Zn2 1.9444(16) 1_565 ?

O2 O6 2.751(2) . ?

O3 Zn2 1.9976(15) 2_566 ?

O3 O5 2.867(2) 2_566 ?

O3 O5 2.867(2) . ?

O3 O6 2.958(2) 2_566 ?

O3 O6 3.171(2) . ?

O4 As1 1.6817(15) 1_545 ?

O4 Zn2 1.9578(15) 1_554 ?

O4 O5 2.697(2) . ?

O5 O6 2.792(2) 1_554 ?

O5 O3 2.867(2) 2_566 ?

O5 O6 2.977(3) 2_566 ?

O5 O6 3.083(3) 2_666 ?

O5 O6 3.094(2) . ?

O5 O1 3.353(2) 2_666 ?

O5 Zn2 3.5422(17) 1_554 ?

O5 H1 0.9798(10) . ?

O5 H2 0.9800(10) . ?

O6 O1 2.720(2) 2_666 ?

O6 O5 2.792(2) 1_556 ?

O6 O3 2.958(2) 2_566 ?

O6 O5 2.977(3) 2_566 ?

O6 O5 3.083(3) 2_666 ?

O6 O1 3.339(2) 1_556 ?

O6 H3 0.9799(10) . ?

O6 H4 0.9799(11) . ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

O5 Zn1 O5 180.0 2_566 . ?

O5 Zn1 O3 90.00(6) 2_566 . ?

O5 Zn1 O3 90.00(6) . . ?

O5 Zn1 O3 90.00(6) 2_566 2_566 ?

O5 Zn1 O3 90.00(6) . 2_566 ?

O3 Zn1 O3 180.00(4) . 2_566 ?

O5 Zn1 O6 92.23(7) 2_566 2_566 ?

O5 Zn1 O6 87.77(7) . 2_566 ?

O3 Zn1 O6 86.01(6) . 2_566 ?

O3 Zn1 O6 93.99(6) 2_566 2_566 ?

O5 Zn1 O6 87.77(7) 2_566 . ?

O5 Zn1 O6 92.23(7) . . ?

O3 Zn1 O6 93.99(6) . . ?

O3 Zn1 O6 86.01(6) 2_566 . ?

O6 Zn1 O6 180.0 2_566 . ?

O2 Zn2 O4 117.06(6) 1_545 1_556 ?

O2 Zn2 O1 103.63(7) 1_545 2_666 ?

O4 Zn2 O1 104.91(7) 1_556 2_666 ?

O2 Zn2 O3 114.66(7) 1_545 2_566 ?

O4 Zn2 O3 104.64(7) 1_556 2_566 ?

O1 Zn2 O3 111.65(7) 2_666 2_566 ?

O2 Zn2 O6 144.68(6) 1_545 . ?

O4 Zn2 O6 96.76(6) 1_556 . ?

O1 Zn2 O6 54.77(5) 2_666 . ?

O3 Zn2 O6 61.62(5) 2_566 . ?

O2 Zn2 O5 94.15(5) 1_545 . ?

O4 Zn2 O5 148.54(5) 1_556 . ?

O1 Zn2 O5 68.81(6) 2_666 . ?

O3 Zn2 O5 54.63(5) 2_566 . ?

O6 Zn2 O5 53.67(4) . . ?

O2 Zn2 O5 162.52(5) 1_545 1_556 ?

O4 Zn2 O5 48.97(5) 1_556 1_556 ?

O1 Zn2 O5 74.37(5) 2_666 1_556 ?

O3 Zn2 O5 81.55(5) 2_566 1_556 ?

O6 Zn2 O5 47.83(4) . 1_556 ?

O5 Zn2 O5 101.03(4) . 1_556 ?

O2 As1 O1 110.45(8) . . ?

O2 As1 O4 112.10(8) . 1_565 ?

O1 As1 O4 111.91(8) . 1_565 ?

O2 As1 O3 107.90(8) . . ?

O1 As1 O3 109.35(8) . . ?

O4 As1 O3 104.87(8) 1_565 . ?

O2 As1 O6 56.20(6) . . ?

O1 As1 O6 85.40(6) . . ?

O4 As1 O6 162.43(6) 1_565 . ?

O3 As1 O6 70.37(6) . . ?

O2 As1 O5 108.82(6) . . ?

O1 As1 O5 61.76(6) . . ?

O4 As1 O5 137.54(6) 1_565 . ?

O3 As1 O5 50.54(6) . . ?

O6 As1 O5 52.72(4) . . ?

As1 O1 Zn2 116.90(9) . 2_666 ?

As1 O1 O6 148.09(9) . 2_666 ?

Zn2 O1 O6 88.79(7) 2_666 2_666 ?

As1 O1 O5 90.74(7) . . ?

Zn2 O1 O5 150.92(8) 2_666 . ?

O6 O1 O5 62.13(6) 2_666 . ?

As1 O1 O6 104.71(8) . 1_554 ?

Zn2 O1 O6 123.25(7) 2_666 1_554 ?

O6 O1 O6 71.96(7) 2_666 1_554 ?

O5 O1 O6 50.50(5) . 1_554 ?

As1 O1 O5 104.77(7) . 2_666 ?

Zn2 O1 O5 77.83(6) 2_666 2_666 ?

O6 O1 O5 60.20(6) 2_666 2_666 ?

O5 O1 O5 86.88(6) . 2_666 ?

O6 O1 O5 127.53(6) 1_554 2_666 ?

As1 O2 Zn2 129.56(9) . 1_565 ?

As1 O2 O6 93.41(8) . . ?

Zn2 O2 O6 131.07(8) 1_565 . ?

As1 O3 Zn2 111.52(8) . 2_566 ?

As1 O3 Zn1 122.77(8) . . ?

Zn2 O3 Zn1 122.64(8) 2_566 . ?

As1 O3 O5 124.48(8) . 2_566 ?

Zn2 O3 O5 90.74(6) 2_566 2_566 ?

Zn1 O3 O5 44.37(4) . 2_566 ?

As1 O3 O5 101.99(7) . . ?

Zn2 O3 O5 139.30(8) 2_566 . ?

Zn1 O3 O5 44.36(4) . . ?

O5 O3 O5 88.73(6) 2_566 . ?

As1 O3 O6 162.50(9) . 2_566 ?

Zn2 O3 O6 81.93(6) 2_566 2_566 ?

Zn1 O3 O6 50.27(5) . 2_566 ?

O5 O3 O6 64.15(6) 2_566 2_566 ?

O5 O3 O6 61.45(6) . 2_566 ?

As1 O3 O6 79.04(6) . . ?

Zn2 O3 O6 145.93(8) 2_566 . ?

Zn1 O3 O6 45.85(4) . . ?

O5 O3 O6 58.84(6) 2_566 . ?

O5 O3 O6 61.42(6) . . ?

O6 O3 O6 96.12(6) 2_566 . ?

As1 O4 Zn2 124.07(9) 1_545 1_554 ?

As1 O4 O5 131.30(9) 1_545 . ?

Zn2 O4 O5 97.83(7) 1_554 . ?

Zn1 O5 O4 119.61(8) . . ?

Zn1 O5 O6 122.65(8) . 1_554 ?

O4 O5 O6 95.24(7) . 1_554 ?

Zn1 O5 O3 45.64(5) . 2_566 ?

O4 O5 O3 79.12(6) . 2_566 ?

O6 O5 O3 153.98(9) 1_554 2_566 ?

Zn1 O5 O3 45.63(5) . . ?

O4 O5 O3 151.60(9) . . ?

O6 O5 O3 81.72(7) 1_554 . ?

O3 O5 O3 91.27(6) 2_566 . ?

Zn1 O5 O6 49.94(5) . 2_566 ?

O4 O5 O6 91.06(7) . 2_566 ?

O6 O5 O6 89.26(7) 1_554 2_566 ?

O3 O5 O6 65.68(6) 2_566 2_566 ?

O3 O5 O6 60.78(6) . 2_566 ?

Zn1 O5 O6 130.64(8) . 2_666 ?

O4 O5 O6 101.42(7) . 2_666 ?

O6 O5 O6 75.27(7) 1_554 2_666 ?

O3 O5 O6 130.68(8) 2_566 2_666 ?

O3 O5 O6 105.01(7) . 2_666 ?

O6 O5 O6 160.83(9) 2_566 2_666 ?

Zn1 O5 O6 47.43(5) . . ?

O4 O5 O6 128.49(8) . . ?

O6 O5 O6 135.36(9) 1_554 . ?

O3 O5 O6 59.35(6) 2_566 . ?

O3 O5 O6 64.13(6) . . ?

O6 O5 O6 97.37(7) 2_566 . ?

O6 O5 O6 86.28(7) 2_666 . ?

Zn1 O5 O1 90.70(6) . . ?

O4 O5 O1 149.59(8) . . ?

O6 O5 O1 67.33(6) 1_554 . ?

O3 O5 O1 127.32(7) 2_566 . ?

O3 O5 O1 53.91(5) . . ?

O6 O5 O1 112.47(7) 2_566 . ?

O6 O5 O1 51.26(5) 2_666 . ?

O6 O5 O1 69.40(6) . . ?

Zn1 O5 O1 87.87(6) . 2_666 ?

O4 O5 O1 86.17(6) . 2_666 ?

O6 O5 O1 142.26(8) 1_554 2_666 ?

O3 O5 O1 63.28(5) 2_566 2_666 ?

O3 O5 O1 113.43(7) . 2_666 ?

O6 O5 O1 128.46(7) 2_566 2_666 ?

O6 O5 O1 67.54(6) 2_666 2_666 ?

O6 O5 O1 49.71(5) . 2_666 ?

O1 O5 O1 93.12(6) . 2_666 ?

Zn1 O5 Zn2 74.49(5) . . ?

O4 O5 Zn2 68.42(5) . . ?

O6 O5 Zn2 161.60(7) 1_554 . ?

O3 O5 Zn2 34.62(4) 2_566 . ?

O3 O5 Zn2 116.67(6) . . ?

O6 O5 Zn2 99.10(6) 2_566 . ?

O6 O5 Zn2 99.01(6) 2_666 . ?

O6 O5 Zn2 60.08(4) . . ?

O1 O5 Zn2 122.93(6) . . ?

O1 O5 Zn2 33.36(3) 2_666 . ?

Zn1 O5 Zn2 138.67(8) . 1_554 ?

O4 O5 Zn2 33.20(4) . 1_554 ?

O6 O5 Zn2 62.08(5) 1_554 1_554 ?

O3 O5 Zn2 109.69(6) 2_566 1_554 ?

O3 O5 Zn2 135.49(7) . 1_554 ?

O6 O5 Zn2 91.99(6) 2_566 1_554 ?

O6 O5 Zn2 90.67(5) 2_666 1_554 ?

O6 O5 Zn2 159.97(7) . 1_554 ?

O1 O5 Zn2 122.89(6) . 1_554 ?

O1 O5 Zn2 111.07(5) 2_666 1_554 ?

Zn2 O5 Zn2 101.03(4) . 1_554 ?

Zn1 O5 H1 117(2) . . ?

O4 O5 H1 3(2) . . ?

O6 O5 H1 99(2) 1_554 . ?

O3 O5 H1 76(2) 2_566 . ?

O3 O5 H1 152(2) . . ?

O6 O5 H1 91(2) 2_566 . ?

O6 O5 H1 102(2) 2_666 . ?

O6 O5 H1 125(2) . . ?

O1 O5 H1 152(2) . . ?

O1 O5 H1 84(2) 2_666 . ?

Zn2 O5 H1 65(2) . . ?

Zn2 O5 H1 37(2) 1_554 . ?

Zn1 O5 H2 120(3) . . ?

O4 O5 H2 96(3) . . ?

O6 O5 H2 3(3) 1_554 . ?

O3 O5 H2 152(3) 2_566 . ?

O3 O5 H2 80(3) . . ?

O6 O5 H2 87(3) 2_566 . ?

O6 O5 H2 78(3) 2_666 . ?

O6 O5 H2 135(3) . . ?

O1 O5 H2 68(3) . . ?

O1 O5 H2 145(3) 2_666 . ?

Zn2 O5 H2 164(3) . . ?

Zn2 O5 H2 63(3) 1_554 . ?

H1 O5 H2 100(3) . . ?

Zn1 O6 O1 100.04(7) . 2_666 ?

Zn1 O6 O2 94.07(7) . . ?

O1 O6 O2 139.42(8) 2_666 . ?

Zn1 O6 O5 119.42(8) . 1_556 ?

O1 O6 O5 80.48(7) 2_666 1_556 ?

O2 O6 O5 124.30(8) . 1_556 ?

Zn1 O6 O3 43.72(4) . 2_566 ?

O1 O6 O3 70.65(6) 2_666 2_566 ?

O2 O6 O3 136.98(8) . 2_566 ?

O5 O6 O3 82.73(7) 1_556 2_566 ?

Zn1 O6 O5 42.29(4) . 2_566 ?

O1 O6 O5 128.38(8) 2_666 2_566 ?

O2 O6 O5 86.50(7) . 2_566 ?

O5 O6 O5 90.74(7) 1_556 2_566 ?

O3 O6 O5 57.77(6) 2_566 2_566 ?

Zn1 O6 O5 131.35(8) . 2_666 ?

O1 O6 O5 66.60(6) 2_666 2_666 ?

O2 O6 O5 75.49(6) . 2_666 ?

O5 O6 O5 104.73(7) 1_556 2_666 ?

O3 O6 O5 134.40(8) 2_566 2_666 ?

O5 O6 O5 160.83(9) 2_566 2_666 ?

Zn1 O6 O5 40.35(5) . . ?

O1 O6 O5 70.10(6) 2_666 . ?

O2 O6 O5 99.41(7) . . ?

O5 O6 O5 135.36(9) 1_556 . ?

O3 O6 O5 56.49(6) 2_566 . ?

O5 O6 O5 82.63(7) 2_566 . ?

O5 O6 O5 93.72(7) 2_666 . ?

Zn1 O6 O3 40.16(4) . . ?

O1 O6 O3 124.05(8) 2_666 . ?

O2 O6 O3 54.55(5) . . ?

O5 O6 O3 145.56(8) 1_556 . ?

O3 O6 O3 83.88(6) 2_566 . ?

O5 O6 O3 55.48(5) 2_566 . ?

O5 O6 O3 107.31(7) 2_666 . ?

O5 O6 O3 54.46(5) . . ?

Zn1 O6 As1 69.87(5) . . ?

O1 O6 As1 124.39(7) 2_666 . ?

O2 O6 As1 30.39(4) . . ?

O5 O6 As1 153.22(7) 1_556 . ?

O3 O6 As1 113.08(7) 2_566 . ?

O5 O6 As1 81.01(5) 2_566 . ?

O5 O6 As1 80.11(5) 2_666 . ?

O5 O6 As1 69.08(5) . . ?

O3 O6 As1 30.59(3) . . ?

Zn1 O6 Zn2 75.99(5) . . ?

O1 O6 Zn2 36.44(4) 2_666 . ?

O2 O6 Zn2 165.59(8) . . ?

O5 O6 Zn2 70.08(5) 1_556 . ?

O3 O6 Zn2 36.45(4) 2_566 . ?

O5 O6 Zn2 92.74(6) 2_566 . ?

O5 O6 Zn2 103.04(6) 2_666 . ?

O5 O6 Zn2 66.25(5) . . ?

O3 O6 Zn2 113.72(6) . . ?

As1 O6 Zn2 135.32(6) . . ?

Zn1 O6 O1 151.47(8) . 1_556 ?

O1 O6 O1 108.04(7) 2_666 1_556 ?

O2 O6 O1 67.75(6) . 1_556 ?

O5 O6 O1 62.17(6) 1_556 1_556 ?

O3 O6 O1 144.09(7) 2_566 1_556 ?

O5 O6 O1 112.15(7) 2_566 1_556 ?

O5 O6 O1 67.22(6) 2_666 1_556 ?

O5 O6 O1 158.79(7) . 1_556 ?

O3 O6 O1 120.55(7) . 1_556 ?

As1 O6 O1 97.35(5) . 1_556 ?

Zn2 O6 O1 125.36(6) . 1_556 ?

Zn1 O6 H3 112(3) . . ?

O1 O6 H3 30(3) 2_666 . ?

O2 O6 H3 109(3) . . ?

O5 O6 H3 99(3) 1_556 . ?

O3 O6 H3 97(3) 2_566 . ?

O5 O6 H3 152(3) 2_566 . ?

O5 O6 H3 38(3) 2_666 . ?

O5 O6 H3 72(3) . . ?

O3 O6 H3 115(3) . . ?

As1 O6 H3 101(3) . . ?

Zn2 O6 H3 66(3) . . ?

O1 O6 H3 95(3) 1_556 . ?

Zn1 O6 H4 118(3) . . ?

O1 O6 H4 128(3) 2_666 . ?

O2 O6 H4 24(3) . . ?

O5 O6 H4 106(3) 1_556 . ?

O3 O6 H4 160(3) 2_566 . ?

O5 O6 H4 103(3) 2_566 . ?

O5 O6 H4 62(3) 2_666 . ?

O5 O6 H4 119(3) . . ?

O3 O6 H4 79(3) . . ?

As1 O6 H4 53(3) . . ?

Zn2 O6 H4 163(3) . . ?

O1 O6 H4 45(3) 1_556 . ?

H3 O6 H4 99(4) . . ?

loop_

_geom_hbond_atom_site_label_D

_geom_hbond_atom_site_label_H

_geom_hbond_atom_site_label_A

_geom_hbond_distance_DH

_geom_hbond_distance_HA

_geom_hbond_distance_DA

_geom_hbond_angle_DHA

_geom_hbond_site_symmetry_A

O5 H1 O4  0.9798(10) 1.720(4) 2.697(2) 175(3) .

O5 H2 O6  0.9800(10) 1.814(4) 2.792(2) 176(4) 1_554

O6 H3 O1  0.9799(10) 1.94(3) 2.720(2) 135(3) 2_666

O6 H4 O2  0.9799(11) 1.90(3) 2.751(2) 143(4) .

_diffrn_measured_fraction_theta_max    0.999

_diffrn_reflns_theta_full              30.24

_diffrn_measured_fraction_theta_full   0.999

_refine_diff_density_max    0.608

_refine_diff_density_min   -0.703

_refine_diff_density_rms    0.108