#

# h,k,l, Fc-squared, Fo-squared, sigma(Fo-squared) and status flag

#

data_shelxl

_shelx_title ' 2c in P2/c'

_shelx_refln_list_code          4

_shelx_F_calc_maximum      443.43

_exptl_crystal_F_000      1236.00

_reflns_d_resolution_high  0.8409

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x, y, -z+1/2'

'-x, -y, -z'

'x, -y, z-1/2'

_cell_length_a     5.4206

_cell_length_b     7.1249

_cell_length_c    29.3141

_cell_angle_alpha  90.000

_cell_angle_beta   94.698

_cell_angle_gamma  90.000

_shelx_F_squared_multiplier     1.000

loop_

_refln_index_h

_refln_index_k

_refln_index_l

_refln_F_squared_calc

_refln_F_squared_meas

_refln_F_squared_sigma

_refln_observed_status

5   0  -4       69.22       11.57     58.52 <

3   0  -2        4.80      -27.06     27.06 <

5   0  -2        1.23       71.24     55.75 <

1   0   0       68.99      -10.54     10.54 <

1   0   0      190.26      -21.28     21.28 <

2   0   0   165951.20   178182.02   8975.81 o

3   0   0       15.82       32.03     18.43 <

3   0   0       43.43       53.66     33.31 <

4   0   0    50229.57    48511.57   2472.49 o

5   0   0       18.03       70.78     64.54 <

6   0   0       77.52       86.74     69.62 <

0   1   0       59.54       71.48     15.96 o

1   1   0     2067.75     1168.82     76.33 o

2   1   0     4009.78     3525.90    137.79 o

3   1   0     4092.87     2515.74    153.82 o

4   1   0       16.92       18.52     32.97 <

5   1   0     2718.82     2874.67    260.69 o

6   1   0      240.13       11.97     41.26 <

0   2   0    23884.01    24079.99   1243.99 o

1   2   0      338.44       33.03     21.40 <

2   2   0     9635.66     7545.38    404.33 o

4   2   0     6129.80     6858.67    273.31 o

5   2   0     6202.02      647.90     84.66 o

6   2   0     1670.95     7500.04    438.10 o

0   3   0     5552.87     7173.20    390.92 o

1   3   0     4605.37     5205.21    335.86 o

2   3   0     6319.68     6430.92    355.99 o

3   3   0    12934.09    11851.94    631.71 o

4   3   0       13.15       48.81     56.90 <

5   3   0     8308.64    11248.01    519.76 o

6   3   0     1412.66      942.59    121.90 o

0   4   0   175910.84   231302.69  11658.56 o

1   4   0     3302.83     3904.11    215.00 o

2   4   0    47256.87    50570.13   1820.02 o

3   4   0     3634.11     3276.30    215.12 o

4   4   0     9903.47     7986.72    451.52 o

5   4   0     1236.31     1391.71    138.21 o

0   5   0      562.00      952.54    101.31 o

1   5   0     3692.25     4512.19    194.04 o

2   5   0      134.88       43.98     35.44 <

4   5   0      269.33      109.64     77.72 <

5   5   0     3311.04      454.76     92.06 o

0   6   0    55567.52    70376.05   3592.50 o

1   6   0     2942.82     3349.74    160.13 o

2   6   0    15632.75    15916.94    604.62 o

3   6   0     2392.00     2322.01    125.04 o

4   6   0     7051.52     7359.22    302.58 o

0   7   0     6592.53     8261.52    480.20 o

1   7   0      468.56      617.60     70.64 o

2   7   0     6697.27     7216.51    459.85 o

3   7   0     6295.02     6441.59    276.44 o

0   8   0     5238.08     5770.53    364.08 o

1   8   0      665.06      637.40     77.41 o

2   8   0     5363.74     5672.13    276.88 o

-6   1   1      128.63      212.34     75.18 o

-5   1   1     3806.86     4343.74    185.35 o

-4   1   1      618.20      700.45     71.20 o

-3   1   1     8130.65     9708.93    298.28 o

-2   1   1       12.52      116.88     59.10 <

-1   1   1     5012.37     5614.25    210.00 o

0   1   1      701.25      728.67     28.02 o

1   1   1    12880.00    13062.16    669.65 o

2   1   1      310.63      306.64     28.25 o

3   1   1    13012.82    13520.82    410.29 o

4   1   1      337.63      267.48     43.72 o

5   1   1     3928.53     2150.36    114.07 o

6   1   1       96.08      219.14     53.87 o

-6   2   1     9430.10     8364.45    480.43 o

-5   2   1      323.19     1403.43    301.51 o

-4   2   1     2979.93     3515.63    193.84 o

-3   2   1    17805.27    19361.46   1002.97 o

-2   2   1     1507.14     1036.04     85.12 o

-1   2   1      829.53      442.07     36.09 o

0   2   1    18410.58    20290.88    780.68 o

1   2   1     1088.86      842.90     69.16 o

2   2   1    99198.95   112874.91   5698.36 o

3   2   1    40502.94    40745.52   2079.03 o

4   2   1    31388.76    29227.67   1200.62 o

5   2   1    10970.78    16846.78    517.58 o

6   2   1    14741.13    12834.55    706.89 o

-6   3   1       27.92       13.88     70.55 <

-5   3   1     6415.67     5030.78    215.78 o

-4   3   1      216.81      175.57     41.97 o

-3   3   1     8474.32     7142.90    396.70 o

-2   3   1       66.23      129.68     46.15 o

-1   3   1    11506.27    11578.65    430.40 o

0   3   1      716.78      866.76     52.32 o

1   3   1    14266.10    14262.01    525.10 o

2   3   1      228.41       65.92     41.64 <

3   3   1     9585.62     6556.52    369.40 o

4   3   1     2765.51     2259.22    164.93 o

5   3   1     4793.54     1336.75    120.74 o

-5   4   1     1969.90     2059.92    119.46 o

-4   4   1     1899.30     3024.17    206.79 o

-3   4   1     5548.78     5146.68    306.26 o

-2   4   1      430.59      543.69    123.98 o

-1   4   1     7915.85     7403.03    287.92 o

0   4   1    32626.77    41323.34   1492.75 o

1   4   1     5882.99     5724.23    228.47 o

2   4   1    20130.39    22999.07   1197.27 o

3   4   1     4292.68     4163.38    257.91 o

4   4   1    11778.09    11560.72    631.48 o

5   4   1     1043.34     1387.63    108.25 o

-5   5   1     5775.55     7113.40    300.05 o

-4   5   1       10.99       82.01     46.99 <

-3   5   1     6874.45     6515.12    649.64 o

-2   5   1       39.54       40.52     35.90 <

-1   5   1    10162.08    10944.24    483.79 o

0   5   1     1302.66     2149.68    110.89 o

1   5   1    25186.92    26376.12    968.69 o

2   5   1     5040.65     6162.23    338.76 o

3   5   1    22880.14    22399.24    828.48 o

4   5   1      134.28       86.05     72.17 <

5   5   1     7082.29     9677.61    555.61 o

-4   6   1     4598.08     6025.81    256.88 o

-3   6   1    11382.14    12553.74    485.83 o

-2   6   1      305.95      405.27     59.58 o

-1   6   1     5695.10     5173.74    223.58 o

0   6   1    12657.62    13358.80    514.32 o

1   6   1     6241.09     6415.11    267.88 o

2   6   1    14496.20    13992.89    535.63 o

3   6   1      909.56      462.47     60.50 o

4   6   1    11628.08     9222.39    369.02 o

-3   7   1     2338.42     1852.26    318.98 o

-2   7   1       83.98      166.56     56.79 o

-1   7   1      246.91      453.11     61.58 o

0   7   1     3090.83     2907.57    149.40 o

1   7   1     3186.30     4197.08    196.49 o

2   7   1     6220.48     6238.30    326.26 o

-2   8   1      225.72      703.38     79.25 o

-1   8   1      368.94      537.52    117.62 o

0   8   1     9517.33     9955.03    406.86 o

1   8   1     2364.88     2387.81    187.59 o

2   8   1    15417.90    17732.43    683.64 o

-6   0   2    40788.98    34379.36   1779.48 o

-5   0   2        3.39      156.83     62.69 o

-4   0   2   172844.09   152413.20   7691.11 o

-3   0   2       13.21       79.03     21.10 o

-2   0   2   196628.78   197412.25   7146.96 o

-1   0   2      115.16       57.28     12.95 o

-1   0   2       42.23       20.82     14.57 <

1   0   2       84.62      137.40     23.83 o

1   0   2      232.27      233.16     27.29 o

2   0   2     6699.83     5615.55    300.94 o

3   0   2      499.11      463.32     58.52 o

4   0   2    23299.20    26017.22   1346.46 o

5   0   2      184.92      332.63     83.50 o

6   0   2      546.59      293.53     77.72 o

-6   1   2      241.34      173.71     70.55 o

-5   1   2      807.42       92.78     39.49 o

-4   1   2       15.58       69.72     25.56 o

-3   1   2     3506.60     2776.66    167.70 o

-2   1   2     2360.10     3001.98     97.38 o

0   1   2      129.10       55.38     14.46 o

1   1   2    18922.47    15765.64    568.54 o

2   1   2      236.96      132.91     22.40 o

3   1   2    13507.38    13767.27    554.80 o

4   1   2      888.75      738.70     97.04 o

5   1   2    13522.59    13777.00    523.97 o

6   1   2     1022.59      778.63     92.64 o

-6   2   2     2343.07     2110.25    176.03 o

-5   2   2     1086.95      630.34     59.33 o

-4   2   2     4987.12     4189.30    176.89 o

-3   2   2     8191.82     4008.59    387.91 o

-2   2   2     7772.15     6416.51    246.81 o

-1   2   2      689.81      323.57     42.03 o

0   2   2    18964.16    18636.89    557.15 o

1   2   2    10922.38     5655.57    306.95 o

2   2   2     1466.84     1047.61     88.36 o

3   2   2     6215.39     5056.93    290.06 o

4   2   2     1314.94     3314.92    212.58 o

5   2   2     1248.52     1842.05    171.44 o

6   2   2       20.24     2851.84    210.72 o

-6   3   2     1807.87     2007.32    174.41 o

-5   3   2     1289.03      555.61     83.04 o

-4   3   2     2600.83     2772.16    129.78 o

-3   3   2     8426.54     8133.37    445.97 o

-2   3   2     4762.72     5013.60    390.69 o

-1   3   2    19706.49    21342.25    640.76 o

0   3   2     2451.24     3105.17    128.80 o

1   3   2    43441.53    47899.98   2435.48 o

2   3   2     7047.39     8061.67    438.57 o

3   3   2    20075.34    22102.51   1149.62 o

4   3   2     3471.64     3788.65    240.80 o

5   3   2    13133.67    20846.98   1239.14 o

-5   4   2      816.32      249.65     56.51 o

-4   4   2    33816.39    30449.61   1578.70 o

-3   4   2     2261.30     2021.89    151.97 o

-2   4   2    54813.85    60950.35   2189.92 o

-1   4   2     4588.92     4374.78    459.96 o

0   4   2       82.96      109.33     32.91 o

1   4   2     4572.58     4372.33    180.87 o

2   4   2     5835.77     6080.72    349.51 o

3   4   2     1539.26     1197.73    118.20 o

4   4   2    14915.72    16246.86    869.50 o

5   4   2      231.07       19.04     75.52 <

-5   5   2     1462.58      163.02     52.35 o

-4   5   2      818.94      898.88     74.85 o

-3   5   2     2566.06     1021.89     74.96 o

-2   5   2       57.15       49.72     35.56 <

-1   5   2     9292.72    12689.36    482.24 o

0   5   2     2035.38     2183.97    112.12 o

1   5   2    13077.96    16438.77    616.21 o

2   5   2      760.13      913.86     70.46 o

3   5   2     2040.96     1788.27    155.44 o

4   5   2      645.34      439.49     90.67 o

5   5   2     1796.26      491.07    104.09 o

-4   6   2    18253.97    16480.09    623.99 o

-3   6   2     5638.90     5410.96    786.46 o

-2   6   2    14521.10    15778.66    599.55 o

-1   6   2     2650.10     3312.10    175.91 o

0   6   2     9565.72     9810.53    388.46 o

1   6   2      811.26      722.20     71.05 o

2   6   2     1566.77     1585.83    196.15 o

3   6   2     5023.30     4923.23    216.71 o

4   6   2      658.79     1465.35    102.84 o

-3   7   2     3335.66     3729.66    180.74 o

-2   7   2     5173.15     6427.61    408.03 o

-1   7   2     8047.17     8534.38    349.74 o

0   7   2      217.91      447.74     76.56 o

1   7   2    17264.97    17254.86    660.04 o

2   7   2      239.47      796.04     78.24 o

3   7   2     9261.89     8866.64    362.17 o

-2   8   2     5149.61     5815.25    260.40 o

-1   8   2     4589.30     3636.88    180.53 o

0   8   2       62.38      116.54     45.98 o

1   8   2     5156.02     5228.03    238.80 o

2   8   2      501.01     1374.94    154.98 o

-6   1   3       55.58      144.11     68.47 o

-5   1   3     2215.84     3839.43    151.60 o

-4   1   3      357.09      543.00     38.77 o

-3   1   3     9216.98    11333.33    345.25 o

-2   1   3      437.43      375.94     18.48 o

-1   1   3    15183.28    14333.83    759.51 o

0   1   3     1221.81     1397.50     75.64 o

1   1   3    13760.72     9889.26    511.20 o

2   1   3     3181.82     3123.87    127.41 o

3   1   3     8940.88     7792.47    298.74 o

4   1   3     1128.61     1539.27    116.58 o

5   1   3     8680.57    11877.47    457.89 o

6   1   3     3376.57     2529.64    137.60 o

-6   2   3     1136.44     1163.27    130.46 o

-5   2   3     2863.61     3131.47    145.49 o

-4   2   3     6239.69     6769.31    340.38 o

-3   2   3    19052.46    24089.51   1717.37 o

-2   2   3   105265.70   113973.81   4387.98 o

-1   2   3    26860.95    24307.53    721.92 o

0   2   3    98720.79   117442.37   3453.72 o

1   2   3   101501.09    95283.44   4810.12 o

2   2   3    84706.98    89896.42   4544.58 o

3   2   3     7022.00     6582.66    365.70 o

4   2   3    23028.67    20186.06   1243.65 o

5   2   3     3895.47     3985.75    177.45 o

6   2   3     1136.77     1175.76    135.09 o

-6   3   3       16.20     1249.31    137.63 o

-5   3   3     3486.48     4550.69    226.80 o

-4   3   3      195.67      108.21     39.67 o

-3   3   3     8648.52     6867.88    277.11 o

-2   3   3      573.59      384.02     30.43 o

-1   3   3    19061.22    21521.26    645.07 o

0   3   3     5155.13     6608.87    252.54 o

-3   0   4       93.93       58.29     32.61 <

-1   0   4        1.74      -18.50     18.50 <

-5   0   6       10.84       -3.24     62.22 <

-3   0   6      386.51      219.98     46.03 o

-5   0   8     2864.12      230.15     74.71 o

5   0   0        6.46       63.61     52.05 <

3   0   2      179.76      129.21     24.98 o

1   3   3    17995.50    18664.98    966.88 o

2   3   3     6371.96     5941.47    333.32 o

4   3   3      357.65      432.32     80.96 o

5   3   3     2355.19     1267.53    145.38 o

-5   4   3     2152.87     2359.12    128.26 o

-4   4   3     4281.27     5096.74    608.70 o

-3   4   3     6729.34     6126.96    198.88 o

-2   4   3    30420.23    30709.90    918.73 o

-1   4   3     4995.97     5419.54    218.48 o

0   4   3     3346.77     2958.52    130.44 o

1   4   3     4369.98     4430.50    182.39 o

2   4   3     8758.16     9159.47    504.03 o

3   4   3     2694.41     2176.64    162.84 o

4   4   3       64.63      872.04    110.10 o

5   4   3     1690.95      733.72    109.18 o

-5   5   3     3958.28     5729.85    281.39 o

-4   5   3       24.11       34.30     43.82 <

-3   5   3    18337.21    17932.37   1595.12 o

-2   5   3     5784.52     7018.49    281.92 o

-1   5   3    32690.01    34520.34   1256.39 o

0   5   3     3569.04     4740.27    236.75 o

1   5   3    11226.06    11520.74    520.68 o

2   5   3     5160.58     6331.59    258.28 o

3   5   3      115.81      442.96     87.20 o

4   5   3     3352.61     3873.77    259.30 o

5   5   3     5465.44     7537.52    450.13 o

-4   6   3     8585.91     7518.32    445.97 o

-3   6   3     1196.99      557.97     97.73 o

-2   6   3    15938.21    14983.42    571.74 o

-1   6   3      434.06      315.87     53.24 o

0   6   3    26913.40    30131.64   1109.03 o

1   6   3     4855.08     4931.79    215.62 o

2   6   3     8322.51     8281.79    332.41 o

3   6   3     2061.15     1708.34    105.74 o

4   6   3     1726.72     1815.10    202.05 o

-3   7   3     2332.87     1115.85    127.45 o

-2   7   3     7299.04     7189.83    302.76 o

-1   7   3     6271.62     8572.02    349.57 o

0   7   3     4462.09     4798.01    215.98 o

1   7   3     6058.22     7844.22    443.77 o

2   7   3     4267.07     3287.23    162.64 o

-2   8   3    24635.86    24314.05    918.33 o

-1   8   3     4811.68     4836.37    223.87 o

0   8   3     6710.35     7374.40    353.33 o

1   8   3     5202.88     4902.44    227.27 o

-5   0   4      189.57      128.84     60.60 o

-4   0   4    22900.03    16953.74    910.44 o

-3   0   4      257.93      290.48     27.90 o

-2   0   4    11552.70    10251.87    379.91 o

-1   0   4        4.62      -22.90     22.90 <

0   0   4     4919.47     3269.45    123.38 o

1   0   4     1144.73     1488.72     97.61 o

1   0   4     3157.57     2742.89    156.14 o

2   0   4    10802.26     7920.10    419.60 o

3   0   4     7518.93     7130.18    390.45 o

4   0   4      387.62      655.07     88.82 o

5   0   4    11820.75    13573.59    737.19 o

6   0   4     2686.07     3479.85    243.80 o

-6   1   4       88.06       74.25     61.30 <

-5   1   4     2963.63     2858.17    106.52 o

-4   1   4       12.73       90.20     25.54 o

-3   1   4    11135.20    11695.84    308.43 o

-2   1   4      608.63      336.84     22.81 o

-1   1   4    36889.84    32687.92    977.06 o

0   1   4     1870.59     1525.09     51.57 o

1   1   4    32092.87    27750.53   1175.28 o

2   1   4     5989.27     5085.73    197.74 o

3   1   4    21739.28    20832.40    761.86 o

4   1   4     1960.49     1965.64    104.41 o

5   1   4     6412.32     2317.46    255.95 o

6   1   4      489.24     2665.65    223.22 o

-6   2   4     1677.37     4153.20    270.17 o

-5   2   4      545.94      951.67     72.14 o

-4   2   4     6153.96     8658.68   1417.59 o

-2   2   4      739.13      991.82     84.43 o

-1   2   4    37692.09    34696.95   1958.05 o

0   2   4     6075.84     6333.34    241.55 o

1   2   4    20627.47    18583.56    956.01 o

2   2   4     1382.72     1370.06    101.55 o

3   2   4     2143.90     2042.10    372.64 o

4   2   4      167.50      507.50     78.65 o

5   2   4     1709.07     1937.39    110.18 o

6   2   4       61.61       77.95     72.40 <

-6   3   4      726.06      214.43     82.81 o

-5   3   4     9021.21    11495.58    448.73 o

-4   3   4       29.63      295.55     69.74 o

-3   3   4    19003.00    18926.14    985.85 o

-2   3   4     7112.02     9252.45    285.44 o

-1   3   4    47625.42    52304.73   1548.16 o

0   3   4    22545.78    31876.41    948.32 o

1   3   4    36378.37    37380.16   1907.16 o

2   3   4     4071.44     3589.26    217.20 o

3   3   4    19402.10    20030.42   1045.99 o

4   3   4     4436.78     4033.84    252.82 o

5   3   4     3789.14     5593.93    408.61 o

-5   4   4     1165.07     1294.38     91.91 o

-4   4   4     4400.55     5665.92    340.26 o

-3   4   4     2603.06     2089.94    164.97 o

-2   4   4    15858.15    15029.94    459.81 o

-1   4   4     1963.96     2117.65    145.90 o

0   4   4     9196.00    11249.57    423.63 o

1   4   4      988.20      814.11     58.53 o

2   4   4    25830.71    23900.95   1242.61 o

3   4   4     2528.83     2214.58    164.93 o

4   4   4     2710.11     2143.56    170.25 o

5   4   4     3728.15     4629.70    299.78 o

-5   5   4     2322.27      902.11     82.97 o

-4   5   4       99.09       57.83     44.56 <

-3   5   4     8603.42     3344.30    211.65 o

-2   5   4      962.20     1119.25    106.52 o

-1   5   4     5056.70     5872.86    245.88 o

0   5   4     3376.01     3838.39    249.70 o

1   5   4     1473.42     1115.62    113.11 o

2   5   4     8517.30     8786.36    345.45 o

4   5   4     5075.15     4270.47    278.96 o

-4   6   4     4179.88     5097.18    324.07 o

-3   6   4     2288.48     2674.50    137.23 o

-2   6   4      881.87     1263.94     89.66 o

-1   6   4     3239.93     3990.30    182.20 o

0   6   4      544.71      943.82     79.15 o

1   6   4    21413.41    22489.92   1103.36 o

2   6   4     2133.90     2485.21    128.87 o

3   6   4     4479.10     4441.32    200.65 o

4   6   4     1148.52      852.61    125.60 o

-3   7   4     9117.53     8587.89    352.32 o

-2   7   4      102.41      477.48     68.04 o

-1   7   4    16589.43    15723.35    603.77 o

0   7   4     3220.64     3785.91    180.65 o

1   7   4     8317.02     7698.80    413.12 o

2   7   4    10379.82    11030.54    438.40 o

3   7   4     6360.60     5843.80    256.00 o

-2   8   4     1305.68     1984.01    133.43 o

-1   8   4     3355.15     3358.60    171.85 o

0   8   4     2722.72     3325.85    173.25 o

1   8   4      794.38      908.68     86.46 o

-5   1   5     2232.84     2194.71     87.75 o

-4   1   5      140.91      173.61     25.91 o

-2   1   5     5279.85     4983.35    158.06 o

-1   1   5    25480.46    23090.03   1726.74 o

0   1   5      112.85       23.30     10.59 o

1   1   5    45590.84    39341.61   1163.00 o

2   1   5    38923.57    39087.43   2433.05 o

3   1   5    34133.39    33926.18   1229.00 o

4   1   5     8375.58     6949.81    491.42 o

5   1   5    15426.18    18890.93    731.99 o

6   1   5     4804.60     5185.71    233.03 o

-6   2   5    14154.67    12586.81    687.69 o

-5   2   5    17030.57    23100.27    864.19 o

-4   2   5    33804.78    34151.51   1361.73 o

-3   2   5    12691.29    12240.44    377.85 o

-2   2   5    76591.59    82263.34   2447.56 o

-1   2   5    33773.56    31959.94    945.72 o

0   2   5    69668.77    84604.91   3067.26 o

1   2   5     3756.73     3668.35    286.36 o

2   2   5     2366.48     1557.19    111.03 o

3   2   5     2070.16     2541.47    340.84 o

4   2   5      682.87      317.49     46.94 o

5   2   5     2977.67     3755.59    173.11 o

6   2   5      440.95      365.39     62.08 o

-6   3   5       71.82      491.88     77.74 o

-5   3   5     3776.40     1398.85     91.67 o

-4   3   5     2470.81     2517.31    122.18 o

-2   3   5     5161.18     5217.70    167.41 o

-1   3   5    13851.04    16699.07    503.56 o

0   3   5       75.97       20.96     17.21 <

1   3   5    12840.44    11985.87    631.94 o

2   3   5      219.34      338.87     61.07 o

3   3   5     2459.89     3051.92    198.70 o

4   3   5     3804.94     3561.04    232.24 o

5   3   5     1463.33     1438.53    140.64 o

-5   4   5     1161.12     1523.38    101.73 o

-4   4   5     8163.77     9249.11    360.04 o

-3   4   5     2622.44     2152.83    129.82 o

-2   4   5     3777.92     4912.08    298.51 o

-1   4   5     2025.52     1799.07    116.58 o

0   4   5     5830.90     5347.87    214.35 o

1   4   5     1763.15     1986.04    140.41 o

2   4   5     3665.07     3298.73    210.72 o

3   4   5     3094.78      819.54     97.61 o

4   4   5     2922.07     3261.26    225.07 o

5   4   5     1751.87      887.31    116.12 o

-5   5   5     8679.99    10885.76    434.48 o

-4   5   5      368.15      186.64     52.10 o

-3   5   5     4209.82     4316.61    209.50 o

-2   5   5     9164.33     9651.20    307.21 o

-1   5   5     3826.57     3993.25    175.96 o

0   5   5     2715.24     3056.06    141.07 o

1   5   5    23489.01    23519.09    866.79 o

2   5   5    31669.29    34482.52   1784.57 o

3   5   5    27461.08    28665.97   1497.97 o

4   5   5     6329.14     5540.60    345.58 o

5   5   5    10678.56    15227.46    835.96 o

-4   6   5     9730.47     8073.93    470.72 o

-3   6   5     2198.20     1445.93    128.38 o

-2   6   5     7835.03     8239.98    331.27 o

-1   6   5    12029.65    13784.27   1793.82 o

0   6   5     1700.93     2085.26    117.08 o

1   6   5     7718.36    10223.32    402.11 o

2   6   5      237.30      201.29     47.81 o

4   6   5      993.03      897.95    125.83 o

-2   7   5     2912.76     2872.93    265.78 o

-1   7   5     3055.63     3824.34    181.61 o

0   7   5     1565.11     1875.34    117.58 o

1   7   5     2315.17     2484.99    432.21 o

2   7   5     1374.16     1285.57     96.92 o

3   7   5       87.56      132.44    102.82 <

-1   8   5      903.71      812.63     83.15 o

0   8   5    17054.71    16886.10    889.74 o

1   8   5      487.29      551.15     73.11 o

-5   0   6       29.16       84.31     38.04 o

-4   0   6    21640.01    20493.33    761.29 o

-3   0   6     1063.42     2113.38    295.85 o

-2   0   6     4270.99     4353.51    247.50 o

-1   0   6    20151.89    19039.25   1006.90 o

-1   0   6     7340.05     8349.88    436.48 o

0   0   6    19809.49    13058.23    501.37 o

1   0   6    42464.41    36468.19   1329.39 o

2   0   6    39300.15    45664.58   2321.67 o

3   0   6    29945.29    31178.71   1601.37 o

4   0   6     7672.51     8680.19    484.83 o

5   0   6    14407.17    19828.71   1055.24 o

6   0   6     3189.95     2531.24    196.15 o

-5   1   6     9319.16    12686.03    485.81 o

-4   1   6     1473.03     1365.39     62.46 o

-3   1   6    19673.09    20540.39    718.33 o

-2   1   6     4910.39     5725.14    314.41 o

-1   1   6    23231.91    23604.01   1605.54 o

0   1   6     8847.17     8402.92    256.20 o

1   1   6    26865.78    27550.46   1739.89 o

2   1   6      358.19      506.80     56.90 o

3   1   6     8706.07     8377.25    323.51 o

4   1   6     1437.29     2703.34    284.63 o

5   1   6     2412.38     2685.82    138.88 o

6   1   6     2801.17     2762.20    149.31 o

-6   2   6      760.46     7393.18    423.76 o

-5   2   6     5728.20     3240.84    534.10 o

-4   2   6      682.22     3139.82    198.00 o

-3   2   6     3245.82     1911.46     92.60 o

-2   2   6     1184.76     1568.46     62.17 o

-1   2   6     4884.85     4195.69    136.64 o

0   2   6      371.92      419.56     48.23 o

1   2   6     1966.99     1704.90    158.91 o

2   2   6      287.36      366.63     55.51 o

4   2   6      344.85      810.38     66.72 o

5   2   6     2175.08      768.42     99.93 o

6   2   6       41.81      268.59     58.21 o

-5   3   6    12119.83    20001.47    957.51 o

-4   3   6     5167.48     5221.23    174.81 o

-3   3   6    27426.21    28297.22    736.08 o

-2   3   6     5569.21     4936.04    158.64 o

-1   3   6    27434.26    30024.51    894.58 o

0   3   6    12933.20    14584.03    592.60 o

1   3   6    16995.09    16280.63    846.83 o

2   3   6     1356.72     1378.15    109.64 o

3   3   6      688.53      583.60     84.20 o

4   3   6    10821.13    10019.72    555.15 o

5   3   6      867.63     1163.73    127.22 o

-5   4   6      404.55      142.50     71.59 <

-4   4   6    17004.80    15334.71    614.05 o

-3   4   6     1479.25     1162.08    122.45 o

-2   4   6    13824.97    14793.33    452.93 o

-5   0  10     4772.96      286.36     79.80 o

5   0   2       66.93      197.46     44.30 o

3   0   4     2716.32     2727.16    173.02 o

1   0   6    15360.83    20412.54   1083.00 o

-1   4   6     4302.20     4347.53    147.63 o

0   4   6    37106.78    40793.10   1215.06 o

1   4   6    10029.33     9621.63    520.68 o

2   4   6    11023.09    12179.01    656.00 o

3   4   6    11868.59    11102.03    607.42 o

4   4   6     9606.59     9018.83    511.89 o

5   4   6     5682.62     6325.67    385.13 o

-5   5   6     2594.31      458.23     83.97 o

-4   5   6     1405.04     1131.41     80.02 o

-3   5   6      301.29      431.33     43.12 o

-2   5   6    10585.19    10423.94    330.13 o

-1   5   6     8706.58    12020.11    377.89 o

0   5   6     6052.74     6702.83    269.88 o

1   5   6    15255.04    17124.15    639.36 o

2   5   6     6235.89     6332.15    373.57 o

4   5   6     1214.22     1510.23    153.36 o

-4   6   6      974.08     1185.20     94.26 o

-3   6   6     4052.93     4027.47    183.34 o

-2   6   6     1970.88     2421.69    126.29 o

-1   6   6    20834.87    18463.27    898.18 o

0   6   6     3977.57     4141.23    185.97 o

1   6   6     2599.99     2984.57    146.30 o

2   6   6     7722.43     7534.44    306.54 o

3   6   6     5778.44     5768.90    249.91 o

4   6   6     1989.95     1901.84    182.97 o

-3   7   6     8680.55     8719.55    355.50 o

-2   7   6    10758.62    11957.39    469.49 o

-1   7   6     4201.55     3564.24    243.57 o

0   7   6    14534.32    16971.37    648.11 o

1   7   6     2155.89     2099.55    122.23 o

2   7   6     4507.23     4319.92    199.89 o

3   7   6      182.50      319.75     59.49 o

-1   8   6      230.99      413.16     65.98 o

0   8   6     7474.99     6887.73    507.03 o

1   8   6     1879.47     2316.25    159.03 o

-5   1   7    12306.51    12890.92    492.41 o

-4   1   7     2085.62     1873.41     77.13 o

-3   1   7    35031.75    38620.81   1160.32 o

-2   1   7    39124.46    41583.83   1490.42 o

-1   1   7    71250.85    63281.09   1887.62 o

0   1   7    44005.92    42219.01   1257.02 o

1   1   7    57335.19    48314.14   1427.74 o

2   1   7    38933.92    37892.23   1526.08 o

3   1   7    15765.89    16446.86    610.65 o

4   1   7     9470.53     8563.60    338.31 o

5   1   7     2092.26     2287.49    153.24 o

6   1   7      709.83     1824.30    120.10 o

-5   2   7      852.68     2447.74    188.17 o

-4   2   7    17210.35    17125.95    795.48 o

-3   2   7     4818.44     6183.79    199.14 o

-2   2   7     1176.18     1080.88     48.14 o

-1   2   7     5225.74     3762.56    106.02 o

0   2   7     1934.63     2252.53    133.73 o

1   2   7     1878.30     1702.79     62.76 o

2   2   7     1253.28     1107.52     92.99 o

3   2   7    11249.71    10955.62    415.53 o

4   2   7     9005.05     8099.52    829.02 o

5   2   7     1548.43     3540.54    166.83 o

6   2   7      310.93      484.15     69.87 o

-5   3   7     5214.21     1999.92    159.84 o

-4   3   7      377.43      557.19     94.69 o

-3   3   7     8863.35     5127.02    308.34 o

-2   3   7      396.22      341.72     25.57 o

-1   3   7     9889.79    10840.07    331.99 o

0   3   7    16527.58    18075.75    670.93 o

1   3   7     2122.82     2367.54    283.59 o

2   3   7     7842.11     7237.50    399.71 o

4   3   7     4932.31     5166.80    312.96 o

5   3   7      920.57      177.65     70.32 o

-5   4   7      623.04      931.86    144.80 o

-4   4   7       40.20      553.55     45.93 o

-3   4   7     1480.81     1461.69    102.62 o

-2   4   7     8361.42     7773.69    247.24 o

-1   4   7     3787.14     4773.87    159.75 o

0   4   7      321.09      513.19     52.37 o

1   4   7     6619.83     7290.24    404.56 o

2   4   7     8560.33     7845.85    438.10 o

3   4   7     4804.42     3753.95    244.03 o

4   4   7      196.98      682.60    105.48 o

5   4   7     1634.25     2379.73    190.60 o

-5   5   7     4502.31     6209.70    416.01 o

-4   5   7     3655.61     4006.34    148.15 o

-3   5   7    24937.41    24721.04    863.90 o

-2   5   7    28742.29    32201.06    967.43 o

-1   5   7    40590.02    41382.16   1236.63 o

0   5   7    28206.00    31639.11   1153.60 o

1   5   7    27531.91    27254.89    999.93 o

2   5   7    18636.31    18434.60    978.68 o

3   5   7     5549.38     5162.18    320.60 o

4   5   7    11334.02    10371.54    591.23 o

-4   6   7      678.95      539.70     70.09 o

-3   6   7     2701.73     2576.52    300.47 o

-2   6   7      199.30      132.97     49.62 o

-1   6   7     1062.96     1117.15     83.59 o

0   6   7     1773.20     1733.14    100.04 o

1   6   7      152.87      261.12     45.69 o

2   6   7     5666.37     6286.73    263.73 o

3   6   7     2889.01     2612.66    201.24 o

4   6   7     2036.03     1663.59    171.86 o

-2   7   7     1610.30     1410.32    101.46 o

-1   7   7      798.09     1083.25     86.84 o

0   7   7      164.09      266.49     53.21 o

1   7   7     1902.61     1672.32    144.45 o

2   7   7      163.28      368.03    111.84 o

3   7   7     1532.84     1486.31    107.56 o

-1   8   7     3114.62     3293.17    169.03 o

0   8   7       45.96      155.56     52.50 o

1   8   7     4212.46     4172.39    201.92 o

-5   0   8     7851.83    11910.23    661.55 o

-4   0   8      545.84      799.64     95.99 o

-3   0   8    26235.62    32165.25   1704.07 o

-2   0   8    78490.77    73687.27   3859.20 o

-1   0   8    65643.76    68308.59   3576.54 o

-1   0   8    23962.35    31714.52   1156.37 o

0   0   8      731.13     1315.29     60.49 o

1   0   8    56269.36    55282.24   2009.86 o

1   0   8    20314.51    25599.47   1355.95 o

2   0   8    41195.70    41034.89   2091.98 o

3   0   8     8751.77    10247.79    555.38 o

4   0   8     2653.67     1975.17    157.99 o

5   0   8     1137.14     1565.75    147.81 o

6   0   8     1347.87     1180.61    140.17 o

-5   1   8     4574.37     2608.40    102.61 o

-4   1   8     2169.08     2799.48    168.87 o

-3   1   8    13138.95    15015.12    773.51 o

-2   1   8      791.59      576.43    104.44 o

-1   1   8    26261.00    26600.44   1002.49 o

0   1   8     3984.21     2859.26     93.87 o

1   1   8    21569.01    19481.92    506.31 o

2   1   8    20968.43    19495.72    585.84 o

3   1   8     7681.58     7893.54    308.70 o

4   1   8    12169.58    12011.50    461.48 o

5   1   8     2164.06     2304.87    210.03 o

6   1   8     5303.32     4612.24    216.17 o

-6   2   8       35.07      485.99    107.79 o

-5   2   8     1982.05     2094.81    111.58 o

-4   2   8      388.24      543.94     42.13 o

-3   2   8     1675.56     1646.44    102.76 o

-2   2   8      346.38      336.35     28.47 o

-1   2   8      738.16      751.56     72.86 o

0   2   8      911.14      898.40     39.99 o

1   2   8     2376.80     2152.12     79.33 o

2   2   8      208.89      204.71     46.96 o

3   2   8     1657.69      758.01     84.89 o

4   2   8      213.87      554.08    120.51 o

5   2   8     1640.95      501.37     61.02 o

-5   3   8     5687.29     6703.32    462.97 o

-4   3   8     2560.49     3085.61    114.92 o

-3   3   8     1035.05      724.11     58.34 o

-2   3   8      596.50      810.26     40.14 o

-1   3   8     1162.08     1518.24    105.68 o

0   3   8    45981.77    55505.31   2048.50 o

1   3   8    13771.42    12499.45    472.75 o

2   3   8    45717.63    48474.10   2473.65 o

3   3   8     8157.35     7264.57    412.20 o

4   3   8    34338.14    33327.59   1726.05 o

5   3   8     4182.84     4647.51    298.62 o

-5   4   8     3071.86     4613.08    443.66 o

-4   4   8     2950.79     2061.51    128.54 o

-3   4   8     8068.38     9223.01    297.67 o

-2   4   8    20187.41    18716.07    572.35 o

-1   4   8    16277.32    17006.83    517.94 o

0   4   8     3917.90     3341.67    118.64 o

1   4   8    14986.82    15272.11    805.89 o

2   4   8    11482.27    11348.83    615.75 o

3   4   8     5360.71     4878.59    299.32 o

4   4   8      676.92      322.45     84.20 o

5   4   8      771.23      377.96     91.37 o

-5   5   8     1993.18      592.48    130.23 o

-4   5   8     4387.18     3787.63    142.76 o

-3   5   8    10255.51     3229.57    204.71 o

-2   5   8     4480.72     4941.48    170.09 o

-1   5   8    10568.11    13730.28    427.70 o

0   5   8     3105.76     3302.91    149.24 o

1   5   8     3029.50     3006.01    244.73 o

2   5   8      741.40      746.90     97.84 o

3   5   8      257.99      166.08     70.78 o

4   5   8      100.27      388.14    101.78 o

-4   6   8     1290.34     1379.39    102.41 o

-3   6   8     8787.36     9001.13    292.64 o

-2   6   8     8680.17     8617.38    343.01 o

-1   6   8      318.84      593.02     93.80 o

0   6   8     3037.18     2762.57    135.83 o

1   6   8     5474.73     4285.39    354.95 o

2   6   8     6776.55     6526.29    273.48 o

3   6   8     1135.59      935.65    121.67 o

4   6   8     3392.11     2704.03    218.36 o

-3   7   8      144.71       28.22     78.88 <

-2   7   8     3079.37     3466.50    168.94 o

-1   7   8      874.07      948.18     81.35 o

0   7   8     5392.60     5970.56    257.03 o

1   7   8     5147.28     5236.66    232.42 o

2   7   8    15876.16    16677.26    640.31 o

3   7   8     2959.50     3159.55    161.73 o

-1   8   8     2928.57     3929.71    307.64 o

0   8   8      590.90      495.88     86.86 o

1   8   8     3719.66     5031.54    395.89 o

-5   1   9    16220.72    18838.01    579.29 o

-4   1   9    11476.46    10811.18    346.23 o

-3   1   9    18376.51    19085.82    581.75 o

-2   1   9    44621.83    45154.11   1820.22 o

-1   1   9    16992.98    17374.55    653.76 o

0   1   9    10996.03    10513.01    320.59 o

1   1   9     5359.23     6078.81    164.56 o

2   1   9     2375.74     2291.21    195.36 o

3   1   9     1102.25      952.32     67.50 o

4   1   9     7404.03     8842.08    351.06 o

5   1   9      293.72      682.77     73.45 o

6   1   9     4599.89     4432.26    210.82 o

-6   2   9      470.46      105.02    116.12 <

-5   2   9      647.83     1750.80    135.55 o

-4   2   9     1739.93     1586.37     71.26 o

-3   2   9     8178.55    10233.95    320.38 o

-2   2   9     1470.85     1109.62     50.46 o

-1   2   9     2263.29     3236.62    200.39 o

0   2   9    37989.86    43230.27   1528.32 o

1   2   9    48772.91    48468.08   1451.62 o

2   2   9      903.04      653.41     47.62 o

3   2   9     7868.04     6703.99    267.50 o

4   2   9     3016.53     3012.88    239.06 o

5   2   9    12508.19    14038.28    539.75 o

-5   3   9     2113.40     1759.26    104.99 o

-4   3   9     4586.62     4514.32    157.21 o

-3   3   9     1338.15     1418.74     74.01 o

-2   3   9    10306.21     9348.87    295.38 o

-1   3   9     5015.60     5839.95    191.37 o

0   3   9     5142.64     5257.71    172.53 o

1   3   9     4568.30     5180.65    170.38 o

2   3   9     3801.67     3487.95    217.90 o

3   3   9     3447.13     2289.52    165.62 o

4   3   9      172.35     2048.96    162.61 o

5   3   9     1266.25     1732.52    160.30 o

-5   4   9     1522.41      913.21     80.55 o

-4   4   9     2999.29     3254.22    123.22 o

-3   4   9     6159.73     6553.74    264.89 o

-2   4   9     3255.08     4455.67    207.87 o

-1   4   9    10592.44    11749.38    363.81 o

0   4   9      907.79     1022.79     53.78 o

1   4   9     8901.54     9418.32    367.99 o

2   4   9     1077.28     1074.10    125.72 o

3   4   9     5331.46     4587.83    287.98 o

4   4   9      752.40      641.43    103.63 o

5   4   9     3566.07     2477.58    195.69 o

-5   5   9    13339.43    15956.97    618.47 o

-4   5   9     9094.56     7401.99    248.49 o

-3   5   9    12184.16    11088.39    400.68 o

-2   5   9    20401.03    20504.72    623.40 o

-1   5   9     4313.48     3969.62    169.43 o

0   5   9    17927.93    18599.40    605.37 o

1   5   9      385.02      528.63     57.16 o

2   5   9      834.44      689.31     96.92 o

3   5   9     1533.98     1763.06    157.99 o

4   5   9     1670.79     1312.46    149.43 o

-4   6   9     1180.75     1348.77     81.61 o

-3   6   9     3404.12     3197.68    256.51 o

-2   6   9     6700.17     6147.82    210.11 o

-1   0  10     4612.10     6467.89    371.25 o

-5   0  12      698.55      197.08     75.64 o

-3   0  12      470.82      211.88     56.67 o

-5   0  14     1949.85      190.83     65.46 o

5   0   8      408.27      135.09     84.20 <

-1   6   9     2614.37     3007.53    145.55 o

0   6   9     4123.01     3990.19    178.77 o

1   6   9     9005.56     7799.44    316.00 o

2   6   9     8322.19     7414.82    305.03 o

3   6   9     3414.32     3029.26    222.06 o

4   6   9     1380.01     1395.73    164.23 o

-3   7   9      380.45      360.47     68.72 o

-2   7   9       82.88      283.90     55.94 o

-1   7   9     4144.19     4088.87    202.40 o

0   7   9     1196.22     1417.35    100.51 o

1   7   9     3722.32     3958.02    186.75 o

2   7   9     1273.85     1645.72    112.00 o

3   7   9     3767.29     3657.09    246.93 o

-1   8   9     7119.79     6864.17    295.86 o

0   8   9      126.82      199.22     52.66 o

1   8   9     9210.56     8717.70    363.27 o

-5   0  10    13058.03    19396.16   1055.24 o

-4   0  10     8275.81     8773.64    502.41 o

-3   0  10    14876.10    16484.18    894.48 o

-2   0  10    16502.84    21038.01   1124.41 o

-1   0  10    12614.17    12541.71    683.99 o

0   0  10    66834.77    64543.23   2349.81 o

1   0  10      135.79      265.78     70.43 o

1   0  10       48.25      105.48     42.56 o

2   0  10     5249.59     4750.91    274.80 o

3   0  10     2446.14     2804.42    196.15 o

3   0  10     6805.50     6753.37    384.67 o

4   0  10     3018.13     3188.86    219.05 o

5   0  10     8464.45     9515.00    541.73 o

6   0  10     5905.93     6108.70    382.36 o

-5   1  10     7829.10     4535.53    200.35 o

-4   1  10     3870.03     4090.92    143.71 o

-3   1  10    12286.63    12142.87    557.71 o

-2   1  10    23325.21    22239.16    672.88 o

-1   1  10    13409.51    10554.52    404.33 o

0   1  10    44089.60    41864.43   1252.90 o

1   1  10     3490.69     3581.94    104.10 o

2   1  10    22650.34    19779.14    594.90 o

3   1  10      811.63      985.67    119.36 o

4   1  10     9851.57    10507.61    605.92 o

5   1  10      315.05      273.47     55.70 o

-6   2  10       23.94      148.27    113.34 <

-5   2  10     1416.25     1160.51     63.24 o

-4   2  10      201.29      906.51     87.67 o

-2   2  10      347.95      193.43     25.06 o

-1   2  10    17807.62    23226.48    873.61 o

0   2  10      553.35      588.30     35.19 o

1   2  10    19092.33    24682.88    746.13 o

2   2  10      500.54      412.58     38.50 o

4   2  10       40.45      178.31     67.66 o

-5   3  10     1558.19     1567.87    100.30 o

-4   3  10    18971.88    17815.46    550.45 o

-3   3  10     6376.43     5859.99    195.27 o

-2   3  10    57409.96    58335.89   1890.71 o

-1   3  10    11750.65    11126.08    298.19 o

0   3  10    87127.94    94661.59   3266.30 o

1   3  10     3972.13     3997.54    174.84 o

2   3  10    89022.61   101907.73   5161.02 o

3   3  10     4559.36     4344.49    268.55 o

4   3  10     9472.08     8377.87    476.27 o

5   3  10      174.85      165.39     79.34 o

-5   4  10     4091.84     6284.25    268.25 o

-4   4  10     8119.50     8805.59    286.37 o

-3   4  10     7143.69     7484.25    247.27 o

-2   4  10     4719.91     5458.82    163.47 o

-1   4  10     5190.88     6152.40    174.93 o

0   4  10    10950.07    12658.51    390.75 o

1   4  10     2502.02     2931.01    160.33 o

2   4  10     1165.11      980.23     69.74 o

3   4  10     3613.19     2761.63    196.15 o

4   4  10      106.71      324.99     85.82 o

5   4  10     4674.94     5775.15    362.00 o

-5   5  10     4576.19     2466.71    173.25 o

-4   5  10      918.73     1900.24    190.83 o

-2   5  10      736.91      975.44     59.49 o

-1   5  10      721.11      804.34     57.26 o

0   5  10      126.50      274.25     37.43 o

1   5  10     1008.51      839.89     96.69 o

2   5  10      820.33     1356.12     85.32 o

3   5  10      492.66      342.80     81.42 o

4   5  10      726.83     1177.84    138.32 o

-4   6  10     1680.48     1733.46     93.89 o

-3   6  10     1232.79     1024.24     99.28 o

-2   6  10     5632.84     5892.23    202.99 o

-1   6  10     4439.44     5057.45    209.89 o

0   6  10     9306.00     9335.07    368.17 o

1   6  10     6494.17     7466.92    304.14 o

2   6  10     1780.42     1693.53    109.41 o

-3   7  10     2183.06     2022.41    160.41 o

-2   7  10    20770.22    20663.02    777.49 o

-1   7  10     6145.55     5448.23    238.44 o

0   7  10    34032.18    35816.61   1317.49 o

1   7  10     2661.87     2760.72    144.34 o

2   7  10    29674.49    27951.68   1045.18 o

-1   8  10     4453.83     4864.91    226.47 o

0   8  10     1182.21     1114.33     96.58 o

-6   1  11     3906.59     3452.32    257.91 o

-5   1  11     2564.20     2324.30    173.14 o

-4   1  11     4855.09     6585.71    217.22 o

-3   1  11     2778.07     3400.51    189.21 o

-2   1  11     1618.80     1492.85    165.04 o

-1   1  11     2335.61     2563.07    372.06 o

0   1  11    28615.86    26762.27    805.18 o

1   1  11      765.23      880.57     35.22 o

2   1  11    26199.91    24812.37    744.64 o

3   1  11      107.82       62.72     35.60 <

4   1  11    28217.75    27650.80   1020.94 o

5   1  11      581.73      823.79     81.03 o

-6   2  11      505.66      409.65    124.21 o

-5   2  11     5740.35     7620.83    304.23 o

-4   2  11     8536.31     7864.13    254.61 o

-3   2  11     4238.63     4980.32    167.42 o

-2   2  11      703.67      494.50     38.97 o

-1   2  11    50017.02    51421.23   1325.81 o

0   2  11    11110.91    11833.25    362.91 o

1   2  11    11185.54    10855.69    335.60 o

2   2  11     1940.00     1850.82     88.13 o

3   2  11    36200.11    34031.71   1239.72 o

4   2  11       10.09       69.44     42.16 <

5   2  11     4385.57     7509.08    311.75 o

-5   3  11      319.05       72.40     40.84 <

-4   3  11     3404.90     7003.15    459.35 o

-3   3  11     3517.66     3358.55    122.20 o

-2   3  11     1644.88     3044.16    116.59 o

-1   3  11     3899.50     3648.64    108.14 o

0   3  11       27.16       -7.14     54.31 <

1   3  11     4604.28     3796.48    130.36 o

2   3  11     5281.57     5287.62    218.44 o

3   3  11     1850.63     1506.76    134.16 o

4   3  11     1090.41     1397.12    135.09 o

5   3  11      356.58      280.81     89.75 o

-5   4  11     4201.71     3651.29    333.09 o

-4   4  11      361.75      654.44     51.77 o

-3   4  11     5960.72     6251.68    210.92 o

-2   4  11      969.92     1024.88     83.58 o

-1   4  11     6511.90     6244.28    177.96 o

0   4  11    15278.31    14330.64    383.88 o

1   4  11     5623.88     5988.49    199.19 o

2   4  11     3277.36     3293.75    146.84 o

3   4  11     6480.44     4603.10    287.29 o

4   4  11     4179.68     3985.27    265.08 o

-4   5  11     8208.34     7821.03    262.65 o

-3   5  11      484.94      610.98     80.61 o

-2   5  11      727.35      674.09     43.77 o

-1   5  11     2718.67     2137.16     78.99 o

0   5  11     2930.73     2911.75    112.42 o

1   5  11     1227.82     1218.89     81.37 o

2   5  11    10950.93    10312.09    746.90 o

3   5  11     1541.61      939.12    116.81 o

4   5  11    19028.36    18692.28   1012.91 o

-4   6  11     1780.83     1620.50     91.60 o

-3   6  11     2528.53     2480.38    111.04 o

-2   6  11     7883.75     6865.99    202.36 o

-1   6  11    12652.25    12146.23    386.20 o

0   6  11     2246.89     1686.92    100.04 o

1   6  11     7701.96     7642.35    310.68 o

2   6  11     1583.79     1079.55     84.17 o

3   6  11    11238.75     9768.51    563.24 o

-3   7  11     3254.28     3475.57    179.33 o

-2   7  11     1331.19     1661.86     92.00 o

-1   7  11     2983.82     2627.03    140.21 o

0   7  11     7150.38     7079.11    296.62 o

1   7  11     4254.29     3620.68    174.51 o

2   7  11     2122.46     2333.72    202.59 o

0   8  11    10279.46     9810.57    401.52 o

-5   0  12     1899.90     2168.08    178.80 o

-4   0  12     3799.82     2953.85    209.11 o

-3   0  12     1292.26     2310.11    169.55 o

-2   0  12     4479.77     4464.31    270.17 o

-1   0  12     4251.89     5538.00    296.89 o

-1   0  12    11657.68    12188.50    664.10 o

0   0  12       75.46       80.62     20.36 o

1   0  12    29172.99    26249.20   1251.51 o

1   0  12    10539.39    13124.84    713.83 o

2   0  12    15932.83    16944.87    926.29 o

3   0  12    29193.08    28650.70   1486.87 o

4   0  12    18455.87    16741.86    899.57 o

5   0  12     8786.89    11921.33    666.41 o

-6   1  12     4081.32     3573.53    289.14 o

-5   1  12     2102.77     2245.31    254.56 o

-4   1  12    15222.15    14667.65    571.04 o

-3   1  12     2549.17     2696.11     99.26 o

-2   1  12    19721.36    19429.55    592.12 o

-1   1  12      276.28      391.37     38.17 o

0   1  12    21957.00    20991.54    635.59 o

1   1  12       50.46       56.85     13.79 o

2   1  12      568.68      857.49    126.55 o

3   1  12      746.94      341.41     49.20 o

4   1  12      885.60     6100.38    369.17 o

5   1  12      640.83      518.23     70.90 o

-6   2  12      100.84      147.81    111.26 <

-5   2  12      561.17      322.23     38.69 o

-4   2  12      133.60      572.32     45.34 o

-3   2  12     2837.05     3759.51    235.48 o

-2   2  12      862.91      876.82     47.02 o

-1   2  12     4957.59     5382.40    434.98 o

0   2  12       89.83      131.84     20.05 o

1   2  12     5067.41     5819.77    320.64 o

2   2  12      263.32      128.61     29.00 o

3   2  12     3140.56     3229.17    208.76 o

4   2  12       10.85        0.46     37.27 <

5   2  12     2857.00     1180.72     93.63 o

-5   3  12     2414.08     3400.96    182.04 o

-4   3  12    31959.93    33111.65   1004.60 o

-3   3  12     5650.87     6095.37    204.20 o

-2   3  12    79619.79    86877.74   2735.15 o

-1   3  12     2336.15     2665.24    119.89 o

0   3  12    19842.12    19686.81    669.00 o

1   3  12     2554.94     2461.33     92.33 o

2   3  12      338.38      407.97     51.81 o

3   3  12      536.57      420.76     79.80 o

4   3  12      707.91      511.89     92.29 o

5   3  12      789.78      500.79    102.01 o

-5   4  12      820.71      597.72     73.43 o

-4   4  12      263.47      152.42     37.03 o

-3   4  12     2690.07     2999.33    116.25 o

-2   4  12     1483.02     1399.30     57.44 o

-1   4  12     8708.64     8958.12    247.37 o

0   4  12     9118.82     9914.05    314.22 o

1   4  12    16961.43    16483.51    510.33 o

2   4  12     5052.05     5741.80    379.00 o

3   4  12    18644.18    18075.84    964.57 o

4   4  12     5601.46     5362.03    335.86 o

5   4  12    10248.92    12554.89    706.43 o

-4   5  12       69.95      107.25     42.29 o

-3   5  12      633.13      497.97     47.56 o

-2   5  12     1582.03     1505.63     74.71 o

-1   5  12     1767.41     1410.54     93.25 o

0   5  12      875.23      932.22     64.56 o

1   5  12     3057.05     2608.49    106.98 o

2   5  12     1218.33      953.26    181.81 o

3   5  12     5166.81     4873.96    309.73 o

4   5  12      281.57     2510.42    206.56 o

-4   6  12     3809.24     3631.29    147.02 o

-3   6  12     1245.70     1142.14     90.86 o

-2   6  12     2223.10     2330.77     88.88 o

-1   6  12     7587.33     7745.54    224.33 o

0   6  12     3881.23     3954.11    128.25 o

1   6  12     3087.33     3524.58    135.53 o

2   6  12      359.13      241.63     51.68 o

3   6  12    13760.90    13566.88    756.16 o

-3   7  12     2965.39     3123.17    167.63 o

-2   7  12    25440.73    25195.42    776.95 o

-1   7  12     1648.48     2010.68    100.84 o

0   7  12     5212.14     4204.23    193.77 o

1   7  12      556.94      678.84     86.81 o

2   7  12      432.35      761.50     63.13 o

-6   1  13      934.09     2041.79    211.19 o

-5   1  13     1091.04      693.71     72.39 o

-4   1  13    11417.24    12105.98    479.31 o

-3   1  13      530.70      401.66     32.61 o

-2   1  13    23608.40    22659.13    688.69 o

-1   1  13      109.53       93.35     15.41 o

0   1  13   106853.77   102369.20   3049.10 o

1   1  13     1539.22     1189.75     46.01 o

2   1  13    31212.72    30292.22    905.09 o

3   1  13     3383.28     3329.02    155.05 o

4   1  13    17772.43    17246.73    653.92 o

5   1  13      465.93       79.89     48.57 <

-5   2  13     3744.53     8251.40    339.26 o

-4   2  13     2499.07     2664.91    112.47 o

-3   2  13    32158.55    37505.37   1133.38 o

-1   0  14    13487.04    17025.09    634.15 o

-5   0  18      765.68      172.56     73.09 o

-2   2  13     2860.65     2701.52     99.55 o

-1   2  13    13508.65    12540.41    386.16 o

0   2  13      188.74      133.51     21.91 o

1   2  13    37640.76    32094.56    967.74 o

2   2  13     1518.21     1543.44     80.15 o

3   2  13     1000.90     1121.65     80.55 o

4   2  13      223.68      139.32     42.63 o

5   2  13     4010.28     5979.05    261.59 o

-5   3  13     2736.97     2180.14     96.09 o

-4   3  13      432.15     1538.48     94.09 o

-3   3  13     3445.00     3640.24    132.72 o

-2   3  13     5985.31     5462.70    183.80 o

-1   3  13     2656.51     2455.06     79.18 o

0   3  13     4303.24     4096.80    140.83 o

1   3  13      554.46      718.46     46.62 o

2   3  13     4023.81     3921.34    169.83 o

3   3  13      832.41      248.66     60.37 o

4   3  13      287.51      697.64    102.01 o

5   3  13     1441.54      665.71    107.56 o

-5   4  13     1853.33     1773.72    367.67 o

-4   4  13     1676.38     1197.79     70.23 o

-3   4  13     2890.99     3225.51    236.98 o

-2   4  13     7301.35     6454.89    183.99 o

-1   4  13     6319.18     8498.36    235.26 o

0   4  13     2489.00     2286.72     91.58 o

1   4  13    10090.03    12560.65    440.97 o

2   4  13     1357.80     1550.73    186.44 o

4   4  13      344.15      481.59     97.38 o

-4   5  13     3728.92     3384.56    135.23 o

-3   5  13      320.09      436.09     48.16 o

-2   5  13     8972.10     9850.47    274.58 o

-1   5  13     2513.38     2689.31     93.02 o

0   5  13    61521.42    65471.37   1691.96 o

1   5  13     6546.41     6190.36    229.26 o

2   5  13    23165.28    24838.31    930.72 o

3   5  13     4390.17     4427.07    288.68 o

4   5  13    17475.35    16045.38    881.53 o

-4   6  13     1423.31     1368.58    125.47 o

-3   6  13     7970.23     8308.39    282.53 o

-2   6  13      904.71      699.94     49.43 o

-1   6  13     4186.46     4244.62    136.73 o

0   6  13      139.98      190.74     32.74 o

1   6  13     7468.21     6872.04    251.94 o

2   6  13      833.07      604.76     70.43 o

-2   7  13     2142.25     2276.43    124.90 o

-1   7  13     1478.35     1275.34     80.88 o

0   7  13     1346.49     1322.53     80.47 o

1   7  13      168.60      159.75     50.52 o

2   7  13       72.10      113.76     67.49 <

-6   0  14     1517.04     1436.68    179.73 o

-5   0  14     5307.82     7667.28    457.53 o

-4   0  14     1093.19      835.73    109.41 o

-3   0  14    23059.47    24654.56   1328.65 o

-2   0  14    35568.26    33276.23   1770.92 o

-1   0  14    36951.06    36032.08   1908.09 o

0   0  14     9826.95     9391.48    493.62 o

1   0  14    33556.18    29120.93   2024.21 o

1   0  14    12123.54    14588.12    795.71 o

2   0  14     6651.03     6031.13    433.59 o

3   0  14    12785.83    13945.54    752.46 o

4   0  14    10790.49     9962.82    560.01 o

5   0  14     2463.86     3588.57    250.74 o

-6   1  14     4102.58     3864.98    296.77 o

-5   1  14      107.32      177.80     57.44 o

-4   1  14     6670.70    10564.57    424.60 o

-3   1  14      199.06      294.32     63.61 o

-2   1  14      395.68      607.44     59.10 o

-1   1  14      654.33      739.47     50.37 o

0   1  14     1979.54     1931.73    106.98 o

1   1  14     1380.24     1285.98     47.95 o

2   1  14     6405.12     7273.55    311.32 o

3   1  14     2831.07     2815.31    158.49 o

4   1  14     5657.26     7189.85    393.11 o

5   1  14      947.49      896.42     85.51 o

-4   2  14       72.13      101.57     31.29 o

-2   2  14      210.18      177.97     27.70 o

-1   2  14    14044.29    16751.10    511.88 o

0   2  14       46.25       37.89     19.13 <

1   2  14     6308.21     6026.18    323.92 o

2   2  14     3041.27     2957.17    131.22 o

4   2  14      356.08      339.65     55.35 o

-5   3  14     1046.76      891.80     89.22 o

-4   3  14     5939.80     6513.39    219.67 o

-3   3  14     1147.57     1147.89     86.61 o

-2   3  14      195.48      337.03     37.28 o

-1   3  14     1270.32     1211.20     49.79 o

0   3  14      838.26      938.54     51.24 o

1   3  14      787.58      734.11     45.70 o

2   3  14    17855.91    17950.87    745.86 o

3   3  14     4646.91     3881.87    246.58 o

4   3  14      801.88     1053.39    124.91 o

5   3  14     2418.15     2862.71    216.51 o

-5   4  14     4878.49     5771.54    275.73 o

-4   4  14      285.59      849.49     68.29 o

-3   4  14    14479.11    15079.25    474.12 o

-2   4  14    11867.54    10551.25    338.27 o

-1   4  14    27678.49    26004.76    682.67 o

0   4  14     1317.52     1449.73    106.45 o

1   4  14    29875.40    27346.14    832.86 o

2   4  14     2077.24     1997.59     85.93 o

3   4  14    14804.15    12736.70    698.79 o

4   4  14     6576.79     5584.78    349.28 o

-4   5  14      634.78     1642.08    152.20 o

-3   5  14     3734.71     3524.09    165.70 o

-2   5  14      485.92      601.32     58.69 o

-1   5  14     6022.96     5891.99    174.27 o

0   5  14      260.70      274.40     36.12 o

1   5  14     5551.81     4925.28    174.18 o

2   5  14      170.09      497.07    145.84 o

3   5  14     2850.92     2508.11    192.68 o

4   5  14      251.88      484.13    106.63 o

-3   6  14    13583.82    12902.60    417.92 o

-2   6  14      129.96      142.08     33.15 o

-1   6  14     9346.90     8966.71    377.37 o

0   6  14      238.00      389.06     40.26 o

1   6  14    24453.16    20564.66    634.24 o

2   6  14      391.47      373.43     78.30 o

3   6  14     6569.48     6119.34    383.51 o

-2   7  14      821.91     1064.56     79.83 o

-1   7  14      357.09      343.63     51.08 o

0   7  14     5889.82     6267.41    220.46 o

1   7  14     1203.78     1347.25     95.01 o

2   7  14     5250.76     5085.34    188.07 o

-5   1  15      327.01      556.47     75.21 o

-4   1  15    31872.51    29962.66   1137.57 o

-3   1  15     1887.76     2395.45    125.92 o

-2   1  15    38048.06    36752.74   1107.80 o

-1   1  15     2225.44     1632.51     65.72 o

0   1  15    44963.29    43084.84   1293.14 o

1   1  15      959.22     1054.47     43.70 o

2   1  15    21439.39    19450.60    590.28 o

3   1  15     1105.48     1007.46     55.62 o

4   1  15     2375.39     2723.37    269.48 o

5   1  15     1259.78     1822.44    122.41 o

-5   2  15    12189.74    13907.74    550.07 o

-4   2  15       13.84      -17.26     29.38 <

-3   2  15     2825.22     2625.08    102.73 o

-2   2  15      958.00     1188.32     59.50 o

-1   2  15     2675.67     3577.83    184.59 o

0   2  15      451.93      527.70     36.16 o

1   2  15    59524.91    52327.95   1570.14 o

2   2  15     1331.04     1582.10     84.41 o

3   2  15    36845.09    33486.16   1225.65 o

4   2  15      784.23      793.02     75.26 o

5   2  15    29967.79    37815.66   1395.10 o

-5   3  15      262.87      364.65     63.10 o

-4   3  15     1181.97     1254.84     88.71 o

-3   3  15      226.63      241.19     45.07 o

-2   3  15     4351.68     4600.06    160.19 o

-1   3  15      921.92      612.99     39.80 o

0   3  15      115.50      213.50     29.37 o

1   3  15     2365.34     2347.04     92.21 o

2   3  15      394.60      494.30     52.09 o

4   3  15      113.08      202.86     81.88 o

5   3  15      954.67      176.26     79.80 o

-5   4  15     1686.29      873.20    153.59 o

-4   4  15     3185.86     3987.97    149.11 o

-3   4  15     6922.23     7808.84    437.18 o

-2   4  15     1567.49     2112.73     92.08 o

-1   4  15    12344.81    14533.92    469.29 o

0   4  15     1472.20     1090.01     73.45 o

1   4  15    10170.56    11085.07    353.27 o

2   4  15     1650.35     1991.00     86.04 o

3   4  15     3078.45     3150.23    219.05 o

4   4  15     2554.81     2697.55    206.56 o

-4   5  15    22794.78    21788.76    680.10 o

-3   5  15     5287.22     5732.46    202.78 o

-2   5  15    28752.14    27036.82   1460.38 o

-1   5  15     3596.68     4125.87    129.91 o

0   5  15    28654.54    28523.91   1359.10 o

1   5  15     1548.29     1896.95     99.66 o

2   5  15    13614.52    13300.54    515.05 o

3   5  15     4685.24     4333.85    286.83 o

4   5  15      695.10      452.91     98.77 o

-2   6  15      638.96      693.87     49.12 o

-1   6  15     8859.98    10099.09    285.98 o

0   6  15     1245.27     1086.72     59.16 o

1   6  15    12454.59    12250.37    450.48 o

2   6  15       83.40      117.50     47.20 o

3   6  15     6365.58     6504.02    403.18 o

-2   7  15       48.08      110.62     44.91 o

-1   7  15     1183.92      954.47     61.90 o

0   7  15       22.28       80.80     38.69 o

1   7  15      328.82      315.68     47.04 o

2   7  15       56.94      191.15     46.78 o

-5   0  16     8162.74    10097.44    586.37 o

-4   0  16    15405.53    15040.33    837.12 o

-3   0  16    18065.00    19378.35   1057.79 o

-2   0  16    13704.29    11529.49    642.81 o

-1   0  16    14372.28    13475.98    738.58 o

-1   0  16     5237.57     6592.90    258.18 o

0   0  16     6730.82     6203.92    460.89 o

1   0  16     3845.03     3501.85    149.17 o

1   0  16     1392.70     1782.49    136.94 o

2   0  16    21490.26    17946.05    672.29 o

3   0  16      232.41      232.93     75.18 o

5   0  16     2159.12     3009.36    224.60 o

-5   1  16      211.03      340.01     69.97 o

-4   1  16     2320.01     4358.30    301.75 o

-3   1  16     2716.44     3034.46    149.77 o

-2   1  16     8942.51     8282.44    264.30 o

-1   1  16     2468.01     1891.05     73.44 o

0   1  16    18222.65    17356.56    532.71 o

1   1  16     3872.44     3875.75    115.31 o

2   1  16    12830.19    14037.71    433.13 o

3   1  16     1296.91      768.69     71.97 o

4   1  16     4795.98     4600.75    208.94 o

5   1  16      702.32      479.87    128.03 o

-5   2  16     2620.98     2342.91    256.87 o

-4   2  16       11.93       -4.97     29.69 <

-3   2  16     1652.78     1805.03    109.62 o

-2   2  16     2902.70     2915.28    108.81 o

-1   2  16    23599.57    30059.09    907.49 o

0   2  16      358.80      413.75     39.51 o

1   2  16    43902.67    53707.34   1610.80 o

2   2  16     3205.95     2550.46    120.77 o

4   2  16      365.61      620.32    120.51 o

5   2  16     2579.27     2746.44    150.21 o

-5   3  16      149.97      266.75     65.66 o

-4   3  16     1300.34     1529.71     78.88 o

-3   3  16     2216.08     2425.65    101.41 o

-2   3  16    20069.72    20227.04    622.90 o

-1   3  16     4193.87     4160.11    144.37 o

0   3  16     1993.35     1707.64     98.76 o

1   3  16    14055.47    12891.31    403.38 o

2   3  16    13102.71    12616.57    484.75 o

3   3  16     6820.19     6172.31    365.24 o

4   3  16    12954.87    11337.96    637.26 o

-5   4  16     9104.85    11249.97    368.15 o

-4   4  16     3652.50     3858.14    147.63 o

-3   4  16    18697.65    18267.22    570.86 o

-2   4  16     3059.57     2885.55    115.16 o

-1   4  16    17818.79    16638.60    445.94 o

0   4  16     2626.32     3060.29    116.80 o

1   4  16     8018.97     7503.97    248.08 o

2   4  16    10011.64     9197.74    297.19 o

3   4  16     1719.84      659.47     95.99 o

4   4  16      714.30      484.13     96.69 o

-4   5  16      482.32     2447.51    200.32 o

-3   5  16     4145.54     4036.24    154.23 o

-2   5  16       76.91      605.46    101.76 o

-1   5  16     3630.80     3007.83    294.01 o

0   5  16     1025.61      991.09     54.67 o

1   5  16     3427.63     3931.34    146.77 o

2   5  16       25.07       45.15     73.09 <

3   5  16     1642.44     1136.20    128.84 o

4   5  16      318.54      508.19     97.15 o

-3   6  16     6814.12     6190.17    221.74 o

-2   6  16      155.92      212.60     44.74 o

-1   6  16    16102.85    15701.53    429.27 o

0   6  16      580.16      512.85     44.51 o

1   6  16     6088.24     8333.71    387.37 o

2   6  16      982.54      920.78     77.94 o

-2   7  16     5890.89     5077.23    193.31 o

-1   7  16      163.98      302.77     46.61 o

0   7  16     2577.43     2243.86    107.45 o

1   7  16     3292.62     2722.32    136.74 o

-5   1  17      405.49      403.68    144.69 o

-4   1  17    15714.49    15500.87    609.34 o

-3   1  17     1036.04      902.75     76.86 o

-2   1  17    14757.93    15379.32    475.37 o

-3   0  18      336.69      334.71     73.09 o

-1   0  18      553.13      540.84     47.67 o

-5   0  20      526.08       40.25     63.61 <

5   0  14      887.70      179.04     97.15 <

3   0  16       83.01       31.92     66.85 <

5   0  16      777.43      277.57    102.70 o

-1   1  17     3646.72     3330.50    116.23 o

0   1  17     6527.91     6382.71    209.38 o

1   1  17     5524.53     4563.22    133.75 o

2   1  17      100.03      631.52     52.65 o

3   1  17     1415.51     1348.10    139.47 o

4   1  17      238.30      707.54     73.59 o

5   1  17     1403.13     1212.53    102.08 o

-5   2  17     6569.85     8079.54    342.19 o

-4   2  17      509.03      527.78     44.63 o

-3   2  17    23964.96    23068.03    883.72 o

-2   2  17     1158.24     1421.65     98.25 o

-1   2  17   117859.95   102402.25   3055.35 o

0   2  17     4351.18     3473.64    123.54 o

1   2  17    38386.49    37807.03   1708.04 o

2   2  17     1317.47     1416.00    105.36 o

3   2  17    16672.88    17424.51    536.80 o

4   2  17     2045.56     2128.69    125.71 o

5   2  17      374.41      880.90    156.94 o

-5   3  17      446.72      440.13     75.67 o

-4   3  17      272.41      513.10     50.29 o

-3   3  17     2181.96     2373.27    142.72 o

-2   3  17      224.80      472.79    117.33 o

-1   3  17     5225.89     6974.03    263.28 o

0   3  17      424.60      528.98     53.86 o

1   3  17     5554.94     6797.33    223.96 o

2   3  17     1040.65     1053.82     58.39 o

4   3  17     1547.10     3002.42    219.28 o

-4   4  17      408.07      794.14    147.43 o

-3   4  17     8422.51     9193.84    303.49 o

-2   4  17     1697.37     1788.37    113.15 o

-1   4  17     9820.25     9873.18    297.81 o

0   4  17      917.44      829.99     59.06 o

1   4  17     8187.43     7244.72    241.50 o

2   4  17     5518.46     4398.03    156.70 o

3   4  17     6822.53     5771.92    352.98 o

4   4  17      388.11      527.85     98.08 o

-4   5  17    12254.35    12436.16    403.54 o

-3   5  17     2035.85     2262.97    156.43 o

-2   5  17     8744.64     9149.89    309.71 o

-1   5  17     6676.18     6031.73    179.22 o

0   5  17      514.40      869.13     51.80 o

1   5  17     5379.64     5265.19    186.04 o

2   5  17     2453.41     2803.35    155.67 o

3   5  17      676.96      719.38    108.02 o

-3   6  17     5549.37     6100.90    220.81 o

-2   6  17      215.36      316.73     49.80 o

-1   6  17    16673.14    14664.93    402.66 o

0   6  17     1257.22     1652.57     75.30 o

1   6  17     9193.73     7479.43    273.21 o

2   6  17     7828.89     8273.70    698.33 o

3   6  17     7074.66     5833.21    374.03 o

-2   7  17      137.52      195.93     50.38 o

-1   7  17     2242.46     2262.99     95.82 o

0   7  17     1261.45     1497.05     87.86 o

1   7  17     5468.99     4991.89    185.86 o

-5   0  18     2093.90     3966.30    280.58 o

-4   0  18    14832.89    14678.80    822.31 o

-3   0  18      922.84      989.09    120.05 o

-2   0  18     7693.37     8105.39    468.87 o

-1   0  18     1511.75     1213.00    112.19 o

0   0  18     7226.83     7396.40    419.83 o

1   0  18     4519.59     5293.79    319.90 o

1   0  18    12526.20     9806.30    651.26 o

2   0  18    79253.50    76193.42   2774.62 o

3   0  18    22828.34    20305.91   1077.22 o

3   0  18     8193.52     9651.24    561.86 o

4   0  18    11970.68    10161.98    577.82 o

5   0  18    12261.74    15373.65    852.85 o

-5   1  18     1146.47     1459.83    116.96 o

-4   1  18     5711.19     6507.61    282.27 o

-3   1  18     1631.11     1615.98    206.68 o

-2   1  18    14336.92    13742.42    428.86 o

-1   1  18     3191.38     2894.09    105.16 o

0   1  18    10341.05    10099.14    320.07 o

1   1  18     1722.41     1926.27     68.55 o

2   1  18    11696.70    11446.20    309.81 o

3   1  18     1639.32     1539.71     87.70 o

4   1  18     1303.66     1550.50    109.66 o

5   1  18      943.64      527.10     72.39 o

-5   2  18     1448.65      408.43     73.24 o

-4   2  18      628.80      517.61     46.30 o

-2   2  18     3244.36     2695.78    105.43 o

-1   2  18    21011.65    22444.26    684.99 o

0   2  18      864.25      896.84     51.33 o

1   2  18     2983.76     3273.07    296.98 o

2   2  18     1884.94     1992.86    104.01 o

3   2  18     3642.42     3590.57    133.11 o

4   2  18      995.64     1305.81     99.41 o

5   2  18      194.68      488.59     72.78 o

-5   3  18     2975.17     4484.89    216.22 o

-4   3  18     1094.40     1222.54     72.42 o

-3   3  18     8995.04     8481.89    311.24 o

-2   3  18    12537.83    12480.40    395.37 o

-1   3  18    15164.42    13784.95    430.50 o

0   3  18    35068.64    36355.87   1135.73 o

1   3  18     4539.03     4083.58    145.52 o

2   3  18    23961.07    22912.65    701.30 o

3   3  18     1806.80     1638.38    149.20 o

4   3  18    10964.43     9198.56    531.79 o

-4   4  18     7203.56     8100.65    274.22 o

-3   4  18     2397.26     2262.52    101.60 o

-2   4  18     4272.13     5386.22    189.76 o

-1   4  18     3206.97     4095.03    178.02 o

0   4  18     1352.40     1469.69     74.49 o

1   4  18     6309.21     5746.90    198.17 o

2   4  18    10911.07    11154.37    356.72 o

3   4  18     6874.32     6672.87    398.78 o

4   4  18     6083.80     5776.31    365.01 o

-4   5  18      270.01      351.14     55.93 o

-3   5  18     2731.85     2951.57    125.82 o

-2   5  18       44.15      191.02     42.17 o

-1   5  18     2001.09     2813.86     99.05 o

0   5  18      407.49      590.82     45.47 o

1   5  18      357.24      426.84     47.10 o

2   5  18      124.65      159.80     37.22 o

3   5  18      323.54      364.78     84.43 o

-3   6  18     2767.54     3496.10    149.35 o

-2   6  18     1639.66     1587.12    103.46 o

-1   6  18     7397.06     6973.05    207.90 o

0   6  18      871.26      913.80     83.40 o

1   6  18     1104.01     1452.07     83.77 o

2   6  18    10814.07    10837.71    434.25 o

-1   7  18     5294.32     5351.82    172.85 o

0   7  18    20267.63    19261.15    526.11 o

1   7  18     3160.06     3798.97    163.32 o

-5   1  19     1613.24     2196.31    143.74 o

-4   1  19     1237.77     2132.07    126.63 o

-3   1  19     2819.76     2282.70    137.63 o

-2   1  19      207.41      747.68    103.46 o

-1   1  19     4111.55     3113.90    113.03 o

0   1  19     2348.62     2333.24     92.69 o

1   1  19     2531.15     2186.41     76.13 o

2   1  19     7078.68     7782.88    218.66 o

3   1  19     2457.21     2133.55     90.43 o

4   1  19     5212.29     5525.27    245.34 o

5   1  19     2611.05     3063.32    163.48 o

-5   2  19    19651.84    28246.82   1085.87 o

-4   2  19      956.57     1164.49     96.03 o

-3   2  19    30760.55    29798.77    909.89 o

-2   2  19     1539.02     1678.09     78.65 o

-1   2  19     1355.04     1880.54    101.14 o

0   2  19     5836.79     5609.52    189.30 o

1   2  19     1329.42     1269.98     66.36 o

2   2  19     6071.21     5344.97    181.36 o

3   2  19     2869.83     3266.67    124.82 o

4   2  19      958.16      677.51     74.20 o

-5   3  19      947.24      369.17     74.14 o

-4   3  19       87.10      561.28    143.31 o

-2   3  19     1067.75     1079.48     68.05 o

-1   3  19     1718.98     2241.40    180.68 o

0   3  19     6282.85     6032.51    203.57 o

1   3  19      268.18      283.89     37.90 o

2   3  19     6928.23     6851.33    228.93 o

3   3  19      458.01      614.31     92.64 o

4   3  19     6266.90     5839.92    364.55 o

-4   4  19     3328.57     3454.22    139.37 o

-3   4  19     4461.83     4237.70    159.42 o

-2   4  19     2153.95     3037.14    147.32 o

-1   4  19     6492.23     6389.03    186.48 o

0   4  19      518.62      699.29     64.33 o

1   4  19     6764.34     7160.20    240.38 o

2   4  19     5197.44     4361.47    216.14 o

4   4  19     4010.89     3575.84    256.06 o

-4   5  19     1683.75     1838.66    101.44 o

-3   5  19     3055.97     2965.43    127.58 o

-2   5  19     2103.46     2249.22    103.79 o

-1   5  19      978.21     1085.48     58.68 o

0   5  19     7469.67     8199.78    273.71 o

1   5  19      435.82      485.15     50.34 o

2   5  19     8755.46     8702.62    289.25 o

3   5  19     2703.22     2440.57    192.91 o

-3   6  19     8508.67     7240.43    256.59 o

-2   6  19     8164.22     8395.53    289.23 o

-1   6  19     1373.18     1156.04     64.96 o

0   6  19     7715.33     7813.51    230.96 o

1   6  19      419.85      390.96     53.55 o

2   6  19     2719.95     2569.41    200.78 o

-1   7  19     7063.45     5744.69    183.60 o

0   7  19      634.54      789.56     60.88 o

-5   0  20     1440.58     2282.12    210.26 o

-4   0  20     3810.82     3825.43    267.40 o

-3   0  20    10413.31    10463.61    602.80 o

-2   0  20    60856.87    63662.93   3362.11 o

-1   0  20    31525.99    28319.00   1518.10 o

-1   0  20    11506.73    13293.83    506.94 o

0   0  20    66811.20    65984.99   2408.49 o

1   0  20    34457.02    31589.45   1273.60 o

1   0  20    12455.26    16053.71    881.76 o

2   0  20    17570.66    17155.83    647.77 o

3   0  20    15907.84    15153.68    822.54 o

4   0  20     7866.05     8080.63    478.35 o

-5   1  20      506.15      347.62     77.41 o

-4   1  20     4314.48     4561.48    216.97 o

-3   1  20      896.02      867.08     80.98 o

-2   1  20    11601.68    11468.96    458.86 o

-1   1  20     1219.16     1397.26     64.99 o

0   1  20     2605.85     2719.10    105.08 o

1   1  20     2243.40     2649.72     89.23 o

2   1  20     1137.17     1298.47     58.14 o

3   1  20     1908.08     1688.80    441.23 o

4   1  20      757.10     1171.77     95.35 o

-4   2  20      646.01      873.11    122.60 o

-3   2  20     9699.64    10389.62    335.85 o

-2   2  20     2101.99     1972.05     87.44 o

-1   2  20     1041.22     1086.02     58.91 o

0   2  20     2960.13     2929.94    112.44 o

1   2  20     2052.55     1835.85     82.64 o

2   2  20     3622.59     3984.20    143.42 o

3   2  20      779.40      549.08     69.20 o

4   2  20      898.56     1420.90    232.35 o

-5   3  20     2504.99     3747.68    214.89 o

-4   3  20    16967.41    15665.68    496.78 o

-3   3  20     2291.21     2238.86     99.59 o

-2   3  20    25125.25    24639.88    758.01 o

-1   3  20       98.52      197.78     34.46 o

0   3  20    15558.33    15552.24    485.22 o

1   3  20      425.82      440.61     43.86 o

2   3  20     1946.81     1783.56     83.07 o

3   3  20     2417.36     2221.73    119.16 o

4   3  20     6722.80     6252.58    388.83 o

-4   4  20     1578.63     1840.49     96.85 o

-3   4  20     5846.47     6029.21    212.90 o

-2   4  20     7942.42     9113.92    302.21 o

-1   4  20    10412.95     9690.86    270.60 o

0   4  20    33146.07    36032.57   1110.47 o

1   4  20     8795.84     7559.95    251.73 o

2   4  20     8836.98     9048.32    296.06 o

3   4  20     2920.02     3022.32    219.28 o

-3   5  20      358.08      331.54     50.23 o

-2   5  20       86.30      153.49     43.81 o

-1   5  20      497.21      467.33     67.84 o

0   5  20      229.69      257.40     54.84 o

1   5  20     2183.86     2339.78    166.19 o

2   5  20     1326.70     1648.38     86.23 o

-2   6  20    10813.15    10350.29    347.79 o

-1   6  20      514.05      549.03     50.11 o

0   6  20     9917.27     9238.46    267.79 o

1   6  20     2943.97     2319.42    107.96 o

2   6  20     6666.04     6841.73    415.67 o

-5   1  21     1082.42     1658.41    126.34 o

-4   1  21      625.95     1003.78     96.34 o

-3   1  21     1205.18     1429.62    102.62 o

-2   1  21     9996.93     9735.40    396.80 o

-1   1  21     3819.59     3410.41    123.60 o

0   1  21    10479.49     9685.71    310.62 o

1   1  21     7654.46     6651.07    190.90 o

2   1  21     7188.37     7641.20    217.45 o

3   1  21     4863.29     4669.91    167.84 o

4   1  21     1338.55     1589.03    114.37 o

-5   2  21     2266.05     2594.33    158.25 o

-4   2  21     1912.85     2357.53    141.23 o

-3   2  21     3545.03     3682.05    139.00 o

-2   2  21     5151.34     5156.47    181.09 o

-1   2  21     1695.02     1707.87     77.56 o

0   2  21     3022.84     3091.07    119.16 o

1   2  21     1362.82     1521.93     75.21 o

2   2  21     7329.26     8190.59    289.54 o

3   2  21     2843.24     3141.34    124.04 o

4   2  21    15367.84    14044.14    551.58 o

-4   3  21     2924.09     4159.99    461.58 o

-1   0  22     6323.20     8091.80    321.25 o

-5   0  24     1560.26      289.37     80.50 o

-3   0  24      836.07      645.59     99.00 o

-3   3  21      904.10      672.79     56.47 o

-2   3  21     8154.11     7440.57    315.56 o

-1   3  21      922.28      770.59     52.51 o

0   3  21    10359.64    10294.24    331.81 o

1   3  21     1316.57     1384.20    101.24 o

2   3  21     3214.60     2989.91    192.03 o

3   3  21     2344.97     2424.21    177.99 o

4   3  21      252.62      943.29    130.46 o

-4   4  21      904.86     1499.46    201.70 o

-3   4  21     3194.70     3597.85    146.71 o

-2   4  21     3601.50     3773.34    173.55 o

-1   4  21     3700.85     4181.80    132.14 o

0   4  21    21285.29    21347.79    661.48 o

1   4  21     1226.07     1682.97    109.79 o

2   4  21     9060.20     9214.27    302.98 o

3   4  21       91.76      170.94     74.94 o

-3   5  21      357.85      609.42     90.05 o

-2   5  21    11611.29    10601.58    351.81 o

-1   5  21     4493.94     4398.67    141.23 o

0   5  21     4789.88     4474.60    186.11 o

1   5  21    12855.90    10907.89    357.11 o

2   5  21    13079.15    12141.99    794.67 o

3   5  21     7791.49     7711.69    462.62 o

-2   6  21     1781.76     2559.67    121.45 o

-1   6  21     1288.12     1650.59     78.31 o

0   6  21      982.60     1307.07     71.31 o

1   6  21     3294.88     3098.10    253.67 o

2   6  21      505.20      495.24    102.70 o

-5   0  22    12917.40    15644.75    887.77 o

-4   0  22    11918.12    11133.02    646.28 o

-3   0  22    23774.65    22634.52   1237.75 o

-2   0  22    24034.02    23059.21   1253.48 o

-1   0  22    17340.05    16522.58    908.82 o

0   0  22     1299.66      876.53     62.97 o

1   0  22     5877.40     5838.62    241.85 o

1   0  22     2126.85     3037.81    216.74 o

2   0  22     1875.85     1583.21    124.21 o

3   0  22      795.17      682.14    108.25 o

3   0  22     2211.31     2258.76    182.27 o

4   0  22      783.32     1166.27    139.25 o

-5   1  22      916.11      711.52     91.63 o

-4   1  22      989.40     1537.00    115.27 o

-3   1  22     1037.33      827.38     81.02 o

-2   1  22      436.15      821.49    123.52 o

-1   1  22     2781.18     3226.99    119.47 o

0   1  22     2278.21     2245.28     93.80 o

1   1  22     5399.64     5810.46    209.55 o

2   1  22     5822.09     5403.77    161.46 o

3   1  22     3164.87     3417.59    132.15 o

4   1  22     2044.87     2182.96    131.78 o

-5   2  22      964.88     1034.80    107.38 o

-4   2  22     1120.58     1371.94    110.64 o

-3   2  22     1234.19      968.81     87.30 o

-2   2  22     4626.72     4161.71    152.76 o

-1   2  22     2893.19     2206.32     92.22 o

0   2  22      643.42      842.64     57.63 o

1   2  22     1874.18     1751.16     82.71 o

2   2  22      986.16     1711.22    137.02 o

3   2  22     5126.01     4655.37    207.37 o

4   2  22      645.43     3116.12    431.05 o

-4   3  22     6188.53     7762.57    644.90 o

-3   3  22      558.99      678.48     72.56 o

-2   3  22      915.18     1211.27     72.04 o

-1   3  22     1001.86     1058.12     61.93 o

0   3  22    18701.46    18815.86    584.90 o

1   3  22     4306.63     3909.90    217.80 o

2   3  22     6083.86     6614.76    224.10 o

3   3  22     3679.39     3321.07    160.93 o

4   3  22     4425.87     4031.07    284.98 o

-4   4  22     6325.96     6278.95    224.76 o

-3   4  22     5143.84     5123.00    188.86 o

-2   4  22    13150.00    12139.71    393.61 o

-1   4  22     3345.95     2962.24    103.16 o

0   4  22     1206.87     1350.33    184.21 o

1   4  22      961.47      885.90     61.79 o

2   4  22     2313.09     2128.88     98.21 o

3   4  22      160.80      280.81     84.20 o

-3   5  22     1147.73     1125.30     78.49 o

-2   5  22     1290.17     1741.93     95.88 o

-1   5  22     4919.66     5863.49    183.84 o

0   5  22      953.48     1366.81     79.01 o

1   5  22     4272.67     5072.14    185.80 o

2   5  22     1128.46     1186.90     95.68 o

-2   6  22     6611.11     6410.39    234.74 o

-1   6  22     3409.53     2968.30    130.93 o

0   6  22     2860.03     2848.91    129.21 o

1   6  22      997.54     1012.31    140.47 o

-5   1  23     1813.87     2656.54    155.96 o

-4   1  23     5688.16     7066.52    311.72 o

-3   1  23     4998.58     5217.93    239.21 o

-2   1  23     5789.05     5865.81    257.90 o

-1   1  23     7962.85     7485.16    246.57 o

0   1  23     5782.99     5618.72    199.09 o

1   1  23     5522.26     6162.98    180.44 o

2   1  23     1138.64     1408.22     91.68 o

3   1  23     2418.63     2356.83    163.07 o

4   1  23       62.12      163.46     53.01 o

-4   2  23     2604.50     2519.91    176.03 o

-3   2  23     1502.59     1657.04    139.92 o

-2   2  23    10644.13     9766.43    319.12 o

-1   2  23     1165.20     1429.15     98.54 o

0   2  23    34019.29    32282.79    983.66 o

1   2  23      842.78      785.14     56.56 o

2   2  23    39941.03    39402.17   1195.35 o

3   2  23     6471.55     6290.08    268.31 o

4   2  23     9588.35     8697.23    365.05 o

-4   3  23     5563.20     5939.85    272.90 o

-3   3  23     2250.64     2142.45    102.52 o

-2   3  23     2442.69     2566.50    111.86 o

-1   3  23     3149.22     2992.64    122.22 o

0   3  23      320.23      354.63     44.94 o

1   3  23     4627.39     5359.40    189.73 o

2   3  23        3.91       84.73     37.77 o

-4   4  23     5260.81     5023.85    190.35 o

-3   4  23     1153.19      878.86    134.96 o

-2   4  23    12864.63    11734.43    556.93 o

-1   4  23      375.26      533.28     42.91 o

0   4  23     6292.18     5736.14    201.80 o

1   4  23       20.01       12.05     36.55 <

2   4  23     6456.22     5894.79    208.30 o

3   4  23      264.94      221.42    113.69 <

-3   5  23     9622.72     9589.52    325.65 o

-2   5  23    10828.87    10874.25    383.95 o

-1   5  23    11705.41     9942.15    283.44 o

0   5  23    12531.65    12528.61    406.24 o

1   5  23     2686.63     2245.23    105.85 o

2   5  23       52.51       79.64     49.63 <

-1   6  23     1710.19     1503.20     92.65 o

0   6  23     1976.06     2055.84     93.62 o

1   6  23      479.70      618.95     63.74 o

-5   0  24     4216.59     4806.19    333.55 o

-4   0  24     6041.51     6692.30    421.45 o

-3   0  24     2290.66     2496.54    201.70 o

-2   0  24     1493.63     1338.14    137.40 o

-1   0  24      308.82      542.02     56.48 o

-1   0  24      846.39      910.21    116.35 o

0   0  24     2028.70     1762.35     95.94 o

1   0  24      367.05      495.70     95.53 o

1   0  24     1017.04     1182.70     81.79 o

2   0  24     1767.17     1545.73     98.50 o

3   0  24      638.00      773.04    116.81 o

3   0  24      228.81      245.19     92.06 o

4   0  24     2716.70     2136.16    194.30 o

-4   1  24     1286.95     1503.21    116.04 o

-3   1  24     4103.35     3972.87    195.89 o

-2   1  24     6208.31     5224.82    357.26 o

-1   1  24     9790.61     8990.94    291.56 o

0   1  24     5235.27     4807.83    170.56 o

1   1  24     7850.32     7222.65    208.23 o

2   1  24     1412.19     1516.78     68.40 o

3   1  24     8315.65     8872.98    294.45 o

4   1  24      158.02      415.16    116.70 o

-4   2  24      529.97     2183.28    261.84 o

-3   2  24     3712.12     3833.84    146.38 o

-2   2  24      710.29     1660.34    307.93 o

-1   2  24     2136.15     1625.68     96.17 o

0   2  24     1349.84     1590.52    295.51 o

1   2  24     4159.18     3740.31    141.84 o

2   2  24     1336.13     2684.21    356.33 o

3   2  24     1527.91     1250.29     91.58 o

4   2  24      911.55     1634.91    176.03 o

-4   3  24     9981.97     8707.02    410.46 o

-3   3  24     3175.46     3451.72    140.44 o

-2   3  24     6280.99     6308.41    293.89 o

-1   3  24     9898.63     9094.13    299.03 o

0   3  24    10536.36    10171.68    383.88 o

1   3  24     9231.52     8349.93    278.72 o

2   3  24      888.91     1095.13     68.19 o

3   3  24    10993.91    10466.34    422.72 o

-3   4  24      251.47      245.27     50.44 o

-2   4  24      910.48     1363.08     81.58 o

-1   4  24       32.40       28.89     40.53 <

0   4  24      302.35      482.43     51.42 o

1   4  24       13.90       30.44     37.47 <

2   4  24     1459.24     1905.07    218.13 o

3   4  24      301.27      144.30    108.25 <

-2   5  24     1304.09     1251.91     96.62 o

-1   5  24     1167.18     1248.68     81.08 o

0   5  24       20.13       23.46     37.74 <

1   5  24     1037.83     1083.93    161.93 o

2   5  24       59.42       66.88     71.01 <

-1   6  24      993.69      858.42     74.16 o

0   6  24     1615.01     1916.97     99.23 o

-4   1  25      691.05      893.55     94.77 o

-3   1  25     1197.92     1265.72    100.74 o

-2   1  25     1219.29     1308.88     97.37 o

-1   1  25     3931.02     4422.34    157.14 o

0   1  25      801.37     1058.95     63.60 o

1   1  25     7221.36     7457.72    250.46 o

2   1  25     1083.18     1157.67     60.41 o

3   1  25     9852.12    11007.18    356.11 o

4   1  25      470.92      434.44     71.93 o

-4   2  25    16404.32    17104.98    685.11 o

-3   2  25     4300.12     5214.26    264.27 o

-2   2  25    39008.50    38337.59   1169.42 o

-1   2  25     2330.11     2636.35    107.64 o

0   2  25    23703.35    20814.43   1289.34 o

1   2  25    11841.25    10026.51    327.31 o

2   2  25     5108.07     4800.80    173.25 o

3   2  25     1884.49     1620.67    106.48 o

-4   3  25      149.64      859.17     94.54 o

-3   3  25     1918.34     1694.93    143.36 o

-2   3  25        3.73       92.36     41.76 o

-1   3  25     3517.71     4176.65    156.08 o

0   3  25     1456.73     1594.00    102.17 o

1   3  25     2600.74     3093.87    133.49 o

2   3  25       26.56       96.82     37.17 o

3   3  25     1092.39     1225.78     99.58 o

-3   4  25       78.04       98.61     43.38 o

-2   4  25     3786.50     4301.32    166.30 o

-1   4  25       31.66       16.02     32.83 <

0   4  25    11470.66    11051.72    362.23 o

1   4  25      641.67      554.83     57.85 o

2   4  25      690.99      885.27    165.39 o

-2   5  25       25.08      138.79     49.21 o

-1   5  25     1987.28     2023.18    116.15 o

0   5  25       17.52       18.54     42.67 <

1   5  25     8611.66     7386.72    258.81 o

2   5  25      474.12      589.82     79.13 o

-4   0  26     1653.12     2250.89    206.79 o

-3   0  26     1122.57     1202.13    145.26 o

-3   0  26      414.54      371.02     84.66 o

-2   0  26      875.45      634.95    111.26 o

-1   0  26     1165.02     1071.20    120.51 o

-1   0  26      424.89      505.67     58.33 o

0   0  26    33039.21    28920.41   1074.60 o

1   0  26      249.88      247.73     76.56 o

1   0  26      691.92      510.60     60.02 o

2   0  26     6681.34     7102.05    295.71 o

3   0  26     1026.58     1088.78    134.39 o

-4   1  26     2302.34     2018.62    134.63 o

-3   1  26     6587.64     5806.88    263.59 o

-2   1  26      871.11      916.74    124.56 o

-1   1  26     6159.13     6512.54    280.51 o

0   1  26      349.56      344.00     57.96 o

1   1  26     7089.45     8380.11    278.96 o

2   1  26      181.23      142.42     32.69 o

3   1  26     3585.22     3966.99    254.67 o

-4   2  26      690.39     2593.03    279.77 o

-3   2  26     3356.02     3705.13    191.87 o

-2   2  26     1625.42     2251.63    161.39 o

-1   2  26     6068.12     6075.41    209.96 o

0   2  26     2933.53     2819.71    147.54 o

1   2  26     3234.22     3861.03    147.90 o

2   2  26     2049.84     1797.25     88.28 o

3   2  26     1295.07     1147.19    258.03 o

-4   3  26     3065.01     3207.07    221.83 o

-3   3  26     9210.11     9381.07    315.82 o

-2   3  26      802.65      902.21     69.67 o

-1   3  26     6710.54     5723.77    202.19 o

0   3  26      681.74      750.59     61.59 o

1   3  26     4984.95     4616.68    197.51 o

2   3  26      259.64      371.86     49.40 o

3   3  26      961.85      804.88     84.96 o

-3   4  26      105.55      162.13     62.42 o

-2   4  26      736.68      858.51     69.40 o

-1   4  26      245.82      329.59    156.37 o

0   4  26     9284.55     9382.36    328.78 o

1   4  26      813.71     1010.57     94.00 o

2   4  26     5366.50     6058.51    268.82 o

-2   5  26       22.12      -17.32     44.16 <

-1   5  26     3792.58     4281.61    170.12 o

0   5  26      156.99      191.68     50.33 o

1   5  26     6756.39     7743.63    271.76 o

-4   1  27       88.50      262.91     83.39 o

-3   0  28      287.96      195.00     76.33 o

-1   0  28       58.76       68.89     41.90 <

-3   0  30       10.56       65.46     71.01 <

3   0  26      367.91      356.22     94.14 o

-3   1  27     9334.88     9044.19    445.27 o

-2   1  27     1188.24     1038.12     93.33 o

-1   1  27    14413.98    13398.93    534.44 o

0   1  27       96.47       92.02     33.15 o

1   1  27    14437.76    13731.14    438.04 o

2   1  27        8.72       75.46     41.90 <

3   1  27     7024.89     7335.07    312.63 o

-4   2  27     7818.45     8657.27    379.40 o

-3   2  27     2328.02     2291.53    149.03 o

-2   2  27     3464.88     3756.56    165.27 o

-1   2  27     8702.38     7177.49    244.05 o

0   2  27     1452.34     1419.21     79.80 o

1   2  27      265.87      353.81     48.23 o

2   2  27     2071.98     2181.78     99.84 o

3   2  27     1301.20     1482.88    109.40 o

-3   3  27     4107.23     5257.48    312.73 o

-2   3  27       61.53       40.55     42.52 <

-1   3  27     3403.37     3528.27    147.68 o

0   3  27       45.07      119.40     41.57 o

1   3  27     2861.57     2416.27    111.37 o

2   3  27      149.66      148.69     59.29 o

-3   4  27      645.91      624.12    116.74 o

-2   4  27     1616.26     1418.15    135.75 o

-1   4  27     2133.18     1563.33    119.93 o

0   4  27      478.33      549.34     59.37 o

1   4  27     2632.90     1932.25    104.75 o

2   4  27      299.42      949.83     92.81 o

-1   5  27    15878.72    13197.36    435.88 o

0   5  27       39.00       54.86     50.26 <

1   5  27    15498.78    13554.31    442.38 o

-4   0  28     4005.03     3675.54    277.81 o

-3   0  28      782.17     1053.16    145.26 o

-2   0  28    12494.97    12458.90    719.84 o

-1   0  28      161.45      120.05     72.17 <

0   0  28    13893.65    12583.35    706.19 o

1   0  28       27.78       18.47     40.56 <

1   0  28        9.84       55.28     67.08 <

2   0  28    31644.80    31371.27   1173.65 o

3   0  28       79.09       85.59     83.73 <

3   0  28      219.16      394.39    104.78 o

-4   1  28       94.47      170.55     65.54 o

-3   1  28     3873.01     4912.08    463.09 o

-2   1  28       96.23       83.60     54.27 <

-1   1  28     5253.65     7141.13    307.14 o

0   1  28      132.90      165.52     37.87 o

1   1  28     4825.49     5325.07    243.59 o

2   1  28      251.90      338.79     40.93 o

3   1  28     1766.71     1741.93    122.60 o

-3   2  28     1065.12     1211.89    108.93 o

-2   2  28     1873.36     2037.59    119.23 o

-1   2  28      164.75      316.04     43.03 o

0   2  28      832.89     1073.88     71.22 o

1   2  28      110.34      132.90     44.60 o

2   2  28      804.01     1073.34    101.80 o

3   2  28      414.27      334.16    100.50 o

-3   3  28     1177.32     1426.82    367.55 o

-2   3  28      399.54      463.22     59.76 o

-1   3  28     1089.40     1402.04    112.43 o

0   3  28     1485.56     1475.24     87.24 o

1   3  28     4893.71     4599.49    175.76 o

2   3  28     2065.89     2444.55    198.12 o

-2   4  28     8748.49     7942.09    277.80 o

-1   4  28     1027.13      952.83     97.78 o

0   4  28     5617.36     5327.94    198.98 o

1   4  28     1137.89     1218.92     85.91 o

0   5  28     2448.22     2390.23    123.65 o

-3   1  29     9742.06     8368.04    360.42 o

-2   1  29        4.81      -32.08     51.07 <

-1   1  29     8380.30     7441.18    320.42 o

0   1  29       10.33       30.14     34.82 <

1   1  29     3651.68     3947.76    171.08 o

2   1  29      865.00      772.50     55.01 o

3   1  29     1228.28      955.32     93.06 o

-3   2  29     2791.34     2607.93    159.92 o

-2   2  29     2639.10     2577.23    147.60 o

-1   2  29      293.09      211.97     39.73 o

0   2  29      945.61     1303.65     79.45 o

1   2  29      139.67      270.62     50.70 o

2   2  29     5824.48     6367.18    225.11 o

-3   3  29     2602.04     2401.44    253.63 o

-2   3  29      244.10      287.31     51.97 o

-1   3  29     4249.00     4013.51    204.82 o

0   3  29      433.29      500.24     57.67 o

1   3  29     5249.52     5635.90    208.04 o

2   3  29      310.37      452.87     77.55 o

-2   4  29      415.46      993.16     82.95 o

-1   4  29     2727.15     1918.45    135.98 o

0   4  29        8.26      209.61     54.74 o

1   4  29     2330.45     2289.98    118.98 o

-3   0  30       29.05       49.96     81.42 <

-2   0  30    24302.87    26298.26   1438.06 o

-1   0  30      855.05      715.22    113.11 o

-1   0  30      312.60      342.68     58.40 o

0   0  30    17381.78    18436.68   1016.85 o

1   0  30      474.05      519.76     98.31 o

1   0  30     1313.79     1248.27    111.38 o

2   0  30     2758.55     2755.23    147.19 o

-3   1  30     3617.72     4432.13    535.60 o

-2   1  30      434.60      379.23     73.38 o

-1   1  30     4824.25     4800.75    226.77 o

0   1  30     1093.16     1356.34     77.41 o

1   1  30     2949.98     2711.66    163.72 o

2   1  30     3081.18     2664.29    116.05 o

-3   2  30      560.17      603.01     83.72 o

-2   2  30      685.77      928.20     74.09 o

-1   2  30       55.00       55.40     58.42 <

0   2  30      992.79     1308.68     80.30 o

1   2  30      266.77      256.17     51.96 o

2   2  30      211.43      565.53     63.13 o

-2   3  30     2190.37     2615.38    194.90 o

-1   3  30    11053.60     9780.97    416.89 o

0   3  30     9994.68     8187.45    486.28 o

1   3  30    10403.76     8647.66    297.07 o

-1   4  30     1109.78     1302.66    116.20 o

0   4  30     9396.27     8723.38    304.11 o

-3   1  31     1269.43     1482.69    117.78 o

-2   1  31     1336.71     1180.91    103.51 o

-1   1  31     1066.54     1502.40    124.33 o

0   1  31      557.53      651.14     57.96 o

1   1  31     1200.06     1647.99     92.02 o

2   1  31     7327.96     7334.90    255.39 o

-2   2  31     6002.07     5680.96    264.97 o

-1   2  31      486.02      571.74    102.24 o

0   2  31    10858.81    10865.09    717.62 o

1   2  31      293.66      345.17     55.49 o

2   2  31     7091.36     7589.64    328.02 o

-2   3  31      210.52      336.89     59.27 o

-1   3  31     3793.29     4991.85    242.85 o

0   3  31        4.23      117.04     49.91 o

1   3  31     3039.34     3489.79    181.50 o

-3   0  32      556.04      617.60    124.68 o

-3   0  32      207.17      109.18     77.26 <

-2   0  32     3498.79     3506.45    261.84 o

-1   0  32      213.96      347.88     60.90 o

-1   0  32      585.93      496.39    100.62 o

0   0  32     8859.45     9007.50    532.48 o

1   0  32       36.51       99.00     74.71 <

1   0  32      100.61      232.61     56.97 o

2   0  32    10959.48    12200.00    488.79 o

-2   1  32     2874.99     2698.93    188.75 o

-1   1  32     2687.05     2467.39    184.82 o

0   1  32      629.71      666.34     65.03 o

1   1  32     3323.19     3091.00    167.55 o

-2   2  32      287.52      655.05    182.39 o

-1   2  32      226.17      240.68     66.66 o

0   2  32       87.43      351.15     56.97 o

1   2  32     1391.67     1614.68     95.35 o

-1   3  32     7994.00     6582.16    301.45 o

0   3  32        7.42       43.89     54.21 <

-2   1  33     7071.67     7389.55    329.45 o

-1   1  33     2228.08     2723.38    155.65 o

0   1  33     6565.62     6557.34    230.77 o

1   1  33     2250.93     2647.87    121.32 o

-1   2  33     3566.33     3204.59    178.28 o

0   2  33     8546.61     9006.37    307.98 o

-1   0  34      981.89     1044.60    136.47 o

-1   0  34      357.47      633.97     73.96 o

0   0  34     2735.58     3227.26    246.12 o

-1   1  34     2060.46     2401.44    176.38 o

0   1  34      910.93      928.78    121.81 o