data_test2

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'H3 As O9 Zn2'

_chemical_formula_weight          352.68

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'O'  'O'   0.0106   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'H'  'H'   0.0000   0.0000

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Zn'  'Zn'   0.2839   1.4301

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'As'  'As'   0.0499   2.0058

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            ?

_symmetry_space_group_name_H-M    ?

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x, y+1/2, -z+1/2'

'-x, -y, -z'

'x, -y-1/2, z-1/2'

_cell_length_a                    11.793(2)

_cell_length_b                    9.1138(14)

_cell_length_c                    6.8265(10)

_cell_angle_alpha                 90.00

_cell_angle_beta                  103.859(9)

_cell_angle_gamma                 90.00

_cell_volume                      712.35(19)

_cell_formula_units_Z             4

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     ?

_cell_measurement_theta_min       ?

_cell_measurement_theta_max       ?

_exptl_crystal_description        ?

_exptl_crystal_colour             ?

_exptl_crystal_size_max           ?

_exptl_crystal_size_mid           ?

_exptl_crystal_size_min           ?

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     3.289

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              672

_exptl_absorpt_coefficient_mu     11.362

_exptl_absorpt_correction_type    ?

_exptl_absorpt_correction_T_min   ?

_exptl_absorpt_correction_T_max   ?

_exptl_absorpt_process_details    ?

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71073

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type   ?

_diffrn_measurement_method        ?

_diffrn_detector_area_resol_mean  ?

_diffrn_standards_number          ?

_diffrn_standards_interval_count  ?

_diffrn_standards_interval_time   ?

_diffrn_standards_decay_%         ?

_diffrn_reflns_number             3233

_diffrn_reflns_av_R_equivalents   0.0351

_diffrn_reflns_av_sigmaI/netI     0.0478

_diffrn_reflns_limit_h_min        -14

_diffrn_reflns_limit_h_max        12

_diffrn_reflns_limit_k_min        -11

_diffrn_reflns_limit_k_max        9

_diffrn_reflns_limit_l_min        -8

_diffrn_reflns_limit_l_max        8

_diffrn_reflns_theta_min          1.78

_diffrn_reflns_theta_max          26.46

_reflns_number_total              1352

_reflns_number_gt                 1106

_reflns_threshold_expression      >2sigma(I)

_computing_data_collection        ?

_computing_cell_refinement        ?

_computing_data_reduction         ?

_computing_structure_solution     'SHELXS-97 (Sheldrick, 1990)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 1997)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.1108P)^2^+37.8672P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      direct

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     mixed

_refine_ls_extinction_method      SHELXL

_refine_ls_extinction_coef        0.016(2)

_refine_ls_extinction_expression

'Fc^*^=kFc[1+0.001xFc^2^\l^3^/sin(2\q)]^-1/4^'

_refine_ls_number_reflns          1352

_refine_ls_number_parameters      114

_refine_ls_number_restraints      0

_refine_ls_R_factor_all           0.1054

_refine_ls_R_factor_gt            0.0863

_refine_ls_wR_factor_ref          0.2344

_refine_ls_wR_factor_gt           0.2213

_refine_ls_goodness_of_fit_ref    1.106

_refine_ls_restrained_S_all       1.106

_refine_ls_shift/su_max           0.000

_refine_ls_shift/su_mean          0.000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symmetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

As As 0.36080(16) 0.91756(16) 0.0952(2) 0.0189(6) Uani 1 1 d . . .

Zn1 Zn 0.6179(2) 0.0413(2) 0.4016(3) 0.0208(8) Uani 0.958(10) 1 d P . .

Zn2 Zn 0.6059(2) 0.7591(2) 0.1490(3) 0.0235(7) Uani 1 1 d . . .

O1 O 0.4319(11) 0.7571(11) 0.0969(16) 0.017(2) Uani 1 1 d . . .

O2 O 0.7964(10) 0.0882(14) 0.5118(17) 0.030(3) Uani 1 1 d . . .

O3 O 0.2201(11) 0.8861(13) 0.081(2) 0.032(3) Uani 1 1 d . . .

O4 O 0.6690(11) 0.8134(12) 0.4307(15) 0.024(3) Uani 1 1 d . . .

O5 O 0.4267(11) 0.0110(11) 0.3102(15) 0.023(3) Uani 1 1 d . . .

O6 O 0.3725(11) 0.0130(12) -0.1104(15) 0.023(3) Uani 1 1 d . . .

As2 As 0.806(3) 0.777(3) 0.492(4) 0.004(11) Uiso 0.048(8) 1 d P . .

As3 As 0.778(4) 0.686(5) 0.484(6) 0.011(17) Uiso 0.031(8) 1 d P . .

O7 O 0.056(3) 0.987(3) -0.203(6) 0.17(2) Uani 0.96(8) 1 d P . .

O8 O 0.913(4) 0.769(4) 0.585(8) 0.18(3) Uani 0.91(9) 1 d P . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

As 0.0380(13) 0.0106(8) 0.0089(8) -0.0008(5) 0.0073(7) 0.0004(6)

Zn1 0.0387(16) 0.0120(10) 0.0129(10) -0.0005(6) 0.0083(9) 0.0015(8)

Zn2 0.0398(15) 0.0198(10) 0.0124(9) -0.0051(6) 0.0093(9) -0.0003(8)

O1 0.020(7) 0.015(5) 0.017(5) 0.001(4) 0.006(5) 0.004(4)

O2 0.009(7) 0.045(8) 0.030(6) 0.027(5) -0.003(5) -0.002(5)

O3 0.022(7) 0.020(6) 0.054(8) -0.017(5) 0.011(6) -0.002(5)

O4 0.048(8) 0.011(5) 0.016(5) 0.006(4) 0.011(5) -0.002(5)

O5 0.048(8) 0.012(5) 0.010(4) -0.002(4) 0.007(5) 0.000(5)

O6 0.038(8) 0.023(6) 0.007(4) 0.004(4) 0.006(5) -0.002(5)

O7 0.10(3) 0.11(3) 0.24(4) -0.03(3) -0.08(2) 0.035(18)

O8 0.11(3) 0.13(4) 0.25(6) 0.00(3) -0.05(3) -0.04(2)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

As O3 1.664(13) . ?

As O6 1.684(10) 1_565 ?

As O1 1.684(10) . ?

As O5 1.714(10) 1_565 ?

As As3 2.92(5) 2_655 ?

As O2 3.512(12) 2_655 ?

As O2 3.609(12) 3_666 ?

As O4 3.625(11) 2_655 ?

Zn1 O1 2.053(10) 2_645 ?

Zn1 O6 2.078(10) 3_655 ?

Zn1 O2 2.103(12) . ?

Zn1 O4 2.159(11) 1_545 ?

Zn1 O5 2.207(10) 3_656 ?

Zn1 O5 2.209(13) . ?

Zn1 Zn2 3.081(2) 1_545 ?

Zn2 O4 1.934(10) 4_575 ?

Zn2 O4 1.952(11) . ?

Zn2 O1 1.997(12) . ?

Zn2 O6 2.117(11) 3_665 ?

Zn2 O5 2.322(10) 2_655 ?

Zn2 As3 2.60(5) 4_575 ?

Zn2 As3 2.75(5) . ?

Zn2 As2 2.83(3) 4_575 ?

Zn2 As2 2.90(3) . ?

Zn2 Zn1 3.081(2) 1_565 ?

O1 Zn1 2.053(10) 2_655 ?

O1 O2 3.035(17) 2_655 ?

O2 O3 2.784(17) 2_645 ?

O2 O3 2.845(18) 3_666 ?

O2 As2 2.85(3) 1_545 ?

O2 O4 2.905(17) 1_545 ?

O2 O1 3.035(16) 2_645 ?

O2 O7 3.12(5) 3_665 ?

O2 O6 3.117(16) 3_655 ?

O2 As 3.512(12) 2_645 ?

O2 As 3.609(12) 3_666 ?

O2 As3 3.68(5) 1_545 ?

O3 O2 2.784(17) 2_655 ?

O3 O2 2.845(18) 3_666 ?

O4 As2 1.60(3) . ?

O4 As3 1.71(5) . ?

O4 Zn2 1.934(10) 4_576 ?

O4 Zn1 2.159(11) 1_565 ?

O4 O6 2.648(14) 3_665 ?

O4 O5 2.814(15) 3_666 ?

O4 O8 2.84(4) . ?

O4 O2 2.905(17) 1_565 ?

O4 O6 3.086(15) 2_655 ?

O4 As3 3.59(4) 4_575 ?

O4 O4 3.603(7) 4_575 ?

O5 As 1.714(10) 1_545 ?

O5 Zn1 2.207(10) 3_656 ?

O5 Zn2 2.322(10) 2_645 ?

O5 O4 2.814(15) 3_666 ?

O6 As 1.684(10) 1_545 ?

O6 Zn1 2.078(10) 3_655 ?

O6 Zn2 2.117(11) 3_665 ?

O6 O4 2.648(14) 3_665 ?

O6 O4 3.086(15) 2_645 ?

O6 O2 3.117(16) 3_655 ?

As2 As3 0.89(5) . ?

As2 O8 1.27(5) . ?

As2 Zn2 2.83(3) 4_576 ?

As2 O2 2.85(3) 1_565 ?

As3 O8 1.75(6) . ?

As3 Zn2 2.60(5) 4_576 ?

As3 As 2.92(5) 2_645 ?

As3 O4 3.59(4) 4_576 ?

As3 O2 3.68(5) 1_565 ?

As3 O4 3.68(4) 4_575 ?

O7 O2 3.12(5) 3_665 ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

O3 As O6 108.6(6) . 1_565 ?

O3 As O1 109.8(6) . . ?

O6 As O1 108.3(5) 1_565 . ?

O3 As O5 112.2(6) . 1_565 ?

O6 As O5 110.3(5) 1_565 1_565 ?

O1 As O5 107.6(6) . 1_565 ?

O3 As As3 68.0(10) . 2_655 ?

O6 As As3 64.4(9) 1_565 2_655 ?

O1 As As3 169.9(9) . 2_655 ?

O5 As As3 82.0(10) 1_565 2_655 ?

O3 As O2 51.0(4) . 2_655 ?

O6 As O2 114.4(4) 1_565 2_655 ?

O1 As O2 59.8(4) . 2_655 ?

O5 As O2 135.3(4) 1_565 2_655 ?

As3 As O2 115.6(10) 2_655 2_655 ?

O3 As O2 50.1(5) . 3_666 ?

O6 As O2 141.8(4) 1_565 3_666 ?

O1 As O2 109.0(4) . 3_666 ?

O5 As O2 65.1(4) 1_565 3_666 ?

As3 As O2 77.5(9) 2_655 3_666 ?

O2 As O2 78.6(3) 2_655 3_666 ?

O3 As O4 94.9(4) . 2_655 ?

O6 As O4 58.1(4) 1_565 2_655 ?

O1 As O4 155.1(5) . 2_655 ?

O5 As O4 64.3(4) 1_565 2_655 ?

As3 As O4 27.7(10) 2_655 2_655 ?

O2 As O4 143.2(3) 2_655 2_655 ?

O2 As O4 89.4(3) 3_666 2_655 ?

O1 Zn1 O6 108.3(4) 2_645 3_655 ?

O1 Zn1 O2 93.8(5) 2_645 . ?

O6 Zn1 O2 96.4(5) 3_655 . ?

O1 Zn1 O4 174.3(4) 2_645 1_545 ?

O6 Zn1 O4 77.3(4) 3_655 1_545 ?

O2 Zn1 O4 85.9(5) . 1_545 ?

O1 Zn1 O5 94.2(4) 2_645 3_656 ?

O6 Zn1 O5 151.7(4) 3_655 3_656 ?

O2 Zn1 O5 99.0(5) . 3_656 ?

O4 Zn1 O5 80.3(4) 1_545 3_656 ?

O1 Zn1 O5 81.2(4) 2_645 . ?

O6 Zn1 O5 89.2(4) 3_655 . ?

O2 Zn1 O5 173.5(5) . . ?

O4 Zn1 O5 98.6(4) 1_545 . ?

O5 Zn1 O5 77.3(4) 3_656 . ?

O1 Zn1 Zn2 145.8(3) 2_645 1_545 ?

O6 Zn1 Zn2 43.2(3) 3_655 1_545 ?

O2 Zn1 Zn2 106.1(4) . 1_545 ?

O4 Zn1 Zn2 39.0(3) 1_545 1_545 ?

O5 Zn1 Zn2 109.3(3) 3_656 1_545 ?

O5 Zn1 Zn2 80.2(3) . 1_545 ?

O4 Zn2 O4 136.0(7) 4_575 . ?

O4 Zn2 O1 115.3(5) 4_575 . ?

O4 Zn2 O1 108.1(5) . . ?

O4 Zn2 O6 99.2(4) 4_575 3_665 ?

O4 Zn2 O6 81.1(4) . 3_665 ?

O1 Zn2 O6 97.8(4) . 3_665 ?

O4 Zn2 O5 82.2(4) 4_575 2_655 ?

O4 Zn2 O5 99.4(4) . 2_655 ?

O1 Zn2 O5 79.6(4) . 2_655 ?

O6 Zn2 O5 177.4(5) 3_665 2_655 ?

O4 Zn2 As3 41.1(11) 4_575 4_575 ?

O4 Zn2 As3 103.1(11) . 4_575 ?

O1 Zn2 As3 143.2(11) . 4_575 ?

O6 Zn2 As3 68.0(11) 3_665 4_575 ?

O5 Zn2 As3 114.2(11) 2_655 4_575 ?

O4 Zn2 As3 102.3(10) 4_575 . ?

O4 Zn2 As3 38.0(10) . . ?

O1 Zn2 As3 132.0(10) . . ?

O6 Zn2 As3 104.8(11) 3_665 . ?

O5 Zn2 As3 76.9(11) 2_655 . ?

As3 Zn2 As3 84.8(15) 4_575 . ?

O4 Zn2 As2 33.0(7) 4_575 4_575 ?

O4 Zn2 As2 104.2(7) . 4_575 ?

O1 Zn2 As2 147.6(6) . 4_575 ?

O6 Zn2 As2 86.0(6) 3_665 4_575 ?

O5 Zn2 As2 96.3(6) 2_655 4_575 ?

As3 Zn2 As2 18.1(11) 4_575 4_575 ?

As3 Zn2 As2 76.7(11) . 4_575 ?

O4 Zn2 As2 104.6(6) 4_575 . ?

O4 Zn2 As2 31.5(6) . . ?

O1 Zn2 As2 138.2(6) . . ?

O6 Zn2 As2 87.0(6) 3_665 . ?

O5 Zn2 As2 94.7(6) 2_655 . ?

As3 Zn2 As2 76.8(11) 4_575 . ?

As3 Zn2 As2 17.8(10) . . ?

As2 Zn2 As2 73.9(7) 4_575 . ?

O4 Zn2 Zn1 137.9(3) 4_575 1_565 ?

O4 Zn2 Zn1 44.1(3) . 1_565 ?

O1 Zn2 Zn1 90.9(3) . 1_565 ?

O6 Zn2 Zn1 42.3(3) 3_665 1_565 ?

O5 Zn2 Zn1 137.1(3) 2_655 1_565 ?

As3 Zn2 Zn1 98.4(10) 4_575 1_565 ?

As3 Zn2 Zn1 79.2(10) . 1_565 ?

As2 Zn2 Zn1 112.1(5) 4_575 1_565 ?

As2 Zn2 Zn1 65.4(5) . 1_565 ?

As O1 Zn2 118.8(6) . . ?

As O1 Zn1 133.6(7) . 2_655 ?

Zn2 O1 Zn1 106.9(5) . 2_655 ?

As O1 O2 91.6(5) . 2_655 ?

Zn2 O1 O2 149.5(5) . 2_655 ?

Zn1 O1 O2 43.7(3) 2_655 2_655 ?

Zn1 O2 O3 96.2(5) . 2_645 ?

Zn1 O2 O3 94.0(5) . 3_666 ?

O3 O2 O3 97.1(5) 2_645 3_666 ?

Zn1 O2 As2 80.1(7) . 1_545 ?

O3 O2 As2 164.5(8) 2_645 1_545 ?

O3 O2 As2 98.1(6) 3_666 1_545 ?

Zn1 O2 O4 47.8(4) . 1_545 ?

O3 O2 O4 142.5(6) 2_645 1_545 ?

O3 O2 O4 96.0(4) 3_666 1_545 ?

As2 O2 O4 32.4(7) 1_545 1_545 ?

Zn1 O2 O1 42.4(3) . 2_645 ?

O3 O2 O1 56.0(4) 2_645 2_645 ?

O3 O2 O1 86.1(5) 3_666 2_645 ?

As2 O2 O1 122.5(8) 1_545 2_645 ?

O4 O2 O1 90.1(4) 1_545 2_645 ?

Zn1 O2 O7 112.8(7) . 3_665 ?

O3 O2 O7 94.7(7) 2_645 3_665 ?

O3 O2 O7 149.3(7) 3_666 3_665 ?

As2 O2 O7 73.3(9) 1_545 3_665 ?

O4 O2 O7 91.6(7) 1_545 3_665 ?

O1 O2 O7 123.6(7) 2_645 3_665 ?

Zn1 O2 O6 41.5(3) . 3_655 ?

O3 O2 O6 95.4(5) 2_645 3_655 ?

O3 O2 O6 134.8(5) 3_666 3_655 ?

As2 O2 O6 71.8(7) 1_545 3_655 ?

O4 O2 O6 52.0(4) 1_545 3_655 ?

O1 O2 O6 65.9(4) 2_645 3_655 ?

O7 O2 O6 71.5(6) 3_665 3_655 ?

Zn1 O2 As 70.5(3) . 2_645 ?

O3 O2 As 27.7(3) 2_645 2_645 ?

O3 O2 As 88.7(4) 3_666 2_645 ?

As2 O2 As 150.2(8) 1_545 2_645 ?

O4 O2 As 118.3(4) 1_545 2_645 ?

O1 O2 As 28.6(2) 2_645 2_645 ?

O7 O2 As 113.6(7) 3_665 2_645 ?

O6 O2 As 82.9(3) 3_655 2_645 ?

Zn1 O2 As 67.3(3) . 3_666 ?

O3 O2 As 99.3(5) 2_645 3_666 ?

O3 O2 As 26.7(3) 3_666 3_666 ?

As2 O2 As 93.1(6) 1_545 3_666 ?

O4 O2 As 78.2(3) 1_545 3_666 ?

O1 O2 As 66.8(3) 2_645 3_666 ?

O7 O2 As 165.9(7) 3_665 3_666 ?

O6 O2 As 108.4(4) 3_655 3_666 ?

As O2 As 80.1(3) 2_645 3_666 ?

Zn1 O2 As3 74.8(9) . 1_545 ?

O3 O2 As3 164.0(9) 2_645 1_545 ?

O3 O2 As3 96.7(7) 3_666 1_545 ?

As2 O2 As3 5.6(10) 1_545 1_545 ?

O4 O2 As3 27.0(8) 1_545 1_545 ?

O1 O2 As3 117.1(9) 2_645 1_545 ?

O7 O2 As3 77.3(10) 3_665 1_545 ?

O6 O2 As3 69.0(8) 3_655 1_545 ?

As O2 As3 145.1(8) 2_645 1_545 ?

As O2 As3 89.4(7) 3_666 1_545 ?

As O3 O2 101.3(5) . 2_655 ?

As O3 O2 103.2(6) . 3_666 ?

O2 O3 O2 106.5(5) 2_655 3_666 ?

As2 O4 As3 30.9(18) . . ?

As2 O4 Zn2 106.0(10) . 4_576 ?

As3 O4 Zn2 90.8(15) . 4_576 ?

As2 O4 Zn2 109.1(10) . . ?

As3 O4 Zn2 97.2(15) . . ?

Zn2 O4 Zn2 123.1(6) 4_576 . ?

As2 O4 Zn1 117.8(11) . 1_565 ?

As3 O4 Zn1 148.7(18) . 1_565 ?

Zn2 O4 Zn1 104.4(5) 4_576 1_565 ?

Zn2 O4 Zn1 97.0(4) . 1_565 ?

As2 O4 O6 108.4(10) . 3_665 ?

As3 O4 O6 124.2(15) . 3_665 ?

Zn2 O4 O6 144.2(7) 4_576 3_665 ?

Zn2 O4 O6 52.2(3) . 3_665 ?

Zn1 O4 O6 50.0(3) 1_565 3_665 ?

As2 O4 O5 119.0(11) . 3_666 ?

As3 O4 O5 130.5(15) . 3_666 ?

Zn2 O4 O5 54.8(3) 4_576 3_666 ?

Zn2 O4 O5 130.4(6) . 3_666 ?

Zn1 O4 O5 50.6(3) 1_565 3_666 ?

O6 O4 O5 99.0(5) 3_665 3_666 ?

As2 O4 O8 7.2(14) . . ?

As3 O4 O8 35.0(19) . . ?

Zn2 O4 O8 102.0(12) 4_576 . ?

Zn2 O4 O8 116.2(12) . . ?

Zn1 O4 O8 113.9(9) 1_565 . ?

O6 O4 O8 111.1(11) 3_665 . ?

O5 O4 O8 111.8(12) 3_666 . ?

As2 O4 O2 71.8(11) . 1_565 ?

As3 O4 O2 102.6(18) . 1_565 ?

Zn2 O4 O2 115.1(5) 4_576 1_565 ?

Zn2 O4 O2 117.6(5) . 1_565 ?

Zn1 O4 O2 46.2(3) 1_565 1_565 ?

O6 O4 O2 68.1(4) 3_665 1_565 ?

O5 O4 O2 69.9(4) 3_666 1_565 ?

O8 O4 O2 67.7(8) . 1_565 ?

As2 O4 O6 87.5(10) . 2_655 ?

As3 O4 O6 59.7(16) . 2_655 ?

Zn2 O4 O6 42.6(3) 4_576 2_655 ?

Zn2 O4 O6 96.2(4) . 2_655 ?

Zn1 O4 O6 145.4(5) 1_565 2_655 ?

O6 O4 O6 147.4(6) 3_665 2_655 ?

O5 O4 O6 97.4(4) 3_666 2_655 ?

O8 O4 O6 88.3(9) . 2_655 ?

O2 O4 O6 144.4(5) 1_565 2_655 ?

As2 O4 As3 71.3(12) . 4_575 ?

As3 O4 As3 77.0(17) . 4_575 ?

Zn2 O4 As3 159.9(9) 4_576 4_575 ?

Zn2 O4 As3 44.9(8) . 4_575 ?

Zn1 O4 As3 93.9(9) 1_565 4_575 ?

O6 O4 As3 47.8(8) 3_665 4_575 ?

O5 O4 As3 144.4(9) 3_666 4_575 ?

O8 O4 As3 77.1(14) . 4_575 ?

O2 O4 As3 83.4(9) 1_565 4_575 ?

O6 O4 As3 117.6(9) 2_655 4_575 ?

As2 O4 O4 87.3(9) . 4_575 ?

As3 O4 O4 79.1(15) . 4_575 ?

Zn2 O4 O4 135.0(6) 4_576 4_575 ?

Zn2 O4 O4 21.9(4) . 4_575 ?

Zn1 O4 O4 106.5(4) 1_565 4_575 ?

O6 O4 O4 56.7(3) 3_665 4_575 ?

O5 O4 O4 150.3(4) 3_666 4_575 ?

O8 O4 O4 94.3(11) . 4_575 ?

O2 O4 O4 109.8(4) 1_565 4_575 ?

O6 O4 O4 97.4(5) 2_655 4_575 ?

As3 O4 O4 27.5(8) 4_575 4_575 ?

As O5 Zn1 120.0(6) 1_545 3_656 ?

As O5 Zn1 121.8(6) 1_545 . ?

Zn1 O5 Zn1 102.7(4) 3_656 . ?

As O5 Zn2 122.2(6) 1_545 2_645 ?

Zn1 O5 Zn2 91.3(4) 3_656 2_645 ?

Zn1 O5 Zn2 91.8(4) . 2_645 ?

As O5 O4 130.8(7) 1_545 3_666 ?

Zn1 O5 O4 49.1(3) 3_656 3_666 ?

Zn1 O5 O4 106.7(5) . 3_666 ?

Zn2 O5 O4 42.9(3) 2_645 3_666 ?

As O6 Zn1 135.1(6) 1_545 3_655 ?

As O6 Zn2 130.3(6) 1_545 3_665 ?

Zn1 O6 Zn2 94.5(4) 3_655 3_665 ?

As O6 O4 163.9(7) 1_545 3_665 ?

Zn1 O6 O4 52.7(3) 3_655 3_665 ?

Zn2 O6 O4 46.7(3) 3_665 3_665 ?

As O6 O4 94.3(5) 1_545 2_645 ?

Zn1 O6 O4 129.9(5) 3_655 2_645 ?

Zn2 O6 O4 38.2(3) 3_665 2_645 ?

O4 O6 O4 77.4(3) 3_665 2_645 ?

As O6 O2 114.6(6) 1_545 3_655 ?

Zn1 O6 O2 42.1(3) 3_655 3_655 ?

Zn2 O6 O2 104.6(4) 3_665 3_655 ?

O4 O6 O2 59.9(4) 3_665 3_655 ?

O4 O6 O2 118.9(5) 2_645 3_655 ?

As3 As2 O8 107(4) . . ?

As3 As2 O4 81(4) . . ?

O8 As2 O4 164(3) . . ?

As3 As2 Zn2 66(3) . 4_576 ?

O8 As2 Zn2 129(3) . 4_576 ?

O4 As2 Zn2 41.0(7) . 4_576 ?

As3 As2 O2 156(4) . 1_565 ?

O8 As2 O2 94(2) . 1_565 ?

O4 As2 O2 75.8(10) . 1_565 ?

Zn2 As2 O2 92.9(8) 4_576 1_565 ?

As3 As2 Zn2 71(3) . . ?

O8 As2 Zn2 156(3) . . ?

O4 As2 Zn2 39.4(7) . . ?

Zn2 As2 Zn2 73.1(7) 4_576 . ?

O2 As2 Zn2 93.4(8) 1_565 . ?

As2 As3 O4 68(4) . . ?

As2 As3 O8 44(3) . . ?

O4 As3 O8 111(3) . . ?

As2 As3 Zn2 96(4) . 4_576 ?

O4 As3 Zn2 48.1(12) . 4_576 ?

O8 As3 Zn2 118(3) . 4_576 ?

As2 As3 Zn2 91(4) . . ?

O4 As3 Zn2 44.8(11) . . ?

O8 As3 Zn2 130(3) . . ?

Zn2 As3 Zn2 79.4(13) 4_576 . ?

As2 As3 As 167(4) . 2_645 ?

O4 As3 As 100(2) . 2_645 ?

O8 As3 As 149(3) . 2_645 ?

Zn2 As3 As 77.3(13) 4_576 2_645 ?

Zn2 As3 As 77.3(12) . 2_645 ?

As2 As3 O4 98(3) . 4_576 ?

O4 As3 O4 76.8(15) . 4_576 ?

O8 As3 O4 98(2) . 4_576 ?

Zn2 As3 O4 32.0(5) 4_576 4_576 ?

Zn2 As3 O4 111.2(15) . 4_576 ?

As As3 O4 81.9(11) 2_645 4_576 ?

As2 As3 O2 18(3) . 1_565 ?

O4 As3 O2 50.5(14) . 1_565 ?

O8 As3 O2 61(2) . 1_565 ?

Zn2 As3 O2 80.0(12) 4_576 1_565 ?

Zn2 As3 O2 79.8(11) . 1_565 ?

As As3 O2 150.3(17) 2_645 1_565 ?

O4 As3 O2 89.0(10) 4_576 1_565 ?

As2 As3 O4 96(3) . 4_575 ?

O4 As3 O4 73.8(15) . 4_575 ?

O8 As3 O4 118(3) . 4_575 ?

Zn2 As3 O4 109.1(15) 4_576 4_575 ?

Zn2 As3 O4 30.9(5) . 4_575 ?

As As3 O4 76.7(10) 2_645 4_575 ?

O4 As3 O4 139.8(15) 4_576 4_575 ?

O2 As3 O4 93.1(11) 1_565 4_575 ?

As2 O8 As3 29(2) . . ?

As2 O8 O4 9.2(18) . . ?

As3 O8 O4 34.1(18) . . ?

_diffrn_measured_fraction_theta_max    0.916

_diffrn_reflns_theta_full              26.46

_diffrn_measured_fraction_theta_full   0.916

_refine_diff_density_max    4.008

_refine_diff_density_min   -1.706

_refine_diff_density_rms    0.491