data_anorp

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'As2 S3'

_chemical_formula_weight          246.02

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'As'  'As'   0.0499   2.0058

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'S'  'S'   0.1246   0.1234

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            ?

_symmetry_space_group_name_H-M    ?

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x, -y, -z'

_cell_length_a                    5.75767(16)

_cell_length_b                    8.7169(3)

_cell_length_c                    10.2682(7)

_cell_angle_alpha                 78.152(7)

_cell_angle_beta                  75.817(7)

_cell_angle_gamma                 89.861(6)

_cell_volume                      488.37(4)

_cell_formula_units_Z             4

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     ?

_cell_measurement_theta_min       ?

_cell_measurement_theta_max       ?

_exptl_crystal_description        ?

_exptl_crystal_colour             ?

_exptl_crystal_size_max           0.07

_exptl_crystal_size_mid           0.06

_exptl_crystal_size_min           0.04

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     3.346

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              456

_exptl_absorpt_coefficient_mu     14.772

_exptl_absorpt_correction_type    ?

_exptl_absorpt_correction_T_min   0.4469

_exptl_absorpt_correction_T_max   0.6259

_exptl_absorpt_process_details    ?

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71075

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type   ?

_diffrn_measurement_method        ?

_diffrn_detector_area_resol_mean  ?

_diffrn_standards_number          ?

_diffrn_standards_interval_count  ?

_diffrn_standards_interval_time   ?

_diffrn_standards_decay_%         ?

_diffrn_reflns_number             12228

_diffrn_reflns_av_R_equivalents   0.0394

_diffrn_reflns_av_sigmaI/netI     0.0227

_diffrn_reflns_limit_h_min        -6

_diffrn_reflns_limit_h_max        6

_diffrn_reflns_limit_k_min        -10

_diffrn_reflns_limit_k_max        10

_diffrn_reflns_limit_l_min        -12

_diffrn_reflns_limit_l_max        12

_diffrn_reflns_theta_min          3.65

_diffrn_reflns_theta_max          25.02

_reflns_number_total              1710

_reflns_number_gt                 1484

_reflns_threshold_expression      >2sigma(I)

_computing_data_collection        ?

_computing_cell_refinement        ?

_computing_data_reduction         ?

_computing_structure_solution     'SHELXS-97 (Sheldrick, 1990)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 1997)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.0242P)^2^+0.2186P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      direct

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     mixed

_refine_ls_extinction_method      none

_refine_ls_extinction_coef        ?

_refine_ls_number_reflns          1710

_refine_ls_number_parameters      91

_refine_ls_number_restraints      0

_refine_ls_R_factor_all           0.0251

_refine_ls_R_factor_gt            0.0208

_refine_ls_wR_factor_ref          0.0507

_refine_ls_wR_factor_gt           0.0492

_refine_ls_goodness_of_fit_ref    1.064

_refine_ls_restrained_S_all       1.064

_refine_ls_shift/su_max           0.001

_refine_ls_shift/su_mean          0.000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symmetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

As1 As 0.39108(7) 0.36238(4) 0.67225(4) 0.02442(11) Uani 1 1 d . . .

As2 As 0.81064(7) 0.17527(4) 0.83715(4) 0.02433(11) Uani 1 1 d . . .

As3 As 0.37392(7) 0.67873(4) 0.83354(4) 0.02455(11) Uani 1 1 d . . .

As4 As 0.93519(6) 0.86377(4) 0.66860(4) 0.02401(11) Uani 1 1 d . . .

S1 S 0.90075(18) 0.92003(11) 0.87870(10) 0.0284(2) Uani 1 1 d . . .

S2 S 0.49936(17) 0.11754(11) 0.75544(11) 0.0304(2) Uani 1 1 d . . .

S3 S 0.75475(17) 0.61916(11) 0.74806(11) 0.0300(2) Uani 1 1 d . . .

S4 S 0.05571(17) 0.27458(11) 0.62594(10) 0.0271(2) Uani 1 1 d . . .

S5 S 0.31075(16) 0.77483(11) 0.62295(10) 0.0275(2) Uani 1 1 d . . .

S6 S 0.24319(18) 0.42417(11) 0.88062(10) 0.0290(2) Uani 1 1 d . . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

As1 0.0243(2) 0.0206(2) 0.0277(2) -0.00577(17) -0.00473(16) -0.00155(15)

As2 0.0265(2) 0.0212(2) 0.0283(2) -0.01095(17) -0.00749(17) 0.00289(15)

As3 0.0268(2) 0.0210(2) 0.0286(2) -0.01117(17) -0.00738(16) 0.00398(15)

As4 0.0267(2) 0.0201(2) 0.0271(2) -0.00593(17) -0.00934(17) 0.00446(15)

S1 0.0382(6) 0.0220(5) 0.0268(5) -0.0060(4) -0.0107(4) 0.0064(4)

S2 0.0245(5) 0.0219(5) 0.0492(7) -0.0124(5) -0.0131(5) 0.0035(4)

S3 0.0239(5) 0.0211(5) 0.0484(7) -0.0133(5) -0.0105(4) 0.0032(4)

S4 0.0284(5) 0.0279(5) 0.0273(5) -0.0070(4) -0.0102(4) 0.0003(4)

S5 0.0245(5) 0.0290(5) 0.0283(5) -0.0065(4) -0.0047(4) 0.0037(4)

S6 0.0358(5) 0.0232(5) 0.0264(5) -0.0058(4) -0.0044(4) -0.0036(4)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

As1 S4 2.2687(10) . ?

As1 S6 2.2741(10) . ?

As1 S2 2.2757(10) . ?

As2 S2 2.2548(10) . ?

As2 S1 2.2615(10) 1_545 ?

As2 S4 2.2758(11) 1_655 ?

As3 S3 2.2553(10) . ?

As3 S6 2.2612(10) . ?

As3 S5 2.2694(11) . ?

As4 S5 2.2674(10) 1_655 ?

As4 S1 2.2712(11) . ?

As4 S3 2.2743(10) . ?

S1 As2 2.2615(10) 1_565 ?

S4 As2 2.2758(11) 1_455 ?

S5 As4 2.2674(10) 1_455 ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

S4 As1 S6 102.18(4) . . ?

S4 As1 S2 94.11(4) . . ?

S6 As1 S2 96.01(4) . . ?

S2 As2 S1 91.28(4) . 1_545 ?

S2 As2 S4 94.62(4) . 1_655 ?

S1 As2 S4 103.34(4) 1_545 1_655 ?

S3 As3 S6 91.84(4) . . ?

S3 As3 S5 93.74(4) . . ?

S6 As3 S5 103.59(4) . . ?

S5 As4 S1 101.68(4) 1_655 . ?

S5 As4 S3 93.98(4) 1_655 . ?

S1 As4 S3 95.90(4) . . ?

As2 S1 As4 100.78(4) 1_565 . ?

As2 S2 As1 100.96(4) . . ?

As3 S3 As4 100.54(4) . . ?

As1 S4 As2 103.95(4) . 1_455 ?

As4 S5 As3 104.15(4) 1_455 . ?

As3 S6 As1 100.45(4) . . ?

_diffrn_measured_fraction_theta_max    0.994

_diffrn_reflns_theta_full              25.02

_diffrn_measured_fraction_theta_full   0.994

_refine_diff_density_max    0.559

_refine_diff_density_min   -0.344

_refine_diff_density_rms    0.107