Supplementary data to the article:

Tab. A1 : Masses of salt used for the preparation of 5L of buffer solutions.

| Input solution | Expected pH | Na2B4O7 (g) | NaOH (g) | KCl (g) |
| --- | --- | --- | --- | --- |
| A | 9.2 | 79.182 | -- | -- |
| B | 10 | 47.669 | 6.597 | -- |
| C | 11 | 39.468 | 8.377 | -- |
| D | 12 | -- | 2.433 | 18.627 |
| E | 13 | -- | 24.055 | 18.626 |

Tab. A2 : Evolution of fluid chemistry, flow rate and saturation index (SI) for the AFm-Cl-9.2 experiment. An initial mass of 1.2340 g has been added into the flow-through reactor whereas 0.9168 g has been retrieved after dissolution experiment.

| Time (h) | Sampled mass (g) | Flow rate (mL min-1) | pH (in) | pH (out) | Al (in) (mol L-1) | Al (out) (mol L-1) | Ca (in) (mol L-1) | Ca (out) (mol L-1) | Cl (in) (mol L-1) | Cl (out) (mol L-1) | Estimated mass from Al (g) | Estimated mass from Ca (g) | BET surface area (m2 g-1) | SI C4AH13 | SI Friedel_Salt | SI Gibbsite | SI Gibbsite(am) | SI Portlandite |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.4 | 27.3 | 0.556 | 9.18 | 9.24 | 9.07E-05 | 4.95E-04 | 0.0 | 1.76E-03 | 0.0 | 1.82E-03 | 1.2311 | 1.2277 | 9.4 | -20.67 | -15.97 | 2.56 | -0.28 | -7.21 |
| 1.1 | 18.8 | 0.499 | 9.18 | 9.23 | 9.07E-05 | 5.64E-04 | 0.0 | 1.79E-03 | 0.0 | 1.88E-03 | 1.2287 | 1.2232 | 9.4 | -20.60 | -15.85 | 2.62 | -0.22 | -7.22 |
| 1.9 | 28.1 | 0.483 | 9.18 | 9.25 | 9.07E-05 | 5.55E-04 | 0.0 | 1.75E-03 | 0.0 | 1.81E-03 | 1.2253 | 1.2167 | 9.4 | -20.52 | -15.85 | 2.60 | -0.24 | -7.19 |
| 2.9 | 28.1 | 0.501 | 9.18 | 9.25 | 9.07E-05 | 5.50E-04 | 0.0 | 1.89E-03 | 0.0 | 1.87E-03 | 1.2219 | 1.2096 | 9.4 | -20.41 | -15.71 | 2.59 | -0.25 | -7.16 |
| 3.9 | 32.4 | 0.499 | 9.18 | 9.15 | 9.07E-05 | 6.06E-04 | 0.0 | 2.04E-03 | 0.0 | 1.89E-03 | 1.2174 | 1.2009 | 9.4 | -20.81 | -15.91 | 2.73 | -0.11 | -7.33 |
| 4.9 | 30.5 | 0.500 | 9.18 | 9.21 | 9.07E-05 | 6.24E-04 | 0.0 | 2.04E-03 | 0.0 | 1.82E-03 | 1.2131 | 1.1927 | 9.4 | -20.43 | -15.67 | 2.68 | -0.16 | -7.21 |
| 14.3 | 519.4 | 0.491 | 9.18 | 9.18 | 9.07E-05 | 5.51E-04 | 0.0 | 1.80E-03 | 0.0 | 1.31E-03 | 1.1499 | 1.0690 | 9.4 | -20.89 | -16.36 | 2.66 | -0.18 | -7.32 |
| 23.6 | 27.7 | 0.468 | 9.18 | 9.19 | 9.07E-05 | 4.78E-04 | 0.0 | 1.33E-03 | 0.0 | 8.63E-04 | 1.1471 | 1.0641 | 9.4 | -21.41 | -17.25 | 2.60 | -0.25 | -7.41 |
| 24.6 | 30.5 | 0.490 | 9.18 | 9.27 | 9.07E-05 | 4.49E-04 | 0.0 | 1.23E-03 | 0.0 | 7.67E-04 | 1.1442 | 1.0592 | 9.4 | -21.10 | -17.20 | 2.49 | -0.35 | -7.28 |
| 25.6 | 32.6 | 0.490 | 9.18 | 9.32 | 9.07E-05 | 4.03E-04 | 0.0 | 1.13E-03 | 0.0 | 6.80E-04 | 1.1415 | 1.0543 | 9.4 | -21.03 | -17.33 | 2.39 | -0.45 | -7.22 |
| 26.7 | 31.8 | 0.491 | 9.18 | 9.31 | 9.07E-05 | 3.94E-04 | 0.0 | 9.91E-04 | 0.0 | 6.32E-04 | 1.1389 | 1.0501 | 9.4 | -21.31 | -17.66 | 2.40 | -0.45 | -7.29 |

Grey data have been selected for the calculation of dissolution rate.

Tab. A3 : Evolution of fluid chemistry, flow rate and saturation index (SI) for the AFm-Cl-10 experiment. An initial mass of 1.1577 g has been added into the flow-through reactor whereas 0.2431 g has been retrieved after dissolution experiment.

| Time (h) | Sampled mass (g) | Flow rate (mL min-1) | pH (in) | pH (out) | Al (in) (mol L-1) | Al (out) (mol L-1) | Ca (in) (mol L-1) | Ca (out) (mol L-1) | Cl (in) (mol L-1) | Cl (out) (mol L-1) | Estimated mass from Al (g) | Estimated mass from Ca (g) | BET surface area (m2 g-1) | SI C4AH13 | SI Friedel_Salt | SI Gibbsite | SI Gibbsite(am) | SI Portlandite |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.5 | 21.6 | 0.514 | 9.85 | 9.97 | 0.0 | 1.15E-03 | 0.0 | 3.19E-03 | 0.0 | 2.98E-03 | 1.1512 | 1.1486 | 13.7 | -14.69 | -11.05 | 2.18 | -0.66 | -5.53 |
| 1.8 | 57.9 | 0.493 | 9.85 | 9.99 | 0.0 | 1.71E-03 | 0.0 | 3.75E-03 | 0.0 | 3.78E-03 | 1.1250 | 1.1199 | 13.7 | -14.01 | -10.20 | 2.33 | -0.51 | -5.43 |
| 3.2 | 25.5 | 0.494 | 9.85 | 9.96 | 0.0 | 1.53E-03 | 0.0 | 3.58E-03 | 0.0 | 3.58E-03 | 1.1147 | 1.1078 | 13.7 | -14.35 | -10.53 | 2.31 | -0.53 | -5.51 |
| 4.1 | 25.3 | 0.493 | 9.85 | 9.94 | 0.0 | 1.49E-03 | 0.0 | 3.36E-03 | 0.0 | 3.36E-03 | 1.1047 | 1.0966 | 13.7 | -14.58 | -10.77 | 2.32 | -0.52 | -5.57 |
| 4.9 | 24.9 | 0.484 | 9.85 | 9.98 | 0.0 | 1.49E-03 | 0.0 | 3.48E-03 | 0.0 | 3.41E-03 | 1.0948 | 1.0851 | 13.7 | -14.29 | -10.55 | 2.28 | -0.56 | -5.48 |
| 5.8 | 25.7 | 0.493 | 9.85 | 10.00 | 0.0 | 1.89E-03 | 0.0 | 4.28E-03 | 0.0 | 3.75E-03 | 1.0820 | 1.0705 | 13.7 | -13.67 | -9.89 | 2.36 | -0.48 | -5.36 |
| 14.3 | 475.5 | 0.489 | 9.85 | 10.07 | 0.0 | 2.06E-03 | 0.0 | 4.52E-03 | 0.0 | 2.73E-03 | 0.8227 | 0.7859 | 13.7 | -13.08 | -9.72 | 2.33 | -0.51 | -5.20 |
| 22.8 | 20.2 | 0.489 | 9.85 | 10.03 | 0.0 | 1.89E-03 | 0.0 | 4.17E-03 | 0.0 | 1.87E-03 | 0.8126 | 0.7748 | 13.7 | -13.49 | -10.38 | 2.33 | -0.51 | -5.30 |
| 23.4 | 16.7 | 0.451 | 9.85 | 10.05 | 0.0 | 1.91E-03 | 0.0 | 4.16E-03 | 0.0 | 1.83E-03 | 0.8041 | 0.7656 | 13.7 | -13.37 | -10.31 | 2.32 | -0.52 | -5.27 |
| 24.3 | 29.8 | 0.487 | 9.85 | 10.04 | 0.0 | 1.85E-03 | 0.0 | 4.05E-03 | 0.0 | 1.77E-03 | 0.7895 | 0.7496 | 13.7 | -13.49 | -10.45 | 2.32 | -0.52 | -5.30 |
| 25.9 | 64.3 | 0.483 | 9.85 | 10.03 | 0.0 | 1.86E-03 | 0.0 | 4.13E-03 | 0.0 | 1.70E-03 | 0.7578 | 0.7145 | 13.7 | -13.52 | -10.49 | 2.33 | -0.51 | -5.31 |
| 27.3 | 20.6 | 0.487 | 9.85 | 10.05 | 0.0 | 1.88E-03 | 0.0 | 4.10E-03 | 0.0 | 1.66E-03 | 0.7475 | 0.7033 | 13.7 | -13.40 | -10.43 | 2.31 | -0.53 | -5.27 |
| 28.9 | 67.9 | 0.479 | 9.85 | 10.02 | 0.0 | 1.93E-03 | 0.0 | 4.10E-03 | 0.0 | 1.61E-03 | 0.7128 | 0.6664 | 13.7 | -13.56 | -10.55 | 2.35 | -0.49 | -5.33 |
| 38.6 | 467.3 | 0.455 | 9.85 | 9.97 | 0.0 | 1.67E-03 | 0.0 | 3.69E-03 | 0.0 | 1.35E-03 | 0.5065 | 0.4385 | 13.7 | -14.13 | -11.17 | 2.34 | -0.50 | -5.47 |
| 47.4 | 15.6 | 0.449 | 9.85 | 9.98 | 0.0 | 1.23E-03 | 0.0 | 2.97E-03 | 0.0 | 9.73E-04 | 0.5014 | 0.4324 | 13.7 | -14.64 | -11.98 | 2.21 | -0.64 | -5.53 |

Grey data have been selected for the calculation of dissolution rate.

Tab. A4 : Evolution of fluid chemistry, flow rate and saturation index (SI) for the AFm-Cl-11 experiment. An initial mass of 1.3250 g has been added into the flow-through reactor whereas 0.0510 g has been retrieved after dissolution experiment.

| Time (h) | Sampled mass (g) | Flow rate (mL min-1) | pH (in) | pH (out) | Al (in) (mol L-1) | Al (out) (mol L-1) | Ca (in) (mol L-1) | Ca (out) (mol L-1) | Cl (in) (mol L-1) | Cl (out) (mol L-1) | Estimated mass from Al (g) | Estimated mass from Ca (g) | BET surface area (m2 g-1) | SI C4AH13 | SI Friedel_Salt | SI Gibbsite | SI Gibbsite(am) | SI Portlandite |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.5 | 33.5 | 0.599 | 10.78 | 11.77 | 6.15E-06 | 4.20E-03 | 0.0 | 9.36E-03 | 0.0 | 8.25E-03 | 1.2878 | 1.2835 | 35.4 | -1.44 | -0.57 | 0.92 | -1.92 | -1.58 |
| 1.3 | 21.3 | 0.515 | 10.78 | 11.78 | 6.15E-06 | 4.73E-03 | 0.0 | 9.91E-03 | 0.0 | 8.47E-03 | 1.2611 | 1.2555 | 35.4 | -1.20 | -0.33 | 0.96 | -1.88 | -1.54 |
| 2.1 | 28.8 | 0.495 | 10.78 | 11.78 | 6.15E-06 | 4.80E-03 | 0.0 | 1.02E-02 | 0.0 | 8.94E-03 | 1.2246 | 1.2167 | 35.4 | -1.15 | -0.23 | 0.96 | -1.88 | -1.53 |
| 3.1 | 27.6 | 0.495 | 10.78 | 11.78 | 6.15E-06 | 5.05E-03 | 0.0 | 1.02E-02 | 0.0 | 8.93E-03 | 1.1878 | 1.1795 | 35.4 | -1.11 | -0.19 | 0.99 | -1.85 | -1.53 |
| 4.1 | 32.2 | 0.494 | 10.78 | 11.79 | 6.15E-06 | 4.97E-03 | 0.0 | 9.96E-03 | 0.0 | 8.53E-03 | 1.1455 | 1.1371 | 35.4 | -1.10 | -0.24 | 0.97 | -1.87 | -1.52 |
| 5.1 | 29.7 | 0.492 | 10.78 | 11.73 | 6.15E-06 | 4.95E-03 | 0.0 | 1.01E-02 | 0.0 | 8.09E-03 | 1.1066 | 1.0973 | 35.4 | -1.42 | -0.49 | 1.03 | -1.81 | -1.63 |
| 14.4 | 454.5 | 0.430 | 10.78 | 11.54 | 6.15E-06 | 4.44E-03 | 0.0 | 8.36E-03 | 0.0 | 4.43E-03 | 0.5733 | 0.5948 | 35.4 | -2.84 | -2.04 | 1.18 | -1.66 | -2.06 |
| 23.7 | 20.5 | 0.344 | 10.78 | 11.60 | 6.15E-06 | 3.41E-03 | 0.0 | 6.75E-03 | 0.0 | 2.27E-03 | 0.5549 | 0.5765 | 35.4 | -3.01 | -2.89 | 1.01 | -1.83 | -2.02 |
| 24.7 | 18.8 | 0.303 | 10.78 | 11.75 | 6.15E-06 | 3.52E-03 | 0.0 | 6.92E-03 | 0.0 | 2.24E-03 | 0.5374 | 0.5593 | 35.4 | -2.09 | -2.29 | 0.87 | -1.97 | -1.72 |
| 25.8 | 27.2 | 0.407 | 10.78 | 11.73 | 6.15E-06 | 3.36E-03 | 0.0 | 6.91E-03 | 0.0 | 1.99E-03 | 0.5133 | 0.5344 | 35.4 | -2.24 | -2.50 | 0.87 | -1.97 | -1.76 |
| 26.9 | 25.6 | 0.413 | 10.78 | 11.72 | 6.15E-06 | 3.13E-03 | 0.0 | 6.66E-03 | 0.0 | 1.98E-03 | 0.4921 | 0.5118 | 35.4 | -2.41 | -2.65 | 0.85 | -1.99 | -1.79 |
| 27.9 | 24.4 | 0.419 | 10.78 | 11.72 | 6.15E-06 | 3.04E-03 | 0.0 | 6.65E-03 | 0.0 | 2.05E-03 | 0.4725 | 0.4904 | 35.4 | -2.44 | -2.65 | 0.84 | -2.00 | -1.79 |
| 28.9 | 25.6 | 0.426 | 10.78 | 11.67 | 6.15E-06 | 3.19E-03 | 0.0 | 6.68E-03 | 0.0 | 2.06E-03 | 0.4509 | 0.4677 | 35.4 | -2.67 | -2.78 | 0.91 | -1.93 | -1.89 |
| 29.9 | 24.0 | 0.428 | 10.78 | 11.71 | 6.15E-06 | 2.92E-03 | 0.0 | 6.54E-03 | 0.0 | 2.08E-03 | 0.4324 | 0.4470 | 35.4 | -2.55 | -2.73 | 0.83 | -2.01 | -1.82 |
| 38.5 | 436.4 | 0.445 | 10.78 | 11.01 | 6.15E-06 | 1.88E-03 | 0.0 | 3.28E-03 | 0.0 | 1.21E-03 | 0.2158 | 0.2578 | 35.4 | -8.00 | -7.22 | 1.36 | -1.48 | -3.44 |
| 47.2 | 28.2 | 0.468 | 10.78 | 10.82 | 6.15E-06 | 6.56E-04 | 0.0 | 1.33E-03 | 0.0 | 3.39E-04 | 0.2110 | 0.2528 | 35.4 | -11.38 | -11.29 | 1.10 | -1.74 | -4.16 |
| 48.1 | 23.8 | 0.461 | 10.78 | 10.87 | 6.15E-06 | 6.05E-04 | 0.0 | 1.24E-03 | 0.0 | 3.30E-04 | 0.2072 | 0.2489 | 35.4 | -11.26 | -11.30 | 1.02 | -1.82 | -4.09 |
| 48.9 | 20.2 | 0.472 | 10.78 | 10.79 | 6.15E-06 | 5.54E-04 | 0.0 | 1.17E-03 | 0.0 | 2.96E-04 | 0.2043 | 0.2458 | 35.4 | -11.90 | -11.87 | 1.06 | -1.78 | -4.27 |
| 49.8 | 29.8 | 0.469 | 10.78 | 10.76 | 6.15E-06 | 5.12E-04 | 0.0 | 1.06E-03 | 0.0 | 2.65E-04 | 0.2003 | 0.2417 | 35.4 | -12.30 | -12.30 | 1.06 | -1.78 | -4.37 |
| 50.6 | 16.3 | 0.469 | 10.78 | 10.76 | 6.15E-06 | 4.43E-04 | 0.0 | 9.06E-04 | 0.0 | 2.45E-04 | 0.1984 | 0.2397 | 35.4 | -12.67 | -12.74 | 1.00 | -1.84 | -4.43 |

Dark and light grey data have been selected for the calculation of dissolution rate at respectively pH~11.71 and pH~10.84.

Tab. A5 : Evolution of fluid chemistry, flow rate and saturation index (SI) for the AFm-Cl-12 experiment. An initial mass of 1.2406 g has been added into the flow-through reactor whereas 0.4350 g has been retrieved after dissolution experiment.

| Time (h) | Sampled mass (g) | Flow rate (mL min-1) | pH (in) | pH (out) | Al (in) (mol L-1) | Al (out) (mol L-1) | Ca (in) (mol L-1) | Ca (out) (mol L-1) | Cl (in) (mol L-1) | Cl (out) (mol L-1) | Estimated mass from Al (g) | Estimated mass from Ca (g) | BET surface area (m2 g-1) | SI C4AH13 | SI Friedel_Salt | SI Gibbsite | SI Gibbsite(am) | SI Portlandite |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.4 | 26.2 | 0.581 | 11.91 | 12.07 | 1.29E-07 | 1.22E-03 | 0.0 | 3.32E-03 | 5.22E-02 | 5.03E-02 | 1.2321 | 1.2291 | 7.1 | -2.78 | -0.95 | 0.07 | -2.77 | -1.49 |
| 9.8 | 506.8 | 0.467 | 11.91 | 12.07 | 1.29E-07 | 1.68E-03 | 0.0 | 2.86E-03 | 5.22E-02 | 5.16E-02 | 1.0073 | 1.0373 | 7.1 | -2.76 | -0.92 | 0.21 | -2.63 | -1.56 |
| 19.4 | 30.1 | 0.457 | 11.91 | 12.09 | 1.29E-07 | 1.63E-03 | 0.0 | 3.42E-03 | 5.22E-02 | 5.12E-02 | 0.9943 | 1.0237 | 7.1 | -2.38 | -0.58 | 0.18 | -2.66 | -1.45 |
| 20.6 | 35.1 | 0.457 | 11.91 | 12.11 | 1.29E-07 | 1.64E-03 | 0.0 | 3.38E-03 | 5.22E-02 | 5.33E-02 | 0.9790 | 1.0080 | 7.1 | -2.30 | -0.51 | 0.16 | -2.68 | -1.42 |
| 21.8 | 33.0 | 0.459 | 11.91 | 12.13 | 1.29E-07 | 1.70E-03 | 0.0 | 3.40E-03 | 5.22E-02 | 5.41E-02 | 0.9642 | 0.9932 | 7.1 | -2.16 | -0.39 | 0.15 | -2.69 | -1.38 |
| 22.9 | 24.9 | 0.457 | 11.91 | 12.12 | 1.29E-07 | 1.58E-03 | 0.0 | 3.39E-03 | 5.22E-02 | 5.43E-02 | 0.9538 | 0.9820 | 7.1 | -2.28 | -0.49 | 0.13 | -2.71 | -1.40 |
| 23.9 | 29.2 | 0.447 | 11.91 | 12.15 | 1.29E-07 | 1.63E-03 | 0.0 | 3.39E-03 | 5.22E-02 | 5.27E-02 | 0.9413 | 0.9689 | 7.1 | -2.08 | -0.38 | 0.11 | -2.73 | -1.34 |
| 32.7 | 467.5 | 0.473 | 11.91 | 12.01 | 1.29E-07 | 1.48E-03 | 0.0 | 2.77E-03 | 5.22E-02 | 5.42E-02 | 0.7584 | 0.7976 | 7.1 | -4.12 | -2.11 | 0.22 | -2.62 | -1.90 |
| 41.5 | 32.7 | 0.465 | 11.91 | 12.09 | 1.29E-07 | 1.09E-03 | 0.0 | 2.15E-03 | 5.22E-02 | 5.32E-02 | 0.7490 | 0.7883 | 7.1 | -3.52 | -1.68 | 0.00 | -2.84 | -1.64 |
| 42.5 | 23.4 | 0.462 | 11.91 | 12.08 | 1.29E-07 | 1.03E-03 | 0.0 | 2.06E-03 | 5.22E-02 | 5.32E-02 | 0.7426 | 0.7819 | 7.1 | -3.69 | -1.84 | -0.01 | -2.85 | -1.68 |
| 43.4 | 24.9 | 0.462 | 11.91 | 11.98 | 1.29E-07 | 9.95E-04 | 0.0 | 1.98E-03 | 5.22E-02 | 5.38E-02 | 0.7361 | 0.7754 | 7.1 | -4.34 | -2.27 | 0.07 | -2.77 | -1.88 |
| 44.4 | 30.8 | 0.461 | 11.91 | 12.00 | 1.29E-07 | 9.02E-04 | 0.0 | 1.94E-03 | 5.22E-02 | 5.22E-02 | 0.7287 | 0.7675 | 7.1 | -4.34 | -2.33 | 0.01 | -2.83 | -1.85 |
| 45.5 | 31.5 | 0.461 | 11.91 | 11.95 | 1.29E-07 | 9.41E-04 | 0.0 | 1.86E-03 | 5.22E-02 | 5.21E-02 | 0.7209 | 0.7597 | 7.1 | -4.65 | -2.54 | 0.08 | -2.76 | -1.96 |
| 46.5 | 24.5 | 0.458 | 11.91 | 11.96 | 1.29E-07 | 9.04E-04 | 0.0 | 1.75E-03 | 5.22E-02 | 5.11E-02 | 0.7150 | 0.7541 | 7.1 | -4.72 | -2.65 | 0.05 | -2.79 | -1.97 |
| 47.2 | 15.3 | 0.461 | 11.91 | 11.90 | 1.29E-07 | 8.19E-04 | 0.0 | 1.76E-03 | 5.22E-02 | 5.19E-02 | 0.7117 | 0.7505 | 7.1 | -5.13 | -2.93 | 0.07 | -2.77 | -2.08 |

Grey data have been selected for the calculation of dissolution rate.

Tab. A6 : Evolution of fluid chemistry, flow rate and saturation index (SI) for the AFm-Cl-13 experiment. An initial mass of 1.0078 g has been added into the flow-through reactor whereas 0.6357 g has been retrieved after dissolution experiment.

| Time (h) | Sampled mass (g) | Flow rate (mL min-1) | pH (in) | pH (out) | Al (in) (mol L-1) | Al (out) (mol L-1) | Ca (in) (mol L-1) | Ca (out) (mol L-1) | Cl (in) (mol L-1) | Cl (out) (mol L-1) | Estimated mass from Al (g) | Estimated mass from Ca (g) | BET surface area (m2 g-1) | SI C4AH13 | SI Friedel_Salt | SI Gibbsite | SI Gibbsite(am) | SI Portlandite |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.3 | 15.2 | 0.490 | 12.83 | 12.75 | 5.49E-07 | 5.79E-04 | 0.0 | 2.28E-03 | 5.18E-02 | 6.31E-02 | 1.0055 | 1.0033 | 6.1 | -0.83 | -0.21 | -0.95 | -3.79 | -0.49 |
| 0.9 | 25.5 | 0.510 | 12.83 | 12.78 | 5.49E-07 | 6.75E-04 | 0.0 | 1.74E-03 | 5.18E-02 | 5.91E-02 | 1.0010 | 0.9974 | 6.1 | -1.02 | -0.52 | -0.92 | -3.76 | -0.56 |
| 9.3 | 461.4 | 0.486 | 12.83 | 12.77 | 5.49E-07 | 6.50E-04 | 0.0 | 1.32E-03 | 5.18E-02 | 5.33E-02 | 0.9217 | 0.9166 | 6.1 | -1.55 | -1.11 | -0.92 | -3.76 | -0.69 |
| 18.3 | 65.6 | 0.479 | 12.83 | 12.77 | 5.49E-07 | 8.87E-04 | 0.0 | 1.74E-03 | 5.18E-02 | 5.16E-02 | 0.9063 | 0.9015 | 6.1 | -0.80 | -0.39 | -0.79 | -3.63 | -0.57 |
| 19.8 | 19.4 | 0.474 | 12.83 | 12.81 | 5.49E-07 | 8.68E-04 | 0.0 | 1.73E-03 | 5.18E-02 | 5.13E-02 | 0.9018 | 0.8971 | 6.1 | -0.67 | -0.35 | -0.84 | -3.68 | -0.51 |
| 21.1 | 56.3 | 0.486 | 12.83 | 12.80 | 5.49E-07 | 8.70E-04 | 0.0 | 1.69E-03 | 5.18E-02 | 5.24E-02 | 0.8889 | 0.8844 | 6.1 | -0.75 | -0.39 | -0.83 | -3.67 | -0.54 |
| 22.6 | 29.5 | 0.476 | 12.83 | 12.80 | 5.49E-07 | 8.75E-04 | 0.0 | 1.71E-03 | 5.18E-02 | 5.19E-02 | 0.8821 | 0.8778 | 6.1 | -0.72 | -0.37 | -0.82 | -3.66 | -0.53 |
| 23.6 | 29.3 | 0.488 | 12.83 | 12.79 | 5.49E-07 | 8.68E-04 | 0.0 | 1.69E-03 | 5.18E-02 | 5.21E-02 | 0.8753 | 0.8712 | 6.1 | -0.79 | -0.41 | -0.82 | -3.66 | -0.55 |
| 24.6 | 29.2 | 0.478 | 12.83 | 12.78 | 5.49E-07 | 8.62E-04 | 0.0 | 1.72E-03 | 5.18E-02 | 5.20E-02 | 0.8687 | 0.8646 | 6.1 | -0.81 | -0.41 | -0.81 | -3.65 | -0.56 |
| 33.2 | 466.0 | 0.482 | 12.83 | 12.72 | 5.49E-07 | 5.46E-04 | 0.0 | 1.02E-03 | 5.18E-02 | 5.32E-02 | 0.8014 | 0.8018 | 6.1 | -2.35 | -1.81 | -0.94 | -3.78 | -0.88 |
| 41.8 | 32.0 | 0.478 | 12.83 | 12.74 | 5.49E-07 | 5.53E-04 | 0.0 | 1.03E-03 | 5.18E-02 | 5.23E-02 | 0.7967 | 0.7974 | 6.1 | -2.24 | -1.75 | -0.96 | -3.80 | -0.84 |
| 44.2 | 103.7 | 0.476 | 12.83 | 12.78 | 5.49E-07 | 5.06E-04 | 0.0 | 9.86E-04 | 5.18E-02 | 5.20E-02 | 0.7828 | 0.7839 | 6.1 | -2.23 | -1.83 | -1.04 | -3.88 | -0.80 |
| 46.3 | 19.3 | 0.482 | 12.83 | 12.82 | 5.49E-07 | 4.84E-04 | 0.0 | 8.96E-04 | 5.18E-02 | 5.15E-02 | 0.7803 | 0.7816 | 6.1 | -2.27 | -1.97 | -1.10 | -3.94 | -0.78 |

Grey data have been selected for the calculation of dissolution rate.