Different crystallization mechanism in Polypropylene-nanoclay nanocomposite with different weight percentage nanoclay additives

Raghavendra R. Hegde, Joseph E. Spruiell and Gajanan S. Bhat 

Department of Materials Science and Engineering,

The University of Tennessee, Knoxville TN 37996-2200, USA

Supporting information

Figures

In this research, linear low-density polyethylene (LLDPE) based maleated wax was used as a compatibilizer between polypropylene and Closite Na+. Schematic of possible interaction between the clay platelet, PP chain and maleated wax is shown in Figure S199-101.

Fig. S 1 Schematic of reaction between (a) maleic anhydride, LLDPE, (b) clay platelets and maleated wax and (c) clay, maleated wax, PP100.

Fig. S 2 Schematic of TEM microtomy sample extraction from the injection molded composites.

Fig. S 3 Photographs of concentrates at (a) PP, (b) PPN1, (c) PPN2, (d) PPN3, (e) PPN10, (f) PPN15 250°C, bright areas indicate the existence of clay tactoids, and the dark areas indicate the molten PP matrix (crystallization conditions are included in experimental section).

Influence of 5wt% maleated wax in PP concentrate on the crystallization and crystallinity wt. % was investigated. Difference in crystallization behavior is not significant. Crystallinity wt. % is slightly lower for PP with wax. This might be due to the hindrance to chain mobility by the maleated wax.

Fig. S 4. Peak crystallization during cooling segment.

Table S 1. Heat of fusion values.

| Sample | Heat of fusion (J/g) |
| --- | --- |
| PP | 98.44 |
| PPM | 95.41 |

Tables

Table S 2 Crystallization kinetics results for Control PP

| Sample | Temperature (°C) | n | exponent | K | t 1/2 (min) | G(1/min)-exp |
| --- | --- | --- | --- | --- | --- | --- |
| PP | 120 | 2.1 | -0.9 | 0.13 | 0.3 | 3.3 |
|  | 123 | 1.9 | -0.6 | 0.25 | 0.4 | 2.5 |
|  | 125 | 1.9 | -0.3 | 0.48 | 1.6 | 0.6 |
|  | 128 | 2.4 | -0.3 | 0.49 | 1.2 | 0.8 |
|  | 130 | 2.6 | -1.0 | 0.11 | 2.0 | 0.5 |
|  | 135 |  |  |  |  |  |

Table S 3 Crystallization kinetics results for PPN1.

| Sample | Temperature (°C) | n | exponent | K | t 1/2 (min) | G(1/min)-exp |
| --- | --- | --- | --- | --- | --- | --- |
| PPN1 | 120 | 2.2 | -0.2 | 0.63 | 0.7 | 1.5 |
|  | 123 | 2.4 | -0.4 | 0.37 | 1.3 | 0.8 |
|  | 125 | 2.4 | -0.9 | 0.12 | 2.0 | 0.5 |
|  | 128 | 2.3 | -1.3 | 0.05 | 4.0 | 0.3 |
|  | 130 | 2.7 | -2.3 | 0.01 | 6.5 | 0.2 |

Table S 4 Crystallization kinetics results for PPN2.

| Sample | Temperature (°C) | n | exponent | K | t 1/2 (min) | G(1/min)-exp |
| --- | --- | --- | --- | --- | --- | --- |
| PPN2 | 120 | 1.9 | -2.7 | 0.002 | 1.7 | 0.6 |
|  | 123 | 2.0 | -2.8 | 0.002 | 1.7 | 0.6 |
|  | 125 | 2.1 | -0.1 | 0.724 | 1.0 | 1.0 |
|  | 128 | 2.4 | -0.9 | 0.126 | 1.9 | 0.5 |
|  | 130 | 2.5 | -1.7 | 0.020 | 4.4 | 0.2 |

Table S 5 Crystallization kinetics results for PPN3.

| Sample | Temperature (°C) | n | exponent | K | t 1/2 (min) | G(1/min)-exp |
| --- | --- | --- | --- | --- | --- | --- |
| PPN5 | 120 | 1.8 | -0.5 | 0.32 | 0.5 | 2.2 |
|  | 123 | 2.0 | -0.2 | 0.49 | 0.7 | 1.5 |
|  | 125 | 2.2 | -0.3 | 0.49 | 1.2 | 0.8 |
|  | 128 | 2.2 | -0.9 | 0.13 | 2.2 | 0.5 |
|  | 130 | 1.8 | -1.0 | 0.10 | 3.3 | 0.3 |

Table S 6 Crystallization kinetics results for PPN10.

| Sample | Temperature (°C) | n | exponent | K | t 1/2 (min) | G(1/min)-exp |
| --- | --- | --- | --- | --- | --- | --- |
| PPN10 | 120 | 1.9 | -0.9 | 0.11 | 0.3 | 3.8 |
|  | 123 | 2.0 | -0.8 | 0.15 | 0.3 | 3.2 |
|  | 125 | 2.0 | -0.4 | 0.36 | 0.5 | 2.0 |
|  | 128 | 2.3 | 0.0 | 0.98 | 0.9 | 1.2 |
|  | 130 | 2.4 | -0.5 | 0.35 | 1.4 | 0.7 |

Table S 7 Crystallization kinetics results for PPN15.

| Sample | Temperature (°C) | n | exponent | K | t 1/2 (min) | G(1/min)-exp |
| --- | --- | --- | --- | --- | --- | --- |
| PPN15 | 120 | 2.0 | -1.1 | 0.08 | 1.3 | 0.8 |
|  | 123 | 2.0 | -1.0 | 0.10 | 0.3 | 4.0 |
|  | 125 | 1.8 | -0.8 | 0.16 | 0.3 | 3.8 |
|  | 128 | 2.0 | -0.3 | 0.49 | 0.6 | 1.7 |
|  | 130 | 2.3 | -0.1 | 0.78 | 1.0 | 1.0 |

####  Corresponding author; Gajanan Bhat, Professor, Department of Materials Science and Engineering
205 TANDEC BUILDING, The University of Tennessee, Knoxville, TN 37996, Phone: 865-974-0976, Fax: 865-974-5236
Email: gbhat@utk.edu