Table Captions

Table 1. Calculated equilibrium lattice parameters (a , b, c), equilibrium volumes (V0 ) and formation enthalpies (ΔH) for the unit cell of XN4(X=Re, Os, W) with the literature data.

Table 2. Calculated elastic constants (Cij), bulk modulus (B), shear modulus (G), Young modulus (E) in GPa and Poisson’s ratio (v) and mechanical stability (MS) for rhenium, osmium and tungsten tetranitrides.

Table 3. Calculated hardness values (in GPa unit) by three different methods for XN4(X=Re, Os, W) compounds

Table 4. Calculated Mulliken bond overlap populations for the characteristic bonds of rhenium, osmium and tungsten tetranitrides.

Table 1. Calculated equilibrium lattice parameters (a , b, c), equilibrium volumes (V0 ) and formation enthalpies (ΔH) for the unit cell of XN4(X=Re, Os, W) with the literature data.

|  |  | ReN4 | OsN4 | WN4 |
| --- | --- | --- | --- | --- |
| a (Å) | CASTEP VASP | 5.095 5.097 5.089a | 5.028 5.116 5.022b | 5.342 5.144 |
| b (Å) | CASTEP VASP | 7.307 7.276 7.274a | 7.425 7.311 7.388b | 7.378 7.373 |
| c (Å) | CASTEP VASP | 8.843 8.879 8.892a | 8.767 8.788 8.786b | 9.006 9.112 |
| V (Å3) | CASTEP VASP | 329.187 329.284 329.070a | 327.285 328.698 | 354.939 345.588 |
| ΔH(eV/XN4) |  | -0.33 | -0.26 | -0.59 |

aRef.[30]  	bRef.[31]

Table 2. Calculated elastic constants (Cij), bulk modulus (B), shear modulus (G), Young modulus (E) in GPa and Poisson’s ratio (v) and mechanical stability (MS) for rhenium, osmium and tungsten tetranitrides.

|  | ReN4 |  | OsN4 |  | WN4 |
| --- | --- | --- | --- | --- | --- |
|  | This study | Ref.[30] | This study | Ref.[31] | This study |
| C11 | 562.0 | 465 | 505.9 | 577 | 509.7 |
| C22 | 824.4 | 700 | 848.4 | 831 | 729.5 |
| C33 | 911.3 | 881 | 923.7 | 855 | 818.6 |
| C44 | 500.0 | 509 | 475.3 | 455 | 445.5 |
| C55 | 127.7 | 78 | 123.4 | 108 | 91.0 |
| C66 | 148.4 | 97 | 149.6 | 103 | 120.4 |
| C12 | 119.3 | 141 | 129.9 | 99 | 124.7 |
| C13 | 84.7 | 133 | 90.9 | 92 | 91.9 |
| C23 | 340.6 | 296 | 334.4 | 322 | 352.5 |
| B | 359.2 | 335.3 | 353.8 | 352 | 338.3 |
| G | 240.9 | 212.7 | 234.8 | 241 | 198.1 |
| E | 590.7 | 526.7 | 576.9 | 532 | 497.2 |
| v | 0.23 | 0.24 | 0.23 | 0.22 | 0.26 |
| B/G | 1.49 | 1.58 | 1.51 | 1.46 | 1.71 |
| MS | Yes | Yes | Yes | Yes | Yes |

Table 3. Calculated hardness values (in GPa unit) by three different methods for XN4(X=Re, Os, W) compounds

| Method | ReN4 | OsN4 | WN4 |
| --- | --- | --- | --- |
| First | 64.3 | 67.3 | 64.5 |
| Second | 53.7 | 63.6 | 47.9 |
| Third | 53.6 | 63.9 | 43.9 |

.

Table 4. Calculated Mulliken bond overlap populations (M) and lengths (d, Å) for the characteristic bonds of rhenium, osmium and tungsten tetranitrides

| Bonds |  | ReN4 |  | OsN4 |  | WN4 |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | M | d | M | d | M | d |
| N-N | 1 | 0.91 | 1.324 | 1.01 | 1.295 | 0.81 | 1.350 |
|  | 2 | 0.57 | 1.454 | 0.50 | 1.495 | 0.75 | 1.368 |
|  | 3 | 0.56 | 1.456 | 0.54 | 1.465 | 0.63 | 1.422 |
|  | 4 | 0.50 | 1.495 | 0.53 | 1.460 | 0.59 | 1.434 |
| N-X | 1 | 0.61 | 1.929 | 0.50 | 1.962 | 0.60 | 2.004 |
|  | 2 | 0.52 | 1.995 | 0.50 | 1.947 | 0.48 | 2.058 |
|  | 3 | 0.44 | 2.011 | 0.38 | 2.050 | 0.37 | 2.069 |
|  | 4 | 0.22 | 2.081 | 0.20 | 2.101 | 0.23 | 2.105 |
|  | 5 | 0.43 | 2.097 | 0.43 | 2.050 | 0.52 | 2.040 |
|  | 6 | 0.20 | 2.282 | 0.20 | 2.162 | - | - |

.