Supplementary file

Foam fractionation synthesis of ZnO and its photocatalysis of the degradation of methylene blue

Shashi B Atla a, Chien-Yen Chen a,e*, Chien-Cheng Chenb, Shao-Ju Shih c, Pin-Yun Lin a, Pei-Hua Chung a, Jheng-Sian Yang a, A. Satyanarayana Reddyd, Kai-Chien Chenga, Young-Fo Changa

a Department of Earth and Environmental Sciences, National Chung Cheng University, 168 University Road, Minhsiung, Chiayi, 62102, Taiwan,

b Department of Biotechnology, National Kaohsiung Normal University, No.62, Shenjhong Rd., Yanchao Township, Kaohsiung County, 82444, Taiwan

cDepartment of Materials Science and Engineering, National Taiwan University of Science and Technology, No.43, Sec. 4, Keelung Rd., Da’an Dist., Taipei 106, Taiwan

d Graduate School of EEWS, Korea Advanced Institute of Science and Technology, Daejeon 305-701, Republic of Korea

eDepartment of Engineering, University of Cambridge, Trumpington Street, Cambridge CB2 1PZ, UK

# Synthesis of ZnO

Zn(NO3)2.6H2O (5.49g) and SDS (1.4g) were dissolved in 200 ml of Milli-Q water so that the final concentration of Zn(NO3)2 and SDS in solution was 0.1 M and 0.02 M, respectively. The resultant solution (without the formation of foam) was exposed with the vapors of (1.5ml of 25% ammonia) ammonia for a period of 30 minutes. The precipitate obtained was then separated by centrifugation at a speed of 3700 rpm for 30 min. The precipitate was washed thrice with Milli-Q water followed by ethanol for the complete removal of the surfactant. Finally, the precipitate was dried in an air oven for 6 h at 50°C (as-synthesized). The precipitates were further calcined at a temperature of 420°C for 4 h (calcined).

## FIG. S1. XRD patterns of as-synthesized and calcined ZnO obtained by conventional method

## FIG. S2. SEM images obtained by conventional method (a) as-synthesized (b) calcined ZnO

The SEM images of the as-synthesized ZnO showed that small plate like structures are adhered together, on calcinations induced the recrystallization process to form large plate like structures

FIG. S3. Photocatalytic degradation of MB with time by ZnO (conventional method).