An active surface enhanced Raman scattering substrate using carbon nanocoils

Dawei Li, Lujun Pana), Shifa Wu and Shuai Li

School of Physics and Optoelectronic Technology, Dalian University of Technology, No.2 Linggong Road, Ganjingzi District, Dalian 116024, PR China

Supplementary Information

FIG. S1. Magnified SEM images of CNCs coated with AgNPs by RFMS for (a) 4 min, (b) 12 min.

FIG. S2. More magnified SEM images of AgNPs on TiO2-CNCs substrates, formed in 3 mM AgNO3 solution with UV light irradiation for 2 h, where TiO2 is formed by sputtering for (a) 15 min, (b) 60 min, and (c) 150 min.

FIG. S3. Optical transmission spectra of TiO2 film prepared by RFMS for (a) 15 min, (b) 60 min, and (c) 150 min. (d) Optical transmission spectra of calcined TiO2 film prepared by a spin-coating. The continuous line represents experimental data and the hollow circle line is the corresponding fitting curve by envelop method. The thicknesses of TiO2 films in Figure S3(a-d) can be measured using the above method, which are calculated to be approximately 40, 103, 177, and 220 nm, respectively.

FIG. S4. (a) and (b) More magnified SEM images of single B-nanostructure. (c) Magnified SEM image of AgNPs formed in the planar area without CNCs.

a) Address all correspondence to this author.   e-mail: lpan@dlut.edu.cn