Supporting Materials

- Strain rate sensitivity (SRS) and activation volume

σ=k⋅εm                                               (1)

lnσ=lnk+m⋅ln {ε                                        (2)

When we have two loading rates, i.e. ε1 and ε2, and the corresponding fracture strengths, σ1 and σ2, can be given in the following equations.

lnσ1=lnk+m⋅ln {ε1                                         (3)

lnσ2=lnk+m⋅ln {ε2                                        (4)

To cancel out k, Eq (3) minus Eq (4), we obtain,

lnσ1σ2=m⋅lnε1ε2                                            (5)

To find out the maximal SRS, we use     ε1=10−3 s-1, σ1=356 MPa,

ε2=892 s-1, σ2=864 MPa,

mmax=lnσ2σ1lnε2ε1=ln864356ln89210−3=0.06,

To find out the minimal SRS, we use      ε1=10−3 s-1, σ1=579 MPa,

ε2=996 s-1, σ2=768 MPa,

mmin=ln768579ln99610−3=0.02,

Thus, the measured SRS ranges within 0.02~0.06.

The activation volume (v*) of plastic deformation is inherently related to the strain rate sensitivityS1 by

v=3  ⋅k⋅Tσ⋅m                                             (6)

## Here k is the Boltzmann constant (1.38×10-23 m2 kg s-2k-1), T is absolute temperature, and σ and m are respectively applied stress and SRS.

Here we take σ=864 MPa and m=0.06 to calculate the activation volume of plastic deformation at dynamic loading

v=3  ⋅1.38⋅10−23⋅293864⋅106⋅0.06=0.135 nm3 =2~3 b3 (︱b︱=0.38 nm for plane spacing in Figure 4 of our manuscript).

The activation volume under quasi-static loading is calculated as follows:

## =0.994nm3=18 b3.

## Here=356 MPa (we take the maximum compressive strength under quasi-static loading) and m=0.02 (we take m=0.02 in order to roughly estimate the maximum activation volume).

- Evaluation of fracture energy dissipation for dynamic/quasi-static compression.

For the quasi-statically compressed sample, the original sample geometry is 2mm x 2mm x 4mm. Upon fracture, the sample was roughly split into two parts with two fracture surfaces. The two fracture surface areas were estimated to be the total of 16mm2(2mm x 4mm x 2).

For the dynamic case, the pristine geometry is 3mm x 3mm x 3mm. The average fragment size is approximately 0.154mm. Here we treat each fragment as an ideal cube. Thus, the created surface area can be estimated to be the total of

3mm0.154mm3∗6∗0.154mm2−6∗3mm2=998mm2

Fig. S1. Schematic illustration of dynamic compression process, for simplicity, each irregular-shaped fragment is treated as an idea cube.

Here we introduce k (J/mm2) as the fracture energy and assume it to be a constant. When we consider the volume effect (sample geometry), we can further obtain the fracture energy dissipation per unit volume, as follows.

For the quasi-static case, the fracture energy dissipation per unit volume is 16mm2 k/2mm x 2mm x 4mm=1 J/mm3.

For the dynamic one, the fracture energy dissipation per unit volume is 998mm2 k/3mm x 3mm x 3mm=37 J/mm3. Thus, the ratio of energy dissipations of dynamic fracture to that of the quasi-static fracture is 37.

- Fractograph observation of dynamic compression nacre along cross section

Fig. S2. Fractography observation in the dynamically-compressed nacre along cross section. (a) The fragment size distribution is typically in the range of submillimeter. (b) The fracture surface viewed from c-axis shows that crack propagates, to a large extent, along the biopolymer interface. (c) Microscopic observation on the cross section confirms the interface-dominated crack failure. (d) A close-up examination shows that the aragonite platelets remain comparatively intact.

- Schematic illustrations of crack propagation when loading from c-axis and cross section, respectively.

Fig. S3. Effect of loading direction on the potential crack path. (a) When loading along nacre’s c-axis, the geometrically staggered aragonite platelets posts a critical crack extension resistance. (b) Comparatively, the biopolymer interface favors the crack propagation (stress release) while loading direction is along nacre’s cross section.