Supporting Materials

A large amount of Ag low-dimensional nanostructures, such as nanowires, nanoribbons, and nanoplates, had been taken from the solution when the photocatalytic growth of Ag NPs was conducted for a longer time using TiO2 or ZnAlO films as the reduction media, as shown in Fig. S1. These SEM images support that the reduced Ag atoms can diffuse into solution.

Fig. S1 Ag low-dimensional nanostructures taken from the solution using TiO2 (a and b) and ZnAlO (c and d) films as the reduction media.

Fig. S2 SEM image of Ag foil grown on a smooth TiO2 film using 3200 mg/L AgNO3 solution.