Table SI. pH of each cation solution, each mixing step and the final solution pH to produce LiFePO4.

|  |  |
| --- | --- |
| **Source** | **pH** |
| Li | 8.69 |
| Fe | ≈ 0 |
| P | 7.88 |
| Li+Fe | 0.40 |
| Final | 0.49 |