Supporting Information

| ZnPcx (basis set for calculation with TD-DFT method) | First allowed electronic transition (eV/f -oscillator strength) | First allowed electronic transition (nm) | Second allowed electronic transition (eV/f -oscillator strength) | Second allowed electronic transition (nm) | Davydov splitting ∆E (eV) |
| --- | --- | --- | --- | --- | --- |
| ZnPc1 (6-31G(d)) | 1.796 (0.4915) | 690.3 | 1.805 (0.4897) | 686.8 | 0.009 |
| (ZnPc)21 (6-31G(d)) | 1.810 (0.7668) | 685.0 | 1.885 (0.7320) | 657.7 | 0.075 |
| (ZnPc)41 (6-31G(d)) | 1.807 (1.3757) | 686.0 | 1.946 (1.1063) | 637.3 | 0.138 |
| (ZnPc)61 (6-31G(d)) | 1.803 (2.0328) | 687.6 | 1.969 (1.4543) | 629.8 | 0.166 |
| ZnPc1 (cc-pVDZ) | 1.789 (0.4979) | 692.9 | 1.799 (0.4964) | 689.1 | 0.010 |
| (ZnPc)21 (cc-pVDZ) | 1.800 (0.7724) | 688.7 | 1.877 (0.7383) | 660.7 | 0.076 |
| (ZnPc)41 (cc-pVDZ) | 1.796 (1.3871) | 690.4 | 1.935 (1.1133) | 640.7 | 0.139 |
| (ZnPc)61 (cc-pVDZ) | 1.789 (2.0550) | 693.0 | 1.957 (1.4634) | 633.5 | 0.168. |
| ZnPc2 (6-31G(d)) | 1.796 (0.4905) | 690.4 | 1.809 (0.4908) | 685.4 | 0.013 |
| (ZnPc)22 (6-31G(d)) | 1.810 (0.7646) | 684.8 | 1.885 (0.7327) | 657.7 | 0.075 |
| (ZnPc)42 (6-31G(d)) | 1.806 (1.3752) | 686.4 | 1.945 (1.1079) | 637.3 | 0.139 |
| (ZnPc)62 (6-31G(d)) | 1.801 (2.0349) | 688.3 | 1.968 (1.4570) | 629.9 | 0.167 |
| ZnPc2 (cc-pVDZ) | 1.789 (0.4969) | 693.0 | 1.803 (0.4975) | 687.7 | 0.014 |
| (ZnPc)22 (cc-pVDZ) | 1.801 (0.7704) | 688.5 | 1.876 (0.7392) | 660.7 | 0.076 |
| (ZnPc)42 (cc-pVDZ) | 1.795 (1.3867) | 690.8 | 1.935 (1.1147) | 640.8 | 0.140 |
| (ZnPc)62 (cc-pVDZ) | 1.789 (2.0550) | 693.0 | 1.957 (1.4634) | 633.5 | 0.168 |
| ZnPc3 (6-31G(d)) | 1.776 (0.4933) | 698.1 | 1.790 (0.4887) | 692.7 | 0.014 |
| (ZnPc)23 (6-31G(d)) | 1.794 (0.7641) | 691.1 | 1.865 (0.7344) | 664.9 | 0.071 |
| (ZnPc)43 (6-31G(d)) | 1.791 (1.3710) | 692.2 | 1.925 (1.1096) | 644.2 | 0.133 |
| (ZnPc)63 (6-31G(d)) | 1.787 (2.0265) | 693.9 | 1.948 (1.4584) | 636.6 | 0.161 |
| ZnPc3 (cc-pVDZ) | 1.769 (0.4992) | 700.9 | 1.783 (0.4950) | 695.2 | 0.015 |
| (ZnPc)23 (cc-pVDZ) | 1.784 (0.7692) | 694.9 | 1.855 (0.7400) | 668.2 | 0.071 |
| (ZnPc)43 (cc-pVDZ) | 1.779 (1.3818) | 696.8 | 1.914 (1.1160) | 647.9 | 0.134 |
| (ZnPc)63 (cc-pVDZ) | 1.774 (2.0473) | 698.9 | 1.936 (1.4656) | 640.4 | 0.162 |
| ZnPc4 (6-31G(d)) | 1.775 (0.4925) | 698.5 | 1.791 (0.4897) | 692.5 | 0.016 |
| (ZnPc)24 (6-31G(d)) | 1.790 (0.7630) | 692.6 | 1.862 (0.7325) | 665.9 | 0.072 |
| (ZnPc)44 (6-31G(d)) | 1.785 (1.3742) | 694.8 | 1.921 (1.1072) | 645.5 | 0.136 |
| (ZnPc)64 (6-31G(d)) | 1.779 (2.0357) | 696.9 | 1.944 (1.4510) | 638.0 | 0.165 |
| ZnPc4 (cc-pVDZ) | 1.768 (0.4984) | 701.4 | 1.784 (0.4961) | 695.0 | 0.016 |
| (ZnPc)24 (cc-pVDZ) | 1.780 (0.7681) | 696.5 | 1.852 (0.7379) | 669.3 | 0.072 |
| (ZnPc)44 (cc-pVDZ) | 1.773 (1.3847) | 699.5 | 1.910 (1.1132) | 649.2 | 0.137 |
| (ZnPc)64 (cc-pVDZ) | 1.766 (2.0540) | 701.9 | 1.932 (1.4621) | 641.8 | 0.166 |

TABLE SI. Calculations of VIS spectra using a different number of monomers units, atomic basis sets, pseudopotentials and values of cutoff of plane-wave kinetic energy

1 plane-wave kinetic energy cutoff of 310 eV/ultrasoft pseudopotentials

2 plane-wave kinetic energy cutoff of 350 eV/ultrasoft pseudopotentials

3 plane-wave kinetic energy cutoff of 700 eV/normconserving pseudopotentials

4 plane-wave kinetic energy cutoff of 900 eV/normconserving pseudopotentials