Supporting Information

Contents

Table S1. Predicted crystal cell parameters for the TCATT

Table S2. The optimized predicted crystal cell parameters and the corresponding experimental values for ATT and TCATT

Table S3. The optimized bond lengths (Å), bond angels (°), dihedral angles (°) of ATT in neutral and ionic states based on B3LYP/6-31G(d,p) and its corresponding experimental values

Table S4. The optimized bond lengths (Å), bond angels (°), dihedral angles (°) of TBATT in neutral and ionic states based on B3LYP/6-31G(d,p) and its corresponding experimental values

Table S5. The optimized bond lengths (Å), bond angels (°), dihedral angles (°) of TCATT in neutral and ionic states based on B3LYP/6-31G(d,p)

Table S1. Predicted crystal cell parameters for the TCATTa

| No. | SGb | total energy (kcal/mol) | a/Å | b/Å | c/Å | α/° | β/° | γ/° |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | P21/C | 53.682 | 7.580 | 26.943 | 10.543 | 90.00 | 96.01 | 90.00 |
| 2 | P21 | 53.682 | 13.615 | 26.943 | 3.790 | 90.00 | 50.37 | 90.00 |
| 3 | P21/C | 53.999 | 7.457 | 10.858 | 27.783 | 90.00 | 73.43 | 90.00 |
| 4 | P21 | 53.999 | 3.729 | 10.858 | 26.827 | 90.00 | No. | 90.00 |
| 5 | P21/C | 54.325 | 10.900 | 54.306 | 10.584 | 90.00 | 159.85 | 90.00 |
| 6 | P21/C | 54.326 | 10.890 | 55.274 | 10.586 | 90.00 | 159.85 | 90.00 |
| 7 | P21/C | 54.561 | 57.355 | 10.866 | 58.699 | 90.00 | 176.58 | 90.00 |
| 8 | P1 | 54.937 | 14.505 | 11.578 | 3.740 | 66.23 | 88.01 | 77.65 |
| 9 | P-1 | 54.937 | 13.524 | 35.486 | 3.740 | 68.32 | 51.60 | 52.86 |
| 10 | P-1 | 54.938 | 11.579 | 7.487 | 16.538 | 75.24 | 59.06 | 66.10 |

a Sort of energy per molecule. b SG=Space Group.

Table S2. The optimized predicted crystal cell parameters and the corresponding experimental values for ATT and TCATT

| No. | SGa | a/Å | b/Å | c/Å | α/° | β/° | γ/° |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ATTb | P21/C | 11.29 | 5.03 | 14.31 | 90.00 | 92.00 | 90.00 |
| ATT | P21 | 11.94 | 4.92 | 14.70 | 90.00 | 91.45 | 90.00 |
| TCATT | P21/C | 7.66 | 27.39 | 10.72 | 90.00 | 96.26 | 90.00 |

a SG=Space Group. b J. L. Brusso et al., Chem. Mater., 2008, 20, 2484–2494.

Table S3. The optimized bond lengths (Å), bond angels (°), dihedral angles (°) of ATT in neutral and ionic states based on B3LYP/6-31G(d,p) and its corresponding experimental values

|  | Expt | Neutral | Anion | Cation |
| --- | --- | --- | --- | --- |
| R(H1-C2) | 1.140 | 1.082 | 1.082 | 1.082 |
| R(C2-S3) | 1.730 | 1.742 | 1.753 | 1.747 |
| R(S3-C4) | 1.726 | 1.753 | 1.769 | 1.744 |
| R(C4-C5) | 1.438 | 1.437 | 1.425 | 1.427 |
| R(C5-C6) | 1.396 | 1.399 | 1.411 | 1.404 |
| R(C5-C7) | 1.429 | 1.443 | 1.444 | 1.440 |
| A(H1-C2-S3) | 120.00 | 119.50 | 119.69 | 119.00 |
| A(C2-S3-C4) | 91.40 | 91.26 | 91.20 | 91.09 |
| A(S3-C4-C5) | 125.88 | 125.83 | 125.06 | 126.40 |
| D(H1-C2-S3-C4) | ‒179.87 | ‒179.97 | 180.01 | 180.02 |
| D(C2-S3-C4-C5) | 178.62 | ‒180.02 | ‒180.02 | ‒180.01 |
| D(S3-C4-C5-C6) | ‒1.14 | ‒0.01 | ‒0.01 | ‒0.02 |
| D(C4-C5-C7-C8) | 178.11 | ‒179.98 | ‒179.99 | 180.00 |

Table S4. The optimized bond lengths (Å), bond angels (°), dihedral angles (°) of TBATT in neutral and ionic states based on B3LYP/6-31G(d,p) and its corresponding experimental values

|  | Expt | Neutral | Anion | Cation |
| --- | --- | --- | --- | --- |
| R(Br1-C2) | 1.865 | 1.881 | 1.894 | 1.865 |
| R(C2-S3) | 1.732 | 1.747 | 1.753 | 1.755 |
| R(S3-C4) | 1.732 | 1.755 | 1.771 | 1.746 |
| R(C4-C5) | 1.427 | 1.435 | 1.423 | 1.426 |
| R(C5-C6) | 1.383 | 1.399 | 1.410 | 1.403 |
| R(C5-C7) | 1.432 | 1.443 | 1.444 | 1.441 |
| A(Br1-C2-S3) | 119.23 | 119.57 | 119.65 | 119.16 |
| A(C2-S3-C4) | 91.29 | 90.56 | 90.23 | 90.60 |
| A(S3-C8-C7) | 125.89 | 125.55 | 124.69 | 126.08 |
| D(Br1-C2-S3-C4) | 178.37 | ‒180.01 | ‒180.01 | ‒180.01 |
| D(C2-S3-C4-C5) | ‒178.88 | 180.01 | 180.02 | 180.00 |
| D(S3-C4-C5-C6) | ‒2.45 | 0.01 | 0.01 | 0.01 |
| D(C4-C5-C7-C8) | ‒179.59 | 180.00 | 180.00 | 180.00 |

Table S5. The optimized bond lengths (Å), bond angels (°), dihedral angles (°) of TCATT in neutral and ionic states based on B3LYP/6-31G(d,p)

|  | Neutral | Anion | Cation |
| --- | --- | --- | --- |
| R(N9-C1) | 1.165 | 1.168 | 1.164 |
| R(C1-C2) | 1.416 | 1.411 | 1.416 |
| R(C2-S3) | 1.751 | 1.767 | 1.764 |
| R(S3-C4) | 1.745 | 1.759 | 1.739 |
| R(C4-C5) | 1.438 | 1.426 | 1.429 |
| R(C5-C6) | 1.398 | 1.408 | 1.404 |
| R(C5-C7) | 1.442 | 1.442 | 1.440 |
| A(C1-C2-S3) | 120.62 | 121.13 | 119.94 |
| A(C2-S3-C4) | 90.88 | 90.83 | 90.75 |
| A(S3-C4-C5) | 125.40 | 124.76 | 125.96 |
| D(C1-C2-S3-C4) | 180.00 | ‒180.00 | ‒180.00 |
| D(C2-S3-C4-C5) | 179.99 | ‒180.00 | 179.99 |
| D(S3-C4-C5-C6) | 0.00 | 0.00 | 0.00 |
| D(C4-C5-C7-C8) | 180.00 | ‒180.00 | 180.00 |