Supporting Information

Fig. S1 The histograms of first and stable (third time) static adsorption capacity (g/m2) n-hexane (a) and (c), and 93# gasoline (b) and (d), respectively. A-F is SBA-15 (A), SBA-15-A (B), SBA-15-B (C), SBA-15-C (D), SG (E) and AC (F), respectively.

Fig. S2 Relationship between first static n-hexane adsorption capacity and structure parameters of

different samples, micro surface area (a), micro pore volume (b), surface area (c) and pore volume

(d), respectively. A-F is SBA-15 (A), SBA-15-A (B), SBA-15-B (C), SBA-15-C (D), SG (E), and AC (F), respectively.

Fig. S3 The histograms of static competitive adsorption capacities of n-hexane and water vapor with the adsorbates of n-hexane and water volume ratio of 4:1 (a) and 1:1 (b), mn-hexane/mwater of 4:1 (c) and 1:1 (d), and desorption capacities of 4:1 (e) and 1:1 (f), respectively. A-F is SBA-15 (A), SBA-15-A (B), SBA-15-B (C), SBA-15-C (D), SG (E), and AC (F), respectively.

Fig. S4 The breakthrough curves for n-hexane of SBA-15 (■), SBA-15-A (●), and SBA-15-C (▲) with the flow rate of 0.10 L/min and the concentration of n-hexane of  0.45 g/L. (a) is the first time, (b) is the comparison of the breakthrough times of 3 times, (c) is the comparison of the equilibrium adsorption capacities of 3 times and (d) is the comparison of the desorption efficiencies of 3 times, respectively.

Table S1 Three successive dynamic n-hexane adsorption and desorption properties of SBA-15, SBA-15-A and SBA-15-C.

| Samples | Breakthrough time (min) | Equilibrium adsorption time (min) | qe (g/gadsorbent) | Desorption efficiency (%) |
| --- | --- | --- | --- | --- |
| SBA-15-1st | 50 | 70 | 0.74 | 99.1 |
| SBA-15-2nd | 51 | 72 | 0.75 | 99.4 |
| SBA-15-3rd | 50 | 70 | 0.74 | 98.9 |
| SBA-15-A-1st | 42 | 64 | 0.66 | 99.3 |
| SBA-15-A-2nd | 43 | 66 | 0.67 | 98.9 |
| SBA-15-A-3rd | 42 | 64 | 0.66 | 98.8 |
| SBA-15-C-1st | 40 | 62 | 0.64 | 98.8 |
| SBA-15-C-2nd | 39 | 62 | 0.63 | 99.4 |
| SBA-15-C-3rd | 40 | 62 | 0.64 | 99.1 |