Supplementary Material

TABLE SI.  Standard crystallographic data for the SrTiO3 lattice structure.

TABLE SII.  Crystallographic data of S3T lattice structure.

TABLE SIII.  Formation enthalpy of Pb-doped Sr3Ti2O7.

TABLE SIV.  Crystallographic data of Sr4Ti3O10 phase in SPT-125 sintered at 1550 °C for 2 h.

FIG.  SI.  Crystal structures of the SrTiO3 and Sr3Ti2O7 phases.

FIG.  SII Rietveld fittings of Sr3Ti2O7.

FIG. SIII.  Crystal structure of Sr4Ti3O10.

TABLE SI.  Standard crystallographic data for the SrTiO3 lattice structure.

| Lattice parameter/10-10m | a=b=c =3.905 |  |  |  |
| --- | --- | --- | --- | --- |
| Bond length/10-10m | Ti-Oi (i=1, 2, 3) | 1.952 | Sr-Oj (j=1, 2, 3, 4, 5, 6) | 2.761 |
| Bond angle/° | O1-Ti-O2 | 90 | O2-Sr-Oi (i=3, 6) | 60 |
|  | O1-Ti-O3 | 90 | O2-Sr-O4 | 90 |
|  | O2-Ti-O3 | 90 | O2-Sr-O5 | 120 |
|  | O1-Ti-O1 | 180 | O3-Sr-O4 | 60 |
|  | O2-Ti-O2 | 180 | O3-Sr-Oi (i=5, 6) | 120 |
|  | O3-Ti-O3 | 180 | O4-Sr-O5 | 60 |
|  | O1-Sr-Oi (i=2, 4, 5, 6) | 60 | O4-Sr-O6 | 90 |
|  |  |  | O5-Sr-O6 | 90 |
|  | O1-Sr-O3 | 90 | Sr-O-Sr | 180 |

TABLE SII.  Crystallographic data of S3T lattice structure.

| Bond length/10-10m |  |  | Bond angle/° |  |
| --- | --- | --- | --- | --- |
| Ti-O1 |  | 1.951 | O1-Ti-O2 | 90 |
| Ti-O2 |  | 1.951 | O1-Ti-O3 | 90 |
| Ti-O3 |  | 1.933 | O2-Ti-O3 | 90 |
| Sr1-O1 |  | 2.759 | O1-Sr1-O2 | 59.85 |
| Sr1-O2 |  | 2.746 | O1-Sr1-O3 | 59.85 |
| Sr1-O3 |  | 2.746 | O2-Sr1-O3 | 60.3 |
| Sr2-O1 |  | 2.761 | O1-Sr2-O2 | 87.89 |
| Sr2-O2 |  | 2.544 | O1-Sr2-O3 | 60.66 |
| Sr2-O3 |  | 2.676 | O2-Sr2-O3 | 133.19 |
| Lattice parameter /10-10m | a=b | 3.9014 | O1-Sr2-O1 | 175.78 |
|  | c | 20.3484 | O3-Sr2-O3 | 62.06 |

TABLE SIII.  Formation enthalpy of Pb-doped Sr3Ti2O7.

| Super cell | Doping concentration | Atomic number |  |  |  | Formation enthalpy/eV |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Sr | Ti | O | Pb | Sr1 position | Sr2 position |
| 1×1×1 | 0 | 6 | 4 | 14 | 0 | -3.438 | -3.438 |
| 2×2×2 | 0.0208 | 48 | 32 | 112 | 1 | -3.417 | -3.422 |
| 2×3×1 | 0.0278 | 35 | 24 | 84 | 1 | -3.408 | -3.414 |
| 3×3×1 | 0.0370 | 52 | 36 | 126 | 2 | -3.404 | -3.410 |
| 2×2×1 | 0.0417 | 23 | 16 | 56 | 1 | -3.393 | -3.399 |
| 3×1×1 | 0.0556 | 17 | 15 | 42 | 1 | -3.378 | -3.385 |
| 2×1×1 | 0.0833 | 11 | 8 | 28 | 1 | -3.348 | -3.356 |
| 1×1×1 | 0.167 | 5 | 4 | 14 | 1 | -3.256 | -3.269 |
| 1×1×1 | 0.334 | 4 | 4 | 14 | 2 | -3.069 | -3.088 |

TABLE SIV.  Crystallographic data of Sr4Ti3O10 phase in SPT-125 sintered at 1550°C for 2 h.

|  | Symbols | Standard data* | SPT-125 |
| --- | --- | --- | --- |
| Lattice parameter/10-10m | a=b | 3.9 | 3.9017 |
|  | c | 28.1 | 28.1499 |
| Ti-O bond length/10-10m | D1 | 1.911 | 1.914 |
|  | D2 | 1.855 | 1.858 |
|  | D3 | 1.967 | 1.970 |
| Sr2-O2 bond length/10-10m | S1 | 2.557 | 2.562 |

* Lattice parameter data from PDF No. 97-003-4630 and the bond length calculated by Jade.

(a) SrTiO3                                                             (b) Sr3Ti2O7

FIG. SI.  Crystal structures of the SrTiO3 and Sr3Ti2O7 phases.

FIG. SII.  Rietveld fitting of Sr3Ti2O7.

FIG. SIII.  Crystal structure of Sr4Ti3O10.