Supplementary Material

Near-zero thermal expansion and phase transition in In0.5(ZrMg)0.75Mo3O12

Luciana P. Prisco,1 Patricia I. Pontón,1 W. Paraguassu2, Carl P. Romao,3 Mary Anne White,3,4,5 Bojan A. Marinkovic1*

1 Departamento de Engenharia Química e de Materiais, Pontifícia Universidade Católica 22451-900 Rio de Janeiro, RJ, Brasil, Brasil

2 Faculdade de Física, Universidade Federal do Pará, P.O. Box 479, Belém, PA, 66075-110, Brasil

3 Department of Chemistry, Dalhousie University, Halifax, Nova Scotia, B3H 4R2, Canada

4 Institute for Research in Materials, Dalhousie University, Halifax, Nova Scotia, B3H 4R2, Canada

5 Department of Physics and Atmospheric Sciences, Dalhousie University, Halifax, Nova Scotia, B3H 4R2, Canada

 Corresponding author. Tel: +55-21-35271954;

E-mail address: bojan@puc-rio.br  (Bojan Marinkovic)

FIG. S1. DSC (black) and first derivate DSC (red) curves of In0.5(ZrMg)0.75Mo3O12 raw precursor powder (inset figure: magnified view of DSC curve, showing the exothermic peak corresponding to crystallization of the In0.5(ZrMg)0.75Mo3O12 phase).

TABLE SI. Mass percentage of each element of In0.5(ZrMg)0.75Mo3O12 obtained by EDS.

| Element | Measure 1 (%) | Measure 2 (%) | Average (%) | Theoretical value (%) |
| --- | --- | --- | --- | --- |
| In | 9.68 | 7.86 | 8.8 | 9.20 |
| Zr | 10.12 | 9.25 | 9.7 | 10.97 |
| Mg | 2.59 | 3.26 | 2.9 | 2.89 |
| Mo | 43.38 | 39.03 | 41.2 | 46.15 |
| O | 34.23 | 45.45 | 39.8 | 30.78 |

FIG. S2. Raman spectra of In0.5(ZrMg)0.75Mo3O12 for different temperatures between 24 °C and 250 °C (blue numbers) in the wavenumber range of (a) 20–120 cm−1, (b) 125–325 cm−1 and (b) 900–990 cm−1.

FIG. S3. Temperature dependence of the orthorhombic unit cell parameters of In0.5(ZrMg)0.75Mo3O12 (estimated standard deviation bars are not shown, because they are smaller than the symbols).