# Supporting Information

Investigation of Thiophene Flanked Diketopyrrolopyrrole Monomers with Straight and Branched Alkyl Chains and their Electropolymerization Study

Supreetha Paleyanda Ponnappa,1 Sivanesan Arumugam,1* Sergei Manzhos,2 Jennifer MacLeod, 1, 3 Henry J. Spratt,3 Anthony O’Mullane,1 Prashant Sonar 1*

1. School of Chemistry, Physics and Mechanical Engineering, Nanotechnology and Molecular Sciences Discipline, Queensland University of Technology (QUT), Brisbane 4001, Australia.

2. Department of Mechanical Engineering, Faculty of Engineering, National University of Singapore Block E2 #07-08, 9 Engineering Drive 1, Singapore 117576.

3. Central Analytical Research Facility (CARF), Institute of Future Environments, Queensland University of Technology (QUT), Brisbane 4001, Australia.

sonar.prashant@qut.edu.au, sivanesan.arumugam@qut.edu.au

Figure S1. 1H (400 MHz, CDCl3) and 13C NMR (100 MHz, CDCl3) spectra of EH-DPP

Figure S2. 1H (400 MHz, CDCl3) and 13C NMR (100 MHz, CDCl3) spectra of Octyl-DPP

Figure S3. Theoretical UV-visible absorption (blue) and photoluminescence (red) spectra of the monomers EH-DPP and Octyl-DPP monomers in DCM. The spectra are broadened by 0.25 eV HWHM.

Figure S4. The above figures are the reduction (-2 V to 0V) and oxidation (0V to +2V) of the electropolymerized polymer thin film poly-(EH-DPP) deposited on glassy-carbon electrodes in 0.1 M TBAPF6/DCM. The scan rate employed in all cases was 0.1 Vs-1.

Figure S5. The above figures are the reduction (-2V to 0V) and oxidation (0V to +2V) of the electropolymerized polymer thin film poly-(Octyl-DPP) deposited on glassy-carbon electrodes in 0.1 M TBAPF6/DCM. The scan rate employed in all cases was 0.1 Vs-1.

Figure S6: Continuous cyclic voltammograms of blank glassy carbon electrode in dichloromethane containing 0.1 M TBAPF6 as supporting electrolyte.

Figure S7: Continuous cyclic voltammograms of ITO electrode in dichlromethane containing 0.1 M TBAPF6 as supporting electrolyte.

Figure S8: The coverage of electropolyemrized oligomer/polymer EH-DPP (upper) and Octyl-DPP (lower) island type AFM micrograph images measured by flooding analysis. The EH-DPP has 16.6% island coverage, whereas the Octyl-DPP has only 2.2% coverage.

Figure S9: The above figures are the oxidation and reduction of monomers [A] EH-DPP and [B] Octyl- DPP (-2V to 2V) on glassy-carbon electrodes in 0.1 M TBAPF6/DCM. The scan rate employed in both cases was 0.1 Vs-1.

Figure S10. Cyclic voltammograms of [A] poly(EH-DPP) and [B] poly(octyl-DPP) deposited on glassy-carbon electrodes in 0.1 M TBAPF6/DCM solution. The scan rate employed in all cases was 10, 20 ,30, 40, 50, 60, 70, 80, 90, 100 mVs-1.

Figure S 11: Linear dependence of anodic oxidation peak current (i) on scan rate of poly(EH-DPP) [A] and poly(octyl-DPP) [B] monomers on GC electrode under irreversible conditions in DCM/0.1M TBAPF6