Supplementary Information

An impedance sensor for the detection of formaldehyde vapor using ZnO

nanoparticles

Padmanathan Karthick  Kannana,b, Ramiah  Saraswathia,*

aDepartment of Materials Science, School of Chemistry, Madurai Kamaraj University, Madurai – 625021,

Tamil Nadu, India.

bSchool of Chemical Engineering, Sungkyunkwan University, Suwon 16419, Republic of Korea

E-mail: drrsaraswathi@gmail.com

Fig. S1. Plots of Z’’ against log frequency at various concentration of formaldehyde (A) laboratory prepared ZnO sample (B) commercial ZnO sample. Concentration of formaldehyde: (a) 100 (b) 200 (c) 300 (d) 400 (e) 500 (f) 600 (g) 700 and (h) 800 ppm

Fig. S2. Nitrogen adsorption and desorption isotherms of ZnO (a) laboratory prepared sample and (b) commercial sample at 77 K

Fig. S3. Stability data of sensor at 100 ppm of formaldehyde for laboratory prepared sample () and commercial sample ()

Table SI. Variation in relaxation frequency (fr) with concentration of formaldehyde

| Concentration of formaldehyde (ppm) | Relaxation frequency, (fr) (Hz) |  |
| --- | --- | --- |
|  | Laboratory prepared ZnO sample | Commercial ZnO sample |
| 100 | 891 | 1260 |
| 200 | 2818 | 1590 |
| 300 | 5000 | 2820 |
| 400 | 7000 | 7000 |
| 500 | 15900 | 11200 |
| 600 | 17800 | 12600 |
| 700 | 28300 | 22400 |
| 800 | 126000 | 25000 |

Table SII.  Equivalent circuit parameters for laboratory prepared ZnO sample on exposure

to air and different concentration of formaldehyde

| Air / Concentration of formaldehyde in ppm | Rg (ohm) | Rgb (ohm) | Cg (F) | Cgb (F) |
| --- | --- | --- | --- | --- |
| Air | 1.598 × 108 | - | 1.167 × 10-11 | - |
| 100 | 5.503 × 106 | 2.544 × 105 | 1.174 × 10-11 | 2.965 × 10-11 |
| 200 | 3.529 × 106 | 2.523 × 105 | 2.058 × 10-11 | 3.708 × 10-11 |
| 300 | 2.343 × 106 | 1.6277 × 105 | 2.446 × 10-11 | 4.605 × 10-11 |
| 400 | 1.466 × 106 | 1.557 × 105 | 1.658 × 10-11 | 3.340 × 10-11 |
| 500 | 7.973 × 105 | 1.520 × 105 | 2.817 × 10-11 | 2.638 × 10-11 |
| 600 | 4.991 × 105 | 1.078 × 105 | 2.535 × 10-11 | 1.304 × 10-9 |
| 700 | 2.245 × 105 | 6.805 × 104 | 3.773 × 10-11 | 1.310 × 10-9 |
| 800 | 1.057 × 105 | 1.522 × 104 | 1.432 × 10-11 | 2.817 × 10-9 |

Table SIII. Equivalent circuit parameters for commercial ZnO sample on exposure to air and

different concentration of formaldehyde

| Air / Concentration of formaldehyde in ppm | Rg (ohm) | Rgb (ohm) | Cg (F) | Cgb (F) |
| --- | --- | --- | --- | --- |
| Air | 1.583 × 108 | - | 1.169 × 10-11 | - |
| 100 | 5.336 × 106 | 2.905 × 105 | 1.030 × 10-11 | 3.332 × 10-11 |
| 200 | 3.445 × 106 | 2.046 × 105 | 1.059 × 10-11 | 4.065 ×10-11 |
| 300 | 3.252 × 106 | 2.023 × 105 | 4.284 × 10-11 | 3.289 × 10-11 |
| 400 | 6.651 × 105 | 1.138 × 105 | 1.951 × 10-11 | 2.960 × 10-11 |
| 500 | 5.253 × 105 | 1.045 × 105 | 2.673 × 10-11 | 2.084 × 10-11 |
| 600 | 2.930 × 105 | 1.013 × 105 | 3.196 × 10-11 | 1.647 × 10-11 |
| 700 | 2.265 × 105 | 9.837 × 104 | 1.316 × 10-11 | 1.038 × 10-9 |
| 800 | 1.314 × 105 | 5.512 × 104 | 1.396 × 10-11 | 1.459 × 10-9 |