New insights on the basicity of ZnAl-Zr hydrotalcites activated at low temperature and their application in transesterification of soybean oil

Supplementary Material

Denis A. Cabrera-Munguiaa, Horacio Gonzáleza,*, Francisco Tzompantzib, Aída Gutiérrez-Alejandrec, Dora A. Solís-Casadosd, José L. Ricoa

aFacultad de Ingeniería Química, Universidad Michoacana de San Nicolás de Hidalgo

58030, Morelia, Michoacán, México

bDepto. de Química, Facultad de Química, Universidad Autónoma Metropolitana- Iztapalapa, 09340, Ciudad de México, México

cUNICAT, Depto. de Ingeniería Química, Facultad de Química, Universidad Nacional Autónoma de México, 04510, Ciudad de México, México

dCentro Conjunto de Investigación en Química Sustentable, UAEM-UNAM, 50200, Toluca, México

TABLE SI. Lattice parameters and textural properties of ZnAl-Zr(X) catalysts. Reproduced with permission from ref. 23. Copyright 2017 Elsevier.

| Catalyst | Parameter a (Å) | Parameter c (Å) | SBET (m2/g) | DBJH (nm) |
| --- | --- | --- | --- | --- |
| ZnAl-Zr(0.0) | 2.9347 | 22.6732 | 30 | 15 |
| ZnAl-Zr(0.10) | 2.9362 | 22.7521 | 41 | 13 |
| ZnAl-Zr(0.25) | 2.9367 | 22.7916 | 76 | 10 |

FIG. S1.  Correlation between catalytic activity and total basicity for ZnAl-Zr(0.0) catalysts activated at different temperatures.

FIG. S2. DTA curves of ZnAl-Zr(X) materials. Reproduced with permission from ref. 23. Copyright 2017 Elsevier.

FIG. S3. XRD patterns of ZnAl-Zr(0.0) as a function of activation temperature (a) 100ºC and 150ºC and (b) 200ºC and 250ºC, identified species: º Hydrozincite (Zn5(CO3)2(OH)6), ▼Zinc carbonate (ZnCO3), ▲ Zincite (ZnO). Reproduced with permission from ref. 23. Copyright 2017 Elsevier.