Supplementary Information

Self-Organized Wrinkling of Liquid Crystalline Polymer with Plasma Treatment

Jaehyun Sim1, Sihwa Oh1, Se-Um Kim2, Kyuyoung Heo3, Seung-Chul Park4, and Jun-Hee Na1,5*

1Department of Electric, Electronic and Communication Engineering Education, Chungnam National University, 99 Deahak-ro, Yuseong-gu, Daejeon 34134, Republic of Korea

2Department of Physics and Astronomy, University of Pennsylvania, Philadelphia, Pennsylvania 19104, USA

3Reliability Assessment Center, Korea Research Institute of Chemical Technology, Daejeon 34114, Republic of Korea

4Department of Nature Inspired Nanoconvergence Systems, Korea Institute of Machinery and Materials, Daejeon 34103, Republic of Korea

5Department of Convergence System Engineering, Chungnam National University, 99 Deahak-ro, Yuseong-gu, Daejeon 34134, Republic of Korea

*E-mail: junhee.na@cnu.ac.kr

Figure S1

Figure S1. Influence of the rubbing process on PVA film. Atomic force microscopic images of (a) unrubbed surface and (b) homogeneously aligned PVA film with 3000 rpm in speed. Here, arrows indicate the location of the scratches that occurred during the rubbing process.