Supplementary Information

Kinetic Control of CeO2 nanoparticles for Catalytic CO Oxidation

Bingqi Han,1 Huixia Li,1 Liping Li,1 Yan Wang,1 Yuelan Zhang,1 Guangshe Li1,a)

1State Key Laboratory of Inorganic Synthesis and Preparative Chemistry, College of Chemistry, Jilin University, Changchun 130012, People’s Republic of

China

a)Address all correspondence to this author. e-mail: guangshe@jlu.edu.cn

Fig. S1. Powder XRD patterns of CeO2 obtained by sintering cerium nitrate at the temperature ranged from 300 to 1000oC for 2h

Table S1 Average particle sizes of CeO2 nanoparticles determined by TEM and XRD analyses

| Label | Nanoparticle Size (avg.) |  |
| --- | --- | --- |
|  | TEM (nm) | XRD (nm) |
| CeO2-700 | 19.1 | 18.9 |
| CeO2-800/8h | 58.0 | 57.5 |
| CeO2-900 | 67.1 | 66.7 |
| CeO2-1000 | 100.3 | 79.7 |

Table S2 Peak areas of O1s components and their ratios

| samples | O1 area | O2 area | Ratio |
| --- | --- | --- | --- |
| Pt/CeO2-500 | 3595.78 | 5791.87 | 0.620 |
| Pt/CeO2-700 | 5168.94 | 8309.08 | 0.622 |
| Pt/CeO2-900 | 1961.06 | 7126.78 | 0.275 |

Fig. S2. TG curve of Ce(NO3)3·6H2O recorded in the temperature range from 25 to 1200oC.

FIG. S3. (a) Nitrogen desorption/adsorption isotherms and (b) the corresponding BJH (Barret-Joyner-Halenda) pore size distribution curves for the given samples.

Table S3 Average particle sizes for the different CeO2 nanoparticles obtained by   XRD analysis.

| samples | Nanoparticle Size (avg.) |
| --- | --- |
| CeO2-600/1h | 13.48948 |
| CeO2-600/2h | 14.6007 |
| CeO2-600/4h | 15.05496 |
| CeO2-600/6h | 16.18135 |
| CeO2-600/8h | 16.31761 |