Supplementary Material for

High-efficiency Photocatalytic Performance and Mechanism of Silver-based Metal-Organic Framework

Xiu-Ju Yin1,2* and Long-Guan Zhu1*

1Department of Chemistry, Zhejiang University, Hangzhou 310027, P. R. China

2College of Chemistry and Biology Engineering, Hechi University, Yizhou 546300, P. R. China

*Correspondence and requests for materials should be addressed to Long-Guan Zhu or Xiu-Ju Yin (Email: gxyxj505@163.com; chezlg@zju.edu.cn)

Figure S1. The TGA for 1.

100 μm

Figure S2.  Scanning electron microscopy (SEM) micrograph of 1.

Figure S3. The N2 adsorption/desorption experiment of 1.

Figure S4. Cyclic voltammograms of 1 on platinum plates in an acetonitrile solution of 0.1 mol·L-1 Bu4NPF6 at a sweep rate of 0.1 V·s-1.

Figure S5. The photocatalytic degradation products of MB by ESI mass spectra.

Figure S6. The PXRD of 1.

Figure S7. Cycle runs of 1 for the degradation of MB.

Table SI. Crystallographic Data of 1.

| 1 |  |
| --- | --- |
| Empirical formula | C18H8Ag3O12 |
| Formula weight | 739.85 |
| Temperature (K) | 296(2) |
| Wavelength (Å) | 0.71073 |
| Crystal system | Orthorhombic |
| Space group | Fddd |
| a (Å); b (Å); c (Å) | 14.8812(7); 25.8729(14); 36.3742(18) |
| α ( º); β ( º); γ ( º) | 90; 90; 90 |
| Volume (Å3); Z | 14004.8(12);195 |
| Dcaled, (g.cm-3) | 2.807 |
| Limiting indices | -20  h  19; -33  k  35; -48  l 44 |
| F(000) | 11217 |
| Θ range for data collection(º) | 3.8 ~29.0 |
| Reflections/parameters/restraints /unique | 3085/301/0 |
| Rint | 0.041 |
| R[F2 > 2σ(F2)] | 0.024 |
| wR(F2) | 0.085 |
| S | 0.97 |
| (Δ/σ)max | 0.001 |
| Δρmax/Δρmin(e Å−3) | 0.88/-1.13 |
| CCDC | 1851398 |

Table SII. Selected Bond Lengths (nm) and Bond Angles (°) for 1.

| 1 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Bond | Dist. (Å) | Bond | Dist. (Å) | Bond | Dist. (Å) |
| Ag(1)-Ag(1)A | 2.9891 (6) | Ag(1)-Ag(2) | 3.3766 (4) | Ag(1)-Ag(4)B | 3.1838 (3) |
| Ag(2)-Ag(2)E | 2.9653 (6) | Ag(2)-Ag(2)A | 2.9677 (6) | Ag(3)-Ag(4) | 3.2111 (6) |
| Ag(1)-O(8) | 2.564 (2) | Ag(1)-O(9)C | 2.271 (2) | Ag(1)-O(10)D | 2.231 (2) |
| Ag(2)-O(3) | 2.477 (2) | Ag(2)-O(5)F | 2.212 (2) | Ag(2)-O(6)G | 2.220 (2) |
| Ag(3)-O(7)B | 2.551 (2) | Ag(3)-O(7) | 2.551 (2) | Ag(3)-O(11)H | 2.499 (2) |
| Ag(3)-O(11)K | 2.499 (2) | Ag(4)-O(8) | 2.108 (2) | Ag(4)-O(8)B | 2.108 (2) |
| Angle | (°) | Angle | (°) | Angle | (°) |
| Ag(4)B-Ag(1)-Ag(2) | 130.492 (10) | O(8)-Ag(1)-Ag(2) | 156.61 (6) | O(8)-Ag(1)-Ag(4)B | 41.30 (5) |
| Ag(2)A-Ag(2)-Ag(1) | 79.544 (8) | Ag(2)E-Ag(2)-Ag(1) | 156.155 (13) | Ag(1)B-Ag(4)-Ag(1) | 155.863 (17) |
| Ag(3)-Ag(4)-Ag(1)B | 102.069 (9) | Ag(3)-Ag(4)-Ag(1) | 102.069 (9) | Ag(4)A-Ag(4)-Ag(1)B | 77.931 (9) |
| Ag(4)A-Ag(4)-Ag(1) | 77.931 (9) | Ag(4)A-Ag(4)-Ag(3) | 180.0 | O(8)B-Ag(4)-Ag(1)B | 53.38 (7) |
| O(9)C-Ag(1)-Ag(2) | 53.10 (6) | O(9)C-Ag(1)-Ag(4)B | 78.42 (6) | O(9)C-Ag(1)-O(8) | 109.12 (8) |
| O(10)D-Ag(1)-Ag(2) | 109.89 (6) | O(10)D-Ag(1)-Ag(4)B | 111.47 (6) | O(10)D-Ag(1)-O(8) | 91.61 (8) |
| O(8)-Ag(4)-Ag(1)B | 125.29 (7) | O(8)-Ag(4)-Ag(1) | 53.38 (7) | O(8)B-Ag(4)-Ag(1) | 125.29 (7) |
| O(8)B-Ag(4)-Ag(3) | 92.56 (7) | O(8)-Ag(4)-Ag(3) | 92.56 (7) | O(8)-Ag(4)-O(8)B | 174.87 (13) |

Symmetry codes:  (A) x, −y+5/4, −z+5/4; (B) −x+5/4, y, −z+5/4; (C) x+1/4, −y+1, z+1/4; (D) x+1/4, y+1/4, −z+1; (E) −x+9/4, y, −z+5/4; (F) −x+2, y+1/4, z+1/4; (G) −x+2, −y+1, −z+1; (H) x−1/4, y−1/4, −z+1; (I) −x+3/2, y−1/4, z+1/4; (J) −x+2, y−1/4, z−1/4; (K) x−1/4, −y+1, z−1/4.

Table SIII. Hydrogen bonds for 1.

| 1 |  |  |  |  |
| --- | --- | --- | --- | --- |
| D–H···A | d(D–H)/Å | d(H···A)/Å | d(D···A)/Å | D–H···A/(º) |
| O(2)-H(2)···O(9)L | 0.82 | 1.77 (1) | 2.582 (4) | 174 (4) |
| O(12)-H(12)···O(7)D | 0.82 | 1.77 (1) | 2.585 (3) | 173 (3) |

Symmetry codes: (D) x+1/4, y+1/4, −z+1; (L) −x+3/2, y−1/4, z+1/4.