Supplementary Material for

The effect of plastic on performance of activated carbon and study on adsorption of methylene blue

Peiyong Maa, Meina Maa, Jinzhou Wua, Guizhi Qianb, , Dongqiang Wuc, Xianwen Zhangb,*

a School of Mechanical Engineering, Heifei University of Technology, 193 Tunxi Road, Hefei, 230009, China

b Advanced Energy Technology and Equipment Research Institute, Heifei University of Technology, 193 Tunxi Road, Hefei, 230009, China

c School of Automotive and Transportation Engineering, Heifei University of Technology, 193 Tunxi Road, Hefei, 230009, China

* Corresponding author. Advanced Energy Technology and Equipment Research Institute, Heifei University of Technology, 193 Tunxi Road, Hefei, 230009, China

E-mail sddress: xianwen.zhang@hfut.edu.cn (X. Zhang)

TABLE SⅠ: Peak assignments for the FTIR spectra of the AC sample

| Wavenumbers (cm-1) | Infrared absorption |
| --- | --- |
| 3440 | -OH stretching |
| 1610~1370 | C=O stretching, C=C stretching of aliphatic ketone |
| 1550~1500 | benzene ring |
| 1373 | CH stretching of alkanes |
| 1100~1020 | C-O、C-O-C stretching |
| 860~670 | Out of plane bending of =CH on benzene ring |

TABLE SⅡ: Parameters and determination coefficients of the isotherm models for MB adsorption onto AC

| Langmuir | Freundlich | Redlich-Peterson | Dubinin-Radushkevich |
| --- | --- | --- | --- |
| qm = 472.19 | KF = 309.23 | KRP = 9400.19 | qm = 470.93 |
| KL = 16.63 | nF=10.73 | aRP = 21.92 | KDR = 1.40*10-8 |
| RL = 0.00007-0.0006 |  | g = 0.9765 | E = 5.97 kJ/mol |
| R2 = 0.9824 | R2 = 0.8919 | R2 = 0.9894 | R2 = 0.9771 |
| Δq (%) = 2.43 | Δq (%) = 4.46 | Δq (%) = 3.56 | Δq (%) = 3.73 |

TABLE SⅢ: Parameters and determination coefficients of the kinetic models for MB adsorption

|  | Initial concentrations (mg/L) |  |  |  |
| --- | --- | --- | --- | --- |
|  | 300 | 400 | 500 | 600 |
| qe.exp (mg/g) | 300.02 | 399.21 | 475.90 | 490.64 |
| Pseudo-1st-order |  |  |  |  |
| qe (mg/g) | 297.56 | 386.46 | 438.23 | 461.96 |
| k1 (1/min) | 2.4742 | 1.6730 | 1.4953 | 1.8976 |
| ho (mg/(g.min)) | 736.21 | 646.54 | 655.30 | 876.59 |
| R2 | 0.9971 | 0.9852 | 0.9600 | 0.9704 |
| Δqe (%) | 1.70 | 3.87 | 6.30 | 5.56 |
| Pseudo-2st-order |  |  |  |  |
| qe (mg/g) | 300.15 | 394.49 | 450.32 | 472.01 |
| k2 (1/min) | 0.0310 | 0.0093 | 0.0062 | 0.0085 |
| ho (mg/(g.min)) | 2794.35 | 1450.86 | 1253.20 | 1889.03 |
| R2 | 0.9994 | 0.9975 | 0.9825 | 0.9875 |
| Δqe (%) | 0.80 | 1.60 | 4.15 | 4.10 |
| Elovich |  |  |  |  |
| α (mg/(g.min)) | 1.26*1031 | 2.15*1012 | 5.75*1008 | 2.79*1011 |
| β (g/mg) | 0.2486 | 0.0765 | 0.0474 | 0.0587 |
| R2 | 0.9963 | 0.9924 | 0.9956 | 0.9971 |
| Δqe (%) | 1.80 | 2.79 | 2.19 | 2.44 |

TABLE SⅣ: Proximate and ultimate analysis of the SS

| Proximate analysis /wt.% (ad) |  |  |  |  | Ultimate analysis /wt.% (ad) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Moisture | Ash | Volatile | Fixed carbon |  | C | H | O | N |
| 9.40 | 3.96 | 73.10 | 13.54 |  | 40.12 | 4.56 | 41.75 | 0.15 |

Ad: air-dried basis

TABLE SⅤ: Components analysis of the SS

| Components analysis /wt.% |  |  |
| --- | --- | --- |
| cellulose | hemicellulose | lignin |
| 50.64 | 17.50 | 18.73 |

TABLE SⅥ: Kinetic and Isotherm models

|  | Freundlich |  |
| --- | --- | --- |
|  | Langmuir |  |
| Isotherm | Redlich-Peterson |  |
|  | Dubinin-Radushkevich |  |
|  | Pseudo-first-order |  |
|  | Pseudo-second-order |  |
| Kinetic |  |  |
|  | Intraparticle diffusion |  |
|  | Elovich |  |

Fig.S1 FTIR spectrum of granular AC with different PP content

(a)                                      (b)

Fig. S2 The TG-DTG curves of AC. (a) Curve of pure SS. (b) Curve of mixture.