Supplementary material

TABLE SⅠ. Fractions of cube texture, LGBs and Ʃ3 boundary in short Ni-5 at%W/Ni-9.3 at%W/Ni-5 at%W composite substrates (1st, 2nd, and 3rd procedures) after furnace-cooled annealing at various temperatures for 1 h

| Deformation | 1st procedure |  | 2ed procedure |  | 3rd procedure |  |
| --- | --- | --- | --- | --- | --- | --- |
| Recrystallization temperature / °C | 1100 | 1200 | 1100 | 1200 | 1100 | 1200 |
| fCube / % (<10°) | 93.1 | 96.0 | 97.2 | 99.6 | 96.5 | 98.5 |
| fLGB / % (2-10°) | 65.4 | 79.0 | 77.1 | 91.8 | 78.3 | 86.0 |
| fΣ3 / % | 11.9 | 6.9 | 6.3 | 0.6 | 8.2 | 2.3 |

TABLE SⅡ. Fractions of cube texture, LGBs and Ʃ3 boundary in short Ni-5 at%W/Ni-9.3 at%W/Ni-5 at%W substrates (2ed and 3rd procedure) after air-cooled annealing process

| Deformation |  |  | 2ed procedure |  |  |  |  | 3rd procedure |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Recrystallization process | 1100°C , 1 h | 1150°C , 1 h |  | 1200°C , 1 h | Two steps | 1100°C , 1 h | 1150°C , 1 h |  | 1200°C , 1 h | Two steps |
| fcube / % (<10°) | 78.8 | 95.1 |  | 97.0 | 99.0 | 75.3 | 88.1 |  | 90.8 | 97.2 |
| fLGB / % (2-10°) | 45.5 | 69.6 |  | 82.8 | 82.2 | 40.7 | 45.8 |  | 63.3 | 80.9 |
| fΣ3 / % | 27.2 | 11.7 |  | 4.9 | 7.8 | 29.0 | 27.2 |  | 19.8 | 7.1 |

TABLE SⅢ. Fractions of cube texture, LGBs and Ʃ3 boundary in the short Ni-5at.%W/Ni-9.3at.%W/Ni-5at.%W substrates (3rd procedure) after air-cooled annealing process

| Recrystallization process | fcube / % (<10°) | fLGB / % (2-10°) | fΣ3 / % |
| --- | --- | --- | --- |
| 1200℃, 2 h | 94.6 | 69.6 | 16.0 |
| 1250℃, 1 h | 97.2 | 72.6 | 13.4 |

15 mm

10 mm

Ni-5at.%W

Ni-9.3at.%W

mold

50 mm

FIG. S1. The schematic diagram of the matrix