Supplementary material:

Novel 4ZnO∙B2O3∙H2O:Ln3+/HTC (where Ln = Eu or Tb) phosphors: synthesis, morphology and luminescence properties

Lili He, Xiao Han, Chunhua Ge*, Rui Zhang, Yufang Hou, Xiangdong Zhang*

College of Chemistry, Liaoning University, Chongshan Road No. 66, Shenyang 110036, P. R. China

E-mail: chhge@lnu.edu.cn (C. Ge), xd623@sina.com (X.-D. Zhang)

FIG. S1. SEM images of 4ZnO·B2O3·H2O (a) and Zn3.64:Eu0.24[B2O7]·H2O (b).

FIG. S1a shows the SEM images of the 4ZnO·B2O3·H2O sample. It can be seen that 4ZnO·B2O3·H2O exhibits rod-like morphology of different sizes. When Eu3+ is doped into 4ZnO·B2O3·H2O lattice, because Eu3+ ions replace part of Zn2 +, the morphology of the sample changes greatly. When the molar ratio of Zn/Eu is 6.5%, the Zn3.64:Eu0.24[B2O7]·H2O sample exhibits a flower-like morphology, as shown in FIG. S1b [1].

TABLE SI: Zn3.64:Eu0.24[B2O7]·H2O/HTCx samples with various glucose concentrations

| samples | Eu/Zn (molar ratio%) | C6H12O6 (mmol) | C6H12O6 (mol%) |
| --- | --- | --- | --- |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC0 | 6.5 | 0.00 | 0.00 |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC5.97 | 6.5 | 0.55 | 5.97 |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC11.27 | 6.5 | 1.10 | 11.27 |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC16.01 | 6.5 | 1.65 | 16.01 |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC20.26 | 6.5 | 2.20 | 20.26 |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC24.10 | 6.5 | 2.75 | 24.10 |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC27.59 | 6.5 | 3.30 | 27.59 |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC30.78 | 6.5 | 3.85 | 30.78 |

TABLE SII: Zn3.55:Tb0.3[B2O7]·H2O/HTCy samples with various glucose concentrations

| samples | Tb/Zn (molar ratio%) | C6H12O6 (mmol) | C6H12O6 (mol%) |
| --- | --- | --- | --- |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC0 | 8.5 | 0.00 | 0.00 |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC5.99 | 8.5 | 0.55 | 5.99 |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC11.30 | 8.5 | 1.10 | 11.30 |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC16.04 | 8.5 | 1.65 | 16.04 |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC20.30 | 8.5 | 2.20 | 20.30 |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC24.15 | 8.5 | 2.75 | 24.15 |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC27.64 | 8.5 | 3.30 | 27.64 |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC30.83 | 8.5 | 3.85 | 30.83 |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC33.75 | 8.5 | 4.40 | 33.75 |

TABLE SIII: ICP analysis results of the Zn3.64:Eu0.24[B2O7]·H2O/HTCx samples.

| samples | Cal (Eu/Zn) (molar ratio%) | Exp (Eu/Zn) (molar ratio%) |  |
| --- | --- | --- | --- |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC0 | 6.5 | 6.30 |  |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC5.97 | 6.5 | 6.32 |  |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC11.27 | 6.5 | 6.28 |  |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC16.01 | 6.5 | 6.31 |  |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC20.26 | 6.5 | 6.34 |  |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC24.10 | 6.5 | 6.30 |  |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC27.59 | 6.5 | 6.29 |  |
| Zn3.64:Eu0.24[B2O7]·H2O/HTC30.78 | 6.5 | 6.31 |  |

TABLE SIV: ICP analysis results of the Zn3.55:Tb0.3[B2O7]·H2O/HTCy samples.

| samples | Cal (Tb/Zn) (molar ratio%) | Exp (Tb/Zn) (molar ratio%) |  |
| --- | --- | --- | --- |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC0 | 8.5 | 8.34 |  |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC5.99 | 8.5 | 8.30 |  |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC11.30 | 8.5 | 8.33 |  |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC16.04 | 8.5 | 8.36 |  |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC20.30 | 8.5 | 8.34 |  |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC24.15 | 8.5 | 8.31 |  |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC27.64 | 8.5 | 8.32 |  |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC30.83 | 8.5 | 8.32 |  |
| Zn3.55:Tb0.3[B2O7]·H2O/HTC33.75 | 8.5 | 8.33 |  |

References

[1] S.W. Cao, Y. Jiao, W.F. Han, C.H. Ge, B. Song, J. Wang , and X.D. Zhang: Hydrothermal synthesis of 4ZnO·B2O3·H2O:Ln3+ (Ln = Eu, Tb) phosphors: Morphology-tunable and luminescence properties. Spectrochim. Acta, Part A 190, 231 (2018).